From ancient pigments to modern optoelectronic applications of arsenic sulfides: bonazziite, the natural analogue of β-As4S4 from Khaidarkan deposit, Kyrgyzstan

Luca Bindi, Giovanni Pratesi, Maurizio Muniz-Miranda, Matteo Zoppi, Laura Chelazzi, Giovanni O. Lepore and Silvio Menchetti

Deposited Material

Table 3. List of calculated and observed squared structure factors for bonazziite.

| h | k | l | Fc | Fo |
| --- | --- | --- | --- | --- |
| 2 | 0 | 0 | 23525.8 | 17649.5 |
| 4 | 0 | 0 | 28308.4 | 21794.7 |
| 6 | 0 | 0 | 125659.2 | 106354.5 |
| 8 | 0 | 0 | 6042.5 | 5786.4 |
| 10 | 0 | 0 | 3050.2 | 3254.7 |
| 12 | 0 | 0 | 7257.2 | 7755.3 |
| 1 | 1 | 0 | 2725.6 | 3050.4 |
| 3 | 1 | 0 | 63638.8 | 64261.5 |
| 5 | 1 | 0 | 541.8 | 586.6 |
| 7 | 1 | 0 | 1065.7 | 1028.8 |
| 9 | 1 | 0 | 7911.4 | 7408.1 |
| 11 | 1 | 0 | 28.0 | –38.0 |
| 0 | 2 | 0 | 14314.3 | 16343.6 |
| 2 | 2 | 0 | 5881.2 | 6267.1 |
| 4 | 2 | 0 | 21966.2 | 22397.6 |
| 6 | 2 | 0 | 1331.0 | 1423.8 |
| 8 | 2 | 0 | 1174.0 | 1252.3 |
| 10 | 2 | 0 | 5974.5 | 5872.7 |
| 12 | 2 | 0 | 94.2 | 103.4 |
| 1 | 3 | 0 | 9786.9 | 10672.8 |
| 3 | 3 | 0 | 54633.1 | 54664.4 |
| 5 | 3 | 0 | 2017.0 | 1988.3 |
| 7 | 3 | 0 | 7348.2 | 7443.2 |
| 9 | 3 | 0 | 4602.7 | 4690.7 |
| 11 | 3 | 0 | 859.4 | 872.7 |
| 0 | 4 | 0 | 1028.1 | 1160.8 |
| 2 | 4 | 0 | 18646.3 | 19768.9 |
| 4 | 4 | 0 | 24488.2 | 24271.8 |
| 6 | 4 | 0 | 1205.4 | 1216.4 |
| 8 | 4 | 0 | 2613.7 | 2604.8 |
| 10 | 4 | 0 | 5733.1 | 6060.5 |
| 12 | 4 | 0 | 393.6 | 348.3 |
| 1 | 5 | 0 | 48232.1 | 50346.0 |
| 3 | 5 | 0 | 1229.1 | 1197.0 |
| 5 | 5 | 0 | 11551.2 | 11763.3 |
| 7 | 5 | 0 | 33461.2 | 33330.1 |
| 9 | 5 | 0 | 363.2 | 398.6 |
| 11 | 5 | 0 | 1457.3 | 1517.2 |
| 0 | 6 | 0 | 11107.6 | 11785.6 |
| 2 | 6 | 0 | 450.9 | 449.1 |
| 4 | 6 | 0 | 3299.6 | 3451.5 |
| 6 | 6 | 0 | 6226.5 | 6383.5 |
| 8 | 6 | 0 | 8.9 | –66.6 |
| 10 | 6 | 0 | 1831.7 | 1866.6 |
| 1 | 7 | 0 | 5300.4 | 5414.5 |
| 3 | 7 | 0 | 22805.7 | 23564.4 |
| 5 | 7 | 0 | 2002.1 | 2186.0 |
| 7 | 7 | 0 | 2914.1 | 3122.0 |
| 9 | 7 | 0 | 2900.7 | 2848.4 |
| 0 | 8 | 0 | 10553.4 | 10727.9 |
| 2 | 8 | 0 | 6531.1 | 6563.6 |
| 4 | 8 | 0 | 10270.7 | 11102.6 |
| 6 | 8 | 0 | 3137.8 | 3213.3 |
| 8 | 8 | 0 | 1379.1 | 1384.5 |
| 1 | 9 | 0 | 141.5 | 86.2 |
| 3 | 9 | 0 | 8933.2 | 9019.7 |
| 5 | 9 | 0 | 307.3 | 228.6 |
| 7 | 9 | 0 | 0.3 | 97.5 |
| 0 | 10 | 0 | 10813.9 | 10589.9 |
| 2 | 10 | 0 | 280.2 | 247.4 |
| 4 | 10 | 0 | 74.6 | –43.0 |
| 6 | 10 | 0 | 4230.6 | 4263.0 |
| 1 | 11 | 0 | 769.2 | 579.8 |
| 3 | 11 | 0 | 1886.0 | 1840.2 |
| 5 | 11 | 0 | 348.7 | 305.6 |
| 0 | 12 | 0 | 1501.5 | 1616.7 |
| 2 | 12 | 0 | 2444.9 | 2304.8 |
| –11 | 1 | 1 | 120.3 | –4.5 |
| –9 | 1 | 1 | 1768.6 | 1822.1 |
| –7 | 1 | 1 | 5408.0 | 5046.5 |
| –5 | 1 | 1 | 5177.3 | 5003.0 |
| –3 | 1 | 1 | 944.4 | 979.7 |
| –1 | 1 | 1 | 37035.0 | 32935.4 |
| 1 | 1 | 1 | 15520.2 | 16869.3 |
| 3 | 1 | 1 | 13699.7 | 14801.6 |
| 5 | 1 | 1 | 31256.3 | 29095.1 |
| 7 | 1 | 1 | 95.8 | 10.1 |
| 9 | 1 | 1 | 1615.3 | 1644.9 |
| 11 | 1 | 1 | 2935.5 | 2914.4 |
| –12 | 2 | 1 | 286.9 | 114.8 |
| –10 | 2 | 1 | 6982.5 | 7005.4 |
| –8 | 2 | 1 | 33.1 | –37.2 |
| –6 | 2 | 1 | 12.9 | –26.1 |
| –4 | 2 | 1 | 44194.3 | 40243.7 |
| –2 | 2 | 1 | 8553.9 | 8474.2 |
| 0 | 2 | 1 | 9937.8 | 10628.7 |
| 2 | 2 | 1 | 90749.6 | 96569.4 |
| 4 | 2 | 1 | 4469.0 | 4770.7 |
| 6 | 2 | 1 | 7505.1 | 7834.4 |
| 8 | 2 | 1 | 20793.7 | 21393.1 |
| 10 | 2 | 1 | 385.5 | 465.9 |
| 12 | 2 | 1 | 851.5 | 883.8 |
| –11 | 3 | 1 | 2501.5 | 2606.0 |
| –9 | 3 | 1 | 5737.4 | 5918.2 |
| –7 | 3 | 1 | 10568.7 | 10125.3 |
| –5 | 3 | 1 | 16453.7 | 15411.9 |
| –3 | 3 | 1 | 19848.8 | 19907.2 |
| –1 | 3 | 1 | 23673.4 | 25583.4 |
| 1 | 3 | 1 | 13087.5 | 14032.9 |
| 3 | 3 | 1 | 17375.9 | 17980.9 |
| 5 | 3 | 1 | 6132.7 | 6382.8 |
| 7 | 3 | 1 | 1.7 | 60.7 |
| 9 | 3 | 1 | 6984.8 | 7311.9 |
| 11 | 3 | 1 | 1001.7 | 1060.5 |
| –12 | 4 | 1 | 829.4 | 843.1 |
| –10 | 4 | 1 | 3999.7 | 4039.4 |
| –8 | 4 | 1 | 1605.3 | 1530.2 |
| –6 | 4 | 1 | 2469.9 | 2348.2 |
| –4 | 4 | 1 | 21025.7 | 20899.4 |
| –2 | 4 | 1 | 6907.7 | 7139.6 |
| 0 | 4 | 1 | 87.7 | 11.6 |
| 2 | 4 | 1 | 8954.5 | 9403.7 |
| 4 | 4 | 1 | 24.1 | 93.4 |
| 6 | 4 | 1 | 470.8 | 444.5 |
| 8 | 4 | 1 | 671.9 | 679.3 |
| 10 | 4 | 1 | 1169.5 | 1239.7 |
| –11 | 5 | 1 | 21.5 | –52.3 |
| –9 | 5 | 1 | 12.9 | –61.0 |
| –7 | 5 | 1 | 395.6 | 132.8 |
| –5 | 5 | 1 | 38.8 | 68.6 |
| –3 | 5 | 1 | 59.2 | 41.2 |
| –1 | 5 | 1 | 312.8 | 369.2 |
| 1 | 5 | 1 | 2.4 | 18.6 |
| 3 | 5 | 1 | 1.0 | 30.2 |
| 5 | 5 | 1 | 7.3 | –62.6 |
| 7 | 5 | 1 | 38.2 | 41.9 |
| 9 | 5 | 1 | 50.8 | 108.2 |
| 11 | 5 | 1 | 51.6 | 5.1 |
| –10 | 6 | 1 | 38.3 | 140.7 |
| –8 | 6 | 1 | 6763.4 | 6576.4 |
| –6 | 6 | 1 | 10784.8 | 10978.0 |
| –4 | 6 | 1 | 34.3 | 103.5 |
| –2 | 6 | 1 | 25786.9 | 27208.4 |
| 0 | 6 | 1 | 12351.1 | 12662.7 |
| 2 | 6 | 1 | 1381.7 | 1489.9 |
| 4 | 6 | 1 | 7249.4 | 7487.0 |
| 6 | 6 | 1 | 5974.8 | 6386.3 |
| 8 | 6 | 1 | 695.0 | 790.1 |
| 10 | 6 | 1 | 29.8 | 47.3 |
| –9 | 7 | 1 | 1104.2 | 1155.0 |
| –7 | 7 | 1 | 6528.4 | 6803.7 |
| –5 | 7 | 1 | 4130.6 | 4338.1 |
| –3 | 7 | 1 | 3833.0 | 4024.3 |
| –1 | 7 | 1 | 8878.8 | 9127.7 |
| 1 | 7 | 1 | 3698.7 | 3697.8 |
| 3 | 7 | 1 | 4740.8 | 5033.4 |
| 5 | 7 | 1 | 1776.3 | 2011.8 |
| 7 | 7 | 1 | 30.7 | –17.2 |
| 9 | 7 | 1 | 2679.8 | 2985.3 |
| –8 | 8 | 1 | 307.6 | 463.1 |
| –6 | 8 | 1 | 419.6 | 504.5 |
| –4 | 8 | 1 | 6352.1 | 6797.9 |
| –2 | 8 | 1 | 77.8 | 3.2 |
| 0 | 8 | 1 | 5218.7 | 5263.1 |
| 2 | 8 | 1 | 7986.9 | 8274.7 |
| 4 | 8 | 1 | 85.9 | 183.2 |
| 6 | 8 | 1 | 4433.0 | 4785.3 |
| 8 | 8 | 1 | 2010.8 | 2221.6 |
| –7 | 9 | 1 | 892.4 | 981.0 |
| –5 | 9 | 1 | 254.2 | 117.4 |
| –3 | 9 | 1 | 344.2 | 373.1 |
| –1 | 9 | 1 | 4139.8 | 4125.1 |
| 1 | 9 | 1 | 907.9 | 988.3 |
| 3 | 9 | 1 | 1471.8 | 1506.2 |
| 5 | 9 | 1 | 4722.1 | 4869.7 |
| 7 | 9 | 1 | 86.3 | 65.8 |
| –6 | 10 | 1 | 74.4 | 16.0 |
| –4 | 10 | 1 | 0.4 | –2.3 |
| –2 | 10 | 1 | 17.3 | 132.4 |
| 0 | 10 | 1 | 42.7 | –22.4 |
| 2 | 10 | 1 | 118.5 | –123.1 |
| 4 | 10 | 1 | 104.9 | 211.9 |
| 6 | 10 | 1 | 0.1 | –198.3 |
| –5 | 11 | 1 | 123.8 | 237.2 |
| –3 | 11 | 1 | 0.5 | –83.5 |
| –1 | 11 | 1 | 1375.1 | 1371.8 |
| 1 | 11 | 1 | 269.2 | 420.6 |
| 3 | 11 | 1 | 196.6 | 75.7 |
| 5 | 11 | 1 | 1329.1 | 1350.7 |
| –2 | 12 | 1 | 381.8 | 241.1 |
| 0 | 12 | 1 | 1998.9 | 1768.9 |
| 2 | 12 | 1 | 507.0 | 548.1 |
| –12 | 0 | 2 | 3528.7 | 3112.2 |
| –10 | 0 | 2 | 3466.8 | 3048.9 |
| –8 | 0 | 2 | 6755.4 | 5907.4 |
| –6 | 0 | 2 | 17024.5 | 15533.8 |
| –4 | 0 | 2 | 16155.6 | 15515.1 |
| –2 | 0 | 2 | 1439.4 | 1428.8 |
| 0 | 0 | 2 | 807.6 | 730.3 |
| 2 | 0 | 2 | 63084.6 | 71877.6 |
| 4 | 0 | 2 | 450.4 | 497.9 |
| 6 | 0 | 2 | 1062.5 | 1002.2 |
| 8 | 0 | 2 | 31684.7 | 32157.2 |
| 10 | 0 | 2 | 1111.0 | 1037.7 |
| 12 | 0 | 2 | 135.3 | 0.0 |
| –13 | 1 | 2 | 733.0 | 882.9 |
| –11 | 1 | 2 | 2305.5 | 2143.2 |
| –9 | 1 | 2 | 3127.2 | 3047.0 |
| –7 | 1 | 2 | 6579.1 | 6325.0 |
| –5 | 1 | 2 | 6818.4 | 6503.3 |
| –3 | 1 | 2 | 4030.4 | 3783.1 |
| –1 | 1 | 2 | 31781.3 | 30214.2 |
| 1 | 1 | 2 | 5195.4 | 5425.1 |
| 3 | 1 | 2 | 12.5 | 44.8 |
| 5 | 1 | 2 | 26536.3 | 27711.7 |
| 7 | 1 | 2 | 1604.0 | 1872.0 |
| 9 | 1 | 2 | 294.0 | 157.9 |
| 11 | 1 | 2 | 5197.3 | 4883.9 |
| –12 | 2 | 2 | 1771.0 | 1918.7 |
| –10 | 2 | 2 | 947.2 | 1048.5 |
| –8 | 2 | 2 | 11686.8 | 11562.3 |
| –6 | 2 | 2 | 21275.2 | 20029.1 |
| –4 | 2 | 2 | 3486.6 | 3211.2 |
| –2 | 2 | 2 | 100906.0 | 95219.4 |
| 0 | 2 | 2 | 34719.3 | 34295.6 |
| 2 | 2 | 2 | 15230.9 | 16481.8 |
| 4 | 2 | 2 | 52956.0 | 55515.0 |
| 6 | 2 | 2 | 9033.1 | 9072.3 |
| 8 | 2 | 2 | 5843.9 | 5640.8 |
| 10 | 2 | 2 | 3591.6 | 3436.5 |
| –11 | 3 | 2 | 62.3 | 194.9 |
| –9 | 3 | 2 | 6555.4 | 6694.8 |
| –7 | 3 | 2 | 2077.7 | 2032.9 |
| –5 | 3 | 2 | 3536.6 | 3343.8 |
| –3 | 3 | 2 | 14241.9 | 13635.2 |
| –1 | 3 | 2 | 10568.1 | 10504.9 |
| 1 | 3 | 2 | 15294.3 | 15594.4 |
| 3 | 3 | 2 | 1753.3 | 1793.5 |
| 5 | 3 | 2 | 16354.8 | 17181.8 |
| 7 | 3 | 2 | 1321.5 | 1432.0 |
| 9 | 3 | 2 | 133.1 | 66.2 |
| 11 | 3 | 2 | 3115.2 | 3233.2 |
| –12 | 4 | 2 | 73.0 | –67.3 |
| –10 | 4 | 2 | 437.3 | 493.1 |
| –8 | 4 | 2 | 6788.7 | 6578.3 |
| –6 | 4 | 2 | 88.7 | 252.4 |
| –4 | 4 | 2 | 4324.6 | 4039.4 |
| –2 | 4 | 2 | 28856.8 | 28815.8 |
| 0 | 4 | 2 | 1331.7 | 1367.8 |
| 2 | 4 | 2 | 5025.2 | 4933.1 |
| 4 | 4 | 2 | 17140.3 | 17232.1 |
| 6 | 4 | 2 | 2065.7 | 2246.9 |
| 8 | 4 | 2 | 1490.1 | 1653.5 |
| 10 | 4 | 2 | 1820.0 | 1851.6 |
| –11 | 5 | 2 | 3720.2 | 3865.0 |
| –9 | 5 | 2 | 2291.4 | 2192.3 |
| –7 | 5 | 2 | 1075.0 | 1146.7 |
| –5 | 5 | 2 | 44283.4 | 41964.5 |
| –3 | 5 | 2 | 9499.8 | 9591.5 |
| –1 | 5 | 2 | 2923.9 | 2842.2 |
| 1 | 5 | 2 | 82617.1 | 86944.5 |
| 3 | 5 | 2 | 5993.5 | 6140.6 |
| 5 | 5 | 2 | 112.1 | 170.7 |
| 7 | 5 | 2 | 16333.9 | 16438.6 |
| 9 | 5 | 2 | 2864.9 | 2982.4 |
| 11 | 5 | 2 | 48.3 | 110.1 |
| –10 | 6 | 2 | 329.8 | 354.4 |
| –8 | 6 | 2 | 5850.6 | 5364.5 |
| –6 | 6 | 2 | 460.2 | 430.7 |
| –4 | 6 | 2 | 3887.9 | 3831.7 |
| –2 | 6 | 2 | 20247.7 | 20757.4 |
| 0 | 6 | 2 | 831.4 | 868.0 |
| 2 | 6 | 2 | 5425.4 | 5318.9 |
| 4 | 6 | 2 | 11010.6 | 11110.1 |
| 6 | 6 | 2 | 574.1 | 621.9 |
| 8 | 6 | 2 | 1601.9 | 1620.4 |
| 10 | 6 | 2 | 954.8 | 834.8 |
| –9 | 7 | 2 | 2259.4 | 2188.0 |
| –7 | 7 | 2 | 2341.5 | 2230.5 |
| –5 | 7 | 2 | 1181.1 | 1103.3 |
| –3 | 7 | 2 | 5296.5 | 5431.1 |
| –1 | 7 | 2 | 9135.6 | 8955.9 |
| 1 | 7 | 2 | 4877.1 | 4847.2 |
| 3 | 7 | 2 | 1830.1 | 1810.8 |
| 5 | 7 | 2 | 10601.0 | 10771.5 |
| 7 | 7 | 2 | 986.3 | 1051.1 |
| 9 | 7 | 2 | 386.7 | 391.3 |
| –8 | 8 | 2 | 180.5 | 134.7 |
| –6 | 8 | 2 | 159.7 | 135.1 |
| –4 | 8 | 2 | 1000.4 | 898.8 |
| –2 | 8 | 2 | 2123.1 | 2194.8 |
| 0 | 8 | 2 | 171.7 | 146.8 |
| 2 | 8 | 2 | 450.4 | 496.3 |
| 4 | 8 | 2 | 1059.0 | 1032.5 |
| 6 | 8 | 2 | 290.0 | –14.4 |
| 8 | 8 | 2 | 0.5 | 77.7 |
| –7 | 9 | 2 | 1606.3 | 1489.3 |
| –5 | 9 | 2 | 409.5 | 208.9 |
| –3 | 9 | 2 | 1458.8 | 1458.9 |
| –1 | 9 | 2 | 6226.6 | 5854.5 |
| 1 | 9 | 2 | 132.2 | 117.3 |
| 3 | 9 | 2 | 647.0 | 430.8 |
| 5 | 9 | 2 | 5354.2 | 5540.8 |
| 7 | 9 | 2 | 45.9 | 78.1 |
| –6 | 10 | 2 | 4934.6 | 5613.3 |
| –4 | 10 | 2 | 7473.3 | 7755.1 |
| –2 | 10 | 2 | 977.2 | 974.6 |
| 0 | 10 | 2 | 4046.6 | 3864.1 |
| 2 | 10 | 2 | 13850.4 | 13394.2 |
| 4 | 10 | 2 | 809.9 | 744.1 |
| 6 | 10 | 2 | 632.5 | 6.6 |
| –5 | 11 | 2 | 832.1 | 691.5 |
| –3 | 11 | 2 | 4.6 | 311.5 |
| –1 | 11 | 2 | 716.1 | 774.8 |
| 1 | 11 | 2 | 1014.4 | 1121.4 |
| 3 | 11 | 2 | 320.8 | 329.3 |
| –2 | 12 | 2 | 873.8 | 779.6 |
| 0 | 12 | 2 | 183.0 | 140.8 |
| –13 | 1 | 3 | 449.9 | 618.5 |
| –11 | 1 | 3 | 10620.3 | 10188.7 |
| –9 | 1 | 3 | 55.6 | 98.4 |
| –7 | 1 | 3 | 15215.9 | 13722.7 |
| –5 | 1 | 3 | 48654.1 | 42821.3 |
| –3 | 1 | 3 | 531.8 | 562.2 |
| –1 | 1 | 3 | 51562.2 | 52405.5 |
| 1 | 1 | 3 | 41933.7 | 41288.7 |
| 3 | 1 | 3 | 10928.2 | 11347.9 |
| 5 | 1 | 3 | 4924.6 | 4888.6 |
| 7 | 1 | 3 | 14056.0 | 14362.8 |
| 9 | 1 | 3 | 3076.0 | 3197.7 |
| 11 | 1 | 3 | 83.4 | 85.7 |
| –12 | 2 | 3 | 1505.0 | 1589.9 |
| –10 | 2 | 3 | 495.0 | 150.5 |
| –8 | 2 | 3 | 14985.0 | 14608.2 |
| –6 | 2 | 3 | 11084.9 | 10560.8 |
| –4 | 2 | 3 | 3555.3 | 3392.1 |
| –2 | 2 | 3 | 33852.7 | 30963.6 |
| 0 | 2 | 3 | 8660.5 | 8467.4 |
| 2 | 2 | 3 | 73.1 | 315.7 |
| 4 | 2 | 3 | 20727.1 | 21520.8 |
| 6 | 2 | 3 | 150.6 | –56.9 |
| 8 | 2 | 3 | 2005.6 | 2069.0 |
| 10 | 2 | 3 | 5565.8 | 5408.0 |
| –11 | 3 | 3 | 14.8 | –142.1 |
| –9 | 3 | 3 | 9776.5 | 9976.7 |
| –7 | 3 | 3 | 5785.0 | 5690.5 |
| –5 | 3 | 3 | 833.0 | 847.6 |
| –3 | 3 | 3 | 37225.8 | 36286.9 |
| –1 | 3 | 3 | 33011.1 | 32675.6 |
| 1 | 3 | 3 | 9840.5 | 9412.8 |
| 3 | 3 | 3 | 34314.4 | 35519.3 |
| 5 | 3 | 3 | 14354.8 | 14473.4 |
| 7 | 3 | 3 | 4758.0 | 5124.6 |
| 9 | 3 | 3 | 4523.5 | 4660.1 |
| 11 | 3 | 3 | 1830.1 | 1868.8 |
| –12 | 4 | 3 | 3393.2 | 3357.7 |
| –10 | 4 | 3 | 3325.0 | 3194.1 |
| –8 | 4 | 3 | 5714.1 | 5525.7 |
| –6 | 4 | 3 | 19841.1 | 19298.9 |
| –4 | 4 | 3 | 49522.5 | 47422.4 |
| –2 | 4 | 3 | 4393.9 | 4218.7 |
| 0 | 4 | 3 | 59948.4 | 62577.3 |
| 2 | 4 | 3 | 59534.5 | 61112.7 |
| 4 | 4 | 3 | 285.7 | 347.2 |
| 6 | 4 | 3 | 28894.3 | 30055.2 |
| 8 | 4 | 3 | 8891.0 | 9046.9 |
| 10 | 4 | 3 | 122.8 | 231.2 |
| –11 | 5 | 3 | 78.2 | –108.5 |
| –9 | 5 | 3 | 168.7 | 172.5 |
| –7 | 5 | 3 | 38.0 | 50.0 |
| –5 | 5 | 3 | 511.4 | 481.0 |
| –3 | 5 | 3 | 461.8 | 487.7 |
| –1 | 5 | 3 | 6.5 | –77.9 |
| 1 | 5 | 3 | 777.2 | 818.6 |
| 3 | 5 | 3 | 191.4 | 174.1 |
| 5 | 5 | 3 | 0.1 | 43.9 |
| 7 | 5 | 3 | 254.0 | 91.9 |
| 9 | 5 | 3 | 8.9 | 12.7 |
| –10 | 6 | 3 | 237.6 | 250.9 |
| –8 | 6 | 3 | 651.4 | 558.9 |
| –6 | 6 | 3 | 3446.6 | 3249.5 |
| –4 | 6 | 3 | 7536.9 | 7106.7 |
| –2 | 6 | 3 | 296.1 | 510.0 |
| 0 | 6 | 3 | 10788.0 | 10585.1 |
| 2 | 6 | 3 | 8272.5 | 8077.1 |
| 4 | 6 | 3 | 1735.6 | 1731.0 |
| 6 | 6 | 3 | 6289.3 | 6533.0 |
| 8 | 6 | 3 | 865.0 | 874.4 |
| –9 | 7 | 3 | 1964.7 | 1951.2 |
| –7 | 7 | 3 | 712.5 | 615.9 |
| –5 | 7 | 3 | 1412.6 | 1381.9 |
| –3 | 7 | 3 | 7213.3 | 7360.5 |
| –1 | 7 | 3 | 6466.7 | 6198.0 |
| 1 | 7 | 3 | 5777.2 | 5511.4 |
| 3 | 7 | 3 | 9440.2 | 9398.4 |
| 5 | 7 | 3 | 4520.1 | 4432.5 |
| 7 | 7 | 3 | 2319.8 | 2276.3 |
| 9 | 7 | 3 | 2249.8 | 2272.6 |
| –8 | 8 | 3 | 8041.7 | 8490.7 |
| –6 | 8 | 3 | 24.1 | –122.2 |
| –4 | 8 | 3 | 4251.9 | 4354.1 |
| –2 | 8 | 3 | 20421.8 | 20380.3 |
| 0 | 8 | 3 | 235.1 | 362.6 |
| 2 | 8 | 3 | 1638.9 | 1669.8 |
| 4 | 8 | 3 | 13930.0 | 13314.6 |
| 6 | 8 | 3 | 388.9 | 214.3 |
| 8 | 8 | 3 | 16.8 | –87.7 |
| –7 | 9 | 3 | 1233.3 | 1267.7 |
| –5 | 9 | 3 | 6175.8 | 6372.6 |
| –3 | 9 | 3 | 4.8 | 52.2 |
| –1 | 9 | 3 | 3033.8 | 3040.1 |
| 1 | 9 | 3 | 5828.5 | 5475.9 |
| 3 | 9 | 3 | 911.6 | 1007.2 |
| 5 | 9 | 3 | 311.7 | 185.3 |
| 7 | 9 | 3 | 2532.3 | 2684.2 |
| –6 | 10 | 3 | 485.7 | 472.4 |
| –4 | 10 | 3 | 517.1 | 460.6 |
| –2 | 10 | 3 | 236.3 | 170.1 |
| 0 | 10 | 3 | 489.8 | 469.4 |
| 2 | 10 | 3 | 403.1 | 288.1 |
| 4 | 10 | 3 | 145.0 | 213.1 |
| –5 | 11 | 3 | 2334.1 | 2542.2 |
| –3 | 11 | 3 | 119.7 | –171.6 |
| –1 | 11 | 3 | 2164.6 | 2200.6 |
| 1 | 11 | 3 | 2362.2 | 2090.1 |
| 3 | 11 | 3 | 491.7 | 370.9 |
| –12 | 0 | 4 | 522.2 | 162.5 |
| –10 | 0 | 4 | 3027.3 | 2971.0 |
| –8 | 0 | 4 | 11413.3 | 10591.8 |
| –6 | 0 | 4 | 12748.4 | 12349.7 |
| –4 | 0 | 4 | 43579.5 | 43325.5 |
| –2 | 0 | 4 | 34471.7 | 32240.3 |
| 0 | 0 | 4 | 14856.0 | 14614.6 |
| 2 | 0 | 4 | 51993.3 | 51863.1 |
| 4 | 0 | 4 | 17429.8 | 17848.3 |
| 6 | 0 | 4 | 896.3 | 863.0 |
| 8 | 0 | 4 | 4056.0 | 4156.2 |
| 10 | 0 | 4 | 5843.3 | 6217.3 |
| –11 | 1 | 4 | 274.9 | 253.7 |
| –9 | 1 | 4 | 4126.9 | 3857.8 |
| –7 | 1 | 4 | 4226.1 | 3973.1 |
| –5 | 1 | 4 | 3691.8 | 3355.9 |
| –3 | 1 | 4 | 21321.3 | 20125.9 |
| –1 | 1 | 4 | 10919.9 | 10770.3 |
| 1 | 1 | 4 | 5935.2 | 5759.2 |
| 3 | 1 | 4 | 15255.8 | 14989.3 |
| 5 | 1 | 4 | 1845.2 | 1866.2 |
| 7 | 1 | 4 | 2940.2 | 2884.0 |
| 9 | 1 | 4 | 2777.8 | 2664.8 |
| 11 | 1 | 4 | 3.7 | 73.5 |
| –12 | 2 | 4 | 68.3 | –51.8 |
| –10 | 2 | 4 | 2174.1 | 2347.0 |
| –8 | 2 | 4 | 48.3 | 9.4 |
| –6 | 2 | 4 | 392.1 | 306.1 |
| –4 | 2 | 4 | 605.9 | 611.7 |
| –2 | 2 | 4 | 2363.2 | 2199.9 |
| 0 | 2 | 4 | 39.4 | –11.5 |
| 2 | 2 | 4 | 118.6 | 169.2 |
| 4 | 2 | 4 | 5822.4 | 5903.5 |
| 6 | 2 | 4 | 2320.8 | 2507.2 |
| 8 | 2 | 4 | 40.6 | 77.4 |
| 10 | 2 | 4 | 729.4 | 657.6 |
| –11 | 3 | 4 | 526.1 | 741.4 |
| –9 | 3 | 4 | 756.3 | 811.5 |
| –7 | 3 | 4 | 653.8 | 653.4 |
| –5 | 3 | 4 | 2368.2 | 2369.8 |
| –3 | 3 | 4 | 5607.0 | 5296.9 |
| –1 | 3 | 4 | 8652.0 | 8252.3 |
| 1 | 3 | 4 | 184.2 | 116.1 |
| 3 | 3 | 4 | 649.3 | 607.5 |
| 5 | 3 | 4 | 2579.6 | 2532.0 |
| 7 | 3 | 4 | 45.0 | 13.6 |
| 9 | 3 | 4 | 54.7 | –151.6 |
| –12 | 4 | 4 | 898.2 | 1271.9 |
| –10 | 4 | 4 | 1400.1 | 1461.2 |
| –8 | 4 | 4 | 17.9 | 45.4 |
| –6 | 4 | 4 | 6704.0 | 6837.5 |
| –4 | 4 | 4 | 1312.8 | 1211.5 |
| –2 | 4 | 4 | 379.2 | 244.1 |
| 0 | 4 | 4 | 19291.7 | 19569.9 |
| 2 | 4 | 4 | 41.3 | 8.8 |
| 4 | 4 | 4 | 1492.1 | 1487.1 |
| 6 | 4 | 4 | 11477.9 | 11795.1 |
| 8 | 4 | 4 | 17.5 | –33.0 |
| 10 | 4 | 4 | 524.2 | 320.4 |
| –11 | 5 | 4 | 296.8 | 112.6 |
| –9 | 5 | 4 | 2443.6 | 2688.3 |
| –7 | 5 | 4 | 2739.2 | 2894.2 |
| –5 | 5 | 4 | 41.5 | –64.6 |
| –3 | 5 | 4 | 8352.3 | 8191.1 |
| –1 | 5 | 4 | 13.7 | 3.9 |
| 1 | 5 | 4 | 4906.4 | 4715.5 |
| 3 | 5 | 4 | 18330.8 | 18189.6 |
| 5 | 5 | 4 | 83.8 | 26.4 |
| 7 | 5 | 4 | 4318.7 | 4276.3 |
| 9 | 5 | 4 | 7171.1 | 7729.1 |
| –10 | 6 | 4 | 1501.7 | 1604.5 |
| –8 | 6 | 4 | 106.7 | 112.8 |
| –6 | 6 | 4 | 1712.0 | 1874.6 |
| –4 | 6 | 4 | 3186.0 | 3203.4 |
| –2 | 6 | 4 | 4188.8 | 4077.9 |
| 0 | 6 | 4 | 2961.8 | 2857.2 |
| 2 | 6 | 4 | 1909.7 | 1889.5 |
| 4 | 6 | 4 | 8310.2 | 8304.1 |
| 6 | 6 | 4 | 2108.2 | 2247.0 |
| 8 | 6 | 4 | 416.4 | 320.9 |
| –9 | 7 | 4 | 430.5 | 361.3 |
| –7 | 7 | 4 | 277.9 | 218.1 |
| –5 | 7 | 4 | 1618.3 | 1711.1 |
| –3 | 7 | 4 | 1460.8 | 1488.2 |
| –1 | 7 | 4 | 2663.0 | 2745.9 |
| 1 | 7 | 4 | 1179.8 | 1179.3 |
| 3 | 7 | 4 | 77.7 | 200.8 |
| 5 | 7 | 4 | 801.6 | 585.2 |
| 7 | 7 | 4 | 575.0 | 615.8 |
| –8 | 8 | 4 | 1596.6 | 1446.6 |
| –6 | 8 | 4 | 457.5 | 520.2 |
| –4 | 8 | 4 | 770.7 | 741.3 |
| –2 | 8 | 4 | 1360.7 | 1332.8 |
| 0 | 8 | 4 | 1471.0 | 1408.5 |
| 2 | 8 | 4 | 1479.5 | 1463.7 |
| 4 | 8 | 4 | 21.0 | –132.4 |
| 6 | 8 | 4 | 1744.6 | 1696.2 |
| –7 | 9 | 4 | 660.0 | 655.3 |
| –5 | 9 | 4 | 183.7 | 125.0 |
| –3 | 9 | 4 | 1551.0 | 1672.5 |
| –1 | 9 | 4 | 1807.1 | 1792.4 |
| 1 | 9 | 4 | 1195.5 | 1067.8 |
| 3 | 9 | 4 | 726.4 | 728.7 |
| 5 | 9 | 4 | 882.7 | 766.3 |
| –6 | 10 | 4 | 3967.0 | 4026.6 |
| –4 | 10 | 4 | 378.6 | 92.6 |
| –2 | 10 | 4 | 33.7 | –65.2 |
| 0 | 10 | 4 | 6434.6 | 6247.5 |
| 2 | 10 | 4 | 276.1 | 162.9 |
| 4 | 10 | 4 | 34.8 | 20.5 |
| –3 | 11 | 4 | 1916.1 | 1632.7 |
| –1 | 11 | 4 | 250.3 | 396.3 |
| 1 | 11 | 4 | 185.2 | –172.3 |
| –11 | 1 | 5 | 2843.5 | 2754.1 |
| –9 | 1 | 5 | 7560.0 | 7406.9 |
| –7 | 1 | 5 | 5226.0 | 4981.3 |
| –5 | 1 | 5 | 12043.1 | 11742.0 |
| –3 | 1 | 5 | 65646.8 | 66397.7 |
| –1 | 1 | 5 | 1397.3 | 1512.5 |
| 1 | 1 | 5 | 28237.1 | 28527.6 |
| 3 | 1 | 5 | 47174.6 | 47423.8 |
| 5 | 1 | 5 | 36.9 | 0.0 |
| 7 | 1 | 5 | 9139.6 | 9478.3 |
| 9 | 1 | 5 | 5485.6 | 5760.4 |
| –12 | 2 | 5 | 918.8 | 937.3 |
| –10 | 2 | 5 | 65.8 | 7.1 |
| –8 | 2 | 5 | 6377.5 | 5968.5 |
| –6 | 2 | 5 | 23478.6 | 21645.1 |
| –4 | 2 | 5 | 242.6 | 377.1 |
| –2 | 2 | 5 | 18192.6 | 17251.1 |
| 0 | 2 | 5 | 63433.8 | 63605.5 |
| 2 | 2 | 5 | 2442.4 | 2453.8 |
| 4 | 2 | 5 | 11945.9 | 12084.5 |
| 6 | 2 | 5 | 22739.1 | 23704.6 |
| 8 | 2 | 5 | 619.6 | 705.4 |
| 10 | 2 | 5 | 949.5 | 1020.5 |
| –11 | 3 | 5 | 26.0 | –85.4 |
| –9 | 3 | 5 | 169.4 | 222.6 |
| –7 | 3 | 5 | 24900.6 | 25171.4 |
| –5 | 3 | 5 | 105.6 | 160.3 |
| –3 | 3 | 5 | 1287.9 | 1257.9 |
| –1 | 3 | 5 | 42804.4 | 42717.4 |
| 1 | 3 | 5 | 5217.4 | 5060.9 |
| 3 | 3 | 5 | 44.0 | 8.4 |
| 5 | 3 | 5 | 19534.7 | 19374.8 |
| 7 | 3 | 5 | 4626.7 | 4665.9 |
| 9 | 3 | 5 | 1045.4 | 993.3 |
| –12 | 4 | 5 | 12.8 | 124.6 |
| –10 | 4 | 5 | 7716.9 | 8241.7 |
| –8 | 4 | 5 | 94.3 | 150.7 |
| –6 | 4 | 5 | 1726.3 | 1763.9 |
| –4 | 4 | 5 | 18124.3 | 19014.2 |
| –2 | 4 | 5 | 715.4 | 617.0 |
| 0 | 4 | 5 | 2654.9 | 2654.0 |
| 2 | 4 | 5 | 8831.5 | 9060.2 |
| 4 | 4 | 5 | 5217.0 | 5289.3 |
| 6 | 4 | 5 | 149.8 | 98.5 |
| 8 | 4 | 5 | 2516.2 | 2716.5 |
| –11 | 5 | 5 | 51.6 | –152.4 |
| –9 | 5 | 5 | 273.8 | 405.7 |
| –7 | 5 | 5 | 81.5 | –149.0 |
| –5 | 5 | 5 | 379.7 | 494.0 |
| –3 | 5 | 5 | 823.8 | 928.7 |
| –1 | 5 | 5 | 438.0 | 545.1 |
| 1 | 5 | 5 | 290.8 | 930.8 |
| 3 | 5 | 5 | 435.9 | 518.1 |
| 5 | 5 | 5 | 254.1 | 349.4 |
| 7 | 5 | 5 | 0.9 | –220.8 |
| 9 | 5 | 5 | 60.1 | 310.8 |
| –10 | 6 | 5 | 8675.7 | 9421.0 |
| –8 | 6 | 5 | 1229.6 | 1299.3 |
| –6 | 6 | 5 | 9974.3 | 10201.7 |
| –4 | 6 | 5 | 28775.1 | 30897.1 |
| –2 | 6 | 5 | 8868.3 | 9123.3 |
| 0 | 6 | 5 | 17183.0 | 17289.7 |
| 2 | 6 | 5 | 22445.7 | 21752.5 |
| 4 | 6 | 5 | 12372.3 | 12198.2 |
| 6 | 6 | 5 | 2352.9 | 2234.4 |
| 8 | 6 | 5 | 6348.4 | 6792.8 |
| –9 | 7 | 5 | 0.9 | –12.4 |
| –7 | 7 | 5 | 7294.7 | 7603.6 |
| –5 | 7 | 5 | 383.1 | 132.1 |
| –3 | 7 | 5 | 41.4 | 9.3 |
| –1 | 7 | 5 | 9839.1 | 9787.4 |
| 1 | 7 | 5 | 104.6 | –52.7 |
| 3 | 7 | 5 | 379.2 | 203.8 |
| 5 | 7 | 5 | 4014.4 | 3930.4 |
| 7 | 7 | 5 | 624.8 | 494.5 |
| –8 | 8 | 5 | 1539.4 | 1239.3 |
| –6 | 8 | 5 | 4608.7 | 4560.1 |
| –4 | 8 | 5 | 433.2 | 648.5 |
| –2 | 8 | 5 | 3404.0 | 3292.6 |
| 0 | 8 | 5 | 10994.3 | 10635.3 |
| 2 | 8 | 5 | 903.2 | 901.7 |
| 4 | 8 | 5 | 1867.6 | 1780.4 |
| 6 | 8 | 5 | 4850.2 | 4614.6 |
| –7 | 9 | 5 | 256.8 | 344.5 |
| –5 | 9 | 5 | 1027.1 | 1002.1 |
| –3 | 9 | 5 | 8154.8 | 8098.8 |
| –1 | 9 | 5 | 4.9 | 168.6 |
| 1 | 9 | 5 | 2205.2 | 2165.9 |
| 3 | 9 | 5 | 6778.2 | 6404.6 |
| 5 | 9 | 5 | 13.8 | –75.8 |
| –6 | 10 | 5 | 0.5 | –248.5 |
| –4 | 10 | 5 | 151.1 | 314.3 |
| –2 | 10 | 5 | 422.3 | 167.8 |
| 0 | 10 | 5 | 1.8 | –186.9 |
| 2 | 10 | 5 | 217.7 | –144.4 |
| –1 | 11 | 5 | 139.1 | –23.5 |
| –12 | 0 | 6 | 5482.3 | 5301.9 |
| –10 | 0 | 6 | 3196.4 | 2722.8 |
| –8 | 0 | 6 | 570.0 | 500.7 |
| –6 | 0 | 6 | 12801.3 | 12569.0 |
| –4 | 0 | 6 | 30852.8 | 29581.2 |
| –2 | 0 | 6 | 3045.0 | 2873.2 |
| 0 | 0 | 6 | 3862.7 | 4085.3 |
| 2 | 0 | 6 | 62380.6 | 64468.4 |
| 4 | 0 | 6 | 43.1 | –16.8 |
| 6 | 0 | 6 | 410.5 | 237.6 |
| 8 | 0 | 6 | 18024.6 | 17888.3 |
| –11 | 1 | 6 | 737.3 | 753.6 |
| –9 | 1 | 6 | 1340.7 | 1292.0 |
| –7 | 1 | 6 | 3077.2 | 3000.3 |
| –5 | 1 | 6 | 1781.3 | 1920.4 |
| –3 | 1 | 6 | 465.1 | 499.2 |
| –1 | 1 | 6 | 14210.2 | 14217.5 |
| 1 | 1 | 6 | 3201.5 | 3100.8 |
| 3 | 1 | 6 | 176.2 | 356.0 |
| 5 | 1 | 6 | 10596.9 | 10283.9 |
| 7 | 1 | 6 | 1792.6 | 1942.9 |
| 9 | 1 | 6 | 309.3 | 324.4 |
| –12 | 2 | 6 | 628.9 | 653.7 |
| –10 | 2 | 6 | 357.9 | 424.0 |
| –8 | 2 | 6 | 3528.8 | 3559.0 |
| –6 | 2 | 6 | 411.2 | 298.3 |
| –4 | 2 | 6 | 828.8 | 759.9 |
| –2 | 2 | 6 | 8572.4 | 8701.5 |
| 0 | 2 | 6 | 170.1 | 197.0 |
| 2 | 2 | 6 | 20.1 | 45.2 |
| 4 | 2 | 6 | 794.2 | 728.3 |
| 6 | 2 | 6 | 32.4 | –62.8 |
| 8 | 2 | 6 | 92.0 | 110.5 |
| –11 | 3 | 6 | 36.7 | –31.9 |
| –9 | 3 | 6 | 2604.8 | 2682.7 |
| –7 | 3 | 6 | 289.5 | 269.3 |
| –5 | 3 | 6 | 2620.0 | 2729.0 |
| –3 | 3 | 6 | 1203.4 | 1202.2 |
| –1 | 3 | 6 | 5917.2 | 5493.6 |
| 1 | 3 | 6 | 1334.8 | 1317.3 |
| 3 | 3 | 6 | 178.8 | 216.7 |
| 5 | 3 | 6 | 6348.9 | 6336.4 |
| 7 | 3 | 6 | 23.4 | –187.8 |
| 9 | 3 | 6 | 173.0 | 323.2 |
| –10 | 4 | 6 | 86.5 | –174.0 |
| –8 | 4 | 6 | 5535.7 | 5887.0 |
| –6 | 4 | 6 | 77.5 | 73.6 |
| –4 | 4 | 6 | 1008.9 | 1091.7 |
| –2 | 4 | 6 | 12849.4 | 13298.3 |
| 0 | 4 | 6 | 242.9 | 373.0 |
| 2 | 4 | 6 | 2174.3 | 2190.2 |
| 4 | 4 | 6 | 4911.2 | 4886.5 |
| 6 | 4 | 6 | 577.4 | 669.9 |
| 8 | 4 | 6 | 1607.1 | 1660.6 |
| –11 | 5 | 6 | 3091.0 | 3450.8 |
| –9 | 5 | 6 | 864.7 | 1020.9 |
| –7 | 5 | 6 | 1240.7 | 1446.3 |
| –5 | 5 | 6 | 23794.5 | 26122.8 |
| –3 | 5 | 6 | 505.5 | 602.8 |
| –1 | 5 | 6 | 935.6 | 1066.2 |
| 1 | 5 | 6 | 21356.2 | 23725.3 |
| 3 | 5 | 6 | 842.2 | 1013.5 |
| 5 | 5 | 6 | 522.0 | 413.7 |
| 7 | 5 | 6 | 2818.1 | 3225.5 |
| –10 | 6 | 6 | 1133.5 | 1381.3 |
| –8 | 6 | 6 | 1713.0 | 2022.2 |
| –6 | 6 | 6 | 105.7 | 4.0 |
| –4 | 6 | 6 | 4512.4 | 4783.5 |
| –2 | 6 | 6 | 5153.1 | 5507.1 |
| 0 | 6 | 6 | 23.9 | 143.1 |
| 2 | 6 | 6 | 3716.3 | 3934.7 |
| 4 | 6 | 6 | 2414.0 | 2399.9 |
| 6 | 6 | 6 | 235.2 | 141.1 |
| –9 | 7 | 6 | 919.4 | 995.7 |
| –7 | 7 | 6 | 1120.2 | 1121.9 |
| –5 | 7 | 6 | 1040.7 | 1021.6 |
| –3 | 7 | 6 | 296.5 | 325.2 |
| –1 | 7 | 6 | 4390.7 | 4586.0 |
| 1 | 7 | 6 | 347.9 | 372.0 |
| 3 | 7 | 6 | 3.4 | 57.8 |
| 5 | 7 | 6 | 2644.9 | 2360.0 |
| –8 | 8 | 6 | 2096.0 | 2196.3 |
| –6 | 8 | 6 | 761.2 | 776.6 |
| –4 | 8 | 6 | 807.8 | 991.7 |
| –2 | 8 | 6 | 7220.2 | 7552.0 |
| 0 | 8 | 6 | 644.2 | 538.5 |
| 2 | 8 | 6 | 2274.8 | 2194.8 |
| 4 | 8 | 6 | 3188.9 | 2907.2 |
| –7 | 9 | 6 | 623.7 | 519.8 |
| –5 | 9 | 6 | 402.0 | 584.1 |
| –3 | 9 | 6 | 251.7 | 253.4 |
| –1 | 9 | 6 | 1759.1 | 1851.9 |
| 1 | 9 | 6 | 959.4 | 817.0 |
| 3 | 9 | 6 | 13.4 | 74.4 |
| –4 | 10 | 6 | 741.3 | 780.2 |
| –2 | 10 | 6 | 503.4 | 37.4 |
| 0 | 10 | 6 | 102.7 | 131.0 |
| 2 | 10 | 6 | 2247.7 | 2198.1 |
| –11 | 1 | 7 | 48.5 | –76.9 |
| –9 | 1 | 7 | 8763.4 | 8701.2 |
| –7 | 1 | 7 | 236.1 | 33.6 |
| –5 | 1 | 7 | 1892.7 | 1850.3 |
| –3 | 1 | 7 | 13967.2 | 13853.4 |
| –1 | 1 | 7 | 5597.1 | 5469.0 |
| 1 | 1 | 7 | 2222.2 | 2197.3 |
| 3 | 1 | 7 | 5289.0 | 5162.1 |
| 5 | 1 | 7 | 9263.9 | 8611.3 |
| 7 | 1 | 7 | 20.1 | 106.7 |
| –10 | 2 | 7 | 65.1 | 198.1 |
| –8 | 2 | 7 | 1462.9 | 1380.2 |
| –6 | 2 | 7 | 7980.3 | 8031.3 |
| –4 | 2 | 7 | 21.4 | 62.0 |
| –2 | 2 | 7 | 2801.5 | 2820.0 |
| 0 | 2 | 7 | 4898.0 | 4726.3 |
| 2 | 2 | 7 | 2625.2 | 2418.4 |
| 4 | 2 | 7 | 4573.0 | 4364.6 |
| 6 | 2 | 7 | 983.2 | 975.3 |
| 8 | 2 | 7 | 2440.8 | 2362.5 |
| –11 | 3 | 7 | 1473.3 | 1613.4 |
| –9 | 3 | 7 | 8.7 | –141.7 |
| –7 | 3 | 7 | 257.1 | 484.3 |
| –5 | 3 | 7 | 17838.5 | 18283.6 |
| –3 | 3 | 7 | 293.8 | 115.1 |
| –1 | 3 | 7 | 425.7 | 497.5 |
| 1 | 3 | 7 | 27620.9 | 26943.5 |
| 3 | 3 | 7 | 387.8 | 453.3 |
| 5 | 3 | 7 | 52.6 | 72.0 |
| 7 | 3 | 7 | 7622.3 | 7026.3 |
| –10 | 4 | 7 | 484.2 | 571.6 |
| –8 | 4 | 7 | 7149.0 | 7545.2 |
| –6 | 4 | 7 | 2886.2 | 2936.8 |
| –4 | 4 | 7 | 1388.7 | 1425.6 |
| –2 | 4 | 7 | 32880.1 | 33307.0 |
| 0 | 4 | 7 | 1239.8 | 1188.1 |
| 2 | 4 | 7 | 3543.8 | 3322.8 |
| 4 | 4 | 7 | 17549.6 | 17281.9 |
| 6 | 4 | 7 | 469.2 | 480.6 |
| –9 | 5 | 7 | 0.6 | –149.1 |
| –7 | 5 | 7 | 225.1 | 299.9 |
| –5 | 5 | 7 | 1.8 | 91.5 |
| –3 | 5 | 7 | 50.9 | 196.3 |
| –1 | 5 | 7 | 907.4 | 872.1 |
| 1 | 5 | 7 | 48.3 | 226.9 |
| 3 | 5 | 7 | 225.8 | 163.2 |
| 5 | 5 | 7 | 591.1 | 663.0 |
| 7 | 5 | 7 | 78.7 | –33.0 |
| –8 | 6 | 7 | 1244.2 | 1318.8 |
| –6 | 6 | 7 | 19.8 | –23.5 |
| –4 | 6 | 7 | 67.8 | 9.5 |
| –2 | 6 | 7 | 7678.9 | 8150.2 |
| 0 | 6 | 7 | 438.8 | 305.9 |
| 2 | 6 | 7 | 565.2 | 435.7 |
| 4 | 6 | 7 | 4145.5 | 4334.0 |
| 6 | 6 | 7 | 150.9 | –144.6 |
| –7 | 7 | 7 | 16.2 | 74.5 |
| –5 | 7 | 7 | 3767.6 | 3985.6 |
| –3 | 7 | 7 | 1217.5 | 1345.7 |
| –1 | 7 | 7 | 164.1 | –83.2 |
| 1 | 7 | 7 | 6515.6 | 6845.6 |
| 3 | 7 | 7 | 1551.7 | 1732.7 |
| 5 | 7 | 7 | 103.4 | –198.3 |
| –6 | 8 | 7 | 4373.1 | 4747.1 |
| –4 | 8 | 7 | 1743.3 | 1953.7 |
| –2 | 8 | 7 | 5.9 | 42.0 |
| 0 | 8 | 7 | 5332.4 | 5596.8 |
| 2 | 8 | 7 | 4672.5 | 4643.1 |
| 4 | 8 | 7 | 102.5 | –57.7 |
| –5 | 9 | 7 | 14.5 | 18.7 |
| –3 | 9 | 7 | 1426.5 | 1550.5 |
| –1 | 9 | 7 | 897.3 | 823.5 |
| 1 | 9 | 7 | 5.6 | 33.2 |
| –10 | 0 | 8 | 5058.7 | 4860.3 |
| –8 | 0 | 8 | 6393.7 | 6074.5 |
| –6 | 0 | 8 | 1491.3 | 1503.0 |
| –4 | 0 | 8 | 24891.0 | 26090.8 |
| –2 | 0 | 8 | 8225.2 | 8784.2 |
| 0 | 0 | 8 | 392.9 | 362.9 |
| 2 | 0 | 8 | 11405.4 | 11506.4 |
| 4 | 0 | 8 | 6530.2 | 6346.8 |
| 6 | 0 | 8 | 198.8 | 68.9 |
| –11 | 1 | 8 | 421.9 | 405.2 |
| –9 | 1 | 8 | 1056.2 | 1042.5 |
| –7 | 1 | 8 | 3386.1 | 3402.7 |
| –5 | 1 | 8 | 1954.7 | 2120.8 |
| –3 | 1 | 8 | 2772.9 | 2803.0 |
| –1 | 1 | 8 | 5337.8 | 5529.2 |
| 1 | 1 | 8 | 3582.2 | 3700.5 |
| 3 | 1 | 8 | 1620.5 | 1643.2 |
| 5 | 1 | 8 | 1102.8 | 1005.6 |
| 7 | 1 | 8 | 2608.2 | 2300.0 |
| –10 | 2 | 8 | 1898.4 | 2049.2 |
| –8 | 2 | 8 | 5283.8 | 5340.8 |
| –6 | 2 | 8 | 7183.0 | 7373.4 |
| –4 | 2 | 8 | 13584.2 | 13704.4 |
| –2 | 2 | 8 | 4713.7 | 4757.8 |
| 0 | 2 | 8 | 19167.1 | 19632.8 |
| 2 | 2 | 8 | 8659.2 | 8850.3 |
| 4 | 2 | 8 | 1509.0 | 1305.8 |
| 6 | 2 | 8 | 8003.1 | 7394.3 |
| –9 | 3 | 8 | 96.7 | 270.9 |
| –7 | 3 | 8 | 7254.6 | 7515.4 |
| –5 | 3 | 8 | 4152.4 | 4242.1 |
| –3 | 3 | 8 | 1297.8 | 1212.5 |
| –1 | 3 | 8 | 13147.3 | 12961.5 |
| 1 | 3 | 8 | 2591.9 | 2481.4 |
| 3 | 3 | 8 | 2233.9 | 2186.1 |
| 5 | 3 | 8 | 2522.0 | 2420.5 |
| –10 | 4 | 8 | 26.4 | –206.1 |
| –8 | 4 | 8 | 277.1 | 531.7 |
| –6 | 4 | 8 | 4192.1 | 4465.9 |
| –4 | 4 | 8 | 0.1 | –44.8 |
| –2 | 4 | 8 | 4.1 | –8.2 |
| 0 | 4 | 8 | 8712.8 | 8603.9 |
| 2 | 4 | 8 | 19.8 | –51.7 |
| 4 | 4 | 8 | 330.8 | 384.2 |
| 6 | 4 | 8 | 3739.3 | 3516.5 |
| –9 | 5 | 8 | 3424.8 | 3609.3 |
| –7 | 5 | 8 | 1731.1 | 1895.6 |
| –5 | 5 | 8 | 1967.6 | 2199.7 |
| –3 | 5 | 8 | 17004.3 | 17771.1 |
| –1 | 5 | 8 | 4162.3 | 4336.0 |
| 1 | 5 | 8 | 57.5 | –156.1 |
| 3 | 5 | 8 | 19639.7 | 18801.1 |
| 5 | 5 | 8 | 776.2 | 706.4 |
| –8 | 6 | 8 | 30.9 | –44.1 |
| –6 | 6 | 8 | 2033.8 | 2212.2 |
| –4 | 6 | 8 | 24.9 | –61.4 |
| –2 | 6 | 8 | 192.8 | 267.5 |
| 0 | 6 | 8 | 5411.7 | 5674.9 |
| 2 | 6 | 8 | 133.6 | 69.2 |
| 4 | 6 | 8 | 600.3 | 615.5 |
| –7 | 7 | 8 | 2699.8 | 2670.0 |
| –5 | 7 | 8 | 3114.9 | 3324.2 |
| –3 | 7 | 8 | 689.4 | 536.5 |
| –1 | 7 | 8 | 4040.2 | 4405.4 |
| 1 | 7 | 8 | 3038.1 | 3249.6 |
| 3 | 7 | 8 | 1034.4 | 1114.9 |
| –6 | 8 | 8 | 79.0 | –256.8 |
| –4 | 8 | 8 | 297.7 | 313.3 |
| –2 | 8 | 8 | 119.5 | 130.1 |
| 0 | 8 | 8 | 846.4 | 782.9 |
| 2 | 8 | 8 | 76.4 | –216.8 |
| –9 | 1 | 9 | 849.1 | 893.4 |
| –7 | 1 | 9 | 1085.0 | 1091.5 |
| –5 | 1 | 9 | 12.8 | –23.9 |
| –3 | 1 | 9 | 2497.4 | 2700.2 |
| –1 | 1 | 9 | 5679.0 | 5699.6 |
| 1 | 1 | 9 | 517.6 | 435.8 |
| 3 | 1 | 9 | 476.4 | 497.6 |
| 5 | 1 | 9 | 1855.7 | 1866.5 |
| –10 | 2 | 9 | 745.2 | 748.1 |
| –8 | 2 | 9 | 7.9 | 76.7 |
| –6 | 2 | 9 | 1485.9 | 1651.2 |
| –4 | 2 | 9 | 7155.7 | 7236.3 |
| –2 | 2 | 9 | 134.1 | 194.1 |
| 0 | 2 | 9 | 2250.8 | 2193.9 |
| 2 | 2 | 9 | 7699.4 | 7762.5 |
| 4 | 2 | 9 | 25.3 | 139.6 |
| –9 | 3 | 9 | 16.2 | 90.1 |
| –7 | 3 | 9 | 1963.6 | 1923.6 |
| –5 | 3 | 9 | 546.3 | 576.8 |
| –3 | 3 | 9 | 1017.6 | 1041.1 |
| –1 | 3 | 9 | 2112.3 | 2151.5 |
| 1 | 3 | 9 | 25.8 | 85.8 |
| 3 | 3 | 9 | 4271.9 | 4205.3 |
| 5 | 3 | 9 | 1379.1 | 1129.2 |
| –8 | 4 | 9 | 138.6 | 99.0 |
| –6 | 4 | 9 | 555.9 | 408.7 |
| –4 | 4 | 9 | 1468.7 | 1497.7 |
| –2 | 4 | 9 | 544.3 | 514.3 |
| 0 | 4 | 9 | 18.6 | 84.1 |
| 2 | 4 | 9 | 1369.7 | 1426.2 |
| 4 | 4 | 9 | 1238.6 | 1325.5 |
| –7 | 5 | 9 | 80.9 | –148.4 |
| –5 | 5 | 9 | 131.0 | 77.9 |
| –3 | 5 | 9 | 50.3 | 140.2 |
| –1 | 5 | 9 | 108.1 | 12.2 |
| 1 | 5 | 9 | 403.4 | 280.2 |
| 3 | 5 | 9 | 41.7 | 29.5 |
| –6 | 6 | 9 | 3.7 | –15.3 |
| –4 | 6 | 9 | 21.8 | 34.6 |
| –2 | 6 | 9 | 792.1 | 985.0 |
| 0 | 6 | 9 | 992.5 | 947.8 |
| 2 | 6 | 9 | 14.0 | 223.6 |
| –5 | 7 | 9 | 336.3 | 463.3 |
| –3 | 7 | 9 | 50.8 | 12.3 |
| –1 | 7 | 9 | 1487.3 | 1493.5 |
| 1 | 7 | 9 | 24.0 | 144.0 |
| –8 | 0 | 10 | 5512.6 | 5320.8 |
| –6 | 0 | 10 | 8153.2 | 8508.5 |
| –4 | 0 | 10 | 1474.0 | 1565.8 |
| –2 | 0 | 10 | 19501.1 | 20329.4 |
| 0 | 0 | 10 | 13368.3 | 14012.9 |
| 2 | 0 | 10 | 31.4 | 43.2 |
| 4 | 0 | 10 | 14490.5 | 13678.1 |
| –7 | 1 | 10 | 9.8 | –142.9 |
| –5 | 1 | 10 | 2699.0 | 2949.3 |
| –3 | 1 | 10 | 945.3 | 1156.6 |
| –1 | 1 | 10 | 790.5 | 879.3 |
| 1 | 1 | 10 | 3780.1 | 3691.3 |
| 3 | 1 | 10 | 804.3 | 843.2 |
| –8 | 2 | 10 | 37.2 | 144.8 |
| –6 | 2 | 10 | 3074.5 | 3141.5 |
| –4 | 2 | 10 | 3156.6 | 3205.6 |
| –2 | 2 | 10 | 759.1 | 753.3 |
| 0 | 2 | 10 | 2943.3 | 3070.6 |
| 2 | 2 | 10 | 2032.3 | 1906.0 |
| –7 | 3 | 10 | 1466.8 | 1475.5 |
| –5 | 3 | 10 | 1582.0 | 1498.9 |
| –3 | 3 | 10 | 3780.7 | 3780.7 |
| –1 | 3 | 10 | 507.6 | 321.3 |
| 1 | 3 | 10 | 4173.0 | 3989.5 |
| 3 | 3 | 10 | 1724.6 | 1794.5 |
| –6 | 4 | 10 | 1621.1 | 1741.4 |
| –4 | 4 | 10 | 3154.3 | 3055.9 |
| –2 | 4 | 10 | 9.0 | –269.4 |
| 0 | 4 | 10 | 1293.9 | 1271.1 |
| 2 | 4 | 10 | 3895.8 | 3586.1 |
| –5 | 5 | 10 | 6.2 | –128.5 |
| –3 | 5 | 10 | 5832.3 | 5800.1 |
| –1 | 5 | 10 | 7045.7 | 7258.3 |
| 1 | 5 | 10 | 303.2 | 366.7 |
| –4 | 6 | 10 | 640.9 | 766.2 |
| –2 | 6 | 10 | 1364.6 | 1488.3 |
| –5 | 1 | 11 | 1498.5 | 1414.0 |
| –3 | 1 | 11 | 2081.9 | 2137.4 |
| –1 | 1 | 11 | 2787.0 | 2806.7 |
| 1 | 1 | 11 | 101.4 | –1.1 |
| –6 | 2 | 11 | 2784.1 | 2724.5 |
| –4 | 2 | 11 | 1101.7 | 1279.7 |
| –2 | 2 | 11 | 6.7 | –130.2 |
| 0 | 2 | 11 | 2622.7 | 2637.9 |
| –5 | 3 | 11 | 3936.6 | 4034.9 |
| –3 | 3 | 11 | 322.5 | –215.1 |
| –1 | 3 | 11 | 89.5 | 21.5 |
| –4 | 4 | 11 | 81.8 | 245.8 |
| –2 | 4 | 11 | 3688.1 | 3798.9 |