data_ashope

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

?

;

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'H8 As2 Fe0.08 Mg0.05 Mn0.05 O12 Zn2.82'

_chemical_formula_weight          542.68

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'O'  'O'   0.0106   0.0060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Zn'  'Zn'   0.2839   1.4301

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'As'  'As'   0.0499   2.0058

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'H'  'H'   0.0000   0.0000

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Fe'  'Fe'   0.3463   0.8444

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Mn'  'Mn'   0.3368   0.7283

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Mg'  'Mg'   0.0486   0.0363

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_symmetry_cell_setting            ?

_symmetry_space_group_name_H-M    ?

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-x+1/2, -y, z+1/2'

'-x, y+1/2, -z'

'x+1/2, -y+1/2, -z+1/2'

'-x, -y, -z'

'x-1/2, y, -z-1/2'

'x, -y-1/2, z'

'-x-1/2, y-1/2, z-1/2'

_cell_length_a                    10.804(2)

_cell_length_b                    19.003(4)

_cell_length_c                    5.1120(10)

_cell_angle_alpha                 90.00

_cell_angle_beta                  90.00

_cell_angle_gamma                 90.00

_cell_volume                      1049.5(4)

_cell_formula_units_Z             4

_cell_measurement_temperature     293(2)

_cell_measurement_reflns_used     ?

_cell_measurement_theta_min       ?

_cell_measurement_theta_max       ?

_exptl_crystal_description        ?

_exptl_crystal_colour             ?

_exptl_crystal_size_max           0.08

_exptl_crystal_size_mid           0.07

_exptl_crystal_size_min           0.07

_exptl_crystal_density_meas       ?

_exptl_crystal_density_diffrn     3.434

_exptl_crystal_density_method     'not measured'

_exptl_crystal_F_000              1034

_exptl_absorpt_coefficient_mu     12.881

_exptl_absorpt_correction_type    ?

_exptl_absorpt_correction_T_min   0.4255

_exptl_absorpt_correction_T_max   0.4658

_exptl_absorpt_process_details    ?

_exptl_special_details

;

?

;

_diffrn_ambient_temperature       293(2)

_diffrn_radiation_wavelength      0.71073

_diffrn_radiation_type            MoK\a

_diffrn_radiation_source          'fine-focus sealed tube'

_diffrn_radiation_monochromator   graphite

_diffrn_measurement_device_type   ?

_diffrn_measurement_method        ?

_diffrn_detector_area_resol_mean  ?

_diffrn_standards_number          ?

_diffrn_standards_interval_count  ?

_diffrn_standards_interval_time   ?

_diffrn_standards_decay_%         ?

_diffrn_reflns_number             3550

_diffrn_reflns_av_R_equivalents   0.0384

_diffrn_reflns_av_sigmaI/netI     0.0413

_diffrn_reflns_limit_h_min        -16

_diffrn_reflns_limit_h_max        16

_diffrn_reflns_limit_k_min        -28

_diffrn_reflns_limit_k_max        28

_diffrn_reflns_limit_l_min        -7

_diffrn_reflns_limit_l_max        7

_diffrn_reflns_theta_min          3.77

_diffrn_reflns_theta_max          32.57

_reflns_number_total              1953

_reflns_number_gt                 1355

_reflns_threshold_expression      >2sigma(I)

_computing_data_collection        ?

_computing_cell_refinement        ?

_computing_data_reduction         ?

_computing_structure_solution     'SHELXS-97 (Sheldrick, 1990)'

_computing_structure_refinement   'SHELXL-97 (Sheldrick, 1997)'

_computing_molecular_graphics     ?

_computing_publication_material   ?

_refine_special_details

;

Refinement of F^2^ against ALL reflections.  The weighted R-factor wR and

goodness of fit S are based on F^2^, conventional R-factors R are based

on F, with F set to zero for negative F^2^. The threshold expression of

F^2^ > 2sigma(F^2^) is used only for calculating R-factors(gt) etc. and is

not relevant to the choice of reflections for refinement.  R-factors based

on F^2^ are statistically about twice as large as those based on F, and R-

factors based on ALL data will be even larger.

;

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'calc w=1/[\s^2^(Fo^2^)+(0.0450P)^2^+0.5000P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      direct

_atom_sites_solution_secondary    difmap

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     mixed

_refine_ls_extinction_method      SHELXL

_refine_ls_extinction_coef        0.0000(2)

_refine_ls_extinction_expression

'Fc^*^=kFc[1+0.001xFc^2^\l^3^/sin(2\q)]^-1/4^'

_refine_ls_number_reflns          1953

_refine_ls_number_parameters      98

_refine_ls_number_restraints      0

_refine_ls_R_factor_all           0.0706

_refine_ls_R_factor_gt            0.0353

_refine_ls_wR_factor_ref          0.0848

_refine_ls_wR_factor_gt           0.0739

_refine_ls_goodness_of_fit_ref    1.015

_refine_ls_restrained_S_all       1.015

_refine_ls_shift/su_max           2.373

_refine_ls_shift/su_mean          0.024

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_symetry_multiplicity

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

As As 0.10007(4) 0.095516(19) 0.71834(7) 0.01728(12) Uani 1 1 d . . .

Zn1 Zn 0.23741(6) 0.2500 0.57469(13) 0.01912(17) Uani 0.82 2 d SP . .

Fe1 Fe 0.23741(6) 0.2500 0.57469(13) 0.01912(17) Uani 0.08 2 d SP . .

Mn1 Mn 0.23741(6) 0.2500 0.57469(13) 0.01912(17) Uani 0.05 2 d SP . .

Mg1 Mg 0.23741(6) 0.2500 0.57469(13) 0.01912(17) Uani 0.05 2 d SP . .

Zn2 Zn 0.14543(4) -0.00046(2) 0.20551(8) 0.01842(12) Uani 1 1 d . . .

O4 O 0.1407(3) 0.17731(15) 0.7895(5) 0.0299(7) Uani 1 1 d . . .

O5 O 0.0996(3) 0.08142(15) 0.3953(6) 0.0389(8) Uani 1 1 d . . .

O6 O 0.4619(3) 0.07907(15) 0.6452(6) 0.0290(6) Uani 1 1 d . . .

O7 O 0.1986(2) 0.03623(14) 0.8592(5) 0.0226(6) Uani 1 1 d . . .

0W1 O 0.1072(4) 0.2500 0.2645(8) 0.0290(10) Uani 1 2 d S . .

OW2 O 0.3858(4) 0.2500 0.8494(10) 0.0366(11) Uani 1 2 d S . .

OW3 O 0.3354(4) 0.17204(19) 0.3427(8) 0.0375(8) Uani 1 1 d . . .

H11 H 0.115(6) 0.290(4) 0.169(13) 0.09(2) Uiso 1 1 d . . .

H31 H 0.380(8) 0.135(6) 0.374(17) 0.13(4) Uiso 1 1 d . . .

H32 H 0.290(9) 0.145(6) 0.286(19) 0.14(4) Uiso 1 1 d . . .

H21 H 0.462(9) 0.2500 0.795(15) 0.06(3) Uiso 1 2 d S . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

As 0.0202(2) 0.01588(19) 0.01579(19) -0.00028(14) 0.00112(14) 0.00072(15)

Zn1 0.0181(3) 0.0218(3) 0.0175(3) 0.000 0.0016(2) 0.000

Fe1 0.0181(3) 0.0218(3) 0.0175(3) 0.000 0.0016(2) 0.000

Mn1 0.0181(3) 0.0218(3) 0.0175(3) 0.000 0.0016(2) 0.000

Mg1 0.0181(3) 0.0218(3) 0.0175(3) 0.000 0.0016(2) 0.000

Zn2 0.0175(2) 0.0217(2) 0.0160(2) -0.00066(17) 0.00024(17) -0.00016(16)

O4 0.0461(19) 0.0187(14) 0.0247(15) -0.0050(12) 0.0138(13) -0.0117(12)

O5 0.074(3) 0.0271(16) 0.0152(15) -0.0048(12) -0.0058(15) 0.0166(15)

O6 0.0194(14) 0.0261(14) 0.0416(17) 0.0077(13) -0.0045(13) -0.0025(11)

O7 0.0191(14) 0.0303(15) 0.0184(12) 0.0058(11) 0.0053(11) 0.0041(11)

0W1 0.029(2) 0.034(3) 0.023(2) 0.000 -0.0035(18) 0.000

OW2 0.020(2) 0.055(3) 0.035(3) 0.000 -0.004(2) 0.000

OW3 0.036(2) 0.0329(19) 0.043(2) 0.0027(16) 0.0028(16) 0.0090(15)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

As O4 1.655(3) . ?

As O5 1.673(3) . ?

As O6 1.677(3) 6_557 ?

As O7 1.709(3) . ?

Zn1 O4 2.051(3) . ?

Zn1 O4 2.051(3) 7_565 ?

Zn1 0W1 2.120(4) . ?

Zn1 OW2 2.131(5) . ?

Zn1 OW3 2.173(4) . ?

Zn1 OW3 2.173(4) 7_565 ?

Zn2 O5 1.899(3) . ?

Zn2 O6 1.916(3) 2_554 ?

Zn2 O7 1.979(3) 2_554 ?

Zn2 O7 1.988(3) 1_554 ?

O6 As 1.677(3) 6_657 ?

O6 Zn2 1.916(3) 2 ?

O7 Zn2 1.979(3) 2 ?

O7 Zn2 1.988(3) 1_556 ?

0W1 H11 0.91(7) . ?

OW2 H21 0.87(9) . ?

OW3 H31 0.86(11) . ?

OW3 H32 0.77(10) . ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

O4 As O5 111.60(15) . . ?

O4 As O6 108.63(14) . 6_557 ?

O5 As O6 112.21(17) . 6_557 ?

O4 As O7 111.18(15) . . ?

O5 As O7 108.19(14) . . ?

O6 As O7 104.86(13) 6_557 . ?

O4 Zn1 O4 84.67(16) . 7_565 ?

O4 Zn1 0W1 93.57(13) . . ?

O4 Zn1 0W1 93.57(13) 7_565 . ?

O4 Zn1 OW2 91.75(14) . . ?

O4 Zn1 OW2 91.75(14) 7_565 . ?

0W1 Zn1 OW2 172.80(19) . . ?

O4 Zn1 OW3 94.67(13) . . ?

O4 Zn1 OW3 178.51(15) 7_565 . ?

0W1 Zn1 OW3 85.14(15) . . ?

OW2 Zn1 OW3 89.60(15) . . ?

O4 Zn1 OW3 178.51(15) . 7_565 ?

O4 Zn1 OW3 94.67(13) 7_565 7_565 ?

0W1 Zn1 OW3 85.14(15) . 7_565 ?

OW2 Zn1 OW3 89.60(15) . 7_565 ?

OW3 Zn1 OW3 85.9(2) . 7_565 ?

O5 Zn2 O6 124.25(14) . 2_554 ?

O5 Zn2 O7 107.49(13) . 2_554 ?

O6 Zn2 O7 108.15(12) 2_554 2_554 ?

O5 Zn2 O7 104.06(13) . 1_554 ?

O6 Zn2 O7 107.78(12) 2_554 1_554 ?

O7 Zn2 O7 103.17(8) 2_554 1_554 ?

As O4 Zn1 130.52(15) . . ?

As O5 Zn2 129.39(17) . . ?

As O6 Zn2 128.12(16) 6_657 2 ?

As O7 Zn2 126.12(14) . 2 ?

As O7 Zn2 115.23(14) . 1_556 ?

Zn2 O7 Zn2 118.63(13) 2 1_556 ?

Zn1 0W1 H11 110(4) . . ?

Zn1 OW2 H21 120(5) . . ?

Zn1 OW3 H31 136(6) . . ?

Zn1 OW3 H32 111(8) . . ?

H31 OW3 H32 83(9) . . ?

loop_

_geom_hbond_atom_site_label_D

_geom_hbond_atom_site_label_H

_geom_hbond_atom_site_label_A

_geom_hbond_distance_DH

_geom_hbond_distance_HA

_geom_hbond_distance_DA

_geom_hbond_angle_DHA

_geom_hbond_site_symmetry_A

OW3 H31 O6  0.86(11) 1.96(10) 2.717(5) 145(9) .

OW3 H32 O5  0.77(10) 2.45(10) 3.087(5) 141(9) .

OW2 H21 O4  0.87(9) 2.41(8) 3.161(5) 144.6(15) 4_556

OW2 H21 O4  0.87(9) 2.41(8) 3.161(5) 144.6(15) 6_657

_diffrn_measured_fraction_theta_max    0.996

_diffrn_reflns_theta_full              32.57

_diffrn_measured_fraction_theta_full   0.996

_refine_diff_density_max    1.244

_refine_diff_density_min   -0.824

_refine_diff_density_rms    0.205