data_obradovicite-NaCu

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

?

;

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'As Cu0.10 Fe1.50 K0.87 Mo4 O26.13'

_chemical_formula_weight          1001.08

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'Mo'  'Mo'  -1.6832   0.6857

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'As'  'As'   0.0499   2.0058

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Cu'  'Cu'   0.3201   1.2651

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Fe'  'Fe'   0.3463   0.8444

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'K'  'K'   0.2009   0.2494

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'O'  'O'   0.0106   0.0060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_symmetry_cell_setting            ?

_symmetry_space_group_name_H-M    Pnmb

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'x, -y, z'

'-x, y+1/2, z-1/2'

'-x, -y+1/2, z-1/2'

'-x, -y, -z'

'-x, y, -z'

'x, -y-1/2, -z+1/2'

'x, y-1/2, -z+1/2'

_cell_length_a                    14.872(4)

_cell_length_b                    11.091(3)

_cell_length_c                    15.032(4)

_cell_angle_alpha                 90.00

_cell_angle_beta                  90.00

_cell_angle_gamma                 90.00

_cell_volume                      2479.4(12)

_cell_formula_units_Z             4

_cell_measurement_temperature     293(2)

_cell_measurement_reflns_used     ?

_cell_measurement_theta_min       ?

_cell_measurement_theta_max       ?

_exptl_crystal_description        ?

_exptl_crystal_colour             ?

_exptl_crystal_size_max           0.06

_exptl_crystal_size_mid           0.04

_exptl_crystal_size_min           0.02

_exptl_crystal_density_meas       ?

_exptl_crystal_density_diffrn     2.682

_exptl_crystal_density_method     'not measured'

_exptl_crystal_F_000              1874

_exptl_absorpt_coefficient_mu     4.477

_exptl_absorpt_correction_type    multiscan

_exptl_absorpt_correction_T_min   0.7750

_exptl_absorpt_correction_T_max   0.9158

_exptl_absorpt_process_details    ABSCOR

_exptl_special_details

;

?

;

_diffrn_ambient_temperature       293(2)

_diffrn_radiation_wavelength      0.71075

_diffrn_radiation_type            MoK\a

_diffrn_radiation_source          'fine-focus sealed tube'

_diffrn_radiation_monochromator   graphite

_diffrn_measurement_device_type   ?

_diffrn_measurement_method        ?

_diffrn_detector_area_resol_mean  ?

_diffrn_standards_number          ?

_diffrn_standards_interval_count  ?

_diffrn_standards_interval_time   ?

_diffrn_standards_decay_%         ?

_diffrn_reflns_number             7967

_diffrn_reflns_av_R_equivalents   0.1584

_diffrn_reflns_av_sigmaI/netI     0.0691

_diffrn_reflns_limit_h_min        -12

_diffrn_reflns_limit_h_max        12

_diffrn_reflns_limit_k_min        -9

_diffrn_reflns_limit_k_max        9

_diffrn_reflns_limit_l_min        -12

_diffrn_reflns_limit_l_max        12

_diffrn_reflns_theta_min          3.04

_diffrn_reflns_theta_max          17.22

_reflns_number_total              815

_reflns_number_gt                 587

_reflns_threshold_expression      >2sigma(I)

_computing_data_collection        ?

_computing_cell_refinement        ?

_computing_data_reduction         ?

_computing_structure_solution     'SHELXS-97 (Sheldrick, 1990)'

_computing_structure_refinement   'SHELXL-97 (Sheldrick, 1997)'

_computing_molecular_graphics     ?

_computing_publication_material   ?

_refine_special_details

;

Refinement of F^2^ against ALL reflections.  The weighted R-factor wR and

goodness of fit S are based on F^2^, conventional R-factors R are based

on F, with F set to zero for negative F^2^. The threshold expression of

F^2^ > 2sigma(F^2^) is used only for calculating R-factors(gt) etc. and is

not relevant to the choice of reflections for refinement.  R-factors based

on F^2^ are statistically about twice as large as those based on F, and R-

factors based on ALL data will be even larger.

;

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'calc w=1/[\s^2^(Fo^2^)+(0.1387P)^2^+58.5759P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      direct

_atom_sites_solution_secondary    difmap

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     mixed

_refine_ls_extinction_method      none

_refine_ls_extinction_coef        ?

_refine_ls_number_reflns          815

_refine_ls_number_parameters      158

_refine_ls_number_restraints      0

_refine_ls_R_factor_all           0.1006

_refine_ls_R_factor_gt            0.0730

_refine_ls_wR_factor_ref          0.2145

_refine_ls_wR_factor_gt           0.1924

_refine_ls_goodness_of_fit_ref    1.067

_refine_ls_restrained_S_all       1.067

_refine_ls_shift/su_max           0.006

_refine_ls_shift/su_mean          0.000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_symmetry_multiplicity

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

Mo1 Mo 0.2094(2) 0.6596(3) 0.47874(18) 0.0310(15) Uani 1 1 d . . .

Mo2 Mo 0.3369(3) 0.5000 0.3221(3) 0.0300(17) Uani 1 2 d S . .

Mo3 Mo 0.3844(3) 0.5000 0.5480(3) 0.0349(18) Uani 1 2 d S . .

Fe1 Fe 0.2011(5) 0.7500 0.2500 0.032(2) Uani 1 2 d S . .

Fe2 Fe 0.0000 0.5000 0.5000 0.030(3) Uani 1 4 d S . .

As As 0.0991(4) 0.5000 0.3073(3) 0.0304(19) Uani 1 2 d S . .

O1 O 0.189(2) 0.5000 0.3773(18) 0.035(9) Uani 1 2 d S . .

O2 O 0.242(2) 0.5000 0.5466(19) 0.034(9) Uani 1 2 d S . .

O3 O 0.2972(13) 0.6256(16) 0.2556(13) 0.026(6) Uiso 1 1 d . . .

O4 O 0.3405(14) 0.3877(16) 0.4340(12) 0.027(6) Uiso 1 1 d . . .

O5 O 0.1997(13) 0.7548(17) 0.3851(13) 0.027(6) Uani 1 1 d . . .

O6 O 0.0942(13) 0.6263(18) 0.5057(12) 0.025(6) Uani 1 1 d . . .

O7 O 0.1086(15) 0.8791(18) 0.2542(13) 0.041(7) Uani 1 1 d . . .

O8 O 0.0068(18) 0.5000 0.3684(17) 0.021(8) Uiso 1 2 d S . .

O9 O 0.3904(13) 0.3806(16) 0.6169(12) 0.025(6) Uiso 1 1 d . . .

O10 O 0.450(2) 0.5000 0.3021(19) 0.043(10) Uani 1 2 d S . .

O11 O 0.2400(14) 0.7612(19) 0.5585(16) 0.043(7) Uani 1 1 d . . .

O12 O 0.5000 0.5000 0.5000 0.029(12) Uiso 1 4 d S . .

Cu Cu 0.0000 0.0000 0.5000 0.11(4) Uani 0.21(4) 4 d SP . .

OW1 O 0.161(4) 0.0000 0.437(3) 0.13(2) Uani 1 2 d S . .

OW2 O -0.030(2) 0.824(3) 0.378(2) 0.139(15) Uani 1 1 d . . .

K1 K 0.182(2) 0.0000 0.618(2) 0.101(19) Uiso 0.47(5) 2 d SP . .

K2 K 0.226(5) 0.7500 0.7500 0.21(4) Uiso 0.40(6) 2 d SP . .

OW3 O 0.155(5) 0.0000 0.789(4) 0.18(3) Uiso 1 2 d S . .

OW4 O 0.425(3) 0.182(4) 0.390(4) 0.16(3) Uiso 0.91(11) 1 d P . .

OW5 O 0.444(6) 0.162(8) 0.533(5) 0.050 Uiso 0.26(4) 1 d P . .

OW6 O 0.273(9) 0.0000 0.464(7) 0.050 Uiso 0.32(7) 2 d SP . .

OW7 O 0.404(5) 0.154(7) 0.317(6) 0.050 Uiso 0.30(5) 1 d P . .

OW8 O 0.36(2) 0.0000 0.461(15) 0.24(16) Uiso 0.37(19) 2 d SP . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

Mo1 0.048(3) 0.030(2) 0.015(2) -0.0024(18) -0.0028(17) -0.0016(18)

Mo2 0.032(4) 0.035(3) 0.023(3) 0.000 -0.001(3) 0.000

Mo3 0.032(4) 0.046(3) 0.027(3) 0.000 -0.002(2) 0.000

Fe1 0.043(6) 0.028(4) 0.023(5) 0.004(4) 0.000 0.000

Fe2 0.036(8) 0.034(7) 0.021(7) 0.000 0.003(5) 0.000

As 0.037(4) 0.035(4) 0.019(3) 0.000 -0.001(3) 0.000

O1 0.06(3) 0.030(19) 0.014(19) 0.000 -0.002(19) 0.000

O2 0.04(2) 0.04(2) 0.02(2) 0.000 -0.002(16) 0.000

O5 0.024(15) 0.035(13) 0.021(12) 0.000(12) 0.002(11) 0.018(11)

O6 0.012(14) 0.047(15) 0.017(13) 0.008(11) 0.008(11) 0.001(11)

O7 0.057(18) 0.048(15) 0.017(13) 0.003(13) 0.020(13) -0.001(13)

O10 0.05(3) 0.04(2) 0.04(2) 0.000 0.033(18) 0.000

O11 0.024(16) 0.032(15) 0.073(18) 0.022(14) -0.006(13) 0.012(12)

Cu 0.14(7) 0.13(6) 0.05(5) 0.000 0.06(4) 0.000

OW1 0.17(6) 0.04(3) 0.18(5) 0.000 -0.12(4) 0.000

OW2 0.12(3) 0.13(3) 0.16(3) 0.07(3) 0.05(3) 0.01(2)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

Mo1 O11 1.71(2) . ?

Mo1 O5 1.765(19) . ?

Mo1 O6 1.799(19) . ?

Mo1 O2 2.101(16) . ?

Mo1 O4 2.13(2) 2_565 ?

Mo1 O1 2.356(18) . ?

Mo2 O10 1.70(3) . ?

Mo2 O3 1.813(19) 2_565 ?

Mo2 O3 1.813(19) . ?

Mo2 O4 2.094(18) . ?

Mo2 O4 2.094(18) 2_565 ?

Mo2 O1 2.34(3) . ?

Mo3 O9 1.684(18) 2_565 ?

Mo3 O9 1.684(18) . ?

Mo3 O12 1.865(5) . ?

Mo3 O2 2.11(3) . ?

Mo3 O4 2.216(19) 2_565 ?

Mo3 O4 2.216(19) . ?

Fe1 O7 1.99(2) . ?

Fe1 O7 1.99(2) 7_575 ?

Fe1 O3 1.988(19) . ?

Fe1 O3 1.988(19) 7_575 ?

Fe1 O5 2.032(19) . ?

Fe1 O5 2.032(19) 7_575 ?

Fe2 O8 1.98(3) . ?

Fe2 O8 1.98(3) 5_566 ?

Fe2 O6 1.98(2) 2_565 ?

Fe2 O6 1.98(2) . ?

Fe2 O6 1.98(2) 5_566 ?

Fe2 O6 1.98(2) 6_556 ?

As O7 1.64(2) 8 ?

As O7 1.64(2) 7_575 ?

As O8 1.65(3) . ?

As O1 1.71(3) . ?

O1 Mo1 2.356(18) 2_565 ?

O2 Mo1 2.101(16) 2_565 ?

O4 Mo1 2.13(2) 2_565 ?

O7 As 1.64(2) 7_575 ?

O11 K2 2.89(2) . ?

O11 K1 2.92(3) 1_565 ?

O12 Mo3 1.865(5) 5_666 ?

Cu K1 3.24(4) . ?

Cu K1 3.24(4) 5_556 ?

OW1 OW6 1.72(14) . ?

OW1 K1 2.74(6) . ?

OW2 K1 2.99(4) 5_566 ?

K1 OW3 2.60(7) . ?

K1 OW6 2.68(12) . ?

K1 O11 2.92(3) 2_565 ?

K1 O11 2.92(3) 1_545 ?

K1 OW2 2.99(4) 6_546 ?

K1 OW2 2.99(4) 5_566 ?

K1 K2 3.47(3) 2_565 ?

K1 K2 3.47(3) 1_545 ?

K2 O11 2.89(2) 7_576 ?

K2 OW3 3.02(4) 7_566 ?

K2 OW3 3.02(4) 1_565 ?

K2 K1 3.47(3) 7_566 ?

K2 K1 3.47(3) 1_565 ?

OW3 K2 3.02(4) 2_565 ?

OW3 K2 3.02(4) 1_545 ?

OW4 OW7 1.18(8) . ?

OW6 OW8 1.3(3) . ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

O11 Mo1 O5 100.8(10) . . ?

O11 Mo1 O6 103.3(10) . . ?

O5 Mo1 O6 103.0(9) . . ?

O11 Mo1 O2 98.8(9) . . ?

O5 Mo1 O2 155.5(9) . . ?

O6 Mo1 O2 86.6(11) . . ?

O11 Mo1 O4 98.1(9) . 2_565 ?

O5 Mo1 O4 88.3(8) . 2_565 ?

O6 Mo1 O4 153.3(8) . 2_565 ?

O2 Mo1 O4 74.4(10) . 2_565 ?

O11 Mo1 O1 169.9(10) . . ?

O5 Mo1 O1 85.6(8) . . ?

O6 Mo1 O1 82.6(10) . . ?

O2 Mo1 O1 73.2(8) . . ?

O4 Mo1 O1 74.1(9) 2_565 . ?

O10 Mo2 O3 102.9(9) . 2_565 ?

O10 Mo2 O3 102.9(9) . . ?

O3 Mo2 O3 100.4(12) 2_565 . ?

O10 Mo2 O4 96.7(10) . . ?

O3 Mo2 O4 89.7(8) 2_565 . ?

O3 Mo2 O4 155.3(8) . . ?

O10 Mo2 O4 96.7(10) . 2_565 ?

O3 Mo2 O4 155.3(8) 2_565 2_565 ?

O3 Mo2 O4 89.7(8) . 2_565 ?

O4 Mo2 O4 73.0(10) . 2_565 ?

O10 Mo2 O1 169.5(12) . . ?

O3 Mo2 O1 83.7(7) 2_565 . ?

O3 Mo2 O1 83.7(7) . . ?

O4 Mo2 O1 74.9(8) . . ?

O4 Mo2 O1 74.9(8) 2_565 . ?

O9 Mo3 O9 103.7(12) 2_565 . ?

O9 Mo3 O12 100.9(7) 2_565 . ?

O9 Mo3 O12 100.9(7) . . ?

O9 Mo3 O2 93.4(8) 2_565 . ?

O9 Mo3 O2 93.4(8) . . ?

O12 Mo3 O2 156.7(8) . . ?

O9 Mo3 O4 92.8(8) 2_565 2_565 ?

O9 Mo3 O4 159.0(8) . 2_565 ?

O12 Mo3 O4 88.4(5) . 2_565 ?

O2 Mo3 O4 72.4(8) . 2_565 ?

O9 Mo3 O4 159.0(8) 2_565 . ?

O9 Mo3 O4 92.8(8) . . ?

O12 Mo3 O4 88.4(5) . . ?

O2 Mo3 O4 72.4(8) . . ?

O4 Mo3 O4 68.4(9) 2_565 . ?

O7 Fe1 O7 92.3(12) . 7_575 ?

O7 Fe1 O3 175.2(8) . . ?

O7 Fe1 O3 89.9(8) 7_575 . ?

O7 Fe1 O3 89.9(8) . 7_575 ?

O7 Fe1 O3 175.2(8) 7_575 7_575 ?

O3 Fe1 O3 88.1(11) . 7_575 ?

O7 Fe1 O5 86.7(8) . . ?

O7 Fe1 O5 92.5(8) 7_575 . ?

O3 Fe1 O5 89.0(8) . . ?

O3 Fe1 O5 91.8(8) 7_575 . ?

O7 Fe1 O5 92.5(8) . 7_575 ?

O7 Fe1 O5 86.7(8) 7_575 7_575 ?

O3 Fe1 O5 91.8(8) . 7_575 ?

O3 Fe1 O5 89.0(8) 7_575 7_575 ?

O5 Fe1 O5 178.8(12) . 7_575 ?

O8 Fe2 O8 179.999(4) . 5_566 ?

O8 Fe2 O6 90.4(8) . 2_565 ?

O8 Fe2 O6 89.6(8) 5_566 2_565 ?

O8 Fe2 O6 90.4(8) . . ?

O8 Fe2 O6 89.6(8) 5_566 . ?

O6 Fe2 O6 89.9(11) 2_565 . ?

O8 Fe2 O6 89.6(8) . 5_566 ?

O8 Fe2 O6 90.4(8) 5_566 5_566 ?

O6 Fe2 O6 90.1(11) 2_565 5_566 ?

O6 Fe2 O6 179.998(1) . 5_566 ?

O8 Fe2 O6 89.6(8) . 6_556 ?

O8 Fe2 O6 90.4(8) 5_566 6_556 ?

O6 Fe2 O6 180.0(8) 2_565 6_556 ?

O6 Fe2 O6 90.1(11) . 6_556 ?

O6 Fe2 O6 89.9(11) 5_566 6_556 ?

O7 As O7 110.2(14) 8 7_575 ?

O7 As O8 112.8(9) 8 . ?

O7 As O8 112.8(9) 7_575 . ?

O7 As O1 106.2(9) 8 . ?

O7 As O1 106.2(9) 7_575 . ?

O8 As O1 108.2(13) . . ?

As O1 Mo2 121.3(14) . . ?

As O1 Mo1 119.9(10) . . ?

Mo2 O1 Mo1 96.4(9) . . ?

As O1 Mo1 119.9(10) . 2_565 ?

Mo2 O1 Mo1 96.4(9) . 2_565 ?

Mo1 O1 Mo1 97.4(10) . 2_565 ?

Mo1 O2 Mo1 114.8(13) 2_565 . ?

Mo1 O2 Mo3 103.8(9) 2_565 . ?

Mo1 O2 Mo3 103.8(9) . . ?

Mo2 O3 Fe1 142.2(11) . . ?

Mo2 O4 Mo1 112.1(9) . 2_565 ?

Mo2 O4 Mo3 107.1(8) . . ?

Mo1 O4 Mo3 99.4(8) 2_565 . ?

Mo1 O5 Fe1 141.3(11) . . ?

Mo1 O6 Fe2 143.9(11) . . ?

As O7 Fe1 129.3(11) 7_575 . ?

As O8 Fe2 126.7(15) . . ?

Mo1 O11 K2 130.7(12) . . ?

Mo1 O11 K1 137.2(12) . 1_565 ?

K2 O11 K1 73.3(9) . 1_565 ?

Mo3 O12 Mo3 180.0 . 5_666 ?

K1 Cu K1 180.000(1) . 5_556 ?

OW6 OW1 K1 70(4) . . ?

OW3 K1 OW6 159(4) . . ?

OW3 K1 OW1 165(2) . . ?

OW6 K1 OW1 37(3) . . ?

OW3 K1 O11 110.3(9) . 2_565 ?

OW6 K1 O11 65.7(8) . 2_565 ?

OW1 K1 O11 74.4(9) . 2_565 ?

OW3 K1 O11 110.3(9) . 1_545 ?

OW6 K1 O11 65.7(8) . 1_545 ?

OW1 K1 O11 74.4(9) . 1_545 ?

O11 K1 O11 129.8(15) 2_565 1_545 ?

OW3 K1 OW2 82.1(16) . 6_546 ?

OW6 K1 OW2 114(2) . 6_546 ?

OW1 K1 OW2 86.2(14) . 6_546 ?

O11 K1 OW2 145.2(15) 2_565 6_546 ?

O11 K1 OW2 68.8(8) 1_545 6_546 ?

OW3 K1 OW2 82.1(16) . 5_566 ?

OW6 K1 OW2 114(2) . 5_566 ?

OW1 K1 OW2 86.2(14) . 5_566 ?

O11 K1 OW2 68.8(8) 2_565 5_566 ?

O11 K1 OW2 145.2(15) 1_545 5_566 ?

OW2 K1 OW2 81.6(16) 6_546 5_566 ?

OW3 K1 Cu 114(2) . . ?

OW6 K1 Cu 87(3) . . ?

OW1 K1 Cu 50.2(14) . . ?

O11 K1 Cu 94.6(9) 2_565 . ?

O11 K1 Cu 94.6(9) 1_545 . ?

OW2 K1 Cu 51.5(10) 6_546 . ?

OW2 K1 Cu 51.5(10) 5_566 . ?

OW3 K1 K2 57.5(8) . 2_565 ?

OW6 K1 K2 113.6(17) . 2_565 ?

OW1 K1 K2 126.1(5) . 2_565 ?

O11 K1 K2 52.9(6) 2_565 2_565 ?

O11 K1 K2 147.4(17) 1_545 2_565 ?

OW2 K1 K2 130.6(16) 6_546 2_565 ?

OW2 K1 K2 66.9(14) 5_566 2_565 ?

Cu K1 K2 118.0(12) . 2_565 ?

OW3 K1 K2 57.5(8) . 1_545 ?

OW6 K1 K2 113.6(17) . 1_545 ?

OW1 K1 K2 126.1(5) . 1_545 ?

O11 K1 K2 147.4(17) 2_565 1_545 ?

O11 K1 K2 52.9(6) 1_545 1_545 ?

OW2 K1 K2 66.9(14) 6_546 1_545 ?

OW2 K1 K2 130.6(16) 5_566 1_545 ?

Cu K1 K2 118.0(12) . 1_545 ?

K2 K1 K2 106.0(11) 2_565 1_545 ?

O11 K2 O11 172(3) 7_576 . ?

O11 K2 OW3 100.2(13) 7_576 7_566 ?

O11 K2 OW3 82.7(13) . 7_566 ?

O11 K2 OW3 82.7(13) 7_576 1_565 ?

O11 K2 OW3 100.2(13) . 1_565 ?

OW3 K2 OW3 139(3) 7_566 1_565 ?

O11 K2 K1 53.8(7) 7_576 7_566 ?

O11 K2 K1 128.2(7) . 7_566 ?

OW3 K2 K1 46.5(13) 7_566 7_566 ?

OW3 K2 K1 124.0(18) 1_565 7_566 ?

O11 K2 K1 128.2(7) 7_576 1_565 ?

O11 K2 K1 53.8(7) . 1_565 ?

OW3 K2 K1 124.0(18) 7_566 1_565 ?

OW3 K2 K1 46.5(13) 1_565 1_565 ?

K1 K2 K1 158(3) 7_566 1_565 ?

K1 OW3 K2 75.9(13) . 2_565 ?

K1 OW3 K2 75.9(13) . 1_545 ?

K2 OW3 K2 133(3) 2_565 1_545 ?

OW8 OW6 OW1 164(10) . . ?

OW8 OW6 K1 123(10) . . ?

OW1 OW6 K1 73(5) . . ?

_diffrn_measured_fraction_theta_max    0.991

_diffrn_reflns_theta_full              17.22

_diffrn_measured_fraction_theta_full   0.991

_refine_diff_density_max    1.479

_refine_diff_density_min   -1.036

_refine_diff_density_rms    0.253