Supporting Information:

Single step aerosol synthesis of nanocomposites by aerosol routes: -Fe2O3/SiO2 and their functionalization**

By Soubir Basak, Vinay Tiwari, Jinda Fan, Samuel Achilefu, Virendra Sethi and Pratim Biswas*

k1,Si = 4.86 x 1017exp(-48288.67/T) cm3 mole-1 s-1

k2,Si = 9.4 x 1039 T-7.91exp(-12660/2T) + 2 x 1023T-3.06exp(-11470/2T) cm3 mole-1 s-1

k1,Fe = 1.5 x 1012exp(-10060.14/T) cm3 mole-1 s-1

k2,Fe = 10(5437/T+8.971) cm3 mole-1 s-1

Figure S1 Plot of rate of oxidation of IPC and formation of Fe2O3 at feed flow rate of 3ccm, total gas flow rate of 10Lpm and 900oC against the normalized residence time.

Figure S2	Plot of rate of oxidation of IPC/TMDS and formation of Fe2O3/SiO2 at feed flow rate of 10ccm, total gas flow rate of 3Lpm and 1200oC against the normalized residence time.

Figure S3	Plot of rate of oxidation of IPC/TMDS and formation of Fe2O3/SiO2 at feed flow rate of 10ccm, total gas flow rate of 10Lpm and 1200oC against the normalized residence time.

Figure S1 Plot of rate of oxidation of IPC and formation of Fe2O3 at feed flow rate of 3ccm, total gas flow rate of 10Lpm and 900oC against the normalized residence time.

Figure S2	Plot of rate of oxidation of IPC/TMDS and formation of Fe2O3/SiO2 at feed flow rate of 10ccm, total gas flow rate of 3Lpm and 1200oC against the normalized residence time.

Figure S3	Plot of rate of oxidation of IPC/TMDS and formation of Fe2O3/SiO2 at feed flow rate of 10ccm, total gas flow rate of 10Lpm and 1200oC against the normalized residence time.

# Text boxes

Feed flow: 1 ccm

Carrier gas flow: 20 lpm

FuAR temperature: 900 oC

Total number concentartion: 5.0x104