Synergistic Effect of Binary Ligands on Nucleation and Growth /Size Effect of Nanocrystals; Studies on Reusability of the Solvent

Chandan H. R, Saravanan V, Ranjith Krishna Pai and Geetha R Balakrishna*

Centre for Nano and Material Sciences, Jain Global Campus, Jain University, Bangalore Rural -562112, India

Table 1: Comparison of nOD and ODE properties

| Solvent | Heat Capacity | Viscosity | Boiling Point | Melting point |
| --- | --- | --- | --- | --- |
| n-octadecane (nOD) | 1.712 J/gK | Solid at STP | 317° C | 26° C-30° C |
| 1-Octadecene (ODE) | ------ | 0.00432pa s | 179°C at 15mm Hg(lit) or 315°C | 15°C |

Table 2. Analysis of peak area for the second time recovered nOD in GCMS report

| Peak | R.T. | Height | Area | Pct Max | Pct Total |
| --- | --- | --- | --- | --- | --- |
| 1 | 5.039 | 141631 | 7194923 | 0.37 | 0.352 |
| 2 | 5.207 | 1726227 | 72820164 | 3.72 | 3.763 |
| 3 | 5.401 | 27651894 | 1.95E+09 | 100 | 95.604 |
| 4 | 6.013 | 130646 | 3626153 | 0.19 | 0.147 |
| 5 | 6.601 | 37832 | 475498 | 0.02 | 0.114 |
| Peak | R.T. | Height | Area | Pct Max | Pct Total |
| 1 | 3.24 | 193212 | 13709450 | 1.06 | 0.490 |
| 2 | 3.855 | 3521469 | 77663689 | 3.45 | 2.348 |
| 3 | 4.815 | 3411369 | 73641668 | 3.19 | 2.05 |
| 4 | 5.087 | 2506878 | 1.68E+08 | 7.47 | 4.209 |
| 5 | 5.359 | 28962523 | 2.25E+09 | 100 | 66.004 |
| 6 | 5.584 | 9944371 | 2.69E+08 | 11.96 | 12.108 |
| 7 | 7.03 | 985826 | 28408357 | 1.26 | 4.51 |
| 8 | 7.653 | 555330 | 17514819 | 0.78 | 3.021 |
| 9 | 8.301 | 1406140 | 32428267 | 4.21 | 5.26 |

Figure 2. a) TEM b) UV- Visible and c) PL spectra of the QD’s synthesized using recovered solvent,  Inset; effect on FWHM (dispersity) as a function of time

Figure 4. Total ion chromatogram of nOD and ODE pure samples before synthesis.

Figure 5: Electron ionization (EI) mass spectra of the detected peaks at the retention times (RTs) a) 5.4 min; m/z of 254 for nOD b) 5.038 min; m/z of  226 for 4-ethyl tetradecane c) 6.01 min; m/z of 324 for n- tricosane d)  6.601min; m/z of 296 for 2-methyl Eicosane and e)  5.207 min; m/z of 254 for 3-methyl heptadecane

Figure 6. Electron ionization (EI) mass spectra of the detected peaks at the retention times (RTs) a) 5.35 min; m/z of 252 for ODE b) 3.24 min; m/z of 210 for methyl-7,9-tridecadienylether c)  5.585 min; m/z of  256 for 1-heptadecanol d)  7.029 min; m/z of 322 for 9-tricosene e)  7.641 min; m/z of 210 for cyclopentadecane f)  8.031 min; m/z of 282 for 6- octadecenoic acid

Figure 7. Depicting the growth and nucleating phase in single ligand (a) OA and (b) ODA  with scan area of 2X2 µm

Figure 8. a FESEM image of the CdSe quantum dots showing fractal structure with corresponding EDS spectra of NCs t = 120 secs

| Time in seconds (sec) | Particle size by UV- Visible (nm) | Crystallite size by XRD (nm) | TEM ( nm) | AFM ( nm) |
| --- | --- | --- | --- | --- |
| 20 | 2.32 | 0.9 | 3±0.11 | - |
| 60 | 2.86 | 1.0 | 3.5±0.1 | 4±0.3 |
| 120 | 3.56 | 1.17 | 4.0±0.1 | 6±0.5 |

Table 4.  particle size of NCs analysed by different techniques

# Text boxes

Table 3. Analysis of peak area for the recovered ODE in GCMS report

Figure 1 ATR IR spectra depicting the reaction of the solvent ODE with Se (resulting in a loss of double bond characteristics) unlike the nOD solvent

c

b

a

Figure 3. IR spectrum of 1-heptadecanol

a

b

c

d

e

a

b

c

d

f

e