SUPPLEMENT

TABLE SI. Layout of magnetoelectric cantilever sensors. If not otherwise stated, in columns Magnetostrictive and Piezoelectric individual layer thicknesses are given in nm. In column Top / rear side deposition MS denotes magnetostrictive phase and PE piezoelectric phase.

| Figure | Magnetostrictive | Piezoelectric | Si cantilever dimension | Top / rear side deposition | Electrode configuration | Electrode dimension |
| --- | --- | --- | --- | --- | --- | --- |
| Fig. 2(a,b,c), 5 | Ta 15 / FeCoSiB 3 µm / Ta 15 | Pt 150 / AlN 1.6 µm / Cr 5 / Au 100 | 25.2 mm x 2.2 mm x 300 µm | Si / MS / PE | Parallel plate | 7.5 mm x 1.2 mm |
| Fig. 3(a,b), 5, 6 | Ta 5 nm / FeCoSiB 4 µm | ZrO2 300 nm / PZT 2 µm / Cr 5 / Au 100 nm | 25 mm x 2.3 mm 300 µm | MS / Si / PE | Interdigital | 1.4 mm effective width, 10 mm length, 15 µm finger width and spacing |
| Fig. 4, 5 | 8x {Ta 7 / Cu 3 / MnIr 7 / FeCoSiB 130} Ta 3 | Ti 20 / Pt 100 / AlN 2 µm / Mo 50 | 25 mm x 3 mm x 650 µm (200 µm trench) | Si / PE / MS | Parallel plate | 11 mm x 2 mm |
| Fig. 5, Section C | 5x {Ta 5 / Cu 3 / MnIr 8 / FeCoSiB 200} Ta 5 | Ta 24 / Pt 150 / AlN 2 µm / Cr 5 / Au 100 | 23.3 mm x 2.3 mm x 350 µm | MS / Si / PE | Parallel plate | 10 mm x 1.2 mm |
| Section C | 5x, 10x, 20x {Ta 5 / Cu 3 / MnIr 8 / FeCoSiB 200} Ta 5 | Ta 24 / Pt 150 / AlN 2 µm / Cr 5 / Au 100 | 25.2 mm x 2.2 mm x 350 µm | MS / Si / PE | Parallel plate | 10 mm x 1.4 mm |