Figure S1. Snapshot of initial FOMs of selected devices of each Type.

Figure S2. Stabilized time of the devices against Mw.

Table S1. Summary of the device types under study

| Identifier | Architecture | Area (cm2) | Cell stack layers [thickness] | Encapsulation |
| --- | --- | --- | --- | --- |
| Type 1 | Standard | 0.24 | ITO + PEDOT:PSS [40 nm] + PCDTBT:PC61BM [90 nm]+ Ca [20 nm] + Al [100 nm] | Glass + Delo-Katiobond (LP655) UV |
| Type 2 | Inverted | 3.75 | ITO + ZnO [30 nm] +PCDTBT:PC70BM [250 nm] + PEDOT:PSS [100 nm] + Ag [100 nm] | Metal lid + Araldite epoxy |
| Type 3 | Standard | 0.16 | ITO + PEDOT:PSS [??] + PCDTBT:PC60BM [250 nm]+ Ca [20 nm] + Al [100 nm] | Glass + Araldite epoxy |
| Type 4 | Inverted | 0.1 | ITO + PEIE [10 nm] +PCDTBT:PC70BM [70 nm] + MoO3 [5 nm] + Ag [100 nm] | Glass + parafilm |
| Type 5 | Standard | 0.045 | ITO + PEDOT:PSS [40 nm] + PCDTBT:PC70BM [90 nm]+ LiF [0.3 nm] + Al [100 nm] | Glass + Ossila epoxy glue |
| Type 6 | Standard | 0.04 | ITO + PEDOT:PSS [30] + PCDTBT:PC60BM [80 nm]+ Ca [5] + Al [100 nm] | Glass + epoxy UV |
| Type 7 | Standard | 0.09 | ITO + PEDOT:PSS [30] + PCDTBT:PC60BM [90 nm]+ Ca [25 nm] + Ag [100 nm] | Glass + glue (LOCTITE 358) UV |

Table S2. Details of the active layer composition and fabrication parameters

| Identifier | PCDTBT:PCBM ratio | Blend concentration (mg/ml) | Spin coating speed (rpm)/time(s) | Annealing temperature /time |
| --- | --- | --- | --- | --- |
| Type 1 | 1:2 | 12 | 1600/15 + +1800/45 | 110°C/5 min |
| Type 2 | 1:4 | 15 | 1000/60 |  |
| Type 3 | 1:4 | 30 | 1500/60 | Vacuum dry/ 20 min |
| Type 4 | 1:4 | 40 | 2400/14 | Vacuum dry/ 1 h |
| Type 5 | 1:4 | 20 | 750/100 |  |
| Type 6 | 1:4 | 20 | 1200/110 | 60oC / 3 min (inert atmosphere) |
| Type 7 | 1:4 | 9 | 1000/60 | 120°C/20 min |

Table S3. Details of HTL and ETL fabrication parameters

| Identifier | HTL | Deposition parameters | HTL annealing | ETL | Deposition |
| --- | --- | --- | --- | --- | --- |
| Type 1 | PEDOT:PSS | SC @ 1800 rpm, 55’’ | 125°C 10 ‘ | Ca | Thermally evaporated |
| Type 2 | PEDOT:PSS | SC @ 1000 rpm, 60´´ | 120°C 10’ | ZnO | SC @ 1000 rpm, 60’’ |
| Type 3 | PEDOT:PSS | SC @ 3500°C, 30’´ | 140°C 30’ | Ca | Thermally evaporated |
| Type 4 | MoO3 | Thermally Evaporated |  | PEIE | SC @ 5000 rpm, 60’’+ annealing 120°C, 10’ |
| Type 5 | PEDOT:PSS | SC | 120°C 20’ | LiF | Thermally evaporated |
| Type 6 | PEDOT:PSS | SC @6000 rpm, 60’´ | 120°C 20’ | Ca | Thermally evaporated |
| Type 7 | PEDOT:PSS | SC @4500rpm 30’’+3500 rpm, 30’’ | 120°C 20’ | Ca | Thermally evaporated |

Table S4. Active layer blend constituents

|  | PCDTBT supplier | Mn (kDa) | Mw (kDa) | PDI | Fullerene | PCBM supplier | Active layer thickness |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Aldrich | Not provided | 100-140 | Not provided | [60]PCBM | Solenne | 90 nm |
| 2 | SJPC | 28.9 | 126.9 | 4.4 | [70]PCBM | nano-C | 250 nm |
| 3 | SJPC | 28.9 | 126.9 | 4.4 | [70]PCBM | Solenne | 250 |
| 4 | SJPC | 28.9 | 126.9 | 4.4 | [70]PCBM | Solenne | 70 nm |
| 5 | Ossilla | 19.0 | 39.0 | 2.05 | [70]PCBM | Solenne | 90 nm |
| 6 | Solaris Corp. | 38.1 | 80.0 | 2.1 | [70]PCBM | Solenne | 80 nm |
| 7 | 1-Material | 17.2 | 43.0 | 2.5 | [70]PCBM | Solenne | 90 nm |

Table S5. Lifetime parameters of the tested devices, extracted from measurements at different degradation conditions

|  | T80 (h) | Ts (h) | PCE (Ts) (norm.) | Ts80 (h) | PCE (Ts80) (norm.) |
| --- | --- | --- | --- | --- | --- |
| Type 2 |  |  |  |  |  |
| D1 | 820 | 1870 | 0.74 | -- | 0.59 |
| L1 | 46 | 680 | 0.47 | -- | 0.38 |
| L2 | 7 | 690 | 0.38 | -- | 0.31 |
| O1 | 6 | 83 | 0.60 | -- | 0.48 |
| Type 3 |  |  |  |  |  |
| D1 | 84 | 187 | 0.77 | 1303 | 0.61 |
| L1 | 7 | 490 | 0.42 | -- | 0.34 |
| L2 | 3 | 325 | 0.76 | 660 | 0.61 |
| O1 | 2 | 32 | 0.41 | -- | 0.33 |
| Type 4 |  |  |  |  |  |
| D1 | 210 | 1340 | 0.39 | 5143 | 0.31 |
| O1 | 1 | 53 | 0.23 | 70 | 0.19 |
| Type 5 |  |  |  |  |  |
| L1 | 94 | 610 | 0.48 | 894 | 0.38 |
| L2 | 9 | 116 | 0.60 | 184 | 0.48 |
| O1 | 0.3 | 5 | 0.77 | 91 | 0.61 |
| Type 6 |  |  |  |  |  |
| D1 | 1130 | 1345 | 0.75 | 1800 | 0.60 |
| L1 | 115 | 200 | 0.77 | 1044 | 0.61 |
| L2 | 39 | 302 | 0.67 | 780 | 0.54 |
| O1 | 2 | 36 | 0.34 | -- | 0.28 |
| Type 7 |  |  |  |  |  |
| D1 | 375 | 866 | 0.35 | -- |  |
| L1 | 39 | -- | -- |  |  |