Supplementary Material

Sandwich-structure styrene-butadiene-styrene block copolymer (SBS)/polypropylene (PP) blends: the role of PP molecular weight

Ping Wang1,2, Yanli Qi1,2, Jun Zhang1,2*

1College of Materials Science & Engineering, Nanjing Tech University, Nanjing 210009, China.

2Jiangsu Collaborative Innovation Center for Advanced Inorganic Function Composites, Nanjing 210009, China.

Corresponding author

Nanjing Tech University, No. 5 Xin Mofan Road, Nanjing, 210009, People’s Republic of China

*E-mail: zhangjun@njtech.edu.cn. Phone: 86-25-83587264. Fax: 86-25-83240205

FIG. S1. Molecular weight distribution curves of PP and SBS.

TABLE SI. The relative molecular weight of PP and SBS.

|  | Relative molecular mass |
| --- | --- |
|  | (g/mol) | (g/mol) | Polydispersity index |
| SBS | 261000 | 277300 | 1.06 |
| PP 001 | 104500 | 1029000 | 9.86 |
| PP 013 | 63000 | 562400 | 8.92 |
| PP 085 | 53700 | 410900 | 7.66 |
| PP 150 | 55500 | 350100 | 6.44 |