We have carried out structural analysis on schisanhenol by means of single crystal. And compared the results of powder and two single-crystal data, the following table lists the parameters of PXRD and two results of single-crystal about schisanhenol.

|  | a (Å) | b (Å) | c (Å) | V (Å3) | Z | space group |
| --- | --- | --- | --- | --- | --- | --- |
| PXRD | 14.6157 | 12.8801 | 11.4907 | 2163.14 | 4 | P212121 |
| SXRD | 14.5995 | 12.8493 | 11.4870 | 2154.88 | 4 | P212121 |
| SXRD(reported) | 14.6730 | 12.8650 | 11.4800 | 2167.06 | 4 | P212121 |

The data of PXRD and SXRD in this table are experimentally measured, and the data of SXRD (reported) are provided by Xu et al., 1982.