Effect of Ultra-Small Chitosan Nanoparticles Doped Brimonidine on Ultra-Structure of Trabecular Meshwork of Glaucoma Patient

Indu Barwal1, Rahul Kumar1, Tanuj Dada2, Subhash Chandra Yadav*1

1Nanotechnology Lab, Electron Microscope Facility, Department of Anatomy, All India Institute of Medical Sciences, New Delhi, 110029

2Dr. Rajendra Prasad Centre for Ophthalmic Sciences, All India Institute of Medical Sciences, New Delhi, 110029

*Corresponding author; Email: subhashmbu@gmail.com

Supplementary Figure: 1

Supplementary Figure 1: Effect of concentration of chitosan on size and zeta potential of chitosan nanoparticles (CS NPs) A- (i) Histogram representing the trend of variation in particle size and zeta potential of CS NPs synthesized at various concentrations of chitosan while keeping other parameters like concentration of STPP and mechanical parameters constant analyzed by zeta sizer (ii) Size distribution analysis of CS NPs synthesized at various concentrations of chitosan reveals the nanoparticle size of 20 to 250 nm by zeta size analysis (iii) zeta potential of CS NPs synthesized at various concentrations of chitosan has shown a continuous increase from 10.0 to 47.0 mV on increase in chitosan concentration (B) TEM analysis of CS NPs synthesized at various chitosan concentrations imaged at 120kV (concentrations are given on each TEM image). TEM imaging of these nanoparticles revealed the size of 20±5 to 50±5 nm at the same condition (0.2% to 0.4 % w/v chitosan) and at higher (0.45% w/v and 0.5% w/v) chitosan concentration revealed heavy aggregation in TEM imaging.

Supplementary Figure 2

iii

iii

ii

ii

i

i

Supplementary Figure 2: Morphological characterization of 0.225% (w/v) chitosan solution in 1% acetic acid (i) TEM image at 120kV (scale bar is given on image) (ii) Size distribution by DLS and (iii) Zeta potential analysis by zeta particle size analyzer.

Supplementary Figure 3

i

i

ii

ii

iii

iii

Supplementary Figure 3: Morphological characterization of the chitosan without using crosslinking agents (STPP) (i) TEM image at 120kV (scale bar is given on image) (ii) Size distribution by DLS and (iii) Zeta potential analysis by zeta particle size analyzer. The chitosan solution (0.225% w/v) in 1% acetic acid was flush mixed with milliQ water instead of STPP as placebo experiment. MilliQ water was added drop-wise to the chitosan solution as described in the methodology section.

Supplementary Figure 4

Supplementary Figure 4: Effect of concentration of STPP on size and zeta potential of chitosan nanoparticles (CS NPs) A- (i) Histogram representing the trend of variation in particle size and zeta potential of CS NPs synthesized at various concentrations of STPP while keeping other parameters like concentration of chitosan (0.225 % w/v) and mechanical parameters constant (ii) Size distribution analysis of CS NPs synthesized at various concentrations of STPP reveals the nanoparticle size of 103±10-25±2.5nm by zeta size analysis (iii) zeta potential of CS NPs synthesized at various concentrations of chitosan has shown a continuous increase from 50-20 mV  on increase in STPP concentration (B) TEM analysis of CS NPs synthesized at various chitosan concentrations imaged at 120kV (concentrations are given on each TEM image). TEM imaging of these nanoparticles revealed the size of 20±5 to 50±5 nm at the same condition (0.5-2.0 mg/ml STPP) and at higher (2.5 mg/ml) STPP concentration revealed heavy aggregation in TEM imaging.

Supplementary Figure 5

Supplementary Figure 5: Effect of chitosan:STPP ratio v/v on size and zeta potential of chitosan nanoparticles (CS NPs) A- (i) Histogram representing the trend of variation in particle size and zeta potential of CS NPs synthesized at varying chitosan:STPP v/v ratio while keeping other parameters like concentration of chitosan (0.225 % w/v), concentration of STPP (2 mg/ml) and mechanical parameters constant (ii) Size distribution analysis of CS NPs synthesized at various concentrations of chitosan: STPP reveals the nanoparticle size of 103±10-25±2.5nm by zeta size analysis (iii) zeta potential of CS NPs synthesized has shown a continuous increase from 27-44 mV  on increase in chitosan:STPP v/v ratio B) TEM analysis of CS NPs synthesized at various chitosan concentrations imaged at 120kV (concentrations are given on each TEM image). TEM imaging of these nanoparticles revealed the size of 20±5 to 50±5 nm at the same condition (0.5-2.0 mg/ml STPP) and at higher (2.5 mg/ml) STPP concentration revealed heavy aggregation in TEM imaging.

Supplementary Figure 6

Supplementary Figure 6: Effect of time of reaction on size and zeta potential of nanobrimonidine (A) Histogram representing variation of size of nanobrimonidine on varying the reaction time from 0 h to 24 h analyzed by zetasizer (B) Size distribution by number of nanobrimonidine synthesized by various reaction times analyzed by zeta particle analyzer (C) Zeta potential analysis of nanobrimonidine synthesized by various reaction times analyzed by zeta particle size analyzer and (D) TEM analysis of nanobrimonidine synthesized by various reaction times image at 120kV (Reaction times are given on each TEM image). The size of nanobrimonidine decreased as the reaction time increased from 0 h to 1 h and further gradually increased again.

Supplementary Figure 7

Supplementary Figure 7: Effect of surfactant capping on size and zeta potential of chitosan nanoparticles (CS NPs) A- (i) Size distribution analysis of US CS NPs with and without surfactant capping (ii) zeta potential of US CS NPs with and without surfactant capping (B) TEM analysis of US CS NPs  with  and without surfactant capping imaged at 120kV.

Supplementary Figure 8

b

b

a

a

Supplementary Figure 8: UV-visible spectroscopic characterization of brimonidine: Absorbance (248 nm and 319 nm) of standard concentrations was plotted against known concentration.

Supplementary Information 9

Calculation detail of Encapsulation and Loading Efficiency:

| S. No | Description | Calculations |
| --- | --- | --- |
| 1 | Concentration of brimonidine in STPP solution: | 1mg in 5 ml = 0.2mg/ml = 200μg/ml |
| 2 | Concentration of brimonidine after completion of reaction (15 ml): | 1mg in 15 ml = 0.067mg/ml =67 μg/ml |
| 3 | Concentration of chitosan in one complete reaction Total amount in one reaction | 0225% in 10 ml =2.25mg/ml =22.5mg |
| 4 | Encapsulation Efficiency (%)= Absorbance of nanobrimonidine using chitosan nanoparticles as blank * 100/ Absorbance of 67 μg/ml Brimonidine | = 1.19*100/3.03 = 39.27% |
| 5 | Amount of brimonidine encapsulated on nanobrimonidine in one reaction (amount encapsulated per reaction)= %EE * Amount of brimonidine taken in one reaction/100 | 39.27* 1.0/100 = 0.3927mg =392.7 μg |
| 6 | Loading efficiency (%, w/w): Total amount of brimonidine encapsulated* 100/ (Total amount of chitosan taken in one reaction+ Amount of encapsulated brimonidine) | 392.7 * 100/ (22500 +392.7) = 1.715% (w/w) = ~ 2% |

Supplementary Figure 10

Supplementary Figure 10: In vitro release scan of brimonidine from the brimonidine loaded ultra small nanobrimonidine nanoparticles at pH 7. There was half release at 45 h and sustained release till 120 h. The nanobrimonidine synthesized from three reaction were suspended in 15ml, 0.5% acetic acid in phosphate buffer (0.05M) at pH 7.4 and release was measured from the dialysate 30 ml having 0.5% acetic acid in phosphate buffer (0.05M) at pH 7.4.

Supplementary Figure 11

Supplementary Figure 11: Confirmation about the mucosa-adhesive nature and retention of nanobrimonidine nanoparticles on ex vivo bull eye cornea using rhodamine labeled nanobrimonidine.