Date: Dec 26, 2013

First thank the reviewers for their coments.

Here are my responses to coment as follows:

- Rapid growth of large scale (600mm aperture) KDP crystal and its optical quality

- The rapid-growth method includes extreme conditions

- The optical parameters of KDP crystals were determined.

- Wei Xiaohong et al.[11]used the ZYGO MST large aperture interferometer to attain the refraction index inhomogeneity distribution of large size KDP crystal with the precision as high as 10-7. The diameter of test aperture is 32( and wavelength of the used interferometer is 633nm.

- From Table 3, we canconclude that thermal annealing can not improve refractive-index nonuniformities of rapidly grown KDP crystals obviously.

Table.3 The comparison of refractive-index nonuniformities\

| Sample | Size | RMS ((10-6) (before annealing) | RMS ((10-6) (after annealing) |
| --- | --- | --- | --- |
| KDP doubler-1(rapid growth) | 330(330 mm | 0.843 | 0.824 |
| KDP doubler-2(rapid growth) | 430(430 mm | 0.572 | 0.699 |
| KDP doubler-3(rapid growth) | 430(430 mm | 0.727 | 0.763 |
| KDP doubler-4(rapid growth) | 45(45 mm | 0.771 | 1.23 |
| KDP doubler-5(slow growth) | 45(45 mm | 1.02 | 1.13 |
| KDP tripler-1(slow growth) | 45(45 mm | 0.469 | 0.736 |

- A self-made MSC type energy meter is used to determine the efficiency with sensitivity of 10 (v/mJ and measuring energy range of 200mJ-20J.

- Optical quality of KDP crystals was characterized.

Best Regards.

Yours Sincerely,

LGH