Supplementary material

Single Precursor Synthesis of Copper Sulfide Nanocrystals Using Aerosol Spray Pyrolysis

Patrick Davis, Lorenzo Mangolini

Mechanical Engineering Department, Materials Science and Engineering Program

University of California, Riverside

Figure 1.	XRD analysis of powder produced at a temperature of 800(C. The peaks are indexed to the digenite phase of copper sulfide (Cu1.8S).

Figure 2. Absorbance spectrum from powder produced at a temperature of 800(C. The powder creates a clear colloidal dispersion in chloroform.