Supporting Information

Solution-based Synthesis of Carbon-Hematite Composite Thin Films for High Performance Supercapacitor Applications

Jinzhan Su*, Shangpu Liu, Jian Wang, Cong Liu, Yufeng Li, Dongyang Wu

International Research Centre for Renewable Energy, State Key Laboratory of Multiphase Flow in Power Engineering, Xi’an Jiaotong University, Shaanxi 710049, P. R. China. E-mail: j.su@mail.xjtu.edu.cn

Supporting Information

Figure S1. SEM images of C/Fe2O3 electrodes with different heating rates: (a) 550℃/40s; (b) 550℃/10min.

Figure S2 I-V curve of different heating rate (time taken to increase temperature to 550oC) of C/Fe2O3 electrode for supercapacitor (0.1V/s)

Figure S3. SEM images of C/Fe2O3 electrodes annealed at 500oC with different heating time: (a) 50min; (b) 72min.

Figure S4. I-V curves of different annealing time (at 550 oC) of C/Fe2O3 electrode for supercapacitor (4 min, 10 min, 20 min and 30min).

Figure S5. I-V curves of different annealing temperature of C/Fe2O3 electrode for supercapacitor (500 oC, 550 oC, 600 oC).

Figure S6. XPS spectra of C/Fe2O3 electrode with different glucose to ferric nitrate weight ratios (C6H12O6: Fe(NO3)3(9H2O). Fe2p for sample with ratio = (a) 2:1 (b) 1:1 (c) 1:2, O1s for sample with ratio(d) 2:1 (e) 1:1 (f) 1:2 , C1s for sample with ratio (g) 2:1 (h) 1:1 (i) 1:2 and (j) full survey spectra.

Figure S7 galvanostatic charge-discharge behaviors for C/Fe2O3 samples with different C/Fe2O3 ratios in 8 M KOH electrolyte (J=1mA/cm2)

Figure S8 Galvanostatic charge/discharge (GCD) curve of C/Fe2O3/Co3O4 electrode Ct1:0.5g/20ml;Ct2:1g/20ml;Ct3:2g/20ml (J=1mA/cm2)