Supplementary Material

Poly(3,4-ethylenedioxythiophene):Sulfonated Poly(diphenylacetylene) Complex as a Hole Injection Material in Organic Light-Emitting Diodes

Jung Jae Kim,a Jin Chul Yang,a Keunbyung Yoon,a,b Giseop Kwak,a,b* and Jin Young Parka,b*

a Major in Polymer Science & Engineering, School of Applied Chemical Engineering, Kyungpook National University, 80 Daehak-ro, Buk-gu, Daegu 41566, Republic of Korea

b Department of Polymer Science & Engineering, School of Applied Chemical Engineering, Kyungpook National University, 80 Daehak-ro, Buk-gu, Daegu 41566, Republic of Korea

*Corresponding Author

Tel.: +82 53 950 5624; Fax: +82 950 6623

E-mail address: gkwak@knu.ac.kr, jinpark@knu.ac.kr

Fig. S1. (a) UV/vis absorption and (b) PL emission spectra ((ex = 430 nm) of PEDOT:SPDPA and SPDPA films.

(c)

| Samples | Oxidation Potential [V][a] | Reduction Potential [V][a] | HOMO [eV] | LUMO [eV] | Bandgap [eV] |
| --- | --- | --- | --- | --- | --- |
| 0.9 V | 0.97 | -0.43 | -5.42 | -4.02 | 1.40 |
| 1.0 V | 0.98 | -0.41 | -5.43 | -4.04 | 1.39 |
| 1.1 V | 0.99 | -0.39 | -5.44 | -4.06 | 1.38 |
| 1.2 V | 0.99 | -0.39 | -5.44 | -4.06 | 1.38 |
| 1.3 V | 1.00 | -0.37 | -5.45 | -4.08 | 1.37 |

[a] HOMO (or LUMO) (eV) = (4.8 ( (Eonset-E1/2(ferrocene)), E1/2 = 0.35 V

Fig. S2. (a) CV voltammogram in an acetonitrile solution with ferrocene (10 mM) and LiClO4 (0.1 M) over a scan range of 0 ( 0.6 V at a scan rate of 0.1 V/s, (b) CV voltammograms of PEDOT:SPDPA films in an acetonitrile solution with LiClO4 (0.1 M) at a scan range of -0.8 ( 1.3 V and a scan rate of 0.1 V/s, (c) summary of the calculated HOMO, LUMO, and bandgaps.

Fig. S3. SEM images of PEDOT:SPDPA films fabricated by electrostatic deposition at various constant voltages (0.9 ( 1.3 V). All scale bars are 1 (m.

Fig. S4. (a) Transmission as a function of wavelength and (b) summary of the transmission values of the PEDOT:SPDPA film, PEDOT:PSS film, and ITO substrate.

Fig. S5. AFM images of PEDOT:SPDPA films (deposited at constant potentials of 0.9 and 1.1 V) after thermal annealing at 160 (C for 20 min. All scale bars are 1 (m.