Supporting Information for:

Increased piezoelectric response in functional nanocomposites through MWCNT interface and fused-deposition modeling 3D printing

Hoejin Kim*, Fernando Torres, Md Tariqul Islam, Md Didarul Islam, Luis A. Chavez, Carlos A. Garcia Rosales, Bethany R. Wilburn, Calvin M. Stewart, Juan C. Noveron, Tzu-Liang B. Tseng, Yirong Lin

The University of Texas at El Paso 500W. University Ave. El Paso Texas, 79968, USA

E-mail: hkim4@miners.utep.edu

Methods

Method S1. 3D printing of MW-CNTs/BaTiO3/PVDF nanocomposites film

For the cyclic load frame test, eight layers are printed with varying concentration of BT powders: 0, 6, 12, and 15 weight percentages and MWCNTs: 0, 0.1, 0.4 weight percentages. Increasing the weight content above 18%-BT would increase severe clogging within the nozzle which could potentially damage the 3D printer. In addition, increasing the weight content above 0.4%-MWCNTs would increase the electrical break down during the electric poling process. For the printing parameter, the film is printed at 230°C of nozzle temperature, 23°C of heating bed temperature, and 10mm/s of extrusion speed. The printing pattern is described in Figure S1. Final film was 0.55 mm in thickness with dimensions of 6 × 35 mm.

Method S2. Calculation of β-phase contents for nanocomposites film

The β-phase contents of each sample are calculated, specifically, at the absorption bands of 764 and 840 cm-1 which are characteristics of α- and β-phases respectively. Assuming that the infrared absorption follows the Lambert-Beer law, Aα and Aβ absorbance at 764 and 840 cm-1, respectively, are given by equation (1) below.[1]:

Aα,β=LogI α,β0I α,β=C·Kα,β·Xα,β·L			(1)

where the subscripts α and β are defined as the crystalline phases, I0 and I are the incident and transmitted intensities of the radiation, respectively. The L is defined as a sample thickness, C is an average monomer concentration, K is the absorption coefficient at the respective wave number, and X is the degree of crystallinity of each phase.[1] For a system containing α- and β-phases, the relative fraction of the β-phase, F(β), can be calculated using equation (2).[1]:

F(β)= XβXα+Xβ= Aβ(Kβ/Kα)Aα+Aβ= Aβ1.26Aα+Aβ				(2)

where Kα (6.1 × 104 cm2/mol) and Kβ (7.7 × 104 cm2/mol) are the absorption coefficients at the respective wave number.

Method S3. Calculation of Piezoelectric Coefficient (d31)

To calculate the piezoelectric coefficient (d31) by using the equation (3) below:

Di=dijσj			(3)

where Di is the electrical displacement, dij is the piezoelectric coefficient, and σj is the applied stress. In this case, subscripts i and j are defined as 3 (applying force direction) and 1 (poling direction) respectively as shown in Figure 2a-i. Therefore, the equation can then be expressed as D3=d31σ1. Considering the areas of the electrode and cross-section of the sample, equation (4) can then be expressed as

QAelect=d31νFAcross			(4)

where Q is charge, Aelect and Across are areas of electrode and cross-section respectively, ν is Poisson’s ratio which is 0.34,[2] and F is an applied force. The Q is equal to CV which are capacitance and voltage, respectively. C can be expressed to εrε0Aelect/d. Then, the piezoelectric coefficient can be expressed as

d31=εrε0AcrossVvdF			(5)

where εr is relative permittivity of the printed nanocomposites film, ε0 is 8.854×10-12 C/Vm, and d is its thickness. Across are 2.47 mm2. Then d31max and d31min are determined at maximum and minimum of voltages and forces as equation (6) describes.

d31max=εrε0AcrossVmaxvdFmax,    d31min= εrε0AcrossVminvdFmin			(6)

Fmax and Fmin are 5 N and 45 N, respectively. Each attained d31 is divided by 2 for ± d31 as shown in following equation (7)

± d31 =  d31max - d31min2  			(7)

Figures and Tables

Figure S1: Printing pattern design

Figure S1. A captured image of concentric fill pattern design created in Slic3r software used for SEM, FTIR, and fatigue load frame test.

Figure S2: Scanning electron microscopy images of the printed nanocomposites

(b)

(a)

(d)

(f)

(e)

(c)

Figure S2. SEM images of (a) 12wt.%-BT/PVDF, (b) 0.1wt.%-MWCNTs/12wt.%-BT/PVDF, (c) 0.4wt.%-MWCNT/PVDF, (d) 0.4wt.%-MWCNT/6wt.%-BT/PVDF, (e) 0.4wt.%-MWCNT/12wt.%-BT/PVDF, (f) 0.4wt.%-MWCNT/18wt.%-BT/PVDF.

Figure S3: Fourier transform infrared spectroscopy (FTIR) spectra

- FTIR spectra before electric poling process

α (763)

β/γ (840)

α (854)

γ (811)

α (795)

α (614)

α (976)

β (1275)

γ (1234)

(b)

(a)

(f)

(e)

(d)

(c)

- FTIR spectra after electric poling process

Figure S3. FTIR spectra of the printed nanocomposites (1) before and (2) after electric poling: (a) 12wt.%-BT/PVDF, (b) 0.1wt.%-MWCNT/12wt.%-BT/PVDF, (c) 0.4wt.%-MWCNT /PVDF, (d) 0.4wt.%-MWCNT/6wt.%-BT/PVDF, (e) 0.4wt.%-MWCNT/12wt.%-BT/PVDF, (f) 0.4wt.%-MWCNT/18wt.%-BT/PVDF.

Table S1: Dielectric Properties of the Printed MWCNT/BT/PVDF Nanocomposites Films

| Composition | Relative Permittivity (εr) at 1 kHz |
| --- | --- |
| 12wt.%-BT/PVDF | 16.9 |
| 0.1wt.%-MWCNT/12wt.%-BT/PVDF | 31.2 |
| 0.4wt.%-MWCNT/PVDF | 30.5 |
| 0.4wt.%-MWCNT/6wt.%-BT/PVDF | 31.7 |
| 0.4wt.%-MWCNT/12wt.%-BT/PVDF | 25.0 |
| 0.4wt.%-MWCNT/18wt.%-BT/PVDF | 36.5 |

References

[1]	V. Sencadas, M. V. Moreira, S. Lanceros-Méndez, A. S. Pouzada, and R. Gregório Filho, "α-to β Transformation on PVDF films obtained by uniaxial stretch," in Materials science forum, 2006, pp. 872-876.

[2]	A. Vinogradov and F. Holloway, "Electro-mechanical properties of the piezoelectric polymer PVDF," Ferroelectrics, vol. 226, pp. 169-181, 1999.