# Supplementary Information

# Raman Investigation of the Air Stability of 2H Polytype HfSe2 Thin Films

Antonio Cruza, Zafer Mutlub, Mihrimah Ozkanc, Cengiz S. Ozkana,d*

a Materials Science and Engineering Program, University of California, Riverside, CA 92507, USA

b Department of Electrical Engineering and Computer Sciences, University of California, Berkeley, CA, 94720, USA

c Department of Electrical and Computer Engineering, University of California, Riverside, CA 92507, USA

d Department of Mechanical Engineering, University of California, Riverside, CA 92507, USA

*Corresponding Author Email: cozkan@engr.ucr.edu

Work performed during postdoctoral studies at University of California, Riverside

FIG. S1. Optical microscopy images of HfSe2 flakes. (a) Image of large HfSe2 flake showing the variations in contrast among the different thicknesses. (b) Smaller HfSe2, with nearby flakes burned by the Raman laser.

(a)

(b)

| Table S1. Height and roughness values for thick and thin regions labeled 1 and 2 in Figure 2. Analysis was carried out in Gwyddion. |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Max height | Avg. height | Median height | Ra (Sa) | Rms (Sq) |
| Thick region | 39.4664 | 2.99 | 2.1259 | 1.87437 | 4.32181 |
| Thin region | 19.0397 | 5.2942 | 4.7738 | 2.01067 | 2.7893 |
| All values in nm |  |  |  |  |  |

FIG. S2. AFM image of HfS2. AFM images of HfS2 flakes showed no changes to the flake surface after long-term air exposure, indicating a high stability in air compared to HfSe2.