SUPPLEMENTARY INFORMATION

Formation of iron-rich clay minerals in FeO-SiO2-H2O system during hydrothermal synthesis as a function of pH

Liva Dzenea,*, Amira Doggaza, Patrick Dutourniéa, Sayako Inoueb, Mustapha Abdelmoulac, Alexandra Jourdaina, Jean-Marc Le Meinsa, Jocelyne Brendléa, Christelle Martind, Nicolas Michaud

aInstitut de Science des Matériaux de Mulhouse CNRS UMR 7361, Université de Haute-Alsace, Université de Strasbourg, 3b rue Alfred Werner, 68093 Mulhouse CEDEX, France

b Geodynamics Research Center (GRC), Ehime University, 2-5 Bunkyo-cho, Matsuyama, Ehime 790-8577, Japan

c LCPME, CNRS-Université de Lorraine UMR7564, 54000 Nancy, France

dAndra, R&D Division, Packages and Materials Department, 1/7 rue Jean Monnet, F-92298 Châtenay-Malabry CEDEX, France

*liva.dzene@uha.fr

Table S1. OH/Fe molar ratio corresponding to each run of experiment.

pH measurements were performed under ambient conditions.

| pHinitial |  | pHfinal | OH/Fe (molar) |
| --- | --- | --- | --- |
| 8.50 | 6.50 | 1.93 |
| 9.00 | 7.82 | 2.02 |
| 9.64 | 8.85 | 2.13 |
| 9.67 | 9.19 | 2.10 |
| 9.76 | 9.64 | 2.13 |
| 10.28 | 10.27 | 2.10 |
| 10.51 | 11.52 | 2.16 |
| 10.54 | 11.33 | 2.19 |
| 10.69 | 12.28 | 2.16 |
| 10.75 | 12.00 | 2.16 |
| 11.16 | 12.61 | 2.21 |
| 11.44 | 12.58 | 2.30 |
| 11.54 | 12.76 | 2.30 |
| 11.63 | 12.92 | 2.30 |
| 12.10 | 13.12 | 2.39 |

Figure S1. Mössbauer spectrum at room temperature of sample with pHi = 8.50.

Table S2. Mössbauer parameters for the synthesis product with pHi = 8.50 at room temperature, where CS is center shift, Δ is quadrupole splitting, H is hyperfine field, and R.A. is relative abundance.

|  | CS (mm/s) | (mm/s) | H (kOe) | R.A. (%) |  |
| --- | --- | --- | --- | --- | --- |
| Doublet (1) | 0.26 | 0.69 |  | 40 | Fe(III) in clay mineral |
| Doublet (2) | 0.49 | 0.71 |  | 33 | Fe(III) in clay mineral |
| Sextet (3) | 0.29 | 0.01 | 489 | 13 | Magnetite, Fe Td |
| Sextet (4) | 0.63 | -0.06 | 458 | 11 | Magnetite, Fe Oh |
| Sextet (5) | 0.24 | -0.15 | 366 | 3 | Goethite |

Figure S2. Mössbauer spectrum at room temperature of sample with pHi = 10.28.

Table S3. Mössbauer parameters for the synthesis product with pHi = 10.28 at room temperature, where CS is center shift, Δ is quadrupole splitting, H is hyperfine field, and R.A. is relative abundance.

|  | CS (mm/s) | (mm/s) | R.A. (%) |  |
| --- | --- | --- | --- | --- |
| Doublet (1) | 0.36 | 0.83 | 91 | Fe(III) in clay mineral and superparamagnetic iron oxide |
| Doublet (2) | 1.07 | 2.62 | 9 | Fe(II) in clay mineral |

Figure S3. Mössbauer spectrum at room temperature of sample with pHi = 11.63.

Table S4. Mössbauer parameters for the synthesis product with pHi = 11.63 at room temperature, where CS is center shift, Δ is quadrupole splitting, H is hyperfine field, and R.A. is relative abundance.

|  | CS (mm/s) | (mm/s) | R.A. (%) |  |
| --- | --- | --- | --- | --- |
| Doublet (1) | 0.36 | 0.79 | 67 | Fe(III) in clay mineral and superparamagnetic iron oxide |
| Doublet (2) | 0.35 | 1.84 | 14 | Fe(III) in clay mineral and superparamagnetic iron oxide |
| Doublet (3) | 1.10 | 2.30 | 14 | Fe(II) in clay mineral |
| Doublet (4) | 1.04 | 2.33 | 5 | Fe(II) in clay mineral |

Possible precipitation reactions of different solid phases identified in synthesis products

Domain I

Magnetite: 3 Fe2+ + 8 OH- → Fe3O4 + 4 H2O + 2 e-	(1)

Goethite: Fe3+ +  2 H2O → -FeOOH + 3 H+ 	(2)

Hematite: 2 -FeOOH → Fe2O3 + H2O 	(3)

FeIII 2:1 clay mineral:

7.11 H4SiO4 + 5.19 Fe2+ + 15.56 OH- →

→  (Si7.11FeIII0.89)IV(FeIII4.30)VIO20(OH)4 + 20 H2O + 5.18 e- 	(4)

Domain II

FeIII/FeII 1:1 clay mineral:

3.14 H3SiO4- + 5.38 Fe2+ + 12.3 OH- →

→  (Si3.14FeIII0.86)IV(FeII0.71FeIII3.81)VIO10(OH)8 + 6.86 H2O + 4.68 e-	(5)

Domain III

FeIII/FeII 1:1 clay mineral:

3.60 H3SiO4- + 4.89 Fe2+ + 10 OH- →

→  (Si3.60FeIII0.40)IV(FeII1.09FeIII3.40)VIO10(OH)8 + 6.4 H2O + 3.82 e-	(6)

FeIII/FeII 2:1 clay mineral:

5.74 H3SiO4- + 7.57 Fe2+ + 15.3 OH- →

→  (Si5.74FeIII2.26)IV(FeII1.68FeIII3.63)VIO20(OH)4 + 14.26 H2O + 5.9 e-	(7)

Figure S4. SAED pattern of sample with pHi = 8.50. The pattern was obtained from the region shown in Figure 2C.

Figure S5. SAED pattern of sample with pHi = 10.28. The pattern was obtained from the region shown in Figure 3C.

Figure S6. TEM image of sample with pHi = 11.63 showing low crystallinity regions in addition to the phase with 7 Å periodicity observed and showed in Fig.4C.

Table S5. Chemical composition of samples. * Total iron as FeO. ** Tetrahedral Fe3+ (Fe3+ (IV) ) was determined assuming there is no tetrahedral vacancy.

| pHi | 8.50 | 10.28 | 11.63 |  |
| --- | --- | --- | --- | --- |
| Type of structure | 2:1 | 1:1 | 1:1 | 2:1 |
| SiO2 | 51.89 | 33.00 | 37.01 | 37.15 |
| FeO* | 45.19 | 60.04 | 60.04 | 56.66 |
| CaO | 2.00 | – | 2.96 | 3.33 |
| Na2O | – | – | – | – |
| K2O | 0.80 | – | – | – |
| Total | 100.00 | 100.00 | 100.00 | 100.00 |
| Fe3+/ΣFe by MS | 1.00 | 0.87 | 0.88 | 0.88 |
| O = | 22 | 14 | 14 | 22 |
| Si | 7.11 | 3.14 | 3.60 | 5.74 |
| Fe3+ (IV)** | 0.89 | 0.86 | 0.40 | 2.26 |
| Σ Tetrahedral cations | 8.00 | 4.00 | 4.00 | 8.00 |
| Fe2+ | - | 0.71 | 1.09 | 1.68 |
| Fe3+ (VI) | 4.30 | 3.81 | 3.40 | 3.63 |
| Σ Octahedral cations | 4.30 | 4.52 | 4.49 | 5.31 |
| Number of octahedral vacancies | 1.70 | 1.48 | 1.76 | 0.98 |