Description of Ar isotherms

Argon physisorption  isotherms are classified as hybrid isotherms composed of a type II adsorption branch combined with a type H3 or H4 hysteresis loop. The sharpness of the “point B” of the adsorption branch is sample-specific and reflects the degree of overlap of mono- and multilayer formation. The absent plateau at maximum experimental partial pressure indicates incomplete pore filling; consequently, the resulting specific pore volumes and porosities should be considered as a guide but not as a fixed physical measure of porosity.

The presence of hysteresis signifies substantial mesoporosity and (delayed) capillary condensation. For all sample, the hysteresis loops close with a distinctive downward step consistently at p/p° ≈ 0.38 to 0.40, corresponding to the critical cavitation-induced pressure for argon. The amount of gas released at this partial pressure, hence the evacuated pore volume, is sample dependent. Nevertheless, this observation implies that the accessibility of a non-negligible fraction of pore volume is controlled by pores ≤ 4 to 5 nm (Ravikovitch and Neimark, 2002; Thommes et al., 2006). Above the critical cavitation pressure desorption proceeds via capillary evaporation and desorption branches commonly display pronounced humps. When pore-size distributions are calculated, these features translate into the dominant pore-size mode of each sample.