Trace and rare earth elements distribution and mobility during diagenetic alteration of volcanic ash to bentonite in Eastern Iranian bentonite deposits

Alireza Namayandeha,b , Soroush Modabberib,*, Alberto López-Galindo c

a Department of Geosciences, Virginia Tech, Blacksburg, VA 24061, USA. anamayandeh@vt.edu

b School of Geology, College of Science, University of Tehran, Enghelab Avenue, P.O. Box 14155-6455 Tehran, Iran. modabberi@ut.ac.ir

c Instituto Andaluz de Ciencias de la Tierra (CSIC-Universidad de Granada), Avda. de las Palmeras, 4, 18100 Armilla, Granada, Spain. alberto@iact.ugr-csic.es

Corresponding Author and email address: modabberi@ut.ac.ir

Journal: CLAYS AND CLAY MINERALS

Prepared: 10/21/2019

Supplementary Data Sections (4 pages)

A. Generalized geological map of the Lut structure zone in the eastern Iran. The location of bentonite deposits in Sarayan and Ferdows are shown by open boxes

B. The chemical composition of the studied samples.

A. Generalized geological map of the Lut structure zone in the Eastern Iran. The location of bentonite deposits in Sarayan and Ferdows are shown by open boxes (Modabberi et al., 2019).

B. The chemical composition of the studied samples

|  | Group 1 |  |  |  |  | Group 2 |  |  |  |  |  |  |  |  |  |  |  | Group 3 |  |  |  |  | Group 4 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | ST | ST21 | SK | SK2 |  | SG-A2 | SG-B | SG-C | SG-D | SG-E | SG-F | SG-G3 | SG2 | SG3 | SP | SP2 |  | FGH | FGH2 | FKH | FKH2 |  | FKHS | FKHS2 |
| Major oxides /%) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| SiO2 | 60.44 | 66.43 | 68.22 | 64.98 |  | 63.81 | 65.09 | 48.14 | 62.56 | 60.06 | 69.44 | 70.40 | 73.51 | 73.38 | 70.36 | 71.33 |  | 65.15 | 70.11 | 51.26 | 54.10 |  | 67.30 | 72.41 |
| Al2O3 | 10.78 | 14.46 | 11.27 | 17.10 |  | 11.76 | 12.10 | 15.56 | 19.38 | 20.18 | 13.18 | 13.86 | 13.80 | 11.06 | 9.75 | 11.64 |  | 12.48 | 12.11 | 13.81 | 15.80 |  | 14.15 | 12.79 |
| Fe2O3 | 1.20 | 4.88 | 1.38 | 3.47 |  | 3.10 | 1.84 | 4.09 | 1.95 | 4.24 | 3.25 | 2.91 | 0.79 | 2.12 | 1.68 | 0.72 |  | 2.55 | 5.02 | 4.77 | 9.71 |  | 3.22 | 1.09 |
| MgO | 1.82 | 0.31 | 1.90 | 0.36 |  | 1.75 | 2.08 | 2.29 | 1.24 | 3.84 | 2.88 | 2.83 | 0.12 | 0.50 | 1.46 | 0.31 |  | 1.98 | 0.76 | 3.01 | 4.31 |  | 3.08 | 0.23 |
| CaO | 0.64 | 3.50 | 0.37 | 2.61 |  | 0.92 | 2.61 | 3.58 | 1.30 | 0.89 | 2.05 | 1.77 | 1.85 | 3.79 | 0.48 | 1.22 |  | 0.60 | 2.49 | 6.07 | 2.24 |  | 1.12 | 0.88 |
| Na2O | 4.60 | 3.40 | 2.36 | 3.21 |  | 2.90 | 1.95 | 6.06 | 4.36 | 4.36 | 2.40 | 2.33 | 3.16 | 0.65 | 2.86 | 5.04 |  | 2.71 | 0.99 | 2.83 | 3.79 |  | 3.37 | 2.19 |
| K2O | 0.13 | 3.11 | 0.12 | 6.46 |  | 0.09 | 0.41 | 0.33 | 5.03 | 0.09 | 0.14 | 0.17 | 5.12 | 0.75 | 0.16 | 1.26 |  | 0.46 | 2.33 | 0.92 | 1.76 |  | 0.71 | 7.20 |
| TiO2 | 0.01 | 0.79 | 0.01 | 0.39 |  | 0.19 | 0.29 | 0.34 | 0.40 | 0.45 | 0.24 | 0.24 | 0.28 | 0.21 | 0.16 | 0.25 |  | 0.29 | 0.55 | 0.86 | 1.06 |  | 0.48 | 0.40 |
| P2O5 | 0.02 | 0.15 | 0.03 | 0.21 |  | 0.02 | 0.03 | 0.04 | 0.05 | 0.03 | 0.02 | 0.02 | 0.04 | 0.06 | 0.02 | 0.03 |  | 0.04 | 0.04 | 0.26 | 0.36 |  | 0.11 | 0.16 |
| MnO | 0.02 | 0.06 | 0.01 | 0.02 |  | 0.01 | 0.03 | 0.02 | 0.13 | 0.01 | 0.03 | 0.02 | 0.01 | 0.04 | 0.01 | 0.02 |  | 0.01 | 0.05 | 0.04 | 0.08 |  | 0.02 | 0.01 |
| LOI | 18.50 | 2.37 | 13.50 | 1.02 |  | 14.60 | 13.10 | 17.80 | 3.34 | 6.91 | 6.20 | 5.74 | 1.13 | 6.88 | 11.80 | 7.84 |  | 12.80 | 5.34 | 15.70 | 6.46 |  | 6.26 | 1.85 |
| Trace elements (ppm) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| As | 3.5 | 48 | 3.9 | 29.1 |  | 3.9 | 7.5 | 3.4 | 5.8 | 1.1 | 15.9 | 8.1 | 4.6 | 4.20 | 7.4 | 4 |  | 1.8 | 12.7 | 3.5 | 18.1 |  | 2.7 | 5.3 |
| Ba | 388 | 378 | 258 | 495 |  | 791 | 578 | 19.4 | 502 | 16.9 | 417 | 13.1 | 468 | 764 | 744 | 1600 |  | 320 | 431 | 469 | 39.4 |  | 490 | 463 |
| Be | 6.4 | 2.9 | 4.5 | 5.7 |  | 1.9 | 2.8 | 2.6 | 3.4 | 1.4 | 1.8 | 3.9 | 2.2 | 2.1 | 2.3 | 1.5 |  | 2.1 | 2.2 | 1.6 | 1.7 |  | 1.8 | 0.9 |
| Cd | 0.07 | 0.16 | 0.05 | 0.18 |  | 0.05 | 0.07 | 0.07 | 0.06 | 0.05 | 0.05 | 0.05 | 0.15 | 0.05 | 0.3 | 0.27 |  | 0.06 | 0.09 | 0.06 | 0.14 |  | 0.08 | <0.05 |
| Co | 3.9 | 11.3 | 0.7 | 1.9 |  | 3.2 | 3.5 | 7.2 | 16.1 | 13.3 | 3 | 5.3 | 0.9 | 1.9 | 0.4 | 1.2 |  | 4.8 | 8.1 | 15.2 | 22.9 |  | 8.1 | 4.3 |
| Cr | 2 | 4 | 2 | 4 |  | 2 | 7 | 2 | 2 | 2 | 4 | 2 | 3 | 19 | 2 | <2 |  | 10 | 40 | 44 | 94 |  | 10 | 15 |
| Cs | 4.3 | 4.5 | 4.8 | 6.2 |  | 5.8 | 11.8 | 2.7 | 2.1 | 2.1 | 6.1 | 5.4 | 2.6 | 7.7 | 3.4 | 8.0 |  | 7.6 | 23.0 | 8.3 | 2.2 |  | 13.7 | 1.6 |
| Cu | 6 | 19.7 | 5 | 11.7 |  | 12 | 8 | 9 | 34 | 25 | 4 | 16 | 14.9 | 51.5 | 2 | 15.7 |  | 5 | 16.6 | 24 | 47.9 |  | 9 | 73 |
| Ga | 21.3 | 17.2 | 19.0 | 22.6 |  | 14.5 | 14.5 | 19.6 | 23.2 | 22.3 | 15.0 | 16.0 | 14.8 | 11.80 | 13.1 | 12.4 |  | 16.4 | 14.1 | 16.5 | 15.9 |  | 14.4 | 11.5 |
| Ge | 0.85 | 1.47 | 0.63 | 1.14 |  | 1.03 | 0.87 | 1.19 | 0.93 | 1.30 | 1.05 | 0.94 | 1.25 | 1.77 | 0.69 | 0.70 |  | 1.01 | 1.60 | 1.57 | 1.48 |  | 1.13 | 1.47 |
| Hf | 3.38 | 8.26 | 2.93 | 10.60 |  | 6.53 | 4.59 | 8.60 | 8.53 | 9.30 | 6.74 | 7.49 | 8.49 | 4.47 | 4.97 | 5.71 |  | 5.51 | 3.78 | 4.97 | 6.09 |  | 4.20 | 3.78 |
| Hg | 0.05 | <0.05 | <0.05 | 0.31 |  | 0.05 | 0.05 | 0.05 | 0.05 | 0.05 | 0.05 | 0.05 | <0.05 | 0.05 | 0.05 | <0.05 |  | 0.05 | 0.05 | 0.06 | <.05 |  | 0.05 | 0.1 |
| In | 0.08 | 0.05 | 0.06 | 0.06 |  | 0.04 | 0.04 | 0.06 | 0.06 | 0.06 | 0.04 | 0.05 | 0.03 | 0.04 | 0.03 | 0.04 |  | 0.04 | 0.05 | 0.05 | 0.04 |  | 0.04 | 0.02 |
| Li | <0.5 | 29.7 | <0.5 | 16.8 |  | <0.5 | <0.5 | <0.5 | <0.5 | <0.5 | <0.5 | <0.5 | 33.2 | 52.90 | <0.5 | 3.5 |  | <0.5 | 45.1 | <0.5 | 156 |  | <0.5 | 19.8 |
| Mo | 0.5 | 1.3 | 0.1 | 1.2 |  | 0.4 | 0.3 | 0.4 | 2.4 | 0.4 | 0.6 | 0.2 | 0.8 | 0.80 | 0.4 | 0.5 |  | 0.9 | 2.6 | 1.2 | 1.1 |  | 0.9 | 1.3 |
| Nb | 17.1 | 17.0 | 13.5 | 35.8 |  | 17.6 | 18.2 | 23.3 | 30.0 | 29.5 | 19.2 | 20.5 | 19.8 | 10.40 | 19.4 | 16.5 |  | 17.3 | 11.6 | 15.6 | 14.1 |  | 14.5 | 11.3 |
| Ni | 2 | 10 | 2 | 3 |  | 6 | 5 | 7 | 8 | 5 | 6 | 8 | 3 | 5.00 | 2 | 4 |  | 8 | 18 | 41 | 139 |  | 9 | 8 |
| Pb | 40.3 | 10.1 | 13.7 | 63.5 |  | 4.4 | 11.9 | 4.7 | 46.9 | 12.0 | 4.7 | 7.7 | 53.2 | 12.10 | 21.4 | 11.9 |  | 18.7 | 21.6 | 13.3 | 11.7 |  | 10.8 | 4.1 |
| Rb | 10 | 106 | 15 | 152 |  | 13 | 38 | 22 | 120 | 4 | 17 | 20 | 174 | 47.80 | 27 | 116 |  | 34 | 122 | 45 | 22 |  | 57 | 197 |

| Table A (continued) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Group 1 |  |  |  |  | Group 2 |  |  |  |  |  |  |  |  |  |  |  | Group 3 |  |  |  |  | Group 4 |  |
|  | ST | ST2 | SK | SK2 |  | SG-A | SG-B | SG-C | SG-D | SG-E | SG-F | SG-G2 | SG23 | SG3 | SP | SP2 |  | FGH | FGH2 | FKH | FKH2 |  | FKHS | FKHS2 |
| Sb | 0.2 | 0.5 | 0.2 | 2.3 |  | 0.2 | 0.6 | 0.2 | 0.2 | 0.1 | 0.3 | 0.2 | 0.4 | 0.7 | 0.7 | 0.2 |  | 0.2 | 0.6 | 0.4 | < 0.1 |  | 0.3 | 0.2 |
| Sc | 4 | 10 | 3 | 10 |  | 6 | 8 | 10 | 10 | 10 | 6 | 7 | 6 | 7 | 7 | 7 |  | 6 | 9 | 11 | 9 |  | 7 | 2 |
| Se | 0.17 | 0.30 | 0.14 | 0.40 |  | 0.15 | 0.19 | 0.36 | 0.32 | 0.16 | 0.10 | 0.26 | 0.15 | 0.21 | 0.21 | <0.05 |  | 0.15 | 0.30 | 0.13 | 0.56 |  | 0.19 | 0.45 |
| Sn | 7.7 | 2.5 | 6.7 | 4.4 |  | 4.5 | 3.4 | 4.4 | 5.4 | 5.0 | 4.6 | 5.0 | 2.6 | 3.6 | 3.6 | 2.7 |  | 4.0 | 2.1 | 2.1 | 1.3 |  | 2.8 | 1.6 |
| Sr | 44 | 426 | 57 | 223 |  | 146 | 231 | 94 | 184 | 137 | 154 | 56 | 135 | 100 | 100 | 618 |  | 120 | 329 | 116 | 114 |  | 181 | 610 |
| Ta | 0.13 | 1.22 | 0.12 | 1.78 |  | 0.47 | 0.4 | 2.26 | 0.28 | 2.58 | 0.16 | 0.15 | 1.73 | 0.26 | 0.26 | 1.47 |  | 0.11 | 0.99 | 0.13 | 1.06 |  | 0.1 | 0.99 |
| Te | <0.2 | <0.2 | <0.2 | <0.2 |  | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 | <0.2 |  | <0.2 | <0.2 | <0.2 | <0.2 |  | <0.2 | <0.2 |
| Th | 12.8 | 7.29 | 9.95 | 16.6 |  | 22.5 | 21 | 21.8 | 23.2 | 26.2 | 23.7 | 24.6 | 16.8 | 21.1 | 21.1 | 18 |  | 20.4 | 10 | 10.8 | 3.82 |  | 16.2 | 12.7 |
| Tl | <0.1 | 0.5 | 0.1 | 1.2 |  | <0.1 | <0.1 | 0.1 | 0.7 | <0.1 | <0.1 | <0.1 | 0.8 | <0.1 | <0.1 | 0.3 |  | 0.1 | 0.6 | 0.3 | 0.3 |  | 0.3 | 0.6 |
| U | 1.9 | 1.48 | 1.3 | 2.08 |  | 4.0 | 6.4 | 5.3 | 7.9 | 10.4 | 3.6 | 4.7 | 3.07 | 2.3 | 2.3 | 3.9 |  | 4.7 | 1.97 | 2.0 | 1.0 |  | 3.8 | 1.58 |
| V | 2 | 91 | 72 | 85 |  | 8 | 23 | 14 | 19 | 15 | 7 | 7 | 8 | 7 | 7 | 8 |  | 20 | 86 | 164 | 50 |  | 43 | 22 |
| Y | 16.1 | 23.9 | 19.9 | 40.2 |  | 31.3 | 35.4 | 53.7 | 60.4 | 37.8 | 35.7 | 33.9 | 39.7 | 26.5 | 26.5 | 37.4 |  | 38.1 | 17.2 | 20.9 | 14.5 |  | 23.6 | 16.8 |
| Zn | 80 | 78.8 | 58 | 59.9 |  | 76 | 54 | 102 | 67 | 147 | 83 | 111 | 52.4 | 188 | 188 | 80 |  | 61 | 81.2 | 68 | 76.2 |  | 56 | 48.9 |
| Zr | 79 | 257 | 70 | 342 |  | 194 | 153 | 333 | 343 | 303 | 211 | 231 | 221 | 152 | 152 | 122 |  | 185 | 107 | 206 | 183 |  | 140 | 96 |
| REEs (ppm) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| La | 17.50 | 29.00 | 15.80 | 45.90 |  | 39.30 | 38.50 | 51.20 | 52.00 | 59.60 | 43.90 | 44.90 | 40.90 | 34.80 | 34.80 | 32.80 |  | 43.00 | 28.00 | 25.00 | 22.20 |  | 29.60 | 24.80 |
| Ce | 40.00 | 56.40 | 34.00 | 83.10 |  | 74.90 | 70.30 | 90.00 | 102.00 | 111.00 | 83.30 | 83.40 | 76.60 | 67.30 | 67.30 | 67.50 |  | 77.60 | 53.60 | 48.10 | 46.60 |  | 54.90 | 43.30 |
| Pr | 4.58 | 6.80 | 4.19 | 9.53 |  | 8.75 | 8.56 | 11.30 | 11.80 | 13.70 | 9.80 | 9.99 | 9.11 | 7.75 | 7.75 | 7.95 |  | 8.68 | 6.29 | 5.80 | 5.66 |  | 6.35 | 5.04 |
| Nd | 17.00 | 27.30 | 16.40 | 36.60 |  | 32.60 | 33.10 | 43.50 | 46.20 | 52.20 | 37.00 | 38.10 | 34.80 | 29.40 | 29.40 | 29.20 |  | 32.50 | 23.50 | 23.40 | 23.00 |  | 24.60 | 19.00 |
| Sm | 4.23 | 5.23 | 4.16 | 7.37 |  | 6.08 | 6.23 | 8.30 | 9.00 | 10.10 | 6.62 | 7.03 | 6.38 | 5.74 | 5.74 | 5.58 |  | 5.93 | 4.28 | 4.59 | 4.35 |  | 4.59 | 3.62 |
| Eu | 0.39 | 1.44 | 0.37 | 1.76 |  | 0.72 | 0.93 | 1.50 | 1.62 | 1.74 | 0.83 | 0.86 | 1.27 | 0.71 | 0.71 | 1.20 |  | 0.77 | 0.99 | 1.10 | 1.17 |  | 0.89 | 0.88 |
| Gd | 3.94 | 4.83 | 4.32 | 7.11 |  | 5.48 | 6.02 | 8.18 | 9.09 | 9.28 | 6.33 | 6.61 | 5.82 | 5.29 | 5.29 | 5.70 |  | 5.84 | 3.97 | 4.36 | 3.59 |  | 4.25 | 3.56 |
| Tb | 0.63 | 0.80 | 0.72 | 1.26 |  | 0.87 | 0.99 | 1.35 | 1.48 | 1.44 | 1.02 | 1.04 | 1.03 | 0.85 | 0.85 | 0.94 |  | 1.00 | 0.57 | 0.66 | 0.63 |  | 0.64 | 0.56 |
| Dy | 3.41 | 4.43 | 3.87 | 7.13 |  | 5.10 | 5.85 | 8.51 | 9.17 | 7.65 | 5.88 | 5.86 | 5.94 | 4.83 | 4.83 | 5.70 |  | 6.05 | 3.31 | 3.91 | 3.25 |  | 3.78 | 2.98 |
| Ho | 0.54 | 0.93 | 0.65 | 1.54 |  | 1.09 | 1.20 | 1.87 | 1.98 | 1.41 | 1.23 | 1.22 | 1.43 | 0.98 | 0.98 | 1.36 |  | 1.29 | 0.64 | 0.79 | 0.67 |  | 0.79 | 0.64 |
| Er | 1.25 | 2.41 | 1.54 | 4.09 |  | 3.22 | 3.49 | 5.65 | 5.69 | 3.95 | 3.56 | 3.46 | 4.17 | 2.84 | 2.84 | 3.92 |  | 4.14 | 1.83 | 2.32 | 1.67 |  | 2.33 | 1.72 |
| Tm | 0.11 | 0.41 | 0.12 | 0.72 |  | 0.31 | 0.34 | 0.57 | 0.56 | 0.37 | 0.35 | 0.33 | 0.77 | 0.28 | 0.28 | 0.73 |  | 0.40 | 0.35 | 0.22 | 0.28 |  | 0.21 | 0.31 |
| Yb | 0.89 | 2.11 | 1.07 | 4.12 |  | 2.95 | 3.24 | 5.58 | 5.18 | 3.39 | 3.39 | 3.03 | 4.31 | 2.78 | 2.78 | 4.15 |  | 3.99 | 2.01 | 1.98 | 1.44 |  | 2.01 | 1.54 |
| Lu | 0.14 | 0.36 | 0.40 | 0.72 |  | 0.45 | 0.48 | 0.54 | 0.56 | 0.58 | 0.58 | 0.39 | 0.74 | 0.44 | 0.44 | 0.73 |  | 0.21 | 0.32 | 0.10 | 0.26 |  | 0.15 | 0.38 |

1 Suffix “2 and 3” show the parent rock samples.

2 Sample SG2 is the parent rocks of the bentonites SG-D, SG-E, SG-F, SG-G. Samples SG-A, SG-B, SG-C (bentonite) and SG3 (volcanic rock) were randomly taken from other horizons of the Chah-Golestan deposit.

3 Sample SG-G was used in the percentage change calculation.