# Naproxen/layered double hydroxide composites for tissue engineering application: physicochemical characterization and biological evaluation

# Marcela P. Bernardo a*; Bruna C.S. Rodrigues a; Tamires D. de Oliveira b, Adriana P. M. Guedes b, Alzir A. Batista b, Luiz H.C. Mattoso a

a Embrapa Instrumentation, Brazilian Agricultural Research Corporation, São Carlos, São Paulo, Brazil

b Department of Chemistry, Federal University of São Carlos, São Paulo, Brazil

SUPPORTING INFORMATION

Figure SI 1. Thermogravimetric (TG) and differential thermogravimetric (DTG) curves of commercial sodium naproxen.

Figure SI 2: Naproxen release at aqueous medium

Figure SI 3. 1H NMR spectrum in D2O for sodium naproxen

Figure SI 4. Cell viability of pure naproxen. IC50: 1.03 ± 0.23 (mg/mL)

Table SI 1. Higuchi and zero-order kinetic parameters obtained for naproxen release from [Mg-Al]-LDH/NAP

| Initial concentration (g/L) | Higuchi | Zero order |
| --- | --- | --- |
|  | R2 | K | R2 | K |
| 1 | 0.87 | 0.0068 | 0.92 | 0.00002 |
| 1.2 | 0.87 | 0.0017 | 0.89 | 0.00004 |
| 1.8 | 0.82 | 0.0028 | 0.24 | 0.00006 |
| 2.5 | 0.80 | 0.0017 | 0.36 | 0.00004 |
| 3 | 0.94 | 0.0019 | 0.78 | 0.00004 |