Supplemental Material

S1: Supplementary FTIR and XRD patterns of unaltered materials	2

S1.1 Assignment of FTIR bands	2

S1.2 Figure: Comparison of FTIR with literature	3

S1.3: Figure: Comparison of XRD patterns with literature	4

S2: Differential scanning calorimetry/evolved gas analysis of unaltered samples	5

S2.1: Figures: Evolved gas analysis	5

S2.2: Differential scanning calorimetry methods	6

S2.2: Figure: Differential scanning calorimetry	7

S3: Microscopy of unaltered samples	7

S3.1: Figure: SEM/EDS of unaltered materials	7

S3.2: Figure: FE-SEM of unaltered samples	8

S4. Dissolution	9

S4.1: Figure: Change in pH over course of reaction (past linear portion used for dissolution rates)	9

S4.2: Figure: Fe release	10

S4.3: Figure: Al release	11

S4.4: Figures: Silica release	12

S5: Figure: Supplementary XRD patterns of altered materials	16

S6: Microscopy of altered materials	17

S6.1 Figures: SEM/EDS of altered materials	17

S6.2: Figures: TEM of altered materials	18

S7: Figure: Comparison with Si from total digestion	22

S8: Balanced chemical equations	22

S8.1: At pH 3	23

S8.2: At pH 5	23

S8.3: At pH 7	23

S8.4: At pH 10	23

S9: Supplemental Tables	25

S9.1: Table: Allophane compositions by SEM/EDS	25

S9.2 Table: Full results of BET surface area and particle size analyses	26

S9.3 Tables: Comparisons with compositions from the literature	27

S9.4: Table: Experiments examined by HRTEM	31

S10. Solution chemistry data sheets	32

# S1: Supplementary FTIR and XRD patterns of unaltered materials

# S1.1 Assignment of FTIR bands

The FTIR spectra for Fe-free allophane, Fe-poor allophane, and Fe-rich allophane are shown in Fig. S1. The broad band at 3400 cm-1 (2.94 μm) is due to stretching vibration of H2O molecules. The band centered at 1645 cm-1 (6.08 μm) is assigned to bending vibration of H2O molecules and is much sharper than the stretching modes. Based on the low intensity of the sharp H2O bending band, compared with the properties of the H2O stretching band, we conclude, in agreement with previous observations, that most of the water in our synthetic materials is likely adsorbed rather than structural (Wada 1989; Ohashi et al. 2002; Montarges-Pelletier et al. 2005). The energy and short lifetime of the vibrational state is typical for water that is not structurally bound, indicating that this band is likely due to adsorbed water. Bands at 1030 cm-1 (9.71 μm) and 940 cm-1 (10.64 μm) are due to Si-O-Al stretching (Bishop et al. 2013). A band due to O-H and/or Al-O bending exists near 620 cm-1 (16.13 μm) (Bishop et al. 2013). Of our synthetic materials, Fe-free allophane has the clearest 620 cm-1 band, although it is shifted to higher wavenumber (~630 cm-1 or 15.87 μm) compared to the reference material described by Rampe et al. (2012) and shown in Fig. S1, which may be due to the higher Si/Al ratio of our material (Si/Al ≈ 1) versus the reference material (Si/Al = 0.44). The band is distinguishable in Fe-poor allophane, and shifted to even higher wavenumber (~696 cm-1 or 14.37 μm), possibly due to the influence of Fe-O bending vibrations. The band is located at ~670 cm-1 (14.93 μm) in Fe-rich allophane, although it is difficult to distinguish in this dataset due to noise.

## S1.2 Figure: Comparison of FTIR with literature

Fig. S1 FTIR spectra from synthetic Fe-free allophane, Fe-poor allophane, and Fe-rich allophane compared to the VNIR pattern of a synthetic allophane with Si/Al ratio of 0.44 (Rampe et al. 2012). Differing Si/Al ratios are likely responsible for the shifts in wavenumber and intensity in the peak around 620 cm-1. Patterns are offset for clarity.

## S1.3: Figure: Comparison of XRD patterns with literature

Fig. S2 Synthetic Fe-free allophane, Fe-poor allophane, and Fe-rich allophane compared with synthetic allophane with a Si/Al ratio of 0.44 (Rampe et al. 2012). Patterns are offset for clarity.

# S2: Differential scanning calorimetry/evolved gas analysis of unaltered samples

## S2.1: Figures: Evolved gas analysis

Fig. S3 Mass-18 H2O release from synthetic Fe-free allophane (a), Fe-poor allophane (b), and Fe-rich allophane (c). Mass-18 H2O release was measured to investigate adsorbed and/or structural water. Samples were run in duplicate to allow estimates of uncertainty. The sharp peak around 130-150ºC with a broad shoulder extending out to ~400°C agrees well with other literature values for allophane EGA (e.g., Bish and Duffy 1990; Rampe et al. 2016).

Fig. S4 Mass-32 O2 release from synthetic Fe-free allophane (a), Fe-poor allophane (b), and Fe-rich allophane (c). Mass-32 O2 release was measured to provide a baseline comparison with the O2 releases due to per/chlorate in martian samples (e.g., Sutter et al. 2017). Samples were run in duplicate to allow estimates of uncertainty. The O2 release occurs concurrently with the H2O release in all samples, indicating that the O2 release is due to fragmentation of water in the mass spectrometer.

# S2.2: Differential scanning calorimetry methods

Differential scanning calorimetry (DSC) and evolved gas analysis (EGA) were conducted on unaltered samples of Fe-free allophane, Fe-poor allophane, and Fe-rich allophane under SAM-like conditions (i.e., ramp rate of 35°C per minute, pressure of 30 mbar, and helium carrier gas). The DSC curves (Fig. S5) were used to identify the characteristic exothermic peak of allophane transformation to mullite at ~900°C.

## S2.2: Figure: Differential scanning calorimetry

Fig. S5 Differential scanning calorimetry (DSC) curves for Fe-free allophane, Fe-poor allophane, and Fe-rich allophane. The exothermic peak at 950 ± 14°C is characteristic of the transformation of allophane to mullite (Ossaka et al. 1971). This peak shifts to lower temperatures as Fe content increases (924 ± 1°C in Fe-poor allophane and 791 ± 1°C in Fe-rich allophane) due to the formation of an intermediate silico-alumina spinel phase during the transformation to mullite (Ossaka et al. 1971).

# S3: Microscopy of unaltered samples

## S3.1: Figure: SEM/EDS of unaltered materials

Fig. S6 SEM images of unaltered synthetic Fe-free allophane (a), Fe-poor allophane (b), and Fe-rich allophane (c). The "fluffy" texture of the grains is indicative of nanoball structures.

## S3.2: Figure: FE-SEM of unaltered samples

Fig. S7 FE-SEM images of synthetic Fe-free allophane (a), Fe-poor allophane (b), and Fe-rich allophane (c). The "fluffy" texture of the grains indicates that they are aggregates of nanoballs, each ~5 nm in diameter. The apparent “smooth” regions in the Fe-rich allophane sample (right) are likely more of the same nanoball texture that is significantly out of focus due to the topography of the samples.

# S4. Dissolution

## S4.1: Figure: Change in pH over course of reaction (past linear portion used for dissolution rates)

Fig. S8 Change in pH with time over course of entire experiment for (a) initial pH of 3, (b) initial pH of 5, (c) initial pH of 7, and (d) and initial pH of 10. Linear regions used for rate determination are shaded. Solutions were not buffered and were allowed to exchange with the atmosphere. Full data sheets for all experiments are given in Section S10.

## S4.2: Figure: Fe release

Fig. S9 Moles of Fe released into solution with time for Fe-rich allophane duplicates in experiments with initial pH of 3. Data Sheets S36-S38 (Section S9 below) show Fe concentration in solution and solution pH for each experiment with Fe above the practical quantitation limit of the spectrometer (0.2 mg L-1) at each time point.

## S4.3: Figure: Al release

Fig. S10 Moles of Al released into solution with time for Fe-free allophane, Fe-poor allophane, and Fe-rich allophane in experiments with initial pH of 3. Data Sheets S26-S35 (Section S10 below) show Al concentration in solution and solution pH for each experiment with Al above the practical quantitation limit of the spectrometer (1.0 mg  L-1) at each time point.

## S4.4: Figures: Silica release

Fig. S11 Silica release from Fe-free allophane, Fe-poor allophane, and Fe-rich allophane duplicates for experiments with initial pH of 3.

Fig. S12 Silica release from Fe-free allophane, Fe-poor allophane, and Fe-rich allophane duplicates for experiments with initial pH of 5.

Fig. S13 Silica release from Fe-free allophane, Fe-poor allophane, and Fe-rich allophane duplicates for experiments with initial pH of 7. Insets show an expanded view of the first four days. Note scale differences.

Fig. S14 Silica release from Fe-free allophane, Fe-poor allophane, and Fe-rich allophane duplicates for experiments with initial pH of 10. Data Sheets S1-S25 (Section S10 below) show silica concentration in solution and solution pH for each experiment at each time point.

# S5: Figure: Supplementary XRD patterns of altered materials

Fig. S15 XRD patterns for unreacted Fe-free allophane, Fe-poor allophane, Fe-rich allophane (a), and the final solid material from all Fe-free allophane (b), Fe-poor allophane (c), and Fe-rich allophane (d) dissolution experiments. Patterns are offset for clarity. Minor quartz impurities are likely the result of grinding in agate mortar and pestle. Broad low-angle peaks (~10° 2θ) may indicate the formation of clay mineral precursors. Ph? = possible incipient phyllosilicate, Qtz = quartz.

# S6: Microscopy of altered materials

## S6.1 Figures: SEM/EDS of altered materials

Fig. S16 SEM of Fe-rich allophane reacted in 0.1M NaCl solution at pH ~4 for two days. Although selected grains are smaller than those in the unaltered Fe-rich allophane, overall grain-size distribution did not appear significantly different.

Fig. S17 SEM of Fe-rich allophane reacted in 0.1M NaCl solution at pH ~4 for one month.

## S6.2: Figures: TEM of altered materials

Fig. S18 TEM image of Fe-rich allophane agglomerate grain reacted in a solution with initial pH of 10 for 57 days that contains several incipient phyllosilicate structures. Some grains (e.g. Fig. 9a) were much richer in incipient phyllosilicate structures than the one shown here.

Fig. S19 TEM image of incipient phyllosilicate structure developing from poorly-crystalline Fe-rich allophane reacted in a solution with initial pH of 3 for 181 days. Some phyllosilicate-like structures, like the one above, were observed.

Fig. S20 TEM of Fe-free allophane reacted in a solution with initial pH of 10 for 57 days. While incipient phyllosilicate structures were seen in this sample, they were much less abundant than in Fe-rich allophane reacted in solution with initial pH of 10 for the same amount of time (Fig S18, Fig 9a).

Fig. S21 TEM image of Fe-free allophane reacted in solution with initial pH of 10 for 57 days, showcasing the beam-sensitive nature of the "blobby" material. The image on the left was taken before exposing the material to the high-energy STEM beam. The image on the right was taken after exposing the material to the STEM beam for less than one minute.

## S7: Figure: Comparison with Si from total digestion

Fig. S22 Comparison of the difference in wt.% SiO2 between unaltered and altered samples (from total digestions) versus the wt.% SiO2 released into solution (calculated from moles Si released and the total reacted sample mass). The lack of change above error in SiO2 content observed in Fe-free allophane and Fe-poor allophane samples (except Fe-poor allophane reacted at pH 7) indicates either congruent dissolution or re-precipitation of an SiO2-rich phase prior to the end of these experiments. Error bars represent the 1-σ standard deviation between two runs of each sample. The dashed line indicates no change in the SiO2 content between reacted and unreacted samples. Open points represent the starting materials

# S8: Balanced chemical equations

Chemical equations for the dissolution of Fe-free allophane, Fe-poor allophane, and Fe-rich allophane were obtained for each pH condition. The composition of the starting material was based on the ratios of Al, Fe, and Si used in the synthesis process (see Table 1). Speciation of Al, Fe, and Si with pH was taken into account with regard to the starting pH of each experiment, in order to reflect the initial production or uptake of H+ ions that resulted in pH change.

## S8.1: At pH 3

Fe-free allophane: (Al2O3)(SiO2)2•3H2O + 6H+ → 2Al3+ + 2H4SiO4 + 2H2O

Fe-poor allophane: (Fe2O3)0.01(Al2O3)0.99(SiO2)2•3H2O + 5.98H+ → 1.98Al3+ + 0.02Fe(OH)2+ + 2H4SiO4 + 1.98H2O

Fe-rich allophane: (Fe2O3)0.5(Al2O3)0.5(SiO2)2•3H2O + 5H+ → Al3+ + Fe(OH)2+ +2H4SiO4 + H2O

## S8.2: At pH 5

Fe-free allophane: (Al2O3)(SiO2)2•3H2O + 2H2O + 2H+ → 2Al(OH)2+ + 2H4SiO4

Fe-poor allophane: (Fe2O3)0.01(Al2O3)0.99(SiO2)2•3H2O + 2.02H2O + 1.98H+ → 1.98Al(OH)2+ + 0.02Fe(OH)3 + 2H4SiO4

Fe-rich allophane: (Fe2O3)0.5(Al2O3)0.5(SiO2)2•3H2O + 3H2O + H+ → Al(OH)2+ + Fe(OH)3 + 2H4SiO4

## S8.3: At pH 7

Fe-free allophane: (Al2O3)(SiO2)2•3H2O + 4H2O → 2Al(OH)3 + 2H4SiO4

Fe-poor allophane: (Fe2O3)0.01(Al2O3)0.99(SiO2)2•3H2O + 4H2O → 1.98Al(OH)3 + 0.02Fe(OH)3 + 2H4SiO4

Fe-rich allophane: (Fe2O3)0.5(Al2O3)0.5(SiO2)2•3H2O + 4H2O → Al(OH)3 + Fe(OH)3 + 2H4SiO4

## S8.4: At pH 10

Fe-free allophane: (Al2O3)(SiO2)2•3H2O + 6H2O → 2Al(OH)4- + 2H3SiO4- + 4H+

Fe-poor allophane: (Fe2O3)0.01(Al2O3)0.99(SiO2)2•3H2O + 6H2O → 1.98Al(OH)4- + 0.02Fe(OH)4- + 2H3SiO4- + 4H++

Fe-rich allophane: (Fe2O3)0.5(Al2O3)0.5(SiO2)2•3H2O + 6H2O → Al(OH)4- + Fe(OH)4- + 2H3SiO4- + 4H+

# S9: Supplemental Tables

## S9.1: Table: Allophane compositions by SEM/EDS

Table S1. Table of experiments examined by TEM for the presence of alteration products.

Table S1. EDS results from selected grains of unaltered synthetic Fe-free allophane, unaltered synthetic Fe-poor allophane, and unaltered synthetic Fe-rich allophane, as well as synthetic Fe-rich allophane reacted at pH ~4 for approximately 2 days, and synthetic Fe-rich allophane reacted at pH ~4 for approximately 4 months. Values were obtained by averaging the atomic percentages for each element from 2-4 EDS spectra taken from multiple grains within each sample. The rough surfaces of the grains may be responsible for high uncertainties. Decreasing Si, Fe, and Al values and increasing O values may indicate that the material becomes more hydrous with increasing reaction time. The total values are low due to the presence of a large amount of water in the samples. Error represents the 1-σ standard deviation between the multiple EDS spectra.

| Sample ID | Reaction time (hrs) | Final pH | Si (wt%) | Al (wt%) | Fe (wt%) | Na (wt%) | Cl (wt%) | O (wt%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fe-free allophane-0 | 0 | N/A | 11.61 ± 6.62 | 10.84 ± 5.76 | N/A | 4.98 ± 3.98 | N/A | 62.59 ± 2.29 |
| Fe-poor allophane-0 | 0 | N/A | 10.26 ± 5.31 | 8.71 ± 4.68 | N/A | 4.30 ± 2.49 | N/A | 63.07 ± 0.60 |
| Fe-rich allophane-0 | 0 | N/A | 3.98 ± 2.05 | 1.86 ± 0.75 | 4.93 ± 2.38 | 1.33 ± 0.63 | 0.23 ± 0.22 | 65.94 ± 2.90 |
| Fe-rich allophane-2d | 46 | 5.35 | 1.46 ± 1.32 | 1.14 ± 0.71 | 2.69 ± 1.55 | 0.78 ± 0.66 | N/A | 68.96 ± 2.23 |
| Fe-rich allophane-4mo | 739 | 6.54 | 0.63 ± 0.85 | 0.81 ± 0.27 | 0.86 ± 0.65 | 0.69 ± 0.26 | 0.045 ± 0.11 | 69.65 ± 1.09 |

## S9.2 Table: Full results of BET surface area and particle size analyses

Table S2. Particle size analysis and BET specific surface areas for Fe-free allophane, Fe-poor allophane, and Fe-rich allophane. The graphic mean particle size is calculated by averaging the particle sizes at the 16th percentile, the 50th percentile, and the 84th percentile (Mz = (16th + 50th +84th) / 3), where each percentile represents the theoretical sieve size at which 16%, 50%, and 84% of the particles would pass through. The graphic standard deviation represents the width of the particle size distribution (SD = 84th – 16th) / 2), and is not an indication of variability between measurements. Uncertainty is not calculated on individual BET SSA measurements; samples were run in duplicate to allow estimates of uncertainty (given in Section 3.1.5). Duplicates are denoted by the "-1" and "-2" suffixes.

| Material | Mass (mg) | Graphic mean particle size (µm) | Graphic standard deviation | BET SSA (m2/g) |
| --- | --- | --- | --- | --- |
| Fe-free allophane-1 | 408.5 | 165.3 | 91.12 | 385.62 |
| Fe-free allophane-2 | 408.5 | 169.6 | 87.85 | 385.91 |
| Fe-poor allophane-1 | 400.8 | 132.3 | 83.04 | 410.87 |
| Fe-poor allophane-2 | 400.8 | 133.99 | 80.28 | 389.52 |
| Fe-rich allophane-1 | 402.0 | 161.6 | 44.35 | 507.27 |
| Fe-rich allophane-2 | 402.0 | 171.4 | 61.39 | 507.70 |

## S9.3 Tables: Comparisons with compositions from the literature

Table S3. Composition of our unaltered synthetic Fe-free allophane, as measured by ICP-MS after total digestion, compared with compositions of several natural and synthetic allophanes from the literature. “NR” = Not reported.

| Sample | SiO2/Al2O3 ratio | SiO2 (wt%) | Al2O3 (wt%) | FeOT (wt%) |
| --- | --- | --- | --- | --- |
| Unaltered Fe-free allophane1 | 0.939 | 30.23 | 32.18 | 0 |
| Silica Springs (1013)2 | 1.10 | 33.37 | 43.84 | 0.28 |
| Ohakune; W-133.23 | 0.830 | NR | NR | NR |
| 9054,5,6 | 0.910 | NR | NR | NR |
| 10414,5,7 | 1.03 | NR | NR | NR |
| A.P.; W-164.28 | 1.12 | NR | NR | NR |
| Ki-P9 | 1.19 | NR | NR | NR |
| Ki-G9 | 0.960 | NR | NR | NR |
| Ku-P10,11 | 1.22 | NR | NR | NR |
| Ku-G10,11 | 1.02 | NR | NR | NR |
| Tirau; W-130.23 | 1.26 | NR | NR | NR |
| Taupo; W132.33 | 1.29 | NR | NR | NR |
| Ka-P12 | 1.30 | NR | NR | NR |
| Mt. Schank; W-139.313,14 | 1.31 | NR | NR | NR |
| PA15 | 1.54 | NR | NR | NR |
| PA-P15 | 1.75 | NR | NR | NR |
| VA6,15 | 1.77 | NR | NR | NR |
| Mazama; W-159.38 | 1.97 | NR | NR | NR |
| Fe-free allophane New Zealand soils16 | 1.20 | NR | NR | NR |
| Fe-free allophane New Zealand soils16 | 0.51 | NR | NR | NR |
| Synthetic Fe-free allophane 117 | 0.44 | NR | NR | NR |
| Synthetic Fe-free allophane 217 | 0.58 | NR | NR | NR |
| Synthetic Fe-free allophane 317 | 0.92 | NR | NR | NR |

1This study

2Theng et al. (1982)

3Gibbs (1968)

4Aomine and Yoshinaga (1955)

5Yoshinaga and Aomine (1962a, b)

6Wada and Tokashiki (1972)

7Wada and Greenland (1970)

8Dudas (1973)

9Wada and Matsubara (1968)

10Yoshinaga and Yamaguchi (1970)

11Tazaki (1971)

12Aomine and Mizota (1973)

13Wada and Matsubara (1968)

14Hamblin and Greenland (1972)

15Aomine and Wada (1962)

16Birrell and Fieldes (1952)

17Rampe et al. (2012)

Table S4. Composition of our unaltered synthetic Fe-poor allophane, as measured by ICP-MS after total digestion, compared with compositions of several natural Fe-poor allophanes from the literature.

| Sample | Si/Al+Fe ratio | SiO2 (wt%) | Al2O3 (wt%) | FeOT (wt%) |
| --- | --- | --- | --- | --- |
| Unaltered Fe-poor allophane1 | 1.04 | 29.62 | 28.01 | 0.47 |
| Fe-free allophane Misotsuchu2 | 0.810 | 28.31 | 34.41 | 0.56 |
| Fe-free allophane Kanumatsuchi2 | 0.849 | 29.17 | 33.81 | 0.56 |
| Fe-free allophane-like sample3 | 0.551 | 19.9 | 27.6 | 8.5 |
| Waxy-Pan4 | 0.673 | 29.52 | 39.49 | 4.39 |
| Egmont4 | 0.804 | 32.09 | 32.88 | 7.01 |

1This study

2Kitagawa (1974)

3Gérard et al. (2007)

4de Roy et al. (1980)

Table S5. Composition of our unaltered synthetic Fe-rich allophane, as measured by ICP-MS after total digestion, compared with compositions of several natural hisingerites from the literature. “NR” = Not reported.

| Sample | Si/Al+Fe ratio | SiO2 (wt%) | Al2O3 (wt%) | Fe2O3 (wt%) | FeO (wt%) |
| --- | --- | --- | --- | --- | --- |
| Unaltered Fe-rich allophane1 | 0.82 | 30.19 | 17.54 | 19.28 | NR |
| Riddarhyttan (EMP)2 | 0.80 | 35.83 | 0.56 | 44.08 | 0 |
| Gillinge2 | 0.91 | 36.98 | 0.05 | 40.57 | 0 |
| Solberg2 | 1.80 | 38.78 | 0.83 | 20.69 | 0 |
| Broken Hill2 | 0.91 | 36.63 | 0.96 | 39.23 | 0 |
| Canby2 | 0.89 | 37.62 | 1.46 | 40.79 | NR |
| Bellevue King2 | 1.09 | 38.97 | 1.91 | 33.8 | NR |
| 700802 | 0.91 | 36.98 | 0.05 | 40.57 | NR |
| 48-18172 | 0.99 | 39.01 | 2.92 | 36.38 | NR |
| Hisinger3 | 0.48 | 27.5 | 5.5 | 51.5 | 0 |
| Rammelsberg4 | 1.07 | 32.18 | 0 | 30.1 | 8.63 |
| MGIU 400/45 | 1.74 | 34.21 | 0.97 | 18.68 | 1.55 |
| MGIU 400/2 (L&J)6 | 0.94 | 35.24 | 2 | 35.51 | 2.4 |
| MGIU 400/22 | 1.80 | 38.78 | 0.83 | 20.69 | 0 |

1This study

2Eggleton and Tilley (1998)

3Hisinger (1828)

4Rammelsberg (1848)

5Mackenzie and Berezowski (1980)

6Lindqvist and Jansson (1962)

Table S6. Putative compositions, in weight percent, of the martian amorphous soil component, as calculated by Dehouck et al. (2014) and Vaniman et al. (2014), compared with the compositions of our unreacted synthetic Fe-free allophane, Fe-poor allophane, and Fe-rich allophane measured by ICP-MS after total digestion. “NA” = None added.

| Oxide (wt%) | Mars amorphous soil component (Dehouck et al., 2014) | Mars amorphous soil component (Vaniman et al., 2014) | Synthetic Fe-free allophane (this study) | Synthetic Fe-poor allophane (this study) | Synthetic Fe-rich allophane (this study) |
| --- | --- | --- | --- | --- | --- |
| SiO2 | 31.9-37.1 | 30.10-32.94 | 29.51-30.95 | 29.15-30.09 | 29.94-30.44 |
| Al2O3 | 2.8-5.9 | 4.14-9.08 | 31.59-32.77 | 27.39-28.63 | 17.34-17.74 |
| FeOT | 23.7-27.7 | 23.04-33.46 | 0* | 0.46-0.49* | 18.94-19.62* |
| SO3 | 11.0-16.1 | 8.72-10.76 | NA | NA | NA |
| Na2O | 3.6-4.4 | 3.68-5.98 | NA | NA | NA |
| CaO | 3.7-5.4 | 6.46-11.61 | NA | NA | NA |
| P2O5 | 2.1-3.1 | 2.28-2.87 | NA | NA | NA |
| TiO2 | 2.1-2.9 | 2.03-2.98 | NA | NA | NA |
| MgO | 1.2-4.8 | 0.01-0.07 | NA | NA | NA |
| Cl | 1.4-2.0 | 1.08-1.31 | NA | NA | NA |
| Cr2O3 | 1.1-1.6 | 1.07-1.30 | NA | NA | NA |
| MnO | 0.9-1.4 | 0.66-0.75 | NA | NA | NA |
| K2O | 0.8-1.1 | 0.56-1.44 | NA | NA | NA |

*Calculated as wt% Fe2O3

## S9.4: Table: Experiments examined by HRTEM

Table S7. Table of experiments examined by HRTEM for the presence of alteration products.

| Experiment | Initial pH | Final pH | Total Experiment Time |
| --- | --- | --- | --- |
| FRA_pH0_3 | 3.01 | 4.78 | 181 days |
| FRA_pH0_10 | 10.36 | 6.39 | 57 days |
| FPA_pH0_10 | 10.36 | 8.59 | 57 days |

# S10. Solution chemistry data sheets

Data Sheet S1. Dissolved silica analysis for experiment Al+Si-p3.5-1

Material: Fe-free allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 385.6192 m2/g

Batch ID: Al+Si-p3.5-1	Material mass: 0.1501 g	Total Surface Area (BET): 57.8814 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.25 | 170 | 0.62344 | 3.99561 x 10-6 |
| 10800 | 3.38 | 160 | 1.52098 | 9.74798 x 10-6 |
| 18000 | 3.48 | 150 | 2.36683 | 1.48678 x 10-5 |
| 86400 | 4.08 | 140 | 5.62654 | 3.34381 x 10-5 |
| 97200 | 4.10 | 130 | 6.06911 | 3.58017 x 10-5 |
| 192000 | 4.28 | 120 | 7.75414 | 4.42012 x 10-5 |
| 278400 | 4.31 | 110 | 8.67957 | 4.84848 x 10-5 |
| 451200 | 4.31 | 100 | 9.52142 | 5.20818 x 10-5 |
| 627600 | 4.34 | 90 | 10.02826 | 5.40669 x 10-5 |
| 969600 | 4.34 | 80 | 11.27198 | 5.84952 x 10-5 |
| 1732800 | 4.42 | 70 | 15.00643 | 7.04622 x 10-5 |

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9989 | N/A |
| Si release rate | 7.55 x 10-10 | 2.54 x 10-11 |

Diss. Rate Mineral (rdiss)	1.30 x 10-12 mol m-2 s-1

Uncertainty of fit		4.38 x 10-13 mol m-2 s-1

Data Sheet S2. Dissolved silica analysis for experiment Al+Si-p3.5-2

Material: Fe-free allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 385.6192 m2/g

Batch ID: Al+Si-p3.5-2	Material mass: 0.1499 g	Total Surface Area (BET): 57.8043 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.25 | 170 | 0.65475 | 4.19627 x 10-6 |
| 10800 | 3.38 | 160 | 1.40991 | 9.03612 x 10-6 |
| 18000 | 3.48 | 150 | 2.18205 | 1.37098 x 10-5 |
| 86400 | 4.08 | 140 | 5.81134 | 3.43855 x 10-5 |
| 97200 | 4.10 | 130 | 5.97961 | 3.52842 x 10-5 |
| 192000 | 4.28 | 120 | 7.55600 | 4.31421 x 10-5 |
| 278400 | 4.31 | 110 | 8.37674 | 4.69411 x 10-5 |
| 451200 | 4.31 | 100 | 9.96674 | 5.37347 x 10-5 |
| 627600 | 4.34 | 90 | 10.08559 | 5.42002 x 10-5 |
| 969600 | 4.34 | 80 | 11.23109 | 5.82788 x 10-5 |
| 1732800 | 4.42 | 70 | 14.85432 | 6.98894 x 10-5 |

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9820 | N/A |
| Si release rate | 3.22 x 10-10 | 2.52 x 10-11 |

Diss. Rate Mineral (rdiss)	5.57 x 10-12 mol m-2 s-1

Uncertainty of fit		4.35 x 10-13 mol m-2 s-1

Data Sheet S3. Dissolved silica analysis for experiment 1:99-p3.5-1

Material: Fe-poor allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 350.2424 m2/g

Batch ID: 1:99-p3.5-1	Material mass: 0.1503 g	Total Surface Area (BET): 52.6414 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.21 | 170 | 0.48140 | 3.08530 x 10-6 |
| 10800 | 3.34 | 160 | 1.17056 | 7.50215 x 10-6 |
| 18000 | 3.43 | 150 | 1.93204 | 1.21113 x 10-5 |
| 86400 | 4.04 | 140 | 5.17694 | 3.05972 x 10-5 |
| 97200 | 4.04 | 130 | 5.54620 | 3.25693 x 10-5 |
| 192000 | 4.27 | 120 | 6.68938 | 3.82678 x 10-5 |
| 278400 | 4.29 | 110 | 7.89359 | 4.38417 x 10-5 |
| 451200 | 4.35 | 100 | 9.34076 | 5.00250 x 10-5 |
| 627600 | 4.33 | 90 | 9.72676 | 5.15369 x 10-5 |
| 969600 | 4.36 | 80 | 11.10038 | 5.64277 x 10-5 |
| 1732800 | 4.35 | 70 | 14.55117 | 6.74857 x 10-5 |

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9837 | N/A |
| Si release rate | 3.00 x 10-10 | 2.23 x 10-11 |

Diss. Rate Mineral (rdiss)	5.70 x 10-12 mol m-2 s-1

Uncertainty of fit		4.23 x 10-13 mol m-2 s-1

Data Sheet S4. Dissolved silica analysis for experiment 1:99-p3.5-2

Material: Fe-poor allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 350.2424 m2/g

Batch ID: 1:99-p3.5-2	Material mass: 0.1502 g	Total Surface Area (BET): 52.6064 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.24 | 170 | 0.53769 | 3.44607 x 10-6 |
| 10800 | 3.38 | 160 | 1.68775 | 1.08168 x 10-5 |
| 18000 | 3.48 | 150 | 2.30931 | 1.45791 x 10-5 |
| 86400 | 4.13 | 140 | 5.45357 | 3.24916 x 10-5 |
| 97200 | 4.14 | 130 | 5.84633 | 3.45892 x 10-5 |
| 192000 | 4.31 | 120 | 7.05800 | 4.06291 x 10-5 |
| 278400 | 4.32 | 110 | 8.20371 | 4.59323 x 10-5 |
| 451200 | 4.35 | 100 | 9.50207 | 5.14798 x 10-5 |
| 627600 | 4.35 | 90 | 9.89773 | 5.30294 x 10-5 |
| 969600 | 4.38 | 80 | 11.01385 | 5.70034 x 10-5 |
| 1732800 | 4.37 | 70 | 14.91793 | 6.95140 x 10-5 |

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9662 | N/A |
| Si release rate | 7.73 x 10-10 | 1.45 x 10-10 |

Diss. Rate Mineral (rdiss)	1.47 x 10-11 mol m-2 s-1

Uncertainty of fit		2.75 x 10-12 mol m-2 s-1

Data Sheet S5. Dissolved silica analysis for experiment 50:50-p3.5-1

Material: Fe-rich allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 507.2660 m2/g

Batch ID: 50:50-p3.5-1	Material mass: 0.1496 g	Total Surface Area (BET): 75.8870 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.07 | 170 | 0.00156* | 1.00003 x 10-8* |
| 10800 | 3.08 | 160 | 0.39471 | 2.52970 x 10-6 |
| 18000 | 3.07 | 150 | 0.53403 | 3.37301 x 10-6 |
| 86400 | 3.25 | 140 | 2.37561 | 1.38643 x 10-5 |
| 97200 | 3.23 | 130 | 2.87626 | 1.65382 x 10-5 |
| 192000 | 3.38 | 120 | 4.5101 | 2.46823 x 10-5 |
| 278400 | 3.46 | 110 | 6.09358 | 3.20120 x 10-5 |
| 451200 | 3.63 | 100 | 8.77310 | 4.34607 x 10-5 |
| 627600 | 3.73 | 90 | 10.01703 | 4.83326 x 10-5 |
| 969600 | 3.89 | 80 | 11.78698 | 5.46346 x 10-5 |
| 1732800 | 3.97 | 70 | 16.61515 | 7.01065 x 10-5 |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9937 | N/A |
| Si release rate | 1.65 x 10-10 | 7.55 x 10-12 |

Diss. Rate Mineral (rdiss)	2.17 x 10-12 mol m-2 s-1

Uncertainty of fit		9.95 x 10-14 mol m-2 s-1

Data Sheet S6. Dissolved silica analysis for experiment 50:50-p3.5-2

Material: Fe-rich allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 507.2660 m2/g

Batch ID: 50:50-p3.5-2	Material mass: 0.1503 g	Total Surface Area (BET): 76.2421 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.07 | 170 | 0.18210* | 1.16709 x 10-6* |
| 10800 | 3.12 | 160 | 0.62043 | 3.97631 x 10-6 |
| 18000 | 3.12 | 150 | 0.80165 | 5.07327 x 10-6 |
| 86400 | 3.35 | 140 | 3.64721 | 2.12841 x 10-5 |
| 97200 | 3.35 | 130 | 4.08779 | 2.36372 x 10-5 |
| 192000 | 3.54 | 120 | 6.60463 | 3.61831 x 10-5 |
| 278400 | 3.64 | 110 | 7.58111 | 4.07029 x 10-5 |
| 451200 | 3.81 | 100 | 10.10778 | 5.14985 x 10-5 |
| 627600 | 3.88 | 90 | 11.15160 | 5.55867 x 10-5 |
| 969600 | 3.96 | 80 | 12.68994 | 6.10641 x 10-5 |
| 1732800 | 4.00 | 70 | 17.10026 | 7.51969 x 10-5 |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9739 | N/A |
| Si release rate | 1.89 x 10-10 | 1.55 x 10-11 |

Diss. Rate Mineral (rdiss)	2.48 x 10-12 mol m-2 s-1

Uncertainty of fit		2.03 x 10-13 mol m-2 s-1

Data Sheet S7. Dissolved silica analysis for experiment Blank-p3.5

Material: None	Initial pH: 3.01	Solution: 0.01M NaCl	Specific Surface Area (BET): N/A

Batch ID: Blank-p3.5	Material mass: 0 g	Total Surface Area (BET): N/A

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.04 | 170 | BD | BD |
| 10800 | 3.03 | 160 | 0.03013* | 1.93098 x 10-7* |
| 18000 | 3.02 | 150 | 0.03866* | 2.44721 x 10-7* |
| 86400 | 3.05 | 140 | BD | BD |
| 97200 | 3.01 | 130 | 0.04399* | 2.28530 x 10-7* |
| 192000 | 3.03 | 120 | 0.09207* | 4.68197 x 10-7* |
| 278400 | 3.02 | 110 | 0.45904 | 2.16679 x 10-6 |
| 451200 | 3.02 | 100 | 0.17628* | 9.58641 x 10-7* |
| 627600 | 3.00 | 90 | BD | BD |
| 969600 | 3.02 | 80 | BD | BD |
| 1732800 | 3.02 | 70 | BD | BD |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%. Error bars are typically smaller than the points.

Data Sheet S8. Dissolved silica analysis for experiment Al+Si-p5-1

Material: Fe-free allophane  Initial pH: 5.04  Solution: 0.01M NaCl	Specific Surface Area (BET): 385.6192 m2/g

Batch ID: Al+Si-p5-1	Material mass: 0.1496 g	Total Surface Area (BET): 57.766 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 5.04 | 180 |  | 0 |
| 3600 | 5.84 | 170 | 0.61379 | 3.9338 x 10-6 |
| 7200 | 5.87 | 160 | 0.64217 | 4.1156 x 10-6 |
| 10800 | 5.90 | 150 | 0.77116 | 4.8964 x 10-6 |
| 14400 | 6.11 | 140 | 0.87969 | 5.5147 x 10-6 |
| 18000 | 6.10 | 130 | 0.91104 | 5.6821 x 10-6 |
| 21600 | 6.32 | 120 | 1.11111 | 6.6794 x 10-6 |
| 78600 | 6.50 | 110 | 2.25139 | 1.1957 x 10-5 |
| 93600 | 6.47 | 100 | 3.27573 | 1.6334 x 10-5 |
| 169200 | 6.56 | 90 | 3.25261 | 1.6244 x 10-5 |
| 262800 | 6.67 | 80 | 3.83064 | 1.8302 x 10-5 |
| 435600 | 6.72 | 70 | 4.45403 | 2.0299 x 10-5 |
| 694800 | 6.89 | 60 | 4.82977 | 2.1370 x 10-5 |
| 1040400 | 6.85 | 50 | 5.64941 | 2.3413 x 10-5 |

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9743 | N/A |
| Si release rate | 1.26 x 10-10 | 1.44 x 10-13 |

Diss. Rate Mineral (rdiss)	2.17 x 10-12 mol m-2 s-1

Uncertainty of fit		1.44 x 10-13 mol m-2 s-1

Data Sheet S9. Dissolved silica analysis for experiment Al+Si-p5-2

Material: Fe-free allophane  Initial pH: 5.04  Solution: 0.01M NaCl	Specific Surface Area (BET): 385.6192 m2/g

Batch ID: Al+Si-p5-2	Material mass: 0.1501 g	Total Surface Area (BET): 57.881 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 5.04 | 180 |  | 0 |
| 3600 | 5.71 | 170 | 1.02201 | 6.5501 x 10-6† |
| 7200 | 5.77 | 160 | 0.69032 | 4.4242 x 10-6 |
| 10800 | 5.80 | 150 | 0.71039 | 4.5457 x 10-6 |
| 14400 | 5.94 | 140 | 0.88213 | 5.5241 x 10-6 |
| 18000 | 6.00 | 130 | 0.97530 | 6.0217 x 10-6 |
| 21600 | 6.00 | 120 | 1.21505 | 7.2168 x 10-6 |
| 78600 | 6.42 | 110 | 2.38875 | 1.2650 x 10-5 |
| 93600 | 6.39 | 100 | 2.96964 | 1.5132 x 10-5 |
| 169200 | 6.57 | 90 | 3.14124 | 1.5804 x 10-5 |
| 262800 | 6.59 | 80 | 3.80099 | 1.8153 x 10-5 |
| 435600 | 6.76 | 70 | 4.63123 | 2.0816 x 10-5 |
| 694800 | 6.78 | 60 | 4.68390 | 2.0964 x 10-5 |
| 1040400 | 6.83 | 50 | 5.80981 | 2.3770 x 10-5 |

†Omitted from rate calculation

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9874 | N/A |
| Si release rate | 1.19 x 10-10 | 5.97 x 10-12 |

Diss. Rate Mineral (rdiss)	2.05 x 10-12 mol m-2 s-1

Uncertainty of fit		1.03 x 10-13 mol m-2 s-1

Data Sheet S10. Dissolved silica analysis for experiment 1:99-p5-1

Material: Fe-poor allophane  Initial pH: 5.04  Solution: 0.01M NaCl	Specific Surface Area (BET): 350.2424 m2/g

Batch ID: 1:99-p5-1	Material mass: 0.1498 g	Total Surface Area (BET): 52.466 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 5.04 | 180 |  | 0 |
| 3600 | 5.59 | 170 | 0.66661 | 4.2723 x 10-6 |
| 7200 | 5.57 | 160 | 0.66922 | 4.2890 x 10-6 |
| 10800 | 5.54 | 150 | 0.72749 | 4.6418 x 10-6 |
| 14400 | 5.71 | 140 | 0.93762 | 5.8398 x 10-6 |
| 18000 | 5.65 | 130 | 1.07461 | 6.5705 x 10-6 |
| 21600 | 5.81 | 120 | 1.12704 | 6.8318 x 10-6 |
| 78600 | 6.05 | 110 | 2.23641 | 1.1967 x 10-5 |
| 93600 | 5.98 | 100 | 2.61468 | 1.3583 x 10-5 |
| 169200 | 6.13 | 90 | 3.05807 | 1.5320 x 10-5 |
| 262800 | 6.17 | 80 | 3.87508 | 1.8229 x 10-5 |
| 435600 | 6.19 | 70 | 4.60542 | 2.0569 x 10-5 |
| 694800 | 6.26 | 60 | 5.63096 | 2.3490 x 10-5 |
| 1040400 | 6.37 | 50 | 5.86422 | 2.4072 x 10-5 |

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9840 | N/A |
| Si release rate | 1.02 x 10-10 | 5.31 x 10-12 |

Diss. Rate Mineral (rdiss)	1.95 x 10-12 mol m-2 s-1

Uncertainty of fit		1.01 x 10-13 mol m-2 s-1

Data Sheet S11. Dissolved silica analysis for experiment 1:99-p5-2

Material: Fe-poor allophane  Initial pH: 5.04  Solution: 0.01M NaCl	Specific Surface Area (BET): 350.2424 m2/g

Batch ID: 1:99-p5-2	Material mass: 0.1499 g	Total Surface Area (BET): 52.501 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 5.04 | 180 |  | 0 |
| 3600 | 5.56 | 170 | 1.26441 | 8.1036 x 10-6† |
| 7200 | 5.55 | 160 | 0.77553 | 4.9703 x 10-6 |
| 10800 | 5.49 | 150 | 0.75806 | 4.8646 x 10-6 |
| 14400 | 5.67 | 140 | 0.85282 | 5.4044 x 10-6 |
| 18000 | 5.68 | 130 | 1.15778 | 7.0332 x 10-6 |
| 21600 | 5.72 | 120 | 1.14451 | 6.6971 x 10-6 |
| 78600 | 6.01 | 110 | 2.26313 | 1.2145 x 10-5 |
| 93600 | 6.05 | 100 | 2.25757 | 1.3531 x 10-5 |
| 169200 | 6.03 | 90 | 3.31736 | 1.6389 x 10-5 |
| 262800 | 6.11 | 80 | 3.67665 | 1.7669 x 10-5 |
| 435600 | 6.19 | 70 | 4.63010 | 2.0724 x 10-5 |
| 694800 | 6.19 | 60 | 5.44277 | 2.3039 x 10-5 |
| 1040400 | 6.27 | 50 | 5.70910 | 2.3703 x 10-5 |

†Omitted from rate calculation

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.8635 | N/A |
| Si release rate | 9.87 x 10-11 | 6.27 x 10-12 |

Diss. Rate Mineral (rdiss)	1.88 x 10-12 mol m-2 s-1

Uncertainty of fit		1.19 x 10-13 mol m-2 s-1

Data Sheet S12. Dissolved silica analysis for experiment 50:50-p5-1

Material: Fe-rich allophane  Initial pH: 5.04  Solution: 0.01M NaCl	Specific Surface Area (BET): 507.2660 m2/g

Batch ID: 50:50-p5-1	Material mass: 0.1496 g	Total Surface Area (BET): 75.887 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 5.04 | 180 |  | 0 |
| 3600 | 5.33 | 170 | 0.91638 | 8.1036 x 10-6† |
| 7200 | 5.51 | 160 | 0.91530 | 4.9703 x 10-6† |
| 10800 | 5.63 | 150 | 0.82197 | 4.8646 x 10-6 |
| 14400 | 6.01 | 140 | 1.04073 | 5.4044 x 10-6 |
| 18000 | 5.89 | 130 | 1.16415 | 7.0332 x 10-6 |
| 21600 | 5.94 | 120 | 1.42513 | 6.6971 x 10-6 |
| 78600 | 6.47 | 110 | 3.36038 | 1.2145 x 10-5 |
| 93600 | 6.56 | 100 | 4.30817 | 1.3531 x 10-5 |
| 169200 | 6.78 | 90 | 5.91635 | 1.6389 x 10-5 |
| 262800 | 6.83 | 80 | 6.93831 | 1.7669 x 10-5 |
| 435600 | 6.95 | 70 | 8.41950 | 2.0724 x 10-5 |
| 694800 | 6.96 | 60 | 9.98684 | 2.3039 x 10-5 |
| 1040400 | 7.06 | 50 | 10.36728 | 2.3703 x 10-5 |

†Omitted from rate calculation

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9926 | N/A |
| Si release rate | 1.83 x 10-10 | 7.87 x 10-12 |

Diss. Rate Mineral (rdiss)	2.41 x 10-12 mol m-2 s-1

Uncertainty of fit		1.04 x 10-13 mol m-2 s-1

Data Sheet S13. Dissolved silica analysis for experiment 50:50-p5-2

Material: Fe-rich allophane  Initial pH: 5.04  Solution: 0.01M NaCl	Specific Surface Area (BET): 507.2660 m2/g

Batch ID: 50:50-p5-2	Material mass: 0.1501 g	Total Surface Area (BET): 76.141 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 5.04 | 180 |  | 0 |
| 3600 | 5.35 | 170 | 0.79987 | 5.1264 x 10-6† |
| 7200 | 5.50 | 160 | 0.69402 | 4.4480 x 10-6 |
| 10800 | 5.51 | 150 | 0.64202 | 4.1332 x 10-6 |
| 14400 | 5.74 | 140 | 0.26866 | 2.0062 x 10-6 |
| 18000 | 5.85 | 130 | 1.02319 | 6.0360 x 10-6 |
| 21600 | 5.93 | 120 | 1.28075 | 7.3199 x 10-6 |
| 78600 | 6.49 | 110 | 2.74231 | 1.4085 x 10-5 |
| 93600 | 6.46 | 100 | 3.09740 | 1.5602 x 10-5 |
| 169200 | 6.64 | 90 | 4.50155 | 2.1102 x 10-5 |
| 262800 | 6.78 | 80 | 5.37456 | 2.4210 x 10-5 |
| 435600 | 6.87 | 70 | 7.10158 | 2.9744 x 10-5 |
| 694800 | 6.96 | 60 | 9.28816 | 3.5973 x 10-5 |
| 1040400 | 7.06 | 50 | 11.57553 | 4.1674 x 10-5 |

†Omitted from rate calculation

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9305 | N/A |
| Si release rate | 1.41 x 10-10 | 1.72 x 10-11 |

Diss. Rate Mineral (rdiss)	1.85 x 10-12 mol m-2 s-1

Uncertainty of fit		2.26 x 10-13 mol m-2 s-1

Data Sheet S14. Dissolved silica analysis for experiment Blank-p5

Material: None	Initial pH: 4.99	Solution: 0.01M NaCl	Specific Surface Area (BET): N/A

Batch ID: Blank-p5	Material mass: 0 g	Total Surface Area (BET): N/A

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 5.04 | 180 |  | 0 |
| 3600 | 4.99 | 170 | 0.21962 | 1.40753 x 10-6 |
| 7200 | 4.93 | 160 | 0.17534* | 1.12377 x 10-6* |
| 10800 | 4.95 | 150 | 0.29501 | 1.84810 x 10-6 |
| 14400 | 5.00 | 140 | 0.03313* | 3.56198 x 10-7* |
| 18000 | 4.92 | 130 | 0.06137* | 5.07037 x 10-7* |
| 21600 | 5.00 | 120 | 0.27988 | 1.59628 x 10-6 |
| 78600 | 4.96 | 110 | 0.29713 | 1.67613 x 10-6 |
| 93600 | 4.94 | 100 | BD | BD |
| 169200 | 4.93 | 90 | BD | BD |
| 262800 | 5.01 | 80 | BD | BD |
| 435600 | 4.61 | 70 | BD | BD |
| 694800 | 4.42 | 60 | BD | BD |
| 1040400 | 4.61 | 50 | BD | BD |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%.

Data Sheet S15. Dissolved silica analysis for experiment Al+Si-p8-1

Material: Fe-free allophane  Initial pH: 6.99  Solution: 0.01M NaCl	Specific Surface Area (BET): 385.6192 m2/g

Batch ID: Al+Si-p8-1	Material mass: 0.1500 g	Total Surface Area (BET): 57.8429 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 6.99 | 180 |  | 0 |
| 3600 | 6.76 | 170 | 0.42231 | 2.70659 x 10-6 |
| 14400 | 7.16 | 160 | 0.70033 | 4.48840 x 10-6 |
| 25200 | 6.95 | 150 | 1.34712 | 8.40337 x 10-6 |
| 90000 | 7.12 | 140 | 2.42705 | 1.45557 x 10-5 |
| 108000 | 7.17 | 130 | 2.69658 | 1.59952 x 10-5 |
| 194400 | 7.22 | 120 | N/A | N/A |
| 280800 | 7.36 | 110 | N/A | N/A |
| 8060400 | 7.20 | 100 | 8.20587254 | 3.50609 x 10-5 |

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9585 | N/A |
| Si release rate | 1.22 x 10-10 | 1.47 x 10-11 |

Diss. Rate Mineral (rdiss)	2.11 x 10-12 mol m-2 s-1

Uncertainty of fit		2.45 x 10-13 mol m-2 s-1

Data Sheet S16. Dissolved silica analysis for experiment Al+Si-p8-2

Material: Fe-free allophane  Initial pH: 6.99  Solution: 0.01M NaCl	Specific Surface Area (BET): 385.6192 m2/g

Batch ID: Al+Si-p8-2	Material mass: 0.1502 g	Total Surface Area (BET): 57.9200 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 6.99 | 180 |  | 0 |
| 3600 | 6.65 | 170 | 0.34720 | 2.22519 x 10-6 |
| 14400 | 6.75 | 160 | N/A | N/A |
| 25200 | 6.7 | 150 | 1.19857 | 7.25491 x 10-6 |
| 90000 | 7.01 | 140 | 2.76481 | 1.61776 x 10-5 |
| 108000 | 7.06 | 130 | 2.67765 | 1.57121 x 10-5 |
| 194400 | 7.24 | 120 | 3.11976 | 1.79159 x 10-5 |
| 280800 | 7.2 | 110 | 3.86712 | 2.13752 x 10-5 |
| 8060400 | 7.2 | 100 | 7.21570396 | 3.56825 x 10-5 |

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9536 | N/A |
| Si release rate | 1.32 x 10-10 | 2.06 x 10-11 |

Diss. Rate Mineral (rdiss)	2.28 x 10-12 mol m-2 s-1

Uncertainty of fit		3.56 x 10-13 mol m-2 s-1

Data Sheet S17. Dissolved silica analysis for experiment 1:99-p8-1

Material: Fe-poor allophane  Initial pH: 6.99  Solution: 0.01M NaCl	Specific Surface Area (BET): 350.2424 m2/g

Batch ID: 1:99-p8-1	Material mass: 0.1502 g	Total Surface Area (BET): 52.6064 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 6.99 | 180 |  | 0 |
| 3600 | 6.38 | 170 | 0.20628 | 1.32206 x 10-6 |
| 14400 | 6.37 | 160 | 0.31738 | 2.03407 x 10-6 |
| 25200 | 6.37 | 150 | 0.56756 | 3.54841 x 10-6 |
| 90000 | 6.36 | 140 | 1.37401 | 8.14270 x 10-6 |
| 108000 | 6.4 | 130 | 1.49695 | 8.79925 x 10-6 |
| 194400 | 6.44 | 120 | 1.74751 | 1.00483 x 10-5 |
| 280800 | 6.4 | 110 | 2.07447 | 1.15617 x 10-5 |
| 8060400 | 6.4 | 100 | 6.90833 | 3.22151 x 10-5 |

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9890 | N/A |
| Si release rate | 7.31 x 10-11 | 4.45 x 10-12 |

Diss. Rate Mineral (rdiss)	1.39 x 10-12 mol m-2 s-1

Uncertainty of fit		8.46 x 10-14 mol m-2 s-1

Data Sheet S18. Dissolved silica analysis for experiment 1:99-p8-2

**This experiment was omitted from the final dataset due to the anomalous mass, high standard error, and poor R2 value.

Material: Fe-poor allophane  Initial pH: 6.99  Solution: 0.01M NaCl	Specific Surface Area (BET): 350.2424 m2/g

Batch ID: 1:99-p8-2	Material mass: 0.0737 g	Total Surface Area (BET): 25.8129 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 6.99 | 180 |  | 0 |
| 3600 | 6.37 | 170 | 0.03077* | 1.97219 x 10-7* |
| 14400 | 6.37 | 160 | 0.58864 | 3.77259 x 10-6 |
| 25200 | 6.4 | 150 | 0.29342 | 1.98567 x 10-6 |
| 90000 | 6.35 | 140 | 0.77023 | 4.70196 x 10-6 |
| 108000 | 6.42 | 130 | 0.57539 | 3.66139 x 10-6 |
| 194400 | 6.41 | 120 | 1.07378 | 6.14575 x 10-6 |
| 280800 | 6.42 | 110 | 1.13292 | 6.41948 x 10-6 |
| 8060400 | 6.24 | 100 | 5.63154 | 2.56406 x 10-5 |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.5575 | N/A |
| Si release rate | 3.84 x 10-11 | 2.42 x 10-11 |

Diss. Rate Mineral (rdiss)	1.49 x 10-12 mol m-2 s-1

Uncertainty of fit		9.36 x 10-13 mol m-2 s-1

Data Sheet S19. Dissolved silica analysis for experiment 50:50-p8-1

Material: Fe-rich allophane  Initial pH: 6.99  Solution: 0.01M NaCl	Specific Surface Area (BET): 507.2660 m2/g

Batch ID: 50:50-p8-1	Material mass: 0.1497 g	Total Surface Area (BET): 75.9377 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 6.99 | 180 |  | 0 |
| 3600 | 5.94 | 170 | 0.18687* | 1.19763 x 10-6* |
| 14400 | 5.70 | 160 | 0.90425 | 5.79531 x 10-6 |
| 25200 | 5.42 | 150 | 0.97387 | 6.21672 x 10-6 |
| 90000 | 5.24 | 140 | 3.00071 | 1.77634 x 10-5 |
| 108000 | 5.27 | 130 | 3.48126 | 2.03300 x 10-5 |
| 194400 | 5.22 | 120 | 4.40980 | 2.49585 x 10-5 |
| 280800 | 5.21 | 110 | 5.29977 | 2.90780 x 10-5 |
| 8060400 | 5.00 | 100 | 13.36705 | 6.35467 x 10-5 |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9860 | N/A |
| Si release rate | 1.74 x 10-10 | 1.20 x 10-11 |

Diss. Rate Mineral (rdiss)	2.29 x 10-12 mol m-2 s-1

Uncertainty of fit		1.58 x 10-13 mol m-2 s-1

Data Sheet S20. Dissolved silica analysis for experiment 50:50-p8-2

Material: Fe-rich allophane  Initial pH: 6.99  Solution: 0.01M NaCl	Specific Surface Area (BET): 507.2660 m2/g

Batch ID: 50:50-p8-2	Material mass: 0.1499 g	Total Surface Area (BET): 76.0392 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 6.99 | 180 |  | 0 |
| 3600 | 6.05 | 170 | 0.27037 | 1.73277 x 10-6 |
| 14400 | 5.69 | 160 | 0.92160 | 5.90655 x 10-6 |
| 25200 | 5.46 | 150 | 1.10247 | 7.00132 x 10-6 |
| 90000 | 5.24 | 140 | 3.05910 | 1.81480 x 10-5 |
| 108000 | 5.24 | 130 | 3.60788 | 2.10790 x 10-5 |
| 194400 | 5.19 | 120 | N/A | N/A |
| 280800 | 5.20 | 110 | 5.47730 | 2.84474 x 10-5 |
| 8060400 | 5.08 | 100 | 13.57007 | 6.30251 x 10-5 |

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9903 | N/A |
| Si release rate | 1.76 x 10-10 | 1.00 x 10-11 |

Diss. Rate Mineral (rdiss)	2.31 x 10-12 mol m-2 s-1

Uncertainty of fit		1.32 x 10-13 mol m-2 s-1

Data Sheet S21. Dissolved silica analysis for experiment Blank-p8

Material: None	Initial pH: 6.99	Solution: 0.01M NaCl	Specific Surface Area (BET): N/A

Batch ID: Blank-p8	Material mass: 0 g	Total Surface Area (BET): N/A

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 6.99 | 180 |  | 0 |
| 3600 | 6.46 | 170 | 0.01573* | 1.00839 x 10-7* |
| 14400 | 6.41 | 160 | 0.18931* | 1.21330 x 10-6* |
| 25200 | 6.4 | 150 | 0.20731 | 1.32222 x 10-6 |
| 90000 | 6.42 | 140 | 0.18965* | 1.22164 x 10-6* |
| 108000 | 6.4 | 130 | 0.09643* | 7.23741 x 10-7* |
| 194400 | 6.4 | 120 | 0.21401 | 1.30987 x 10-6 |
| 280800 | 6.38 | 110 | BD | BD |
| 8060400 | 4.38 | 100 | 0.096494* | 7.03620 x 10-7* |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%.

Data Sheet S22. Dissolved silica analysis for experiment Al+Si-p10.3-1

Material: Fe-free allophane  Initial pH: 10.36  Solution: 0.01M NaCl	Specific Surface Area (BET): 385.6192 m2/g

Batch ID: Al+Si-p10.3-1	Material mass: 0.1504 g	Total Surface Area (BET): 57.9971 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 10.36 | 180 |  | 0 |
| 3600 | 9.94 | 170 | 0.13828* | 8.8625 x 10-7* |
| 10800 | 9.62 | 160 | 0.19394* | 1.2430 x 10-6* |
| 21600 | 9.39 | 150 | 0.57550 | 3.6884 x 10-6 |
| 86400 | 8.73 | 140 | 1.23329 | 7.9041 x 10-6 |
| 97200 | 8.70 | 130 | 1.28252 | 8.2196 x 10-6 |
| 108000 | 8.00 | 120 | 1.34882 | 8.6446 x 10-6 |
| 183600 | 8.02 | 110 | 1.59671 | 1.0233 x 10-5 |
| 356400 | 8.01 | 100 | 2.49581 | 1.5996 x 10-5 |
| 957300 | 7.89 | 90 | 2.80389 | 1.7970 x 10-5 |
| 1562100 | 7.79 | 80 | 2.87474 | 1.8424 x 10-5 |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9663 | N/A |
| Si release rate | 7.81 x 10-11 | 8.42 x 10-12 |

Diss. Rate Mineral (rdiss)	1.35 x 10-12 mol m-2 s-1

Uncertainty of fit		1.45 x 10-13 mol m-2 s-1

Data Sheet S23. Dissolved silica analysis for experiment Al+Si-p10.3-2

Material: Fe-free allophane  Initial pH: 10.36  Solution: 0.01M NaCl	Specific Surface Area (BET): 385.6192 m2/g

Batch ID: Al+Si-p10.3-2	Material mass: 0.1502 g	Total Surface Area (BET): 57.9200 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 10.36 | 180 |  | 0 |
| 3600 | 9.90 | 170 | 0.18916* | 1.2123 x 10-6* |
| 10800 | 9.62 | 160 | 0.20052 | 1.2851 x 10-6 |
| 21600 | 9.39 | 150 | 0.63471 | 4.0679 x 10-6 |
| 86400 | 8.61 | 140 | 1.25017 | 8.0124 x 10-6 |
| 97200 | 8.46 | 130 | 1.27559 | 8.1753 x 10-6 |
| 108000 | 7.82 | 120 | 1.18912 | 7.6210 x 10-6 |
| 183600 | 7.95 | 110 | 1.63182 | 1.0458 x 10-5 |
| 356400 | 8.04 | 100 | 2.39583 | 1.5355 x 10-5 |
| 957300 | 7.60 | 90 | 3.09747 | 1.9852 x 10-5 |
| 1562100 | 7.76 | 80 | 3.15923 | 2.0248 x 10-5 |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9504 | N/A |
| Si release rate | 7.55 x 10-11 | 9.96 x 10-12 |

Diss. Rate Mineral (rdiss)	1.30 x 10-12 mol m-2 s-1

Uncertainty of fit		1.72 x 10-13 mol m-2 s-1

Data Sheet S24. Dissolved silica analysis for experiment 1:99-p10.3-1

Material: Fe-poor allophane  Initial pH: 10.36  Solution: 0.01M NaCl  Specific Surface Area (BET): 350.2424 m2/g

Batch ID: 1:99-p10.3-1	Material mass: 0.1503 g	Total Surface Area (BET): 52.6414 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 10.36 | 180 |  | 0 |
| 3600 | 9.81 | 170 | 0.11607* | 7.5308 x 10-7* |
| 10800 | 9.59 | 160 | 0.12619* | 8.0873 x 10-7* |
| 21600 | 9.25 | 150 | 0.35463 | 2.8661 x 10-6 |
| 86400 | 7.98 | 140 | 0.99220 | 6.3590 x 10-6 |
| 97200 | 7.80 | 130 | 0.89042 | 5.7067 x 10-6 |
| 108000 | 7.55 | 120 | 0.88463 | 5.6696 x 10-6 |
| 183600 | 7.48 | 110 | 1.22009 | 7.8196 x 10-6 |
| 356400 | 7.47 | 100 | 2.02449 | 1.2975 x 10-5 |
| 957300 | 7.32 | 90 | 2.52143 | 1.6160 x 10-5 |
| 1562100 | 7.18 | 80 | 2.58314 | 1.6555 x 10-5 |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9312 | N/A |
| Si release rate | 5.76 x 10-11 | 9.04 x 10-12 |

Diss. Rate Mineral (rdiss)	1.09 x 10-12 mol m-2 s-1

Uncertainty of fit		1.72 x 10-13 mol m-2 s-1

Data Sheet S25. Dissolved silica analysis for experiment 1:99-p10.3-2

Material: Fe-poor allophane  Initial pH: 10.36  Solution: 0.01M NaCl  Specific Surface Area (BET): 350.2424 m2/g

Batch ID: 1:99-p10.3-2	Material mass: 0.1496 g	Total Surface Area (BET): 52.3962 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 10.36 | 180 |  | 0 |
| 3600 | 9.78 | 170 | 0.11750* | 1.3155 x 10-6* |
| 10800 | 9.49 | 160 | 0.27599 | 1.7688 x 10-6 |
| 21600 | 9.18 | 150 | 0.76731 | 2.2728 x 10-6 |
| 86400 | 8.02 | 140 | 1.10943 | 7.1103 x 10-6 |
| 97200 | 7.60 | 130 | 0.98693 | 6.3252 x 10-6 |
| 108000 | 7.48 | 120 | 1.05290 | 6.7480 x 10-6 |
| 183600 | 7.41 | 110 | 1.14753 | 7.3545 x 10-6 |
| 356400 | 7.39 | 100 | 2.37914 | 1.5248 x 10-5 |
| 957300 | 7.23 | 90 | 2.4942 | 1.5698 x 10-5 |
| 1562100 | 7.18 | 80 | 2.69451 | 1.7269 x 10-5 |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9430 | N/A |
| Si release rate | 3.75 x 10-11 | 3.77 x 10-12 |

Diss. Rate Mineral (rdiss)	7.16 x 10-32 mol m-2 s-1

Uncertainty of fit		7.19 x 10-14 mol m-2 s-1

Data Sheet S26. Dissolved silica analysis for experiment 50:50-p10.3-1

Material: Fe-rich allophane  Initial pH: 10.36  Solution: 0.01M NaCl	Specific Surface Area (BET): 507.266 m2/g

Batch ID: 50:50-p10.3-1	Material mass: 0.1497 g	Total Surface Area (BET): 75.9377 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 10.36 | 180 |  | 0 |
| 3600 | 10.04 | 170 | 0.20526 | 1.4484 x 10-6 |
| 10800 | 9.73 | 160 | 0.37307 | 2.3910 x 10-6 |
| 21600 | 9.43 | 150 | 0.71901 | 4.9177 x 10-6 |
| 86400 | 7.25 | 140 | 1.98938 | 1.2750 x 10-5 |
| 97200 | 6.99 | 130 | 1.88120 | 1.2057 x 10-5 |
| 108000 | 7.08 | 120 | 1.95460 | 1.2527 x 10-5 |
| 183600 | 6.82 | 110 | 2.46158 | 1.5776 x 10-5 |
| 356400 | 6.72 | 100 | 4.52585 | 2.9006 x 10-5 |
| 957300 | 6.58 | 90 | 5.22729 | 3.3502 x 10-5 |
| 1562100 | 6.56 | 80 | 5.16958 | 3.3132 x 10-5 |

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9651 | N/A |
| Si release rate | 1.11 x 10-10 | 1.05 x 10-11 |

Diss. Rate Mineral (rdiss)	1.45 x 10-12 mol m-2 s-1

Uncertainty of fit		1.38 x 10-13 mol m-2 s-1

Data Sheet S27. Dissolved silica analysis for experiment 50:50-p10.3-2

Material: Fe-rich allophane  Initial pH: 10.36  Solution: 0.01M NaCl	Specific Surface Area (BET): 507.266 m2/g

Batch ID: 50:50-p10.3-2	Material mass: 0.1503 g	Total Surface Area (BET): 76.2421 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 10.36 | 180 |  | 0 |
| 3600 | 10.03 | 170 | 0.22600 | 2.6071 x 10-7 |
| 10800 | 9.78 | 160 | 0.49974 | 3.2028 x 10-6 |
| 21600 | 9.42 | 150 | 0.12207* | 4.6082 x 10-6* |
| 86400 | 7.34 | 140 | 2.02721 | 1.2992 x 10-5 |
| 97200 | 6.85 | 130 | 1.66260 | 1.0656 x 10-5 |
| 108000 | 6.99 | 120 | 1.57180 | 1.0074 x 10-5 |
| 183600 | 6.75 | 110 | 2.43908 | 1.5632 x 10-5 |
| 356400 | 6.66 | 100 | 4.49912 | 2.8835 x 10-5 |
| 957300 | 6.55 | 90 | 5.18363 | 3.3222 x 10-5 |
| 1562100 | 6.51 | 80 | 6.12844 | 3.9277 x 10-5 |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%.

Linear Fit

| Regression analysis |  | Std. Error |
| --- | --- | --- |
| R Squared | 0.9145 | N/A |
| Si release rate | 1.14 x 10-10 | 2.02 x 10-11 |

Diss. Rate Mineral (rdiss)	1.50 x 10-12 mol m-2 s-1

Uncertainty of fit		2.65 x 10-13 mol m-2 s-1

Data Sheet S28. Dissolved silica analysis for experiment Blank-p10.3

Material: None	Initial pH: 10.36 	Solution: 0.01M NaCl	Specific Surface Area (BET): N/A

Batch ID: Blank-p10.3	Material mass: 0 g	Total Surface Area (BET): N/A

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Si (ppm) | Moles Si released |
| --- | --- | --- | --- | --- |
| 0 | 9.91 | 180 |  | 0 |
| 3600 | 10.18 | 170 | BD | BD |
| 10800 | 10.11 | 160 | BD | BD |
| 21600 | 10.05 | 150 | 0.12207* | 7.82379 x 10-7* |
| 86400 | 9.95 | 140 | 0.15954* | 1.02252 x 10-6* |
| 97200 | 9.94 | 130 | BD | BD |
| 108000 | 9.89 | 120 | 0.15283* | 9.79499 x 10-7* |
| 183600 | 9.8 | 110 | BD | BD |
| 356400 | 9.72 | 100 | 0.32095 | 2.05697 x 10-6 |
| 957300 | 9.56 | 90 | BD | BD |
| 1562100 | 9.21 | 80 | BD | BD |

*Below practical quantitation limit (<0.2 ppm)

Si Release

Analytical uncertainty is 10%. Error bars are smaller than the points.

Data Sheet S29. Dissolved Al analysis for experiment Al+Si-p3.5-1

Material: Fe-free allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 385.6192 m2/g

Batch ID: Al+Si-p3.5-1	Material mass: 0.1501 g	Total Surface Area (BET): 57.8814 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Al (ppm) | Moles Al released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.25 | 170 | 1.92255 | 1.28258 x 10-5 |
| 10800 | 3.38 | 160 | 1.75224 | 1.16896 x 10-5 |
| 18000 | 3.48 | 150 | 0.88649* | 6.23482 x 10-6* |
| 86400 | 4.08 | 140 | 4.67470 | 2.86989 x 10-5 |
| 97200 | 4.10 | 130 | 3.12696 | 2.00944 x 10-5 |
| 192000 | 4.28 | 120 | 2.51791 | 1.69342 x 10-5 |
| 278400 | 4.31 | 110 | 2.63445 | 1.74957 x 10-5 |
| 451200 | 4.31 | 100 | 1.78043 | 1.36975 x 10-5 |
| 627600 | 4.34 | 90 | 2.21760 | 1.54798 x 10-5 |
| 969600 | 4.34 | 80 | 1.90785 | 1.43318 x 10-5 |
| 1732800 | 4.42 | 70 | 1.29105 | 1.22744 x 10-5 |

*Below practical quantitation limit (<1.0 ppm)

Al Release

Analytical uncertainty is 10%.

Data Sheet S30. Dissolved Al analysis for experiment Al+Si-p3.5-2

Material: Fe-free allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 385.6192 m2/g

Batch ID: Al+Si-p3.5-2	Material mass: 0.1499 g	Total Surface Area (BET): 57.8043 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Al (ppm) | Moles Al released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.25 | 170 | 1.70567 | 1.13789 x 10-5 |
| 10800 | 3.38 | 160 | 1.46358 | 9.76391 x 10-6 |
| 18000 | 3.48 | 150 | 0.88296* | 6.10559 x 10-5* |
| 86400 | 4.08 | 140 | 4.42170 | 2.70903 x 10-5 |
| 97200 | 4.10 | 130 | 2.79917 | 1.80700 x 10-5 |
| 192000 | 4.28 | 120 | 2.16845 | 1.47974 x 10-5 |
| 278400 | 4.31 | 110 | 2.47821 | 1.62899 x 10-5 |
| 451200 | 4.31 | 100 | 1.45728 | 1.17493 x 10-5 |
| 627600 | 4.34 | 90 | 2.08310 | 1.43007 x 10-5 |
| 969600 | 4.34 | 80 | 1.75398 | 1.30809 x 10-5 |
| 1732800 | 4.42 | 70 | 1.25180 | 1.14058 x 10-5 |

*Below practical quantitation limit (<1.0 ppm)

Al Release

Analytical uncertainty is 10%.

Data Sheet S31. Dissolved Al analysis for experiment 1:99-p3.5-1

Material: Fe-poor allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 350.2424 m2/g

Batch ID: 1:99-p3.5-1	Material mass: 0.1503 g	Total Surface Area (BET): 52.6414 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Al (ppm) | Moles Al released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.21 | 170 | 1.98146 | 1.32187 x 10-5 |
| 10800 | 3.34 | 160 | 2.09513 | 1.39771 x 10-5 |
| 18000 | 3.43 | 150 | 1.76427 | 1.18925 x 10-5 |
| 86400 | 4.04 | 140 | 5.66020 | 3.49953 x 10-5 |
| 97200 | 4.04 | 130 | 4.43361 | 2.81762 x 10-5 |
| 192000 | 4.27 | 120 | 3.25739 | 2.20731 x 10-5 |
| 278400 | 4.29 | 110 | 3.62953 | 2.38661 x 10-5 |
| 451200 | 4.35 | 100 | 2.30624 | 1.79808 x 10-5 |
| 627600 | 4.33 | 90 | 3.13407 | 2.13558 x 10-5 |
| 969600 | 4.36 | 80 | 2.90467 | 2.05056 x 10-5 |
| 1732800 | 4.35 | 70 | 2.33121 | 1.85927 x 10-5 |

Al Release

Analytical uncertainty is 10%.

Data Sheet S32. Dissolved Al analysis for experiment 1:99-p3.5-2

Material: Fe-poor allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 350.2424 m2/g

Batch ID: 1:99-p3.5-2	Material mass: 0.1502 g	Total Surface Area (BET): 52.6064 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Al (ppm) | Moles Al released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.24 | 170 | 2.04277 | 1.36278 x 10-5 |
| 10800 | 3.38 | 160 | 2.50000 | 1.66781 x 10-5 |
| 18000 | 3.48 | 150 | 2.10593 | 1.41952 x 10-5 |
| 86400 | 4.13 | 140 | 5.55018 | 3.46195 x 10-5 |
| 97200 | 4.14 | 130 | 4.17811 | 2.69917 x 10-5 |
| 192000 | 4.31 | 120 | 3.29745 | 2.24222 x 10-5 |
| 278400 | 4.32 | 110 | 3.43744 | 2.30967 x 10-5 |
| 451200 | 4.35 | 100 | 3.10266 | 2.16077 x 10-5 |
| 627600 | 4.35 | 90 | 2.76524 | 2.02321 x 10-5 |
| 969600 | 4.38 | 80 | 2.68842 | 1.99474 x 10-5 |
| 1732800 | 4.37 | 70 | 2.15872 | 1.81806 x 10-5 |

Al Release

Analytical uncertainty is 10%.

Data Sheet S33. Dissolved Al analysis for experiment 50:50-p3.5-1

Material: Fe-rich allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 507.2660 m2/g

Batch ID: 50:50-p3.5-1	Material mass: 0.1496 g	Total Surface Area (BET): 75.8870 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Al (ppm) | Moles Al released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.07 | 170 | 1.29015 | 8.60689 x 10-6 |
| 10800 | 3.08 | 160 | 0.22201* | 1.48106 x 10-6* |
| 18000 | 3.07 | 150 | 0.50716* | 3.27770 x 10-6* |
| 86400 | 3.25 | 140 | N/A | N/A |
| 97200 | 3.23 | 130 | 2.61974 | 1.45641 x 10-5 |
| 192000 | 3.38 | 120 | 4.10983 | 2.22957 x 10-5 |
| 278400 | 3.46 | 110 | 5.36622 | 2.83492 x 10-5 |
| 451200 | 3.63 | 100 | 6.49740 | 3.33801 x 10-5 |
| 627600 | 3.73 | 90 | 7.25085 | 3.64518 x 10-5 |
| 969600 | 3.89 | 80 | 6.37419 | 3.32027 x 10-5 |
| 1732800 | 3.97 | 70 | 8.89289 | 4.16041 x 10-5 |

*Below practical quantitation limit (<1.0 ppm)

Al Release

Analytical uncertainty is 10%.

Data Sheet S34. Dissolved Al analysis for experiment 50:50-p3.5-2

Material: Fe-rich allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 507.2660 m2/g

Batch ID: 50:50-p3.5-2	Material mass: 0.1503 g	Total Surface Area (BET): 76.2421 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Al (ppm) | Moles Al released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.07 | 170 | 1.44570 | 9.64462 x 10-6 |
| 10800 | 3.12 | 160 | 0.63351* | 4.22629 x 10-6* |
| 18000 | 3.12 | 150 | 1.03564 | 6.75997 x 10-6 |
| 86400 | 3.35 | 140 | 4.99046 | 3.02120 x 10-5 |
| 97200 | 3.35 | 130 | 4.00653 | 2.47419 x 10-5 |
| 192000 | 3.54 | 120 | 4.62576 | 2.79550 x 10-5 |
| 278400 | 3.64 | 110 | 7.04278 | 3.96005 x 10-5 |
| 451200 | 3.81 | 100 | 6.90269 | 3.89774 x 10-5 |
| 627600 | 3.88 | 90 | 8.03478 | 4.35928 x 10-5 |
| 969600 | 3.96 | 80 | 6.52934 | 3.80132 x 10-5 |
| 1732800 | 4.00 | 70 | 9.05375 | 4.64337 x 10-5 |

*Below practical quantitation limit (<1.0 ppm)

Al Release

Analytical uncertainty is 10%.

Data Sheet S35. Dissolved Al analysis for experiment Blank-p3.5

Material: None	Initial pH: 3.01	Solution: 0.01M NaCl	Specific Surface Area (BET): N/A

Batch ID: Blank-p3.5	Material mass: 0 g	Total Surface Area (BET): N/A

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Al (ppm) | Moles Al released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.04 | 170 | 0.79447* | 5.30007 x 10-6* |
| 10800 | 3.03 | 160 | BD | BD |
| 18000 | 3.02 | 150 | 1.08562 | 6.61731 x 10-6* |
| 86400 | 3.05 | 140 | 0.38084* | 2.43792 x 10-6* |
| 97200 | 3.01 | 130 | BD | BD |
| 192000 | 3.03 | 120 | BD | BD |
| 278400 | 3.02 | 110 | 0.15291* | 1.10114 x 10-6* |
| 451200 | 3.02 | 100 | BD | BD |
| 627600 | 3 | 90 | 0.11898* | 9.62818 x 10-7* |
| 969600 | 3.02 | 80 | 0.12734* | 9.93818 x 10-7* |
| 1732800 | 3.02 | 70 | BD | BD |

*Below practical quantitation limit (<1.0 ppm)

Al Release

Analytical uncertainty is 10%. Error bars are smaller than the points.

Data Sheet S36. Dissolved Fe analysis for experiment 50:50-p3.5-1

Material: Fe-rich allophane  Initial pH: 3.01  Solution: 0.01M NaCl	Specific Surface Area (BET): 507.2660 m2/g

Batch ID: 50:50-p3.5-1	Material mass: 0.1496 g	Total Surface Area (BET): 75.8879 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Fe (ppm) | Moles Fe released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.07 | 170 | 0.140817598* | 4.53884 x 10-7* |
| 10800 | 3.08 | 160 | 0.122647323* | 3.95318 x 10-7* |
| 18000 | 3.07 | 150 | 0.153659716* | 4.89724 x 10-7* |
| 86400 | 3.25 | 140 | 0.2727395 | 8.30896 x 10-7 |
| 97200 | 3.23 | 130 | 0.296661764 | 8.95151 x 10-7 |
| 192000 | 3.38 | 120 | 0.409877568 | 1.17898 x 10-6 |
| 278400 | 3.46 | 110 | 0.44567439 | 1.26231 x 10-6 |
| 451200 | 3.63 | 100 | 0.48634088 | 1.34969 x 10-6 |
| 627600 | 3.73 | 90 | 0.443861187 | 1.26602 x 10-6 |
| 969600 | 3.89 | 80 | 0.3453857 | 1.08968 x 10-6 |
| 1732800 | 3.97 | 70 | 0.240194559 | 9.20154 x 10-7 |

*Below practical quantitation limit (<0.2 ppm Fe)

Fe Release

Analytical uncertainty is 10%.

Data Sheet S37. Dissolved Fe analysis for experiment 50:50-p3.5-2

Material: Fe-rich allophane  Initial pH: 3.01  Solution: 0.01M NaCl Specific Surface Area (BET): 507.2660 m2/g

Batch ID: 50:50-p3.5-2	Material mass: 0.1503 g	Total Surface Area (BET): 76.2421 m2

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Fe (ppm) | Moles Fe released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.07 | 170 | 0.113315754* | 3.65240 x 10-7* |
| 10800 | 3.12 | 160 | 0.15801996* | 5.09331 x 10-7* |
| 18000 | 3.12 | 150 | 0.209302962 | 6.65444 x 10-7 |
| 86400 | 3.35 | 140 | 0.353962302 | 1.07990 x 10-6 |
| 97200 | 3.35 | 130 | 0.353024065 | 1.07738 x 10-6 |
| 192000 | 3.54 | 120 | 0.425870329 | 1.26000 x 10-6 |
| 278400 | 3.64 | 110 | 0.43948409 | 1.29170 x 10-6 |
| 451200 | 3.81 | 100 | 0.405464619 | 1.21859 x 10-6 |
| 627600 | 3.88 | 90 | 0.319258809 | 1.04879 x 10-6 |
| 969600 | 3.96 | 80 | 0.264877349 | 9.51412 x 10-7 |
| 1732800 | 4.00 | 70 | 0.195920333* | 8.40281 x 10-7* |

*Below practical quantitation limit (<0.2 ppm Fe)

Fe Release

Analytical uncertainty is 10%.

Data Sheet S38. Dissolved Fe analysis for experiment Blank-p3.5

Material: None	Initial pH: 3.01	Solution: 0.01M NaCl	Specific Surface Area (BET): N/A

Batch ID: Blank-p3.5	Material mass: 0 g	Total Surface Area (BET): N/A

N/A = no analysis. BD = below detection.

| Time (sec) | pH | Volume (mL) | Concentration Fe (ppm) | Moles Fe released |
| --- | --- | --- | --- | --- |
| 0 | 3.01 | 180 |  | 0 |
| 3600 | 3.04 | 170 | 0.091898404* | 2.96208 x 10-7* |
| 10800 | 3.03 | 160 | 0.118778825* | 3.82849 x 10-7* |
| 18000 | 3.02 | 150 | 0.104364283* | 3.38969 x 10-7* |
| 86400 | 3.05 | 140 | 0.203954458 | 6.24302 x 10-7 |
| 97200 | 3.01 | 130 | 0.119996682* | 3.98791 x 10-7* |
| 192000 | 3.03 | 120 | 0.114370361* | 3.84686 x 10-7* |
| 278400 | 3.02 | 110 | 0.13596569* | 4.34957 x 10-7* |
| 451200 | 3.02 | 100 | 0.108524695* | 3.75992 x 10-7* |
| 627600 | 3 | 90 | 0.137266621* | 4.32606 x 10-7* |
| 969600 | 3.02 | 80 | 0.091430128* | 3.50528 x 10-7* |
| 1732800 | 3.02 | 70 | 0.085845016* | 3.41527 x 10-7* |

*Below practical quantitation limit (<0.2 ppm)

Fe Release

Analytical uncertainty is 10%.