Zirconia-intercalated Kaolinite: Synthesis, characterisation and Removal Activity Evaluation

Khaled S. Abou-El-Sherbini1,*, Mohammed A. Wahba1, Elsayed A. Drweesh1, Adel I. M. Akarish2, Seham A. Shaban1, and Eman A. M. Elzahany1

1 Department of Inorganic Chemistry, National Research Centre, 33 El Bohouth st. (former Eltahrir st.), Dokki, Giza 12622, Egypt

2 Geological Sciences Department, National Research Centre, 33 El Bohouth st. (former Eltahrir st.), Dokki, Giza 12622, Egypt

3 Department of Catalysis, Petroleum Refining Division, Egyptian Petroleum Research Institute, Egypt

Table S1. Codes and synthesis parameters of kaolin-modified zirconia samples

| Label | Parent sample | Initial ZrOCl2·8H2O content | Initial activation with 5M HCl | Highest treatment temperature (°C) |
| --- | --- | --- | --- | --- |
| UnK | raw kaolin | none | none | 110 |
| UnKZS100 | UnK | yes | none | 100 |
| UnKZS200 | UnKZS100 | yes | none | 200 |
| UnKZS300 | UnKZS200 | yes | none | 300 |
| UnKZS500 | UnKZS300 | yes | none | 500 |
| HK | UnK | none | yes | 70 |
| HK300 | HK | none | yes | 300 |
| HK500 | HK | none | yes | 500 |
| HKZS | HK | yes | yes | 70 |
| HKZS100 | HK | yes | yes | 100 |
| HKZS200 | HKZS100 | yes | yes | 200 |
| HKZS300 | HKZS200 | yes | yes | 300 |
| HKZS500 | HKZS300 | yes | yes | 500 |
| HK-S-HCl | HK | none | yes + 10M HCl | 70 |
| HK-S-HCl100 | HK | none | yes + 10M HCl | 100 |
| HK-S-HCl200 | HK | none | yes + 10M HCl | 200 |
| ZrOCl2-S | ZrOCl2 8H2O | yes | none | 70 |
| ZrOCl2-S100 | ZrOCl2-S | yes | none | 100 |
| ZrOCl2-S200 | ZrOCl2-S100 | yes | none | 200 |

Fig. S2. EDX of zirconia-intercalated kaolinite in the HKZS300

Fig. S3. EDX elemental mapping of HKZS300

Fig. S4. Particle-size mapping of HK and HKZS300 using a Malvern ZetaSizer instrument