A novel process FOR intercalatinG alkylammonium ions in A THAI bentonite and ITS EFFECT ON adsorption performance

Supporting Information

# Sonchai Intachai1,2, Chomponoot Suppaso1, and Nithima Khaorapapong1,*

1 Materials Chemistry Research Center, Department of Chemistry and Center of Excellence for Innovation in Chemistry, Faculty of Science, Khon Kaen 40002, Thailand.

2 Department of Chemistry, Faculty of Science, Thaksin University, Phatthalung 93210, Thailand

* E-mail address of corresponding author: nithima@kku.ac.th

(level2)Bentonite Preparation (Industrial Process)

Bentonite was collected from Lopburi mine of Thai Nippon Chemical Industry, Thailand at the depth of 6–10 m from the ground surface after the overburden was taken out. After the mining process, the bentonite is exposed, cleaned, confirmed the grade, and taken to the plant for further purifying processes by a dispersion method in water, then followed by sodium ion treatment at the amount of 1.2 times of the CEC using an aqueous solution of sodium chloride and washed several times. Here, it was called bentonite/T and used as the host in synthesis of organically modified clays by ion exchange reactions of protonated alkylamines. The composition of the clay is reported (Table S1).

(level2)Characterization of the Bentonite

The XRD pattern of bentonite/T clearly showed the reflection characteristic to d00l of smectites at 1.26 nm, which is a characteristic d001 value for Na-montmorillonite, confirming the presence of montmorillonite in the samples together with the reflection due to quartz and cristobalite and so on, while the basal spacing of the montmorillonite/J (sodium montmorillonite, Kunipia F, obtained from Kunimine Industries, Japan, the reference clay mineral sample of the Clay Science Society of Japan, JCSS-3101) was observed at 1.24 nm without any reflection due to quartz, calcite, feldspar, and cristobalite, interpreting to very high montmorillonite content (supporting information).

In DTA curve of bentonite/T (Fig. S1), the endothermic peak observed at around 73°C, accompanying mass loss in the corresponding TGA curve, was due to the dehydration of the adsorbed and/or coordinated water molecules, while the dehydroxylation of the silicate layer started at ~400 to 700°C. The mass loss of bentonite/T (4.0%) at around this temperature range (400–700°C) was larger than that of montmorillonite/J (3.6%) (Table S2), implying that the larger amounts of the impurities (Table S1) such as other minerals and carbonates contained in bentonite/T. Meanwhile, the other mass minerals (quartz and cristobalite) contained in bentonite/T were thermally stable and showed no mass loss by the treatment below 900°C (Dellisanti et al., 2006).

The content of ash (mixed oxide formed as a result of dehydration and dehydroxylation) of bentonite/T was 86.0% and those of montmorillonite/J was 90.0%. The ratio of the hydroxyl group in the silicate layer to the ash was calculated to be around 4.2% for montmorillonite/J and 4.4% for bentonite/T (Table S2). The calculated value for montmorillonite/J (4.2%) was due to the high content of montmorillonite, which showed no reflections in the XRD pattern due to other minerals, while the larger value of bentonite/T (4.4%) was attributed to the dehydroxylation of montmorillonite, the other minerals contents (Table S1), which also decomposed at around 400–700°C. This result confirmed the high amount of montmorillonite in bentonite/T.

Fig. S1. TG-DTA curves of (a, c) montmorillonite/J, (b, d) bentonite/T

Fig. S2. TG-DTA curves of (a, d) bentonite/T, (b, e) C10N-bentonite/T(1), (c, f) C10N-bentonite/T(2)

# Table S1. The chemical composition of refined bentonite (purified one time) of Thai Nippon Chemical

| Chemical composition | Content (wt.%) |
| --- | --- |
| SiO2 TiO2 Al2O3 Fe2O3 MgO CaO Na2O K2O MnO Cr2O3 SrO P2O5 ZrO2 SO3 Cl Loss on Ignition | 58.6 0.26 19.2 2.16 4.20 3.49 1.51 1.12 0.04 0.02 0.05 0.02 0.04 0.35 0.08 9.1 |
| Total | 100 |
| Mineral composition | Montmorillonite Quartz Cristobalite Feldspar Calcite Kaolinite |
| Impurity content (%) |  |
| Quartz Cristobalite | 6.4 3.6 |

Table S2. Quantitative data derived from TGA results of the clays

| Sample | % H2O | %OH | %Ash | %OH/Ash |
| --- | --- | --- | --- | --- |
| Montmorillonite/J | 10.4 | 3.6 | 86.0 | 4.2 |
| Bentonite/T | 6.0 | 4.0 | 90.0 | 4.4 |

# Table S3. Decomposition temperature ranges (Tonset and Ttermination) of the organic component and the corresponding exothermic reaction temperature (Texo)

| Host | Guest | CnN-bentonite/T(1) | CnN-bentonite/T(2) |
| --- | --- | --- | --- |
|  |  | Tonset | Ttermination | Texo | Tonset | Ttermination | Texo |
| Bentonite/T | C8N | 221 | 400 | 318 | 220 | 415 | 323 |
|  | C10N | 225 | 394 | 334 | 223 | 399 | 336 |
|  | C12N | 210 | 413 | 350 | 200 | 393 | 351 |
|  | C18N | 190 | 411 | 366 | 174 | 421 | 367 |

Table S4. Langmuir and Freundlich fitting parameters

| Adsorbent | Langmuir constant | Freundlich constant |
| --- | --- | --- |
|  | qe (mg·g–1) | qm (mg·g–1) | KL (L·mg–1) | R2 | n | KF (L·mg–1) | R2 |
| C8N-bentonite/T(1) | 170 | 192 | 0.1351 | 0.9955 | 2.7518 | 43.2414 | 0.9840 |