Supplementary Materials

Meifuite, a new ferrous phyllosilicate mineral with modulated tetrahedral sheets similar to minnesotaite

Shiyun Jin1, Xiaochun Li2,3*, Franklin Hobbs 1, Stephen Guggenheim4, and Huifang Xu1,*

1 S. W. Bailey X-ray Diffraction Laboratory, Department of Geoscience, University of Wisconsin–Madison, Madison, WI 53706, USA

2 Key Laboratory of Mineral Resources, Institute of Geology and Geophysics, Chinese Academy of Sciences, Beijing 100029, China

3. College of Earth and Planetary Sciences, University of Chinese Academy of Sciences, Beijing 100049, China

4. Department of Earth and Environmental Sciences, University of Illinois at Chicago, Chicago, IL 60607, USA

*Corresponding authors: Prof. Huifang Xu (hfxu@geology.wisc.edu), and Dr. Xiaochun Li (njulxc@163.

Figure S 1 Simulated [100], [010] and [001] zone-axis electron diffraction pattern of minnesotaite, based on the structure shown in Figure 6. The [100] zone-axis shows similar pseudo-extinction as found in meifuite, where 0kl reflection with k=2n+1 are absent.The h0l with h=2n+1 in the [010] zone axis pattern are almost all extinct, with a few weak reflections (marked by red arrows) occuring. This is due to the pseudo-translational symmetry projected along b-axis, where the two adjacent strips are almost identical and can only be distinguished when projected along c* (Figure 6).

Table S1: Minnesotaite structure (cif file)

#======================================================================

# CRYSTAL DATA

#----------------------------------------------------------------------

Minnesotaite

_chemical_name_common                  'minnesotaite                          '

_cell_length_a                         28.47162

_cell_length_b                         9.55530

_cell_length_c                         12.40872

_cell_angle_alpha                      100.68230

_cell_angle_beta                       127.70480

_cell_angle_gamma                      89.89900

_space_group_name_H-M_alt              'P 1'

_space_group_IT_number                 1

loop_

_space_group_symop_operation_xyz

'x, y, z'

loop_

_atom_site_label

_atom_site_occupancy

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_adp_type

_atom_site_B_iso_or_equiv

_atom_site_type_symbol

Fe1        1.0     0.446712      0.413737      0.495203     Biso  1.000000 Fe

Fe2        1.0     0.553288      0.586263      0.504797     Biso  1.000000 Fe

Fe3        1.0     0.446256      0.077893      0.494347     Biso  1.000000 Fe

Fe4        1.0     0.553744      0.922107      0.505653     Biso  1.000000 Fe

Fe5        1.0     0.446260      0.740400      0.504240     Biso  1.000000 Fe

Fe6        1.0     0.553740      0.259600      0.495760     Biso  1.000000 Fe

Fe7        1.0     0.353567      0.584945      0.505256     Biso  1.000000 Fe

Fe8        1.0     0.646433      0.415055      0.494744     Biso  1.000000 Fe

Fe9        1.0     0.353695      0.261350      0.511174     Biso  1.000000 Fe

Fe10       1.0     0.646305      0.738650      0.488826     Biso  1.000000 Fe

Fe11       1.0     0.348648      0.917631      0.501827     Biso  1.000000 Fe

Fe12       1.0     0.651352      0.082369      0.498173     Biso  1.000000 Fe

Fe13       1.0     0.245435      0.424019      0.501260     Biso  1.000000 Fe

Fe14       1.0     0.754565      0.575981      0.498740     Biso  1.000000 Fe

Fe15       1.0     0.153821      0.588352      0.505647     Biso  1.000000 Fe

Fe16       1.0     0.846179      0.411648      0.494353     Biso  1.000000 Fe

Fe17       1.0     0.245268      0.761637      0.494932     Biso  1.000000 Fe

Fe18       1.0     0.754732      0.238363      0.505068     Biso  1.000000 Fe

Fe19       1.0     0.245159      0.086172      0.494917     Biso  1.000000 Fe

Fe20       1.0     0.754842      0.913828      0.505083     Biso  1.000000 Fe

Fe21       1.0     0.050237      0.090696      0.495049     Biso  1.000000 Fe

Fe22       1.0     0.949763      0.909304      0.504951     Biso  1.000000 Fe

Fe23       1.0     0.146290      0.925146      0.498497     Biso  1.000000 Fe

Fe24       1.0     0.853710      0.074854      0.501503     Biso  1.000000 Fe

Fe25       1.0     0.049593      0.747273      0.495734     Biso  1.000000 Fe

Fe26       1.0     0.950407      0.252727      0.504266     Biso  1.000000 Fe

Fe27       1.0     0.147983      0.246669      0.500728     Biso  1.000000 Fe

Fe28       1.0     0.852018      0.753331      0.499272     Biso  1.000000 Fe

Fe29       1.0     0.052135      0.419993      0.504533     Biso  1.000000 Fe

Fe30       1.0     0.947865      0.580007      0.495467     Biso  1.000000 Fe

H1         1.0    -0.029537      0.127851      0.699635     Biso  1.000000 H

H2         1.0     0.029537      0.872149      0.300365     Biso  1.000000 H

H3         1.0     0.768765      0.128814      0.697815     Biso  1.000000 H

H4         1.0     0.231235      0.871186      0.302185     Biso  1.000000 H

H5         1.0     0.867806      0.626999      0.691711     Biso  1.000000 H

H6         1.0     0.132194      0.373001      0.308288     Biso  1.000000 H

H7         1.0     0.367832      0.470885      0.697677     Biso  1.000000 H

H8         1.0     0.632168      0.529115      0.302323     Biso  1.000000 H

H9         1.0     0.571099      0.459529      0.692898     Biso  1.000000 H

H10        1.0     0.428901      0.540471      0.307102     Biso  1.000000 H

H11        1.0     0.469534      0.966154      0.697197     Biso  1.000000 H

H12        1.0     0.530466      0.033846      0.302803     Biso  1.000000 H

H13        1.0     0.266013      0.969251      0.693354     Biso  1.000000 H

H14        1.0     0.733987      0.030749      0.306646     Biso  1.000000 H

H15        1.0     0.069687      0.635864      0.693131     Biso  1.000000 H

H16        1.0     0.930313      0.364136      0.306869     Biso  1.000000 H

H17        1.0     0.168020      0.466822      0.698469     Biso  1.000000 H

H18        1.0     0.831980      0.533178      0.301531     Biso  1.000000 H

H19        1.0     0.166967      0.799601      0.692836     Biso  1.000000 H

H20        1.0     0.833033      0.200399      0.307164     Biso  1.000000 H

H21        1.0     0.168091      0.132074      0.695587     Biso  1.000000 H

H22        1.0     0.831909      0.867926      0.304413     Biso  1.000000 H

H23        1.0     0.667787      0.300389      0.691589     Biso  1.000000 H

H24        1.0     0.332213      0.699611      0.308411     Biso  1.000000 H

H25        1.0     0.668350      0.629614      0.692972     Biso  1.000000 H

H26        1.0     0.331650      0.370386      0.307028     Biso  1.000000 H

H27        1.0     0.671482      0.960520      0.692352     Biso  1.000000 H

H28        1.0     0.328518      0.039480      0.307648     Biso  1.000000 H

O1         1.0     0.749363      0.773887      0.608197     Biso  1.000000 O

O2         1.0     0.250637      0.226113      0.391803     Biso  1.000000 O

O3         1.0     0.641189      0.602986      0.590972     Biso  1.000000 O

O4         1.0     0.358811      0.397014      0.409028     Biso  1.000000 O

O5         1.0     0.750085      0.434568      0.607970     Biso  1.000000 O

O6         1.0     0.249915      0.565432      0.392030     Biso  1.000000 O

O7         1.0     0.744266      0.099931      0.596308     Biso  1.000000 O

O8         1.0     0.255734      0.900069      0.403692     Biso  1.000000 O

O9         1.0     0.999399      0.339332      0.171301     Biso  1.000000 O

O10        1.0     0.000601      0.660668      0.828699     Biso  1.000000 O

O11        1.0     0.043078      0.936838      0.606519     Biso  1.000000 O

O12        1.0     0.956922      0.063162      0.393481     Biso  1.000000 O

O13        1.0     0.683861      0.498127      0.168632     Biso  1.000000 O

O14        1.0     0.316139      0.501873      0.831368     Biso  1.000000 O

O15        1.0     0.853032      0.067423      0.133339     Biso  1.000000 O

O16        1.0     0.146968      0.932577      0.866661     Biso  1.000000 O

O17        1.0     0.908685      0.837403      0.171811     Biso  1.000000 O

O18        1.0     0.091315      0.162597      0.828189     Biso  1.000000 O

O19        1.0     0.849477      0.591781      0.133699     Biso  1.000000 O

O20        1.0     0.150523      0.408219      0.866301     Biso  1.000000 O

O21        1.0     0.720036      0.729513      0.133861     Biso  1.000000 O

O22        1.0     0.279964      0.270487      0.866139     Biso  1.000000 O

O23        1.0     0.238316      0.947363      0.591534     Biso  1.000000 O

O24        1.0     0.761684      0.052637      0.408466     Biso  1.000000 O

O25        1.0     0.142638      0.441653      0.596668     Biso  1.000000 O

O26        1.0     0.857362      0.558347      0.403332     Biso  1.000000 O

O27        1.0     0.246045      0.278053      0.610841     Biso  1.000000 O

O28        1.0     0.753955      0.721947      0.389159     Biso  1.000000 O

O29        1.0     0.340572      0.445215      0.595602     Biso  1.000000 O

O30        1.0     0.659429      0.554785      0.404398     Biso  1.000000 O

O31        1.0     0.343277      0.777369      0.599918     Biso  1.000000 O

O32        1.0     0.656723      0.222631      0.400082     Biso  1.000000 O

O33        1.0     0.952915      0.088242      0.171466     Biso  1.000000 O

O34        1.0     0.047085      0.911758      0.828534     Biso  1.000000 O

O35        1.0     0.941736      0.441830      0.600017     Biso  1.000000 O

O36        1.0     0.058264      0.558170      0.399983     Biso  1.000000 O

O37        1.0     0.140382      0.775769      0.590984     Biso  1.000000 O

O38        1.0     0.859618      0.224231      0.409016     Biso  1.000000 O

O39        1.0     0.139959      0.109693      0.593649     Biso  1.000000 O

O40        1.0     0.860041      0.890307      0.406351     Biso  1.000000 O

O41        1.0     0.950837      0.585165      0.171031     Biso  1.000000 O

O42        1.0     0.049163      0.414835      0.828969     Biso  1.000000 O

O43        1.0     0.046472      0.281642      0.610066     Biso  1.000000 O

O44        1.0     0.953528      0.718358      0.389934     Biso  1.000000 O

O45        1.0     0.041340      0.607224      0.591373     Biso  1.000000 O

O46        1.0     0.958660      0.392776      0.408627     Biso  1.000000 O

O47        1.0     0.841604      0.603461      0.589719     Biso  1.000000 O

O48        1.0     0.158396      0.396539      0.410281     Biso  1.000000 O

O49        1.0     0.944022      0.101424      0.597646     Biso  1.000000 O

O50        1.0     0.055978      0.898576      0.402354     Biso  1.000000 O

O51        1.0     0.942388      0.769627      0.600550     Biso  1.000000 O

O52        1.0     0.057612      0.230373      0.399450     Biso  1.000000 O

O53        1.0     0.845818      0.936850      0.601510     Biso  1.000000 O

O54        1.0     0.154182      0.063150      0.398490     Biso  1.000000 O

O55        1.0     0.845010      0.267794      0.599864     Biso  1.000000 O

O56        1.0     0.154990      0.732206      0.400136     Biso  1.000000 O

O57        1.0     0.641894      0.938239      0.590762     Biso  1.000000 O

O58        1.0     0.358106      0.061761      0.409238     Biso  1.000000 O

O59        1.0     0.641701      0.273358      0.589890     Biso  1.000000 O

O60        1.0     0.358299      0.726642      0.410110     Biso  1.000000 O

O61        1.0     0.246286      0.620324      0.610223     Biso  1.000000 O

O62        1.0     0.753714      0.379676      0.389777     Biso  1.000000 O

O63        1.0     0.442650      0.602486      0.604134     Biso  1.000000 O

O64        1.0     0.557350      0.397514      0.395866     Biso  1.000000 O

O65        1.0     0.343002      0.111136      0.600250     Biso  1.000000 O

O66        1.0     0.656998      0.888864      0.399750     Biso  1.000000 O

O67        1.0     0.442705      0.276435      0.601442     Biso  1.000000 O

O68        1.0     0.557295      0.723565      0.398558     Biso  1.000000 O

O69        1.0     0.546916      0.776795      0.611259     Biso  1.000000 O

O70        1.0     0.453084      0.223205      0.388741     Biso  1.000000 O

O71        1.0     0.440857      0.937111      0.595390     Biso  1.000000 O

O72        1.0     0.559143      0.062889      0.404610     Biso  1.000000 O

O73        1.0     0.542933      0.439548      0.591096     Biso  1.000000 O

O74        1.0     0.457067      0.560452      0.408904     Biso  1.000000 O

O75        1.0     0.593839      0.000768      0.171204     Biso  1.000000 O

O76        1.0     0.406161     -0.000768      0.828797     Biso  1.000000 O

O77        1.0     0.638829      0.252575      0.170941     Biso  1.000000 O

O78        1.0     0.361171      0.747425      0.829059     Biso  1.000000 O

O79        1.0     0.498595      0.501865      0.168090     Biso  1.000000 O

O80        1.0     0.501405      0.498135      0.831910     Biso  1.000000 O

O81        1.0     0.638421      0.746259      0.169861     Biso  1.000000 O

O82        1.0     0.361579      0.253741      0.830139     Biso  1.000000 O

O83        1.0     0.720625      0.246493      0.134858     Biso  1.000000 O

O84        1.0     0.279375      0.753507      0.865142     Biso  1.000000 O

O85        1.0     0.544662      0.113925      0.605421     Biso  1.000000 O

O86        1.0     0.455338      0.886075      0.394579     Biso  1.000000 O

O87        1.0     0.451797      0.750690      0.172298     Biso  1.000000 O

O88        1.0     0.548203      0.249310      0.827702     Biso  1.000000 O

O89        1.0     0.218204      0.571354      0.134633     Biso  1.000000 O

O90        1.0     0.781796      0.428646      0.865367     Biso  1.000000 O

O91        1.0     0.183141      0.339061      0.168180     Biso  1.000000 O

O92        1.0     0.816859      0.660938      0.831820     Biso  1.000000 O

O93        1.0     0.045691      0.089460      0.171286     Biso  1.000000 O

O94        1.0     0.954309      0.910541      0.828714     Biso  1.000000 O

O95        1.0     0.138724      0.089754      0.169260     Biso  1.000000 O

O96        1.0     0.861276      0.910246      0.830740     Biso  1.000000 O

O97        1.0     0.136618      0.586010      0.169732     Biso  1.000000 O

O98        1.0     0.863382      0.413990      0.830268     Biso  1.000000 O

O99        1.0     0.222187      0.092885      0.137366     Biso  1.000000 O

O100       1.0     0.777813      0.907115      0.862634     Biso  1.000000 O

O101       1.0     0.407906      0.998840      0.169662     Biso  1.000000 O

O102       1.0     0.592094      0.001160      0.830338     Biso  1.000000 O

O103       1.0     0.452056      0.251641      0.171202     Biso  1.000000 O

O104       1.0     0.547944      0.748359      0.828798     Biso  1.000000 O

O105       1.0     0.352142      0.749747      0.138501     Biso  1.000000 O

O106       1.0     0.647858      0.250253      0.861499     Biso  1.000000 O

O107       1.0     0.351174      0.227194      0.131735     Biso  1.000000 O

O108       1.0     0.648826      0.772806      0.868265     Biso  1.000000 O

O109       1.0     0.545901      0.754435      0.172741     Biso  1.000000 O

O110       1.0     0.454099      0.245565      0.827259     Biso  1.000000 O

O111       1.0     0.545832      0.248901      0.172698     Biso  1.000000 O

O112       1.0     0.454168      0.751099      0.827302     Biso  1.000000 O

O113       1.0     0.044689      0.594143      0.173413     Biso  1.000000 O

O114       1.0     0.955311      0.405857      0.826587     Biso  1.000000 O

O115       1.0     0.093370      0.840389      0.171681     Biso  1.000000 O

O116       1.0     0.906630      0.159611      0.828319     Biso  1.000000 O

O117       1.0     0.260625      0.889952      0.047037     Biso  1.000000 O

O118       1.0     0.739375      0.110048      0.952963     Biso  1.000000 O

O119       1.0     0.268039      0.387648      0.062290     Biso  1.000000 O

O120       1.0     0.731961      0.612352      0.937710     Biso  1.000000 O

O121       1.0     0.234603      0.113935      0.938851     Biso  1.000000 O

O122       1.0     0.765397      0.886065      0.061149     Biso  1.000000 O

O123       1.0     0.236341      0.611073      0.954007     Biso  1.000000 O

O124       1.0     0.763659      0.388927      0.045993     Biso  1.000000 O

Si1        1.0     0.986603      0.482632      0.771574     Biso  1.000000 Si

Si2        1.0     0.013397      0.517368      0.228426     Biso  1.000000 Si

Si3        1.0     0.800328      0.812462      0.779393     Biso  1.000000 Si

Si4        1.0     0.199672      0.187538      0.220607     Biso  1.000000 Si

Si5        1.0     0.581452      0.151394      0.775592     Biso  1.000000 Si

Si6        1.0     0.418548      0.848606      0.224408     Biso  1.000000 Si

Si7        1.0     0.582127      0.824575      0.780184     Biso  1.000000 Si

Si8        1.0     0.417873      0.175425      0.219816     Biso  1.000000 Si

Si9        1.0     0.801885      0.483941      0.777854     Biso  1.000000 Si

Si10       1.0     0.198115      0.516059      0.222146     Biso  1.000000 Si

Si11       1.0     0.892542      0.981807      0.773731     Biso  1.000000 Si

Si12       1.0     0.107458      0.018193      0.226269     Biso  1.000000 Si

Si13       1.0     0.893205      0.310864      0.772088     Biso  1.000000 Si

Si14       1.0     0.106795      0.689136      0.227912     Biso  1.000000 Si

Si15       1.0     0.300627      0.324978      0.781098     Biso  1.000000 Si

Si16       1.0     0.699373      0.675022      0.218902     Biso  1.000000 Si

Si17       1.0     0.083242      0.315934      0.780122     Biso  1.000000 Si

Si18       1.0     0.916758      0.684066      0.219878     Biso  1.000000 Si

Si19       1.0     0.300365      0.654249      0.780884     Biso  1.000000 Si

Si20       1.0     0.699635      0.345751      0.219116     Biso  1.000000 Si

Si21       1.0     0.986094      0.811387      0.772817     Biso  1.000000 Si

Si22       1.0     0.013906      0.188613      0.227182     Biso  1.000000 Si

Si23       1.0     0.391861      0.821176      0.771736     Biso  1.000000 Si

Si24       1.0     0.608139      0.178824      0.228264     Biso  1.000000 Si

Si25       1.0     0.391673      0.150240      0.771741     Biso  1.000000 Si

Si26       1.0     0.608327      0.849760      0.228259     Biso  1.000000 Si

Si27       1.0     0.285458      0.250016     -0.000043     Biso  1.000000 Si

Si28       1.0     0.714542      0.749984      0.000043     Biso  1.000000 Si

Si29       1.0     0.283277      0.750887      0.001615     Biso  1.000000 Si

Si30       1.0     0.716724      0.249113     -0.001615     Biso  1.000000 Si

Si31       1.0     0.216319      0.493153      0.003458     Biso  1.000000 Si

Si32       1.0     0.783681      0.506847     -0.003458     Biso  1.000000 Si

Si33       1.0     0.080047      0.985715      0.776365     Biso  1.000000 Si

Si34       1.0     0.919953      0.014285      0.223635     Biso  1.000000 Si

Si35       1.0     0.214860      0.009238     -0.000491     Biso  1.000000 Si

Si36       1.0     0.785140     -0.009238      0.000491     Biso  1.000000 Si

Si37       1.0     0.486657      0.319733      0.773803     Biso  1.000000 Si

Si38       1.0     0.513343      0.680267      0.226197     Biso  1.000000 Si

Si39       1.0     0.487207      0.649659      0.776293     Biso  1.000000 Si

Si40       1.0     0.512793      0.350341      0.223707     Biso  1.000000 Si