Supplementary Information

For

Palygorskite supporting homogeneously dispersed Ag nanoparticles: Molten salt method and enhanced antibacterial performance

Qiuzhi He1,2,3,4, Qingze Chen 1,3,4,*, Runliang Zhu1,3,4, Jing Du1,3,4, Shiya He1,3,4, Guocheng Lv5, Cheng Gu6, and Aiqin Wang7

1CAS Key Laboratory of Mineralogy and Metallogeny/Guangdong Provincial Key Laboratory of Mineral Physics and Materials, Guangzhou Institute of Geochemistry, Chinese Academy of Sciences, Guangzhou 510640, China

2Department of Public Health, School of Medicine, Guangxi University of Science and Technology, Liuzhou 545005, Guangxi, China

3CAS Center for Excellence in Deep Earth Science, Guangzhou 510640, China

4University of Chinese Academy of Sciences, Beijing 100049, China

5Beijing Key Laboratory of Materials Utilization of Nonmetallic Minerals and Solid Wastes, National Laboratory of Mineral Materials, School of Materials Sciences and Technology, China University of Geosciences, Beijing, 100083, PR China

6State Key Laboratory of Pollution Control and Resource Reuse, School of the Environment, Nanjing University, Nanjing 210023, PR China

7Key Laboratory of Clay Mineral Applied Research of Gansu Province, Center of Eco-material and Green Chemistry, Lanzhou Institute of Chemical Physics, Chinese

Academy of Sciences, Lanzhou 730000, China

*E-mail: chenqingze@gig.ac.cn

Fig. S1. XRD patterns of silver/palygorskite nanocomposites synthesized without the introduction of molten salt (i.e., 3% Ag/Plg, 6% Ag/Plg, and 9% Ag/Plg).

Fig. S2. The histogram of silver nanoparticles size in 3% Ag/Plg-s (a), 6% Ag/Plg-s (b), and 9% Ag/Plg-s (c), based on Fig. 4d, h, and l, respectively.

Fig. S3. TEM images of the 6% Ag/Plg nanocomposite (without the introduction of NaNO3 molten salt during the synthesis process).

Fig. S4. The histogram of silver nanoparticles size in 6% Ag/APlg-s (a) and 6% Ag/TPlg-s (b), based on Fig. 8c and f, respectively.

Table S1 Meaning of the abbreviations used for silver/palygorskite nanocomposites.

| Abbreviation | Meaning of the abbreviation |
| --- | --- |
| 3% Ag/Plg-s | Sample (with Ag loading amount of 3%, where the “%” was “wt.%”) synthesized by the molten salt method |
| 6% Ag/Plg-s | Sample (with Ag loading amount of 6%) synthesized by the molten salt method |
| 9% Ag/Plg-s | Sample (with Ag loading amount of 9%) synthesized by the molten salt method |
| 3% Ag/Plg | Sample (with Ag loading amount of 3%) synthesized without the introduction of molten salt method |
| 6% Ag/Plg | Sample (with Ag loading amount of 6%) synthesized without the introduction of molten salt method |
| 9% Ag/Plg | Sample (with Ag loading amount of 9%) synthesized without the introduction of molten salt method |
| 6% Ag/APlg-s | Sample (with Ag loading amount of 6%) synthesized by the molten salt method and the acid-activated palygorskite used as support |
| 6% Ag/TPlg-s | Sample (with Ag loading amount of 6%) synthesized by the molten salt method and the thermal-activated palygorskite used as support |

Table S2 Summaries of the antibacterial activity of Ag-based antibacterial materials synthesized in this work and prepared by other methods (the “%” was “wt.%” in the follow table).

| Antibacterial materials | Synthesis method | Ag Content (%) | Average size of Ag (nm) | Usage of antibacterial materials (mg) | Concentration of bacteria (CFU/mL) | Inhibition Zone (mm)/paper diamater (mm) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Silver/palysorkite nanocomposites | Molten salt method | 5.6 | 3.3 | 2.0 | 1*106 | 20.4/10 | This work |
| Ag NPs/chitosans/montmorillonite | Photochemical reduction | / | 3.0 | / | 1*106 | 8.7/6 | (Gabriel et al., 2017) |
| Ag/TiO2/bentonite | Borohydride reduction | 6.0 | / | 0.01 | 1*106 | 15.0/6 | (Krishnan and Mahalingam., 2017) |
| Lecithin/montmorillonite-AgNPs | Ascorbic acid reduction | / | 10.0-30.0 | / | / | 13.2/10 | (Ge et al., 2019) |
| Ag@mesoporous bioactive glass | Chemical reduction | 11.6 | 5.0 | / | / | 24.2/10 | (Shuai et al., 2019) |
| Silver/clay based polyethylene nanocomposites | Borohydride reduction UV photo-treatment | 5.0 | 11.0 15.0 | / | / | 17.2/10 15.5/10 | (Roy et al., 2019) |
| Silver-montmorillonite | Calcination | / | 47.4 | / | / | 27.1/15 | (Roy et al., 2018) |
| Ag NPs@carbon nanotubes | Chemical reduction | 4.0 | 8.0 | 10.0 | / | 26.8/20 | (Xia et al., 2018) |
| Silver-mesoporous graphene composite | Chemical reduction | 5.0 | 5-10 | / | 1*106 | 19.2/15 | (Yang et al., 2019) |

References

Gabriel, J.S., Gonzaga, V.A.M., Poli, A.L., & Schmitt, C.C. (2017). Photochemical synthesis of silver nanoparticles on chitosans/montmorillonite nanocomposite films and antibacterial activity. Carbohydr Polym, 171, 202-210.

Ge, M.Q., Li, J., Song, S.J., Meng, N., & Zhou, N.L. (2019). Development and antibacterial performance of silver nanoparticles-lecithin modified montmorillonite nanoparticle hybrid. Applied Clay Science, 183, 105334.

Krishnan, B., & Mahalingam, S. (2017). “Ag/TiO2/bentonite nanocomposite for biological applications: synthesis, characterization, antibacterial and cytotoxic investigations.” Advanced Powder Technology, 28, 2265-80.

Roy, A., Joshi, M., Butola, B.S., & Malhotra, S. (2018). Antimicrobial and toxicological behavior of montmorillonite immobilized metal nanoparticles. Materials Science & Engineering C, 93, 704-715.

Roy, A., Joshi, M., Butola, B.S., & Ghosh, S. (2019). Evaluation of biological and cytocompatible properties in nano silver-clay based polyethylene nanocomposites. Journal of Hazardous Materials, 384, 121309.

Shuai, C.J., Xu, Y., Feng, P., Wang, G.Y., Xiong, S.X., & Peng, S.P. (2019). Antibacterial polymer scaffold based on mesoporous bioactive glass loaded with in situ grown silver. Chemical Engineering Journal, 374, 304-315.

Xia, L.X., Xu, M., Cheng, G.Z., Yang, L.N., Guo, Y.S., Li, D., Fang, D.W., Zhang, Q., & Liu, H.Y. (2018). Facile construction of Ag nanoparticles encapsulated into carbon nanotubes with robust antibacterial activity. Carbon, 130, 775-781.

Yang, L.N., Meng, F.C., Qu, X.Y., Xia, L.X., Huang, F., Qin, S., Zhang, M.H., Xu, F., Sun, L.X., & Liu, H.Y. (2019). Multiple-twinned silver nanoparticles supported on mesoporous graphene with enhanced antibacterial activity. Carbon, 155, 397-402.