The Formation and Transformation of Manganese Oxide Minerals on the Surface of Kaolinite

F. Zhao1, G. Y. Zhang1, Y. Jiang1, H. Wang2, C. Cao1, Y. B. Qi1, Q. Y. Wang1, H. Y. Zhao1*

1Anhui Province Key Lab of Farmland Ecological Conservation and Pollution Prevention, Key Laboratory of JiangHuai Arable Land Resources Protection and Eco-restoration, College of Resources and Environment, Anhui Agricultural University, Hefei, 230036, China

2Soil and Fertilizer Institute, Anhui Academy of Agricultural Sciences, Hefei, 230031, China

Table S1 Surface area and pore diameter of the kaolinite

|  | Formula | MW (g/mol) | BET Surface area (m2/g) | Average pore diameter (nm) | Mesopore average pore diameter (nm) | t-Plot micropore volume (cm3/g) |
| --- | --- | --- | --- | --- | --- | --- |
| kaolinite | Al2O7Si2•H2O | 258.16 | 9.0074 | 23.5790 | 22.3516 | 0.000191 |

Fig. S1 XRD pattern of kaolinite obtained from Sigma-Aldrich confirming its purity (NO: 14-0164).

Fig. S2 TEM image of kaolinite obtained from Sigma-Aldrich showing plate-like crystals with a straight edge ~500 nm long

Fig. S3 Particle-size distribution of pure kaolinite; the average is 296.9 nm.