Supplementary Information

for

Rare-earth minerals in kaolin ore, mine tailings, and sands – central Georgia, Upper Coastal Plain

Anthony Boxleiter1,* and W. Crawford Elliott1

1 Department of Geosciences, Georgia State University, Atlanta, GA 30302-3965, USA

*Email address of corresponding author: aboxleiter1@student.gsu.edu

A. Separation Techniques

Figure S1  Example of wet sieving method applied for mine tailings sample MT-BNO7-SS;       [A]: wet sieve 325 mesh screen, effluent retained in catchment bucket transferred to settling container; [B]: settling container for 24-hour and 7-day settling trials; [C]: 24-hour settled material, supernatant transferred by decantation; [D]: draining light-subfraction away from the heavy-mineral subfraction in the 24-settled, –325 mesh fraction; [E]: drying the light-subfraction and heavy-mineral subfraction prior to further testing, e.g. XRD to determine the efficiency in concentration the minerals of interest

Figure S2  Separations of heavy minerals from kaolin samples; [A]: Waring blender;               [B]: Eocene kaolin –325 mesh settling stage; [C]: Cretaceous kaolin –325 mesh settling stage;        [D]: Eocene kaolin –325 hand-pan stage; [E]: Cretaceous kaolin –325 mesh hand-pan stage;     [F]: Eocene kaolin +325 mesh retain; [G]: Cretaceous kaolin +325 mesh retain;                       [H]: Eocene kaolin heavy subfraction result; [H’]: Eocene kaolin light subfraction result

B. TGA Analyses

Figure S3 Thermal Gravimetric Analysis (TGA) profile of the mined Eocene kaolin sample. Solid red profile is the weight loss, dashed red line is the 1st derivative profile

Figure S4 Thermal Gravimetric Analysis (TGA) profile of the mined Cretaceous kaolin sample. Solid red profile is the weight loss, dashed red line is the 1st derivative profile

C. Microscopy Analyses – i. Mined Kaolins

Figure S5  Cretaceous kaolin stereomicroscopy results – [Top]: +325 mesh (>45μm) fraction with muscovite/biotite-mica flakes; [Bottom]: –325 mesh (<45 μm) heavy subfraction

Figure S6 Eocene kaolin stereomicroscopy results – [Top]: +325 mesh (>45μm) fraction; [Bottom]: –325 mesh (<45 μm) heavy subfraction

Figure S7 SEM-EDS results of the mined Cretaceous kaolin –325 mesh (<45 μm) heavy subfraction showing: Ti-Fe: ilmenite; Ti: rutile/anatase; Fe-S: pyrite/marcasite; Zr: zircon; Zr-Y: zircon with Y content

Figure S8 SEM-EDS results of the mined Cretaceous kaolin –325 mesh (<45μm) heavy subfraction showing several other minerals identified: Ilm: ilmenite; Fe-S: pyrite/marcasite; Zr: zircon

Figure S9 SEM-EDS results of the mined Cretaceous kaolin –325 mesh (<45 μm) heavy subfraction showing several examples of xenotime grains analyzed

Figure S10  SEM-EDS results of the mined Eocene kaolin –325 mesh (<45 μm) heavy subfraction showing: [A]: zircon (preserved crystal faces), ilmenite (sub-angular) and a Zn-sulfide cluster (sphalerite); [B]: rounded zircons, Fe/Zn-sulfides crystal clusters and ilmenite (sub-angular); [C]: framboidal pyrite examples

Figure S11 SEM-EDS results for the +325 mesh (>45 μm) fraction separated from the Eocene kaolin sample at RGH-073121 – examples of kaolinitic + Fe-sulfide crystal clusters

C. Microscopy Analyses – ii. Kaolin Mine Tailings

Figure S12 SEM-EDS results of Cretaceous kaolin mine tailings (MT-BNO7-SS) showing monazite and xenotime examples of the –325 mesh (<45 μm) heavy subfraction

Figure S13 SEM-EDS results of Cretaceous kaolin mine tailings (MT-BNO7-SS) showing zircon examples in the –325 mesh (<45 μm) heavy subfraction

Figure S14 SEM-EDS results of Cretaceous kaolin mine tailings (MT-BNO7-IP H-P) showing the degree of roundness of the zircon grains with faintly preserved crystal faces, conchoidal fracture surfaces diagnostic of the rounded quartz grains

Figure S15 SEM-EDS results of Cretaceous kaolin mine tailings (MT-BNO7-IP H-P) showing dissolution pitting and etching features along mineral-grain surfaces in monazite and ilmenite

Figure S16 SEM-EDS results of Cretaceous kaolin mine tailings (MT-BNO7-IP H-P) showing monazite examples

Figure S17 SEM-EDS results of Eocene kaolin mine tailings (MT-BNO6) showing several examples of minerals identified in +325 mesh (>45 μm) fraction including roundness of the zircon grains with faintly preserved crystal faces

Figure S18 SEM-EDS results of the Eocene kaolin mine tailings (MT-BNO6) showing several examples monazite (smooth and rounded surfaces, lacking dissolution etching) present in the –325 mesh (<45 μm) heavy subfraction

C. Microscopy Analyses – iii. Sands

Figure S19 Stereomicroscopy – [A]: stereomicroscope and lighting accessories used; [B]: sample under investigation with naked-eye examination; [C]: individual mineral grains extracted with forceps for characterization; [D]: mineral grains under examination at high-magnification (100x)

Figure S20 Stereomicroscopy results for the cross-bedded section (Marion Member sands) – [A]: dark minerals identified, laminations 1–2 mm thick, matrix dominated by quartz and minor mica grains visible under stereomicroscopy examination prior to XRD and SEM-EDS analysis. Scale gradings are 1 mm spacing; [B]: dark mineral grains highly visible by color and opacity contrast to the matrix quartz grains; [C]: extraction of the dark, heavy minerals by forceps presented an efficient means for isolating and examining mineral grains of interest for further study by SEM-EDS

Figure S21 SEM-EDS results of the cross-bedded section of the Marion Member sands showing monazite and xenotime grains

Figure S22 SEM-EDS results of the cross-bedded section of the Marion Member sands showing large monazite grains displaying dissolution pitting and etching along mineral grain surfaces

Figure S23 SEM-EDS results of the mottled section of the Marion Member sands showing ilmenite, zircon and monazite identified

Figure S24 SEM-EDS results of the mottled section of the Marion Member sands showing quartz, zircon and monazite identified

Figure S25 SEM-EDS results of the mottled section of the Marion Member sands showing quartz, ilmenite, zircon and monazite identified

Figure S26 SEM-EDS results of the mottled section of the Marion Member sands showing quartz, ilmenite, xenotime and monazite identified

Figure S27 SEM-EDS results for the sulfide-rich sand sample showing monazite grains displaying dissolution pitting and etching along mineral grain surfaces

Figure S28  SEM-EDS results for a xenotime grain displaying dissolution pitting-etching and secondary formation or possible fibrous-morphology alunite-jarosite-like minerals in the sulfide-rich sand

Figure S29  SEM-EDS results for the sulfide-rich sand sample showing rounded zircon grains

Figure S30  SEM-EDS results for the sulfide-rich sand sample showing examples of the Fe-sulfide minerals

Figure S31  SEM-EDS results for a xenotime grain and populations of rounded zircons and monazite in a matrix of the mostly quartz in the –325 mesh (<45 μm) heavy subfraction of the Eocene sand

Figure S32  SEM-EDS results for monazite grains in the –325 mesh (<45 μm) heavy subfraction of the Eocene sand

Figure S33 SEM-EDS results for zircon and Ti-phases (rutile/anatase/ilmenite) in the –325 mesh (<45 μm) heavy subfraction of the Eocene sand

D. Mineral Separations and Recorded Weights of Fractions

Table S1  Mineral separation fractions and weights (grams) per sample type

|  | Sample ID | Fraction | Weight (g) |
| --- | --- | --- | --- |
| Mine Tailings | MT-BNO7-SS1 | Whole Rock | 200 |
|  |  | >45 μm WF | 186.9 |
|  |  | <45 μm SpF | 9.21 |
|  |  | <45 μm Lt | 3.09 |
|  |  | <45 μm Hv | 0.80 |
|  | MT-BNO7-IP1 | Whole Rock | 200 |
|  | MT-BNO62 | Whole Rock | 200 |
|  |  | >45 μm WF | 182.8 |
|  |  | <45 μm Lt | 2.09 |
|  |  | <45 μm Hv | 0.17 |
| Kaolins | Cretaceous Kaolin1 | Whole Rock | 888.9 |
|  |  | >45 μm WF | 2.29 |
|  |  | <45 μm Lt | 1.31 |
|  |  | <45 μm Hv | 0.13 |
|  | Eocene Kaolin2 | Whole Rock | 591.2 |
|  |  | >45 μm WF | 5.90 |
|  |  | <45 μm Lt | 34.83 |
|  |  | <45 μm Hv | 0.28 |
| Sands | Cross-bedded HMS1 | Whole Rock | 200 |
|  | Mottled HMS1 | Whole Rock | 200 |
|  | Sulfide-rich Sand1 | Whole Rock | 200 |
|  | Eocene Sand2 | Whole Rock | 200 |
|  |  | >45 μm WF | 147.7 |
|  |  | <45 μm Lt | 4.34 |
|  |  | <45 μm Hv | 0.26 |

Notes: Starting weights of all samples ≈200 (g) for mine tailings and sands. Larger starting weights were used for kaolins. Abbreviations: Hv – heavy subfraction; Lt – light subfraction; MT – mine tailings; HMS – heavy-mineral sands; SpF – suspended fraction; 1 – assoc. with Cretaceous Buffalo Creek Mbr mined kaolin; 2 – associated with Eocene Jeffersonville Mbr mined kaolin.

E. Monazite and Xenotime Mineral Grain Chemical Analyses

Table S2: Monazite (Mnz) mineral grain chemical analyses via SEM-EDS.

| Monazite Grains |  |  |
| --- | --- | --- |
| Oxide wt.% | La2O3 | Ce2O3 | Pr2O3 | Nd2O3 | Sm2O3 | Y2O3 | P2O5 |
| Mine Tailings |  |  |  |  |
| BNO7-IP Mnz | 12.50 | 26.60 | 4.00 | 13.40 | 4.90 | 4.10 | 28.6 |
| BNO7-IP Mnz | 12.90 | 25.60 | 3.30 | 11.50 | 4.10 | 4.30 | 32.0 |
| BNO7-IP Mnz | 13.40 | 27.60 | 5.30 | 14.50 | 4.30 | 4.40 | 18.3 |
| BNO7-IP Mnz | 14.00 | 28.90 | 5.50 | 15.40 | 4.60 | - | 26.6 |
| BNO7-SS Mnz | 14.60 | 30.20 | 4.70 | 13.90 | 4.20 | 2.90 | 22.5 |
| BNO7-SS Mnz | 16.40 | 29.50 | 4.30 | 13.00 | 3.20 | 3.60 | 25.7 |
| BNO6 Mnz | 13.90 | 28.60 | 4.20 | 12.80 | 3.70 | 2.80 | 27.8 |
| BNO6 Mnz | 13.00 | 27.30 | 3.50 | 12.20 | 3.60 | 3.20 | 31.2 |
| BNO6 Mnz | 15.80 | 31.20 | 4.20 | 12.30 | 3.20 | 3.60 | 25.9 |
| BNO6 Mnz | 14.80 | 28.60 | 4.60 | 13.30 | 3.70 | 3.90 | 24.4 |
| avg | 14.13 | 28.41 | 4.36 | 13.23 | 3.95 | 3.64 | 26.3 |
| stdev | 1.21 | 1.60 | 0.66 | 1.09 | 0.54 | 0.55 | 3.83 |
| Sands |  |  |  |  |  |
| Cross-bed HMS Mnz | 12.90 | 24.90 | 3.60 | 11.50 | 3.90 | 5.10 | 33.5 |
| Cross-bed HMS Mnz | 12.50 | 26.60 | 3.60 | 13.10 | 4.40 | 5.10 | 31.3 |
| Cross-bed HMS Mnz | - | 34.40 | 6.00 | 12.60 | 2.60 | - | - |
| Cross-bed HMS Mnz | - | 31.20 | 0.00 |  | 3.50 | 5.10 | 25.8 |
| Sulfide-rich Sand Mnz | 11.90 | 25.00 | 3.10 | 11.50 | 3.40 | 4.70 | 34.8 |
| Mottled HMS Mnz | 15.00 | 32.10 | 4.30 | 14.90 | 4.20 | 4.20 |  |
| Mottled HMS Mnz | 14.40 | 27.60 | 3.20 |  | 3.80 | 4.00 | 30.4 |
| Mottled HMS Mnz | 15.90 | 29.40 | 3.40 | 10.00 | 2.50 | 3.80 | 30.5 |
| Mottled HMS Mnz | 16.00 | 31.80 | 4.30 | 12.50 | 3.70 | - | - |
| Mottled HMS Mnz | 14.50 | 30.00 | 4.40 | 13.60 | 4.70 | 4.80 | 22.4 |
| Eocene Sand Mnz | 17.20 | 28.60 | 3.20 |  | 2.50 | - | 31.2 |
| Eocene Sand Mnz | 15.10 | 31.50 | 4.10 | 14.10 | 4.00 | 5.10 | 21.2 |
| Eocene Sand Mnz | 13.80 | 29.30 | 3.90 | 13.60 | 3.90 | 3.20 | 26.9 |
| Eocene Sand Mnz | 11.50 | 25.50 | 3.20 | 11.50 | 3.70 | 5.50 | 33.1 |
| avg | 14.23 | 29.14 | 3.59 | 12.63 | 3.63 | 4.60 | 29.2 |
| stdev | 1.68 | 2.82 | 1.24 | 1.35 | 0.66 | 0.67 | 4.30 |

Table S3: Xenotime (Xtn) mineral grain chemical analyses via SEM-EDS.

| Xenotime Grains |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Oxide wt.% | Eu2O3 | Gd2O3 | Tb2O3 | Dy2O3 | Ho2O3 | Er2O3 | Tm2O3 | Yb2O3 | Lu2O3 | Y2O3 | P2O5 |
| Mine Tailings |  |  |  |  |  |  |  |  |  |  |  |
| BNO7-SS Xtn | - | 5.10 | - | 8.10 | 1.60 | 6.50 | - | 6.70 | - | 35.40 | 31.70 |
| BNO7-SS Xtn | - | 3.00 | - | 7.90 | 2.00 | 6.40 | - | 5.60 | - | 35.80 | 35.80 |
| avg | - | 4.05 | - | 8.00 | 1.80 | 6.45 | - | 6.15 | - | 35.60 | 33.75 |
| stdev | - | 1.05 | - | 0.10 | 0.20 | 0.05 | - | 0.55 | - | 0.20 | 2.05 |
| Sands |  |  |  |  |  |  |  |  |  |  |  |
| Cross-bed Xtn | - | 1.60 | - | 6.60 | 0.90 | 4.00 | - | 4.80 | - | 42.00 | 39.10 |
| Sulfide-rich Sand Xtn | - | 2.30 | - | 7.60 | 1.30 | 5.40 | - | 4.00 | - | 38.70 | 36.00 |
| Mottled HMS Xtn | - | 1.30 | - | 4.70 | 0.90 | 3.60 | - | 4.20 | - | 43.50 | 41.70 |
| Eocene Sand Xtn | - | 1.60 | - | 5.60 | 1.10 | 4.70 | - | 5.40 | - | 40.90 | 40.70 |
| avg | - | 1.70 | - | 6.13 | 1.05 | 4.43 | - | 4.60 | - | 41.28 | 39.38 |
| stdev | - | 0.37 | - | 1.08 | 0.17 | 0.69 | - | 0.55 | - | 1.75 | 2.16 |
| Kaolins |  |  |  |  |  |  |  |  |  |  |  |
| Cretaceous kaolin Xtn | - | 2.10 | - | 6.70 | 0.90 | 5.10 | - | 4.90 | - | 39.90 | 39.50 |
| Cretaceous kaolin Xtn | - | 1.40 | - | 5.70 | 1.00 | 4.00 | - | 4.40 | - | 42.30 | 41.20 |
| Cretaceous kaolin Xtn | - | 2.40 | - | 8.20 | 1.70 | 4.70 | - | 2.50 | - | 43.20 | 34.70 |
| Cretaceous kaolin Xtn | - | 2.40 | - | 6.20 | 0.90 | 4.50 | - | 4.40 | - | 41.80 | 39.70 |
| avg | - | 2.08 | - | 6.70 | 1.13 | 4.58 | - | 4.05 | - | 41.80 | 38.78 |
| stdev | - | 0.41 | - | 0.94 | 0.33 | 0.40 | - | 0.92 | - | 1.20 | 2.44 |