Distribution and Fractionation of Rare Earth Elements (REE) in the Ion Adsorption-type REE Deposit (IAD) at Maofeng Mountain, Guangzhou, China

Yuanyuan Wang1, 2, 3, Liu Liu4, Mingqi Sun1, 2, 3, Jian Huang1, 2, 3, Yufeng Huang1, 2, 3, Xiaoliang Liang1, 2, 3, Wei Tan1, 2, 3, Hongping He1, 2, 3, Jianxi Zhu1, 2, 3*

1 CAS Key Laboratory of Mineralogy and Metallogeny, Guangdong Provincial Key Laboratory of Mineral Physics and Materials, Guangzhou Institute of Geochemistry, Chinese Academy of Sciences, Guangzhou 510640, China.

2 CAS Center for Excellence in Deep Earth Science, Guangzhou 510640, China.

3 University of Chinese Academy of Sciences, Beijing 100049, China.

4 Guangdong Nonferrous Metal Geological Exploration Institute, Guangzhou 510000, China

*E-mail : zhujx@gig.ac.cn

Fig. S1. The positions of the Maofeng regolith (the green pin) and bedrocks (the yellow pin).

Fig. S2. photographs of the different depths of corresponding weathering stages. 0.5m: Brownish red A horizon; 2m: Yellow–mottled white B1 horizon; 3.5m and 4.5m: pink and yellow B2 horizon; 5m and 8m: pale red and yellow with abundant quartz and feldspar grains.

Fig. S3. XRD patterns of soil samples in the regolith at different depths and bedrock samples. Abbreviations: Qtz=Quartz, fs= K-feldspar, Bt=biotite, Kln=Kaolinite.