Supporting Information

Determination of Sulfide Consumption by Fe-bearing Components of Bentonites

Jebril Hadi 1,*, Jean-Marc Greneche2, Paul Wersin1, Petri Koho3, Barbara Pastina3

*E-mail: jebril.hadi@geo.unibe.ch

1 Institute of Geological Sciences, University of Bern, Switzerland

2 Institut des Molécules et Matériaux du Mans, IMMM UMR CNRS 6283, Le Mans Université, Le Mans France

3 Posiva OY, Finland

CONTENTS

Table S1. List of samples studied and chemicals used	4

Table S2. Compositions (wt.%) of the purified montmorillonite and natural bentonites from XRF analyses	5

Table S3. Structural details for purified smectites	5

Table S4. Specifications of studied samples regarding Fe and smectites content and distribution	6

Figure S1. Error in determination of the concentration of control solutions by methylene blue method upon the course of the reported investigation.	7

Polysulfide analysis: method settings	8

Table S5. Initial and final parameters of the solutions employed for calibration of the polysulfide analysis.	8

Figure S2. (left) Colorimetric analysis of a polysulfide solution and (right) calibration curves at 371 nm.	8

Red rubber silicon seal reaction	10

Figure S3. Seal (a) before and (b) after extended reaction with concentrated sulfide solutions	10

Figure S4. Mössbauer spectra of the pristine seal.	10

Calculations formula: How entries in Tables 4, 5 and Fig. were calculated	11

Mössbauer spectrometry: parameters and nomenclature	12

Figure S5. Mössbauer spectra of pristine and reacted PGV montmorillonite.	13

Figure S6. Mössbauer spectra of pristine and reacted UPM montmorillonite.	13

Table S6. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted PGV and UPM purified montmorillonite.	14

Figure S7. Mössbauer spectra of pristine and reacted SWy and PGN montmorillonite.	15

Table S7. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted SWy and PGN purified montmorillonite.	16

Figure S8. Mössbauer spectra of pristine and reacted GeM montmorillonite.	17

Table S8. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted GeM montmorillonite.	18

Figure S9. Mössbauer spectra of pristine and reacted goethite.	19

Figure S10. Mössbauer spectra of pristine and reacted hematite.	20

Figure S11. Mössbauer spectra of pristine and reacted maghemite.	20

Table S9. Refined values of Mössbauer parameters and doublet structural attributions for the raw and reacted (oxyhydr)oxides.	21

Figure S12. Variation of the isomer shift (IS) with the temperature, following the second-order Doppler shift, modeled (lines) by the Debye equation (c.f. Schröder et al., 2020 and ref therein). Data (points) from Schröder et al. (2020) and the present study. IS of present Fe(III)Sx species was modeled using an IS at 0K (IS0) of 0.285 mm·s–1 and a Debye temperature (ΘM) of 350 K.	22

Figure S13. 300K Mössbauer spectra of sample Syn-Mix pristine and reacted with sulfide for 1 h (T7) to 24 h (T12)	23

Figure S14. 300K Mössbauer spectra of sample Syn-Mix reacted with sulfide for 24 h to 1 month (T16)	24

Figure S15. 77K Mössbauer spectra of sample Syn-Mix reacted with sulfide for 1 week (T13) and 1 month (T16).	25

Table S10. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted Syn-Mix.	26

Figure S16. 300K Mössbauer spectra of Wyoming bentonite WyoB pristine and reacted with sulfide for 1 h (T17) to 24 h (T21)	28

Table S11. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted Wyoming bentonite WyoB (samples T17 to T19).	29

Figure S17. 300K Mössbauer spectra of Wyoming bentonite WyoB reacted with sulfide for 48 h (T22) and 1 month (T27)	30

Figure S18. 77K Mössbauer spectra of WyoB reacted with sulfide for 12 h (T20) and 48 h (T22)	30

Table S12. Refined values of Mössbauer parameters and doublet structural attributions for reacted WyoB (samples T20 to T26).	31

Figure S19. Mössbauer spectra of pristine and reacted GreB.	32

Table S13. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted GreB.	33

Figure S20. Mössbauer spectra of pristine and reacted ItaB.	34

Table S14. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted ItaB.	35

Figure S21. Mössbauer spectra of pristine and reacted IndB.	36

Table S15. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted Indian bentonite Asha.	37

Figure S22. Mössbauer spectra of pristine and reacted CzeB.	38

Table S16. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted Czech bentonite Rokle.	39

Figure S23. Mössbauer spectra of pristine and reacted GeoB.	40

Table S17. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted Georgian bentonite Be-Ge.	41

References	42

# Table S1. List of samples studied and chemicals used

| Product/sample name (alternative name) | Origin | Supplier | Specification |
| --- | --- | --- | --- |
| Pure montmorillonites |
| SWy | Wyoming, USA | CMS Source Clays, Chantilly, VA, USA | purified by author (<2 µm) |
| UPM | Wyoming, USA | CMS Source Clays | purified by author (<2 µm) |
| PGV |  | Nanocor Inc., Aberdeen, MS, USA | ≤25 μm |
| PGN |  | Nanocor Inc. | ≤25 μm |
| GeM | Georgia | main author | Bentonite GeoB purified by author (<2 µm) |
| (oxyhydr)oxides |  |  |  |
| Goethite |  | Sigma Aldrich, Saint Louis, MO, USA | powder, <5 μm, 30-63% Fe, |
| Hematite |  | Sigma Aldrich | powder, ≥96% |
| Maghemite |  | Sigma Aldrich | nanopowder, <50 nm |
| Bentonites |  |  |  |
| WyoB (MX80) | Wyoming, USA | SKB, Solna, Sweden | used in ABM and LOT experiments |
|  | Milos, Greece | SKB |  |
| IndB (Asha) | India | SKB | used in ABM experiments |
| CzeB (Rokle) | Czech Republic | SKB | used in ABM experiments |
| ItaB (Be-It) | Laviosa, Italy | A-Insinöörit Oy, Tampere, Finland | batch Be-It-BT0003-Gr-R |
| GeoB (Be-Ge) | Georgia | A-Insinöörit Oy | batch Be-Ge-0001-Gr-R |
| Synthetic mixture |  |  |  |
| Syn-Mix |  | main author | SWy + 0.93 wt.%. goethite |
| Chemicals |  |  |  |
| Na2S 9H2O |  | Sigma Aldrich | ACS reagent > 98.5% (for experiments) |
| Na2S 9H2O |  | Sigma Aldrich | Pure> 99.99% (for calibration) |
| NaCl |  | Sigma Aldrich | EMSURE®, for analysis |
| HCl |  | Sigma Aldrich | Suprapur®, 36% |
| FeCl3.5 H2O |  | Sigma Aldrich | ACS Reagent, p.a. 98-102% |
| N-N-dimethyl-p-phenylenediamine sulfate |  | Sigma-Aldrich | for spectroscopic determination of S2-, Cl2, ≥99.0% |
| elemental sulfur |  | Sigma-Aldrich | Colloidal, powder, ≥99.0% |

# Table S2. Compositions (wt.%) of the purified montmorillonites and natural bentonites from XRF analyses

| Oxide | UPM | PGN | PGV | SWy | GeM | GreB | GeoB | WyoBg | ItaB | IndB | CzeB |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ref data |  |  |  |  |  | 1 | 2 | 3 | 4 | 3 | 3 |
| SiO2 | 66.58 | 64.87 | 65.35 | 65.28 | 66.11 | 67.63 | 64.48 | 59.58 | 62.52 | 49.49 | 51.07 |
| Al2O3 | 22.61 | 23.01 | 20.42 | 21.06 | 21.22 | 18.07 | 20.09 | 18.9 | 18.64 | 19.56 | 16.40 |
| Fe2O3 | 4.99 | 4.74 | 4.42 | 4.13 | 3.90 | 3.09 | 3.56 | 3.91 | 6.48 | 16.74 | 17.87 |
| MgO | 2.70 | 2.57 | 5.41 | 4.74 | 4.68 | 2.421 | 4.46 | 2.56 | 5.27 | 3.09 | 3.90 |
| CaO | 2.92 | 0.73 | 2.32 | 3.09 | 0.00 | 3.225 | 2.61 | 1.39 | 1.67 | 7.33 | 5.02 |
| Na2O |  | 2.75 | 1.20 |  | 3.48 | 0.325 | 3.36 | 1.95 | 2.75 | 1.35 | 0.91 |
| K2O | 0.07 | 0.20 | 0.09 | 1.16 | 0.22 | 1.43 | 0.82 | 0.6 | 1.73 | 0.20 | 0.71 |
| MnO* |  | 0.01 | 0.02 | 0.04 | 0.08 | 0.03 | 0.13 | 0.02 | 0.10 | 0.41 | 0.10 |
| TiO2* | 0.12 | 0.15 | 0.45 | 0.44 | 0.29 | 0.53 | 0.36 | 0.2 | 0.65 | 1.31 | 3.81 |
| P2O5* |  | 0.01 | 0.02 | 0.06 | 0.02 | 0.01 | 0.13 | 0.085 | 0.17 | 0.21 | 0.21 |
| Cl** |  | 0.20 | 0.20 |  |  |  |  |  |  |  |  |

*interpreted as impurities.

1  (Svensson, unpublished)

2  (Kiviranta et al., 2019)

3 (Svensson et al., 2011)

4 (Kiviranta et al., 2017 (unpublished))

# Table S3. Structural details for purified smectites.

| Sample | Structural formula (per O20(OH)4) | Layer chargea | CECb | %redc | mOH | smectite typed |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | meq·g–1 | meq·g–1 |  | meq·g–1 |  |
| UPM | Ca0.37K0.01[Al3.03Mg0.48Fe0.44](Si7.88Al0.12) | 1.01 | 0.99 | 3% | 5.36 | Wyoming mmt |
| PGN | Ca0.10Na0.59K0.04[Al3.07Mg0.46Fe0.43](Si7.81Al0.21) | 1.10 | n.d. | 11% | 5.36 | Wyoming mmt |
| PGV | Ca0.27Na0.28K0.01[Al2.74Mg0.97Fe0.40](Si7.84Al0.17) | 1.12 | 1.26 | 0% | 5.34 | Chambers mmt |
| SWy | Ca0.40K0.15[Al2.81Mg0.84Fe0.37](Si7.83Al0.17) | 1.31 | 1.01 | 17% | 5.31 | Chambers mmt/ill |
| GeM | Na0.80K0.03 [Al2.86Mg0.86Fe0.35](Si7.88Al0.12) | 1.12 | 1.07 | 11% | 5.34 | Chambers mmt |

a Calculated (meq·g–1) from structural formula, taking into account the presence of supernumerary cations or lacunas in the octahedral sheet.

b Determined (meq·g–1) using the hexaamminecobalt method.

c Reduction level of Festr i.e. Fe2+/(Fe2++Fe3+).

d mmt: montmorillonite; ill: illite.

# Table S4. Specifications of studied samples regarding Fe and smectites content and distribution

| Sample | H2Oa | Smectite | (oxyhydr) oxides | total Fe | Fe distribution | Fe reduction level | dom. exc. cat.e |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | total | Festr | Goe | hem | Mag |  |  |
|  | wt.% | wt.% (dry) | mmol·g–1 | % |  |
| purified smectites |  |
| SWy | 15.56 | > 99 | < 0.1 | 2.85 | 0.52 | 0.52 |  |  |  | 17% | Ca |
| UPM | 16.11 | > 99 | < 0.1 | 3.43 | 0.63 | 0.63 |  |  |  | 3% | Ca |
| PGV | 15.84 | > 99 | < 0.1 | 3.10 | 0.56 | 0.56 |  |  |  | 4% | Ca/Na |
| PGN | 9.08 | > 99 | < 0.1 | 3.30 | 0.59 | 0.59 |  |  |  | 11% | Na |
| GeM | 10.56 | > 99 |  | 2.34 | 0.42 | 0.38 | 0.04c | 16% | Na |
| raw bentonites |  |
| WyoBb | 6.77 | ~80 | < 0.1 | 2.70 | 0.48 | 0.48 | tr. | tr. |  | 19% | Na |
| GreB | 2.65 | > 95 | < 0.1 | 2.19 | 0.39 | 0.39 |  |  |  | 13% | Ca |
| IndB | 11.91 | ~80 | 2.99 | 12.50 | 2.06 | 1.15 | 0.78 | 0.12 | Tr | 0% | Na |
| CzeB | 15.56 | ~70 | 2.56 | 9.58 | 2.24 | 1.48 | 0.67 | 0.09 | Tr | 2% | Ca |
| ItaB | 13.18 | 85 | 1.40 | 3.952 | 0.71 | 0.53 | 0.05 | 0.13 |  | 0% | Na |
| GeoB | 11.13 | 91 | 0.37 | 2.13 | 0.38 | 0.34 | 0.04c | 17% | Na |
| Goethite | 0.70% | < 0.05 | 100% | 62.85 | 11.25 |  | 11.25 |  |  | 0% |  |
| Hematite | n.d. | < 0.05 | 100% | 69.94 | 12.52 |  |  | 12.52 |  | 0% |  |
| Maghemite | n.d. | < 0.05 | 100% | 69.94 | 12.52 |  |  |  | 12.52 | 0% |  |
| Synthetic mixture |  |
| Syn-Mix | 15.46% | 99.07% | 0.93% | 3.51% | 0.62 | 0.51 | 0.12 |  |  | 7% | Ca |

a Gravimetrically determined after heating at 105°C for 48 h except for Syn-Mix (calculated)

b Also contains traces of magnetite, ilmenite, and pyrite as determined by SEM and Raman (Hadi et al., 2017).

c The nature of (oxyhydr)oxide(s) has not been determined yet.

d Assumed as pure phases

e Dominant exchangeable cation

# Figure S1. Error in determination of the concentration of control solutions by methylene blue method upon the course of the reported investigation.

# Polysulfide analysis: method settings

A series of concentrated polysulfides solutions in anaerobic conditions were produced through the reaction of concentrated sulfide solutions (100 mM) at two contrasting pH bracketing experimental pH (pH 8 and 13). Two solutions were produced at each pH, using the same sulfide concentration, but varying elemental sulfur amounts. Such solutions turned yellow after only few minutes of mixing, indicating the rapid formation of polysulfides. After 24 h of stirring, the final pH and sulfide concentrations of the supernatant were determined.

# Table S5. Initial and final parameters of the solutions employed for calibration of the polysulfide analysis.

| Solution | initial parameters | final parameters |
| --- | --- | --- |
|  | pH | [sulfide] | S(0)/S(-II) | pH | [sulfide] |
|  |  |  |  |  | final | Delta |
|  |  | (mM) | (mol/mol) |  | (mM) | (mM) |
| V1-A | 13.02 | 105 | 0.44 | 12.96 | 88.2 | 17.1 |
| V1-B | 13.02 | 105 | 0.85 | 12.89 | 71.2 | 34.1 |
| V2-A | 8.03 | 114 | 0.39 | 8.25 | 104.5 | 9.3 |
| V2-B | 8.03 | 114 | 0.79 | 8.72 | 103.5 | 10.3 |

All solutions had to be diluted (10 to 100 fold) with pure deoxygenated water in order to be measured in the correct absorbance range of the spectrophotometer. The pH of the dilutions was not determined. The absorbance of the solution was recorded over the whole visible spectrum. The collected spectra could be de-convoluted into two Gaussian sub-components (Figure S3 left). The global fit was not perfect, but a very good correlation could be found between the height of component B and the polysulfide concentration inferred from the sulfide consumption components (Figure S3 right).

# Figure S2. (left) Colorimetric analysis of a polysulfide solution and (right) calibration curves at 371 nm.

The position of the component B shifted from 368 to 373 nm with decreasing pH. The height relative to the larger component also increased with decreasing pH. The pH of investigated experiments ranged from 5 to 13.5, most being pH ~8-9. It was also observed that the position of component B shifted between 368 and 373 nm, with most samples generally showing an intermediate position of ~371 nm. It was thus decided to employ this wavelength for calibration and determination of polysulfide in all studied samples. Calibration curves were derived from dilutions of the polysulfide stock solutions at various pH, assuming that the total concentration of polysulfide was equal to the corresponding drop in sulfide concentration. Given the uncertainties in sulfide analysis (~2%), that the calibration is based on the difference between two sulfide analysis, and in regard of uncertainties on pH dependence, minimal uncertainties of 5% can be ascribed to the polysulfides determination employing present method.

# Red rubber silicon seal reaction

# Figure S3. Seal (a) before and (b) after extended reaction with concentrated sulfide solutions

# Figure S4. Mössbauer spectra of the pristine seal.

# Calculations formula: How entries in Tables 4, 5 and Fig. were calculated

where:

is the solid liquid ratio in L·Kg–1 (Tables 1 and 2)

is the initial sulfide concentration in mM (Tables 1 and 2)

is the total Fe concentration in the sample in mmol kg–1 (Table S4)

is the maximum Fe reduction level reached in the sample after reaction, in % (Tables 1 and 2)

is the Fe reduction level in the raw sample, in % (Table S4)

where

is the Fe reduction level reached in the sample after reaction, in % (Tables 1 and 2)

is the massic sulfide consumption in mmol·kg–1 (Tables 1 and 2)

where

is the sulfide concentration in mM (Tables 1 and 2)

is the final sulfide concentration

# Mössbauer spectrometry: parameters and nomenclature

The uncertainties are 0.02 mm∙s–1 for IS, QS, 2ε, and FWHM; 0.5 T for Bhf, and 2% for the relative proportion.

The following nomenclature is used in the description of the Mössbauer parameters:

IS = Isomer shift value relative to that of α-Fe at 300 K (mm s–1)

FWHM = full width at half-height of lines (mm s–1)

QS/2ε = Quadrupole splitting/quadrupole shift (mm s–1)

Bhf = magnetic hyperfine field (Tesla, T)

Para-Fe(II/III) = paramagnetic Fe(II/III)

# Figure S5. Mössbauer spectra of pristine and reacted PGV montmorillonite.

# Figure S6. Mössbauer spectra of pristine and reacted UPM montmorillonite.

# Table S6. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted PGV and UPM purified montmorillonite.

| Hyperfine parameters | Attribution | Hyperfine parameters | Attribution |
| --- | --- | --- | --- |
| IS | FW HM | QS or 2ε | Area (%) |  | IS | FW HM | QS or 2ε | Area (%) |  |
| PGV – raw (300K – 12 mm s–1) | UPM – raw (300K – 4 mm s-1) |
| 0.36 | 0.52 | 0.63 | 57% | para-Fe(III) | 0.34 | 0.70 | 0.65 | 97% | para-Fe(III) |
| 0.28 | 1.55 | 0.00 | 39% | para-Fe(III) | 1.12 | 0.44 | 1.95 | 3% | para-Fe(II) |
| PGV – A2 (300K – 12 mm s–1) | UPM – D1 (300K – 12 mm s–1) |
| 0.27 | 0.55 | 0.74 | 20% | para-Fe(III) | 0.28 | 0.63 | 0.72 | 38% | para-Fe(III) |
| 1.13 | 0.37 | 2.78 | 80% | para-Fe(II) | 1.13 | 0.35 | 2.75 | 62% | para-Fe(II) |
| PGV – A2 (300K – 4 mm s–1) | UPM – D1 (300K – 4 mm s–1) |
| 0.36 | 0.63 | 0.65 | 21% | para-Fe(III) | 0.28 | 0.71 | 0.74 | 40% | para-Fe(III) |
| 1.15 | 0.33 | 2.81 | 79% | para-Fe(II) | 1.12 | 0.34 | 2.73 | 40% | para-Fe(II) |
| PGV – A4 (300K – 12 mm s–1) | 1.14 | 0.26 | 3.02 | 20% | para-Fe(II) |
| 0.35 | 0.6 | 0.57 | 59% | para-Fe(III) | UPM – T1 (300K – 4 mm s–1) |
| 0.36 | 3.00 | 0.00 | 31% | para-Fe(III) | 0.32 | 0.65 | 0.68 | 62% | para-Fe(III) |
| 1.13 | 0.41 | 2.65 | 10% | para-Fe(II) | 1.00 | 0.36 | 1.77 | 2% | para-Fe(II) |
| PGV – A5 (300K – 4 mm s–1) | 1.14 | 0.28 | 2.76 | 27% | para-Fe(II) |
| 0.34 | 0.62 | 0.61 | 76% | para-Fe(III) | 1.14 | 0.22 | 3.00 | 9% | para-Fe(II) |
| 1.23 | 0.58 | 2.35 | 14% | para-Fe(II) | UPM – T2 (300K – 4 mm s–1) |
| 1.13 | 0.29 | 2.77 | 10% | para-Fe(II) | 0.33 | 0.69 | 0.67 | 75% | para-Fe(III) |
|  |  |  |  |  | 0.98 | 0.32 | 1.80 | 2% | para-Fe(II) |
|  |  |  |  |  | 1.15 | 0.28 | 2.70 | 8% | para-Fe(II) |
|  |  |  |  |  | 1.15 | 0.27 | 2.90 | 15% | para-Fe(II) |

SWy

# Figure S7. Mössbauer spectra of pristine and reacted SWy and PGN montmorillonite.

# Table S7. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted SWy and PGN purified montmorillonite.

| Hyperfine parameters | Attribution | Hyperfine parameters | Attribution |
| --- | --- | --- | --- |
| IS | FW HM | QS or 2ε | Area (%) |  | IS | FW HM | QS or 2ε | Area (%) |  |
| PGN – raw (300K – 4 mm s–1) | SWy – raw (300K – 4 mm s-1) |
| 0.36 | 0.29 | 0.49 | 10% | para-Fe(III) | 0.34 | 0.62 | 0.51 | 67% | para-Fe(III) |
| 0.35 | 0.50 | 0.85 | 15% | para-Fe(III) | 0.49 | 0.82 | 1.05 | 16% | para-Fe(III) |
| 0.44 | 0.83 | 0.97 | 21% | para-Fe(III) | 1.13 | 0.42 | 2.83 | 17% | para-Fe(II) |
| 0.26 | 1.30 | 0.17 | 43% | para-Fe(III) |  |  |  |  |  |
| 1.14 | 0.44 | 2.87 | 11% | para-Fe(II) |  |  |  |  |  |
| PGN – E1 (300K – 12 mm s–1) | SWy – T35 (300K – 4 mm s–1) |
| 0.31 | 0.54 | 0.73 | 27% | para-Fe(III) | 0.35 | 0.65 | 0.55 | 65% | para-Fe(III) |
| 1.10 | 0.4 | 2.79 | 73% | para-Fe(II) | 1.09 | 0.36 | 1.88 | 2% | para-Fe(II) |
|  |  |  |  |  | 1.11 | 0.27 | 2.59 | 11% | para-Fe(II) |
|  |  |  |  |  | 1.13 | 0.28 | 2.91 | 22% | para-Fe(II) |
| PGN – E1 (300K – 4 mm s–1) | SWy – T36 (300K – 4 mm s–1) |
| 0.33 | 0.59 | 0.74 | 26% | para-Fe(III) | 0.35 | 0.63 | 0.53 | 56% | para-Fe(III) |
| 1.13 | 0.38 | 2.81 | 74% | para-Fe(II) | 1.13 | 0.32 | 0.97 | 1% | para-Fe(III) |
|  |  |  |  |  | 1.17 | 0.3 | 2.12 | 3% | para-Fe(II) |
|  |  |  |  |  | 1.13 | 0.36 | 2.80 | 40% | para-Fe(II) |

GEM

# Figure S8. Mössbauer spectra of pristine and reacted GeM montmorillonite.

# Table S8. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted GeM montmorillonite.

| Hyperfine parameters | Attribution | Hyperfine parameters | Attribution |
| --- | --- | --- | --- |
| IS | FW HM | QS or 2ε | Area (%) |  | IS | FW HM | QS or 2ε | Bhf | Area (%) |  |
| GeM – raw (300K – 12 mm s–1) | GeM – raw (77K – 12 mm s–1) |
| 0.35 | 0.67 | 0.56 | 62% | para-Fe(III) | 0.46 | 0.83 | 0.57 |  | 75% | para-Fe(III) |
| 0.35 | 6.00 | 0.00 | 27% | para-Fe(III) | 0.41 | 0.60 | 0.15 | 57.4 | 2% | ? |
| 1.16 | 0.46 | 2.77 | 11% | para-Fe(II) | 0.41 | 0.60 | 0.15 | 53.8 | 7% | ? |
|  |  |  |  |  | 1.29 | 0.62 | 2.96 |  | 16% | para-Fe(II) |
| GeM – T45 (300K – 12 mm s–1) | GeM – T45 (77K – 12 mm s–1) |
| 0.32 | 0.61 | 0.66 | 50% | para-Fe(III) | 0.43 | 0.77 | 0.65 |  | 54% | para-Fe(III) |
| 0.35 | 6.00 | 0.00 | 18% | para-Fe(II) | 0.43 | 0.60 | 0.55 | 57.1 | 3% | ? |
| 1.12 | 0.36 | 2.77 | 32% | para-Fe(II) | 0.43 | 0.60 | -0.14 | 53.4 | 4% | ? |
|  |  |  |  |  | 1.26 | 0.35 | 3.02 |  | 39% | para-Fe(II) |
| GeM – T46 (300K – 12 mm s–1) | GeM – T46 (77K – 12 mm s–1) |
| 0.33 | 0.66 | 0.63 | 51% | para-Fe(III) | 0.39 | 0.74 | 0.67 |  | 46% | para-Fe(III) |
| 1.13 | 0.39 | 2.78 | 49% | para-Fe(II) | 0.42 | 0.50 | 0.29 | 55.6 | 4% | ? |
|  |  |  |  |  | 0.63 | 0.50 | -0.39 | 43.8 | 3% | ? |
|  |  |  |  |  | 1.26 | 0.35 | 3.03 |  | 47% | para-Fe(II) |

# Figure S9. Mössbauer spectra of pristine and reacted goethite.

# Figure S10. Mössbauer spectra of pristine and reacted hematite.

# Figure S11. Mössbauer spectra of pristine and reacted maghemite.

# Table S9. Refined values of Mössbauer parameters and doublet structural attributions for the raw and reacted (oxyhydr)oxides.

| Sample | experiment | reaction time | (oxyhydr)oxide substrate | reaction product(s) |
| --- | --- | --- | --- | --- |
|  |  |  | IS | QS or 2ε | Bhf | area | IS | QS or 2ε | Bhf | area |
|  |  |  | (mm·S–1) | (mm·S–1) | (T) | (%) | (mm·S–1) | (mm·S–1) | (T) | (%) |
| 300 K |
| Goethite | Raw |  | <0.37> | <-0.25> | <36.1> | 100% | n.a. |
|  | B3 (pH 13) | 11 days | <0.37> | <-0.26> | <36.6> | 98% | 0.16 | 0.55 |  | 2% |
|  | B4 | 17 h | <0.37> | <-0.25> | <36.6> | 95% | 0.16 | 0.55 |  | 5% |
|  | B5 | 22 h | <0.37> | <-0.26> | <36.7> | 96% | 0.16 | 0.57 |  | 4% |
|  | B6 | 6 weeks | <0.37> | -<0.26> | <36.4> | 94% | 0.1 | 0.58 |  | 6% |
| Hematite | Raw |  | 0.38 | -0.20 | 51.7 | 100% | n.a. |
|  | T5 | 24 h | 0.37 | -0.20 | 51.5 | 98% | 0.14 | 0.5 |  | 2% |
|  | T6 | 1 month | 0.38 | -0.20 | 51.00 | 100% | no product |
| Maghemite | Raw |  | <0.32> | <0.00> | <49.5> | 100% | n.a. |
|  | T38 | 24 h | <0.32> | <-0.01> | <48.9> | 95% | 0.15 | 0.49 |  | 5% |
|  | T37 | 1 month | <0.33> | <0.01> | <49.3> | 77% | 0.15 | 0.5 |  | 6% |
|  |  |  |  |  |  |  | <0.47> | <0.00> | <43.3> | 17% |
| 77 K |
| Goethite | Raw |  | 0.49 | -0.24 | 50.2 | 100% |  |  |  |  |
|  | B5 | 22 h | 0.49 | -0.24 | 49.8 | 95% | 0.28 | 0.55 |  | 5% |
|  | B6 | 6 weeks | 0.49 | -0.23 | 49.9 | 90% | 0.27 | 0.55 |  | 10% |
| Hematite | Raw |  | 0.44 | 0.40 | 53.9 | 100% |  |  |  |  |
|  | T5 | 24 h | 0.49 | 0.39 | 53.8 | 95% | 0.27 | 0.54 |  | 5% |
| Maghemite | Raw |  | <0.43> | <0.01> | <52.0> | 100% |  |  |  |  |
|  | T37 | 24 h | <0.44> | <0.01> | <52.1> | 92% | 0.27 | 0.51 |  | 7% |
|  | T38 | 1 month | <0.46> | <0.02> | <52.3> | 84% | 0.27 | 0.52 |  | 10% |
|  |  |  |  |  |  |  | <0.87> | <1.23> | <39.2> | 7% |

# Figure S12. Variation of the isomer shift (IS) with the temperature, following the second-order Doppler shift, modeled (lines) by the Debye equation (c.f. Schröder et al., 2020 and ref therein). Data (points) from Schröder et al. (2020) and the present study. IS of present Fe(III)Sx species was modeled using an IS at 0K (IS0) of 0.285 mm·s–1 and a Debye temperature (ΘM) of 350 K.

# Figure S13. 300K Mössbauer spectra of sample Syn-Mix pristine and reacted with sulfide for 1 h (T7) to 24 h (T12)

# Figure S14. 300K Mössbauer spectra of sample Syn-Mix reacted with sulfide for 24 h to 1 month (T16)

# Figure S15. 77K Mössbauer spectra of sample Syn-Mix reacted with sulfide for 1 week (T13) and 1 month (T16).

# Table S10. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted Syn-Mix.

| Hyperfine parameters | Attribution | Hyperfine parameters | Attribution |
| --- | --- | --- | --- |
| IS | FW HM | QS or 2ε | Bhf | Area (%) |  | IS | FW HM | QS or 2ε | Bhf | Area (%) |  |
| Syn-Mix – raw (300K – 12 mm s–1) | Syn-Mix – T12 (300K – 12 mm s–1) |
| 0.34 | 0.72 | 0.55 |  | 48% | para-Fe(III) | 0.36 | 0.71 | 0.51 |  | 43% | para-Fe(III) |
| 0.36 | 6.00 | 0.00 |  | 25% | para-Fe(III) | 0.37 | 0.51 | -0.28 | 37.9 | 20% | goethite |
| 0.38 | 0.51 | -0.23 | 38.0 | 20% | Goethite | 0.47 | 0.48 | -0.72 | 31.1 | 5% | goethite |
| 1.16 | 0.35 | 2.82 |  | 7% | para-Fe(II) | 1.14 | 0.42 | 2.83 |  | 32% | para-Fe(II) |
| Syn-Mix – T7 (300K – 12 mm s–1) | Syn-Mix – T13 (300K – 12 mm s–1) |
| 0.36 | 0.71 | 0.57 |  | 52% | para-Fe(III) | 0.34 | 0.70 | 0.45 |  | 40% | para-Fe(III) |
| 0.36 | 6.00 | 0.00 |  | 10% | para-Fe(III) |  |  |  |  |  |  |
| 0.38 | 0.32 | -0.28 | 38.2 | 11% | Goethite | 0.37 | 0.54 | -0.28 | 39.1 | 11% | goethite |
| 0.43 | 0.66 | -0.25 | 35.1 | 8% | Goethite | 0.39 | 0.54 | -0.05 | 36.9 | 7% | goethite |
| 1.10 | 0.43 | 2.80 |  | 19% | para-Fe(II) | 1.09 | 0.58 | 2.63 |  | 42% | para-Fe(II) |
| Syn-Mix – T8 (300K – 12 mm s–1) | Syn-Mix – T14 (300K – 12 mm s–1) |
| 0.35 | 0.67 | 0.52 |  | 46% | para-Fe(III) | 0.36 | 0.59 | 0.54 |  | 38% | para-Fe(III) |
| 0.36 | 6.00 | 0.00 |  | 21% | para-Fe(III) |  |  |  |  |  |  |
| 0.38 | 0.36 | -0.3 | 38.2 | 14% | Goethite | 0.40 | 0.61 | -0.18 | 37.9 | 21% | goethite |
| 0.40 | 0.26 | -0.26 | 35.6 | 3% | Goethite | 0.38 | 0.36 | -0.18 | 33.9 | 3% | goethite |
| 1.14 | 0.36 | 2.81 |  | 16% | para-Fe(II) | 1.14 | 0.41 | 2.85 |  | 39% | para-Fe(II) |
| Syn-Mix – T9 (300K – 12 mm s–1) | Syn-Mix – T15 (300K – 12 mm s–1) |
| 0.35 | 0.67 | 0.55 |  | 48% | para-Fe(III) | 0.35 | 0.59 | 0.52 |  | 38% | para-Fe(III) |
| 0.36 | 6.00 | 0.00 |  | 8% | para-Fe(III) |  |  |  |  |  |  |
| 0.37 | 0.42 | -0.25 | 38.0 | 17% | Goethite | 0.38 | 0.34 | -0.28 | 38.6 | 14% | goethite |
| 0.56 | 0.47 | -0.33 | 33.1 | 5% | Goethite | 0.63 | 0.95 | -0.28 | 35 | 8% | goethite |
| 1.13 | 0.44 | 2.85 |  | 22% | para-Fe(II) | 1.14 | 0.38 | 2.82 |  | 40% | para-Fe(II) |
| Syn-Mix – T10 (300K – 12 mm s–1) | Syn-Mix – T16 (300K – 12 mm s–1) |
| 0.36 | 0.63 | 0.52 |  | 42% | para-Fe(III) | 0.33 | 0.66 | 0.55 |  | 40% | para-Fe(III) |
| 0.36 | 6.00 | 0.00 |  | 13% | para-Fe(III) |  |  |  |  |  |  |
| 0.39 | 0.49 | -0.28 | 37.9 | 17% | Goethite | 0.39 | 0.39 | -0.28 | 38.4 | 12% | goethite |
| 0.44 | 0.30 | -0.28 | 35 | 4% | Goethite | 0.47 | 1.10 | -0.51 | 34.4 | 8% | goethite |
| 1.16 | 0.46 | 2.86 |  | 24% | para-Fe(II) | 1.15 | 0.52 | 2.84 |  | 40% | para-Fe(II) |
| Syn-Mix – T11 (300K – 12 mm s–1) |  |
| 0.34 | 0.58 | 0.51 |  | 41% | para-Fe(III) |  |  |  |  |  |  |
| 0.36 | 6.00 | 0.00 |  | 20% | para-Fe(III) |  |  |  |  |  |  |
| 0.37 | 0.34 | -0.26 | 37.9 | 14% | Goethite |  |  |  |  |  |  |
| 1.14 | 0.38 | 2.76 |  | 25% | para-Fe(II) |  |  |  |  |  |  |
| Syn-Mix – T13 (77K – 12 mm s–1) | Syn-Mix – T16 (77K – 12 mm s–1) |
| 0.45 | 0.66 | 0.56 |  | 42% | para-Fe(III) | 0.30 | 0.64 | 0.55 |  | 40% | para-Fe(III) |
| 0.49 | 0.37 | -0.24 | 50.2 | 18% | Goethite | 0.32 | 0.36 | -0.24 | 49.9 | 16% | Goethite |
| 0.49 | 0.50 | 0.18 | 56.0 | 2% | Goethite | 0.32 | 0.44 | 0.10 | 55 | 3% | Goethite |
| 1.25 | 0.37 | 3.03 |  | 38% | para-Fe(II) | 1.10 | 0.36 | 3.01 |  | 41% | para-Fe(II) |

# Figure S16. 300K Mössbauer spectra of Wyoming bentonite WyoB pristine and reacted with sulfide for 1 h (T17) to 24 h (T21)

# Table S11. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted Wyoming bentonite WyoB (samples T17 to T19).

| Hyperfine parameters | Attribution | Hyperfine parameters | Attribution |
| --- | --- | --- | --- |
| IS | FW HM | QS or 2ε | Area (%) |  | IS | FW HM | QS or 2ε | Area (%) |  |
|  | WyoB – raw (300K – 12 mm s–1) |
|  |  |  |  |  | 0.24 | 0.44 | 0.74 | 17% | para-Fe(III) |
|  |  |  |  |  | 0.43 | 0.56 | 0.48 | 21% | para-Fe(III) |
|  |  |  |  |  | 0.08 | 0.87 | 0.7 | 17% | para-Fe(III) |
|  |  |  |  |  | 0.47 | 0.98 | 0.93 | 26% | para-Fe(III) |
|  |  |  |  |  | 1.19 | 0.16 | 3.01 | 2% | para-Fe(II) |
|  |  |  |  |  | 1.28 | 0.26 | 2.52 | 7% | para-Fe(II) |
|  |  |  |  |  | 1.13 | 0.47 | 2.04 | 10% | para-Fe(II) |
| WyoB – T17 (300K – 12 mm s–1) | WyoB – T17 (300K – 4 mm s–1) |
| 0.33 | 0.50 | 0.57 | 30% | para-Fe(III) | 0.35 | 0.56 | 0.61 | 32% | para-Fe(III) |
| 1.14 | 0.37 | 2.79 | 70% | para-Fe(II) | 1.25 | 0.36 | 1.80 | 3% | para-Fe(II) |
|  |  |  |  |  | 1.14 | 0.32 | 2.69 | 34% | para-Fe(II) |
|  |  |  |  |  | 1.14 | 0.28 | 2.9 | 31% | para-Fe(II) |
| WyoB – T18 (300K – 12 mm s–1) | WyoB – T18 (300K – 4 mm s–1) |
| 0.33 | 0.57 | 0.62 | 31% | para-Fe(III) | 0.33 | 0.47 | 0.61 |  | 29% |
| 1.15 | 0.36 | 2.79 | 69% | para-Fe(II) | 1.23 | 0.36 | 1.79 |  | 5% |
|  |  |  |  |  | 1.15 | 0.30 | 2.74 |  | 46% |
|  |  |  |  |  | 1.14 | 0.22 | 2.94 |  | 20% |
| WyoB – T19 (300K – 12 mm s–1) | WyoB – T19 (300K – 4 mm s–1) |
| 0.34 | 0.50 | 0.57 | 26% | para-Fe(III) | 0.35 | 0.5 | 0.62 |  | 27% |
| 1.14 | 0.36 | 2.79 | 74% | para-Fe(II) | 1.55 | 0.36 | 1.74 |  | 5% |
|  |  |  |  |  | 1.16 | 0.29 | 2.69 |  | 30% |
|  |  |  |  |  | 1.15 | 0.28 | 2.9 |  | 38% |

# Figure S17. 300K Mössbauer spectra of Wyoming bentonite WyoB reacted with sulfide for 48 h (T22) and 1 month (T27)

# Figure S18. 77K Mössbauer spectra of WyoB reacted with sulfide for 12 h (T20) and 48 h (T22)

# Table S12. Refined values of Mössbauer parameters and doublet structural attributions for reacted WyoB (samples T20 to T26).

| Hyperfine parameters | Attribution | Hyperfine parameters | Attribution |
| --- | --- | --- | --- |
| IS | FW HM | QS or 2ε | Area (%) |  | IS | FW HM | QS or 2ε | Area (%) |  |
| WyoB – T20 (300K – 4 mm s–1) | WyoB – T23 (300K – 4 mm s–1) |
| 0.33 | 0.51 | 0.62 | 25% | para-Fe(III) | 0.33 | 0.47 | 0.63 | 25% | para-Fe(III) |
| 1.23 | 0.36 | 1.84 | 5% | para-Fe(II) | 1.21 | 0.36 | 1.81 | 5% | para-Fe(II) |
| 1.15 | 0.33 | 2.72 | 44% | para-Fe(II) | 1.15 | 0.28 | 2.71 | 33% | para-Fe(II) |
| 1.14 | 0.28 | 2.93 | 26% | para-Fe(II) | 1.14 | 0.28 | 2.96 | 37% | para-Fe(II) |
| WyoB – T21 (300K – 4 mm s–1) | WyoB – T24 (300K – 4 mm s–1) |
| 0.32 | 0.48 | 0.63 | 27% | para-Fe(III) | 0.33 | 0.47 | 0.60 | 21% | para-Fe(III) |
| 1.18 | 0.36 | 1.80 | 4% | para-Fe(II) | 1.21 | 0.36 | 1.85 | 2% | para-Fe(II) |
| 1.14 | 0.3 | 2.71 | 44% | para-Fe(II) | 1.14 | 0.31 | 2.71 | 48% | para-Fe(II) |
| 1.14 | 0.26 | 2.93 | 26% | para-Fe(II) | 1.14 | 0.28 | 2.95 | 29% | para-Fe(II) |
| WyoB – T22 (300K – 4 mm s–1) | WyoB – T26 (300K – 4 mm s–1) |
| 0.30 | 0.47 | 0.65 | 23% | para-Fe(III) | 0.33 | 0.41 | 0.57 | 20% | para-Fe(III) |
| 1.17 | 0.58 | 2.03 | 9% | para-Fe(II) | 1.3 | 0.36 | 1.79 | 5% | para-Fe(II) |
| 1.14 | 0.28 | 2.74 | 43% | para-Fe(II) | 1.18 | 0.29 | 2.74 | 38% | para-Fe(II) |
| 1.13 | 0.27 | 2.98 | 24% | para-Fe(II) | 1.18 | 0.29 | 2.95 | 37% | para-Fe(II) |
| WyoB – T20 (77K – 4 mm s–1) | WyoB – T22 (77K – 4 mm s–1) |
| 0.45 | 0.59 | 0.61 | 25% | para-Fe(III) | 0.32 | 0.57 | 0.6 | 22% | para-Fe(III) |
| 1.26 | 0.29 | 3.04 | 71% | para-Fe(II) | 1.14 | 0.31 | 3.07 | 58% | para-Fe(II) |
| 1.22 | 0.29 | 2.34 | 4% | para-Fe(II) | 1.12 | 0.40 | 2.87 | 20% | para-Fe(II) |

# Figure S19. Mössbauer spectra of pristine and reacted GreB.

# Table S13. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted GreB.

| Hyperfine parameters | Attribution | Hyperfine parameters | Attribution |
| --- | --- | --- | --- |
| IS | FW HM | QS or 2ε | Area (%) |  | IS | FW HM | QS or 2ε | Area (%) |  |
| GreB – raw (300K – 4 mm s–1) | GreB – raw (300K – 4 mm s–1) |
| 0.33 | 0.59 | 0.6 | 87% | para-Fe(III) |  |  |  |  |  |
| 1.14 | 0.44 | 2.8 | 13% | para-Fe(II) |  |  |  |  |  |
| GreB – T27 (300K – 4 mm s–1) | GreB – T27 (300K – 4 mm s–1) |
| 0.25 | 0.23 | 0.39 | 30% | para-Fe(III) | 0.43 | 0.31 | 0.59 | 65% | para-Fe(III) |
| 0.25 | 0.5 | 0.60 | 29% | para-Fe(III) | 1.30 | 0.45 | 2.78 | 12% | para-Fe(II) |
| 1.22 | 0.36 | 1.16 | 4% | para-Fe(III) | 1.27 | 0.37 | 3.11 | 23% | para-Fe(II) |
| 1.42 | 0.43 | 2.34 | 19% | para-Fe(II) |  |  |  |  |  |
| 1.31 | 0.26 | 2.94 | 18% | para-Fe(II) |  |  |  |  |  |
| GreB – T28 (300K – 4 mm s–1) | GreB – T28 (300K – 4 mm s–1) |
| 0.32 | 0.37 | 0.59 | 64% | para-Fe(III) | 0.43 | 0.43 | 0.58 | 45% | para-Fe(III) |
| 1.14 | 0.35 | 2.78 | 26% | para-Fe(II) | 0.39 | 0.42 | 0.67 | 14% | para-Fe(III) |
| 1.12 | 0.22 | 2.97 | 10% | para-Fe(II) | 1.27 | 0.30 | 2.85 | 14% | para-Fe(II) |
|  |  |  |  |  | 1.26 | 0.30 | 3.13 | 27% | para-Fe(II) |

# Figure S20. Mössbauer spectra of pristine and reacted ItaB.

# Table S14. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted ItaB.

| Hyperfine parameters | Attribution | Hyperfine parameters | Attribution |
| --- | --- | --- | --- |
| IS | FW HM | QS or 2ε | Bhf | Area (%) |  | IS | FW HM | QS or 2ε | Bhf | Area (%) |  |
| ItaB – raw (300K – 12 mm s–1) | ItaB – T12 (77K – 12 mm s–1) |
| 0.34 | 0.58 | 0.57 |  | 72% | para-Fe(III) | 0.46 | 0.63 | 0.60 |  | 75% | para-Fe(III) |
| 0.38 | 0.46 | -0.17 | 50.6 | 18% | Hematite | 0.49 | 0.55 | -0.13 | 53.1 | 18% | hematite |
| 0.35 | 0.57 | -0.09 | 47.9 | 10% | Goethite | 0.5 | 0.45 | -0.22 | 50.8 | 7% | goethite |
| ItaB – T31 (300K – 12 mm s–1) | ItaB – T31 (77K – 12 mm s–1) |
| 0.34 | 0.52 | 0.57 |  | 66% | para-Fe(III) | 0.36 | 0.63 | 0.57 |  | 67% | para-Fe(III) |
| 0.33 | 0.36 | -0.2 | 49 | 27% | goe+hem | 0.39 | 0.39 | -0.16 | 50.9 | 12% | hematite |
|  |  |  |  |  |  | 0.34 | 0.74 | 0.02 | 48.3 | 14% | goethite |
| 1.10 | 0.42 | 2.70 |  | 7% | para-Fe(II) | 1.27 | 0.50 | 2.85 |  | 7% | para-Fe(II) |
| ItaB – T32 (300K – 12 mm s–1) | ItaB – T32 (77K – 12 mm s–1) |
| 0.36 | 0.57 | 0.59 |  | 61% | para-Fe(III) | 0.46 | 0.58 | 0.59 |  | 57% | para-Fe(III) |
| 0.38 | 0.44 | -0.10 | 50.7 | 16% | Hematite | 0.48 | 0.48 | -0.09 | 53 | 22% | hematite |
| 0.35 | 0.54 | -0.25 | 47.5 | 9% | Goethite | 0.45 | 0.76 | -0.18 | 49.3 | 7% | goethite |
| 1.16 | 0.52 | 2.68 |  | 14% | para-Fe(II) | 1.27 | 0.46 | 2.97 |  | 14% | para-Fe(II) |

# Figure S21. Mössbauer spectra of pristine and reacted IndB.

# Table S15. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted Indian bentonite Asha.

| Hyperfine parameters | Attribution | Hyperfine parameters | Attribution |
| --- | --- | --- | --- |
| IS | FW HM | QS or 2ε | Area (%) |  | IS | FW HM | QS or 2ε | Bhf | Area (%) |  |
| IndB – raw (300K – 4 mm s–1) | IndB – T12 (77K – 12 mm s–1) |
| 0.36 | 0.67 | 0.57 | 94% | para-Fe(III) | 0.46 | 0.86 | 0.58 |  | 56% | para-Fe(III) |
| 0.41 | 0.36 | 0.52 | 6% | para-Fe(III) |  |  |  |  |  |  |
|  |  |  |  |  | 0.50 | 0.44 | -0.20 | 54.8 | 6% | hematite |
|  |  |  |  |  | 0.48 |  | -0.18 | 47.4 | 38% | goethite |
| IndB – T29 (300K – 4 mm s–1) | IndB – T29 (77K – 12 mm s–1) |
| 0.37 | 0.45 | 0.55 | 80% | para-Fe(III) | 0.46 | 0.52 | 0.5 |  | 41% | para-Fe(III) |
| 0.85 | 0.36 | 1.82 | 5% | para-Fe(III) |  |  |  |  |  |  |
|  |  |  |  |  | 0.46 | 0.49 | -0.07 | 52.7 | 14% | hematite |
|  |  |  |  |  | <0.49> |  | <-0.24> | <47.9> | 32% | goethite |
| 1.13 | 0.38 | 2.78 | 15% | para-Fe(II) | 1.26 | 0.43 | 2.96 |  | 13% | para-Fe(II) |
| IndB – T30 (300K – 4 mm s–1) | IndB – T30 (77K – 12 mm s–1) |
| 0.37 | 0.48 | 0.59 | 73% | para-Fe(III) | 0.43 | 0.57 | 0.56 |  | 40% | para-Fe(III) |
| 0.19 | 0.36 | 2.12 | 2% | para-Fe(III) |  |  |  |  |  |  |
| 0.98 | 0.44 | 1.6 | 6% | para-Fe(III) |  |  |  |  |  |  |
|  |  |  |  |  | 0.47 | 0.48 | -0.13 | 53 | 13% | hematite |
|  |  |  |  |  | <0.49> |  | <-0.26> | <48.2> | 30% | goethite |
| 1.14 | 0.41 | 2.79 | 19% | para-Fe(II) | 1.26 | 0.46 | 2.94 |  | 17% | para-Fe(II) |

# Figure S22. Mössbauer spectra of pristine and reacted CzeB.

# Table S16. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted Czech bentonite Rokle.

| Hyperfine parameters | Attribution | Hyperfine parameters | Attribution |
| --- | --- | --- | --- |
| IS | FW HM | QS or 2ε | Area (%) |  | IS | FW HM | QS or 2ε | Bhf | Area (%) |  |
| CzeB – raw (300K – 4 mm s–1) | CzeB – T12 (77K – 12 mm s–1) |
| 0.37 | 0.65 | 0.51 | 89% | para-Fe(III) | 0.47 | 0.96 | 0.61 |  | 64% | para-Fe(III) |
| 0.41 | 0.36 | 1.30 | 7% | para-Fe(III) | 0.51 | 0.44 | -0.27 | 52.7 | 4% | Hematite |
|  |  |  |  |  | 0.50 |  | -0.18 | 46.1 | 30% | Goethite |
| 1.07 | 0.49 | 2.31 | 4% | para-Fe(II) | 1.23 | 0.44 | 3.05 |  | 2% | para-Fe(II) |
| CzeB – T33 (300K – 4 mm s–1) | CzeB – T33 (77K – 12 mm s–1) |
| 0.38 | 0.51 | 0.56 | 77% | para-Fe(III) | 0.46 | 0.57 | 0.51 |  | 42% | para-Fe(III) |
|  |  |  |  |  | <0.49> |  | <-0.25> | <47.6> | 36% | goe+hem |
| 1.15 | 0.36 | 1.72 | 4% | para-Fe(II) | 1.25 | 0.48 | 2.94 |  | 22% | para-Fe(II) |
| 1.08 | 0.31 | 2.49 | 7% | para-Fe(II) |  |  |  |  |  |  |
| 1.13 | 0.32 | 2.91 | 12% | para-Fe(II) |  |  |  |  |  |  |
| CzeB – T34 (300K – 4 mm s–1) | CzeB – T34 (77K – 12 mm s–1) |
| 0.36 | 0.53 | 0.55 | 73% | para-Fe(III) | 0.46 | 0.55 | 0.52 |  | 41% | para-Fe(III) |
|  |  |  |  |  | <0.49> |  | <-0.23> | <47.9> | 33% | goe+hem |
| 1.31 | 0.34 | 1.43 | 4% | para-Fe(II) | 1.26 | 0.48 | 2.95 |  | 26% | para-Fe(II) |
| 1.23 | 0.34 | 2.13 | 7% | para-Fe(II) |  |  |  |  |  |  |
| 1.16 | 0.34 | 2.81 | 16% | para-Fe(II) |  |  |  |  |  |  |

# Figure S23. Mössbauer spectra of pristine and reacted GeoB.

# Table S17. Refined values of Mössbauer parameters and doublet structural attributions for pristine and reacted Georgian bentonite Be-Ge.

| Hyperfine parameters | Attribution | Hyperfine parameters | Attribution |
| --- | --- | --- | --- |
| IS | FW HM | QS or 2ε | Bhf | Area (%) |  | IS | FW HM | QS or 2ε | Bhf | Area (%) |  |
| GeoB – raw (300K – 12 mm s–1) | GeoB – raw (77K – 12 mm s–1) |
| 0.36 | 0.56 | 0.57 |  | 59% | para-Fe(III) | 0.46 | 0.80 | 0.60 |  | 72% | para-Fe(III) |
| 0.38 | 4.00 | 0.00 |  | 28% | para-Fe(III) | 0.40 | 0.64 | 0.06 | 54.5 | 7% | oxyhydr. |
|  |  |  |  |  |  | 0.51 | 0.36 | -0.22 | 49.5 | 5% | goethite |
| 1.13 | 0.34 | 2.79 |  | 13% | para-Fe(II) | 1.27 | 0.46 | 2.96 |  | 16% | para-Fe(II) |
| GeoB – T43 (300K – 12 mm s–1) | GeoB – T43 (77K – 12 mm s–1) |
| 0.33 | 0.75 | 0.59 |  | 59% | para-Fe(III) | 0.46 | 0.79 | 0.62 |  | 62% | para-Fe(III) |
| 0.31 | 6.00 | 0.00 |  | 10% | para-Fe(III) | 0.49 | 0.70 | 0.20 | 54.4 | 8% | oxyhydr. |
| 0.27 | 0.36 | -0.12 | 50.4 | 4% | oxyhydr. | 0.50 | 0.50 | -0.22 | 49.9 | 4% | goethite |
| 1.16 | 0.49 | 2.75 |  | 27% | para-Fe(II) | 1.27 | 0.38 | 3.02 |  | 26% | para-Fe(II) |
| GeoB – T44 (300K – 12 mm s–1) | GeoB – T44 (77K – 12 mm s–1) |
| 0.35 | 0.61 | 0.56 |  | 52% | para-Fe(III) | 0.48 | 0.66 | 0.57 |  | 46% | para-Fe(III) |
|  |  |  |  |  |  | 0.48 | 0.60 | 0.30 | 54.5 | 6% | oxyhydr. |
| 0.32 | 0.36 | -0.12 | 50.3 | 5% | oxyhydr. | 0.50 | 0.60 | -0.23 | 49.5 | 2% | goethite |
| 1.13 | 0.42 | 2.78 |  | 43% | para-Fe(II) | 1.26 | 0.39 | 3.01 |  | 46% | para-Fe(II) |

# References

Hadi, J., Wersin, P., Jenni, A. & Greneche, J.M. (2017) Redox evolution and Fe-bentonite interaction in the ABM2 experiment, Äspö Hard Rock Laboratory. Pp. 304. Nagra Technischer Bericht, Nagra, Wettingen, Switzerland.

Kiviranta, L., Kumpulainen, S. & Alastalo, S. (2017 (unpublished)) Characterization results of bentonite Be-It-BT0003-Gr-R. Pp.

Kiviranta, L., Kumpulainen, S. & Kanerva, N. (2019) Be-Ge-0001-Gr-R_data sheet (ID 74670). Pp.

Svensson, D. (unpublished) Characterization of refference bentonites and clay materials from SKB collection.

Svensson, D., Dueck, A., Nilsson, U., Olsson, S., Sandén, T., Lydmark, S., Jägerwall, S., Pedersen, K. & Hansen, S. (2011) Alternative buffer material - Status of the ongoing laboratory investigation of reference materials and test package 1. Pp. 140. In SKB, Ed. SKB Technical Reports, 06, SKB, Stockholm, Sweden.