Table S1: Narsarsukite analytical WDS routine and calibration standards. (1): total integration time, equally distributed between peak and background offsets; (*): synthetic

| Elem | Xtal/Spectr line | Counting time1 | Standard |
| --- | --- | --- | --- |
| Si | TAP/ Kα | 10 | Osumilite |
| Ti | LiF/ Kα | 20 | Titanite |
| Zr | PET/Lα | 30 | ZrO2* |
| Al | TAP/ Kα | 20 | Osumilite |
| Fe | LiF/ Kα | 20 | Mn-olivine |
| Mn | LiF/ Kα | 30 | Mn-olivine |
| Mg | TAP/ Kα | 30 | Mn-olivine |
| Ca | PET/ Kα | 30 | Titanite |
| Ba | LiF/ Lα | 30 | BaAl2Si2O8* |
| Na | TAP/ Kα | 10 | Albite |
| K | PET/ Kα | 20 | Microcline |
| Nb | PET/ Lα | 30 | Nb met.* |
| F | TAP/ Kα | 10 | Apatite |