Supplementary Material

For

The influence of metal cations on the dissolution and transformation of biotite

Shoushu Weia, b, c, Qingze Chena, b, c, Lingya Maa, b, c, Xiangwei Zhanga, b, c, Jingming Weia, b, c, Jiaxin Xi a, b, c, Runliang Zhua, b, c, Jianxi Zhua, b, c*, Hongping Hea, b, c

a CAS Key Laboratory of Mineralogy and Metallogeny, Guangdong Provincial Key Laboratory of Mineral Physics and Materials, Guangzhou Institute of Geochemistry, Chinese Academy of Sciences, Guangzhou 510640, China

b CAS Center for Excellence in Deep Earth Science, Guangzhou 510640, China

c University of Chinese Academy of Sciences, Beijing 100049, China

* Corresponding author

E-mail: zhujx@gig.ac.cn

Figure S1. Magnified XRD pattern of the product from biotite in the blank system after 90 d (Bt-H-90d). At least seven typical reflections suggestive of kaolinite were observed in the XRD pattern, despite the presence of some relatively weak reflections.

Figure S2. FTIR spectrum of the product from biotite in the blank system after 90 d (Bt-H-90d).

Figure S3. The morphology and composition of the original Bt. TEM images (a), HAADF image and EDS mapping (b), and EDS patterns (c).

Figure S4. TEM image (a), HAADF image (b), EDS mapping (c, e, and f), and EDS pattern (d) of Bt-Al-90d.

Figure S5. Schematic diagram showing the influence of various metal cations on the transformation process of biotite.

Table S1. Ionic radii, hydrated ionic radii, charge-to-radius (Z2/r) values, and hydration enthalpies of various cations.

|  | Na+ | K+ | Mg2+ | Ca2+ | Al3+ |
| --- | --- | --- | --- | --- | --- |
| Ionic radius (Å) | 0.97 | 1.33 | 0.66 | 0.99 | 0.53 |
| Hydrated ionic radius (Å) | 3.58 | 3.31 | 4.28 | 4.12 | 4.75 |
| Z2/r value (1/nm) | 9.35 | 6.99 | 61.54 | 36.70 | 147.54 |
| hydration enthalpy (kJ/mol) | -398 | -338 | -1820 | -1580 | -4468 |

Compiled from Refs. (Nightingale Jr, 1959; Tansel, 2012; Volkov and Deamer, 2020).

Table S2. Chemical composition of the original Bt in this work (wt.%).

|  | SiO2 | Al2O3 | MgO | Fe2O3 | K2O | TiO2 | Na2O | CaO | MnO | F | L. O. I.a |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bt | 37.87 | 16.54 | 15.55 | 15.33 | 8.83 | 1.73 | 0.26 | 0.29 | 0.15 | 0.5 | 1.87 |

a Loss on ignition.

Table S3. The solution pH values of different cation systems after 30 d of biotite dissolution experiments with an initial pH of 2.

|  | Control experiment | K system | Na system | Mg system | Ca system | Al system |
| --- | --- | --- | --- | --- | --- | --- |
| pH | 2.53 | 2.30 | 3.53 | 3.55 | 3.94 | 2.63 |

Table S4. Positions and assignments of the FTIR vibrational bands for the samples.

| Wavenumber (cm−1) | Assignments |
| --- | --- |
| 3698, 3670, 3649, 3620 | Al–OH stretching vibration of kaolinite |
| 3561 | Mg–OH stretching vibration of chlorite |
| 3445 | Stretching vibration of interlayer water |
| 1109~1001 | Si–O stretching vibration |
| 913 | Al–OH bending vibration |
| 790, 754, 699 | Si–O–Si(AlVI) stretching vibration of kaolinite |
| 707, 684 | Stretching vibrations of Si(AlIV)–O and Si–O–Si(AlIV) of biotite |
| 538 | Si–O–AlⅥ bending vibration |
| 470, 432 | Si–O bending vibration, Al–O bending vibration, OH translation |

Table S5. Mössbauer parameters of the original biotite and the products in the various cation systems.

|  | ISa (mm/s) | QSb (mm/s) | BHFc (T) | Area ratio (%) | Assignments |
| --- | --- | --- | --- | --- | --- |
| Bt | 1.09 | 2.15 | - | 24.23 | Fe2+M1 |
|  | 1.12 | 2.60 | - | 38.71 | Fe2+M2 |
|  | 0.36 | 0.87 | - | 37.06 | Fe3+M1+M2 |
| Bt-H-90d | 1.15 | 2.24 | - | 5.03 | Fe2+M1+M2 |
|  | 0.35 | 0.87 | - | 29.03 | Fe3+M1+M2 |
|  | 0.37 | −0.19 | 47.50 | 65.94 | Hematite |
| Bt-K-90d | 1.10 | 2.47 |  | 61.36 | Fe2+M1+M2 |
|  | 0.41 | 0.82 |  | 38.64 | Fe3+M1+M2 |
| Bt-Na-90d | 1.14 | 2.33 | - | 13.57 | Fe2+M1+M2 |
|  | 0.35 | 0.94 | - | 56.33 | Fe3+M1+M2 |
|  | 0.35 | −0.17 | 48.53 | 30.10 | Hematite |
| Bt-Mg-90d | 1.14 | 2.22 | - | 15.87 | Fe2+M1+M2 |
|  | 0.34 | 0.93 | - | 58.18 | Fe3+M1+M2 |
|  | 0.41 | −0.22 | 47.93 | 25.96 | Hematite |
| Bt-Ca-90d | 1.20 | 2.32 | - | 18.32 | Fe2+M1+M2 |
|  | 0.34 | 0.93 | - | 61.28 | Fe3+M1+M2 |
|  | 0.38 | −0.23 | 46.77 | 20.40 | Hematite |
| Bt-Al-90d | 0.34 | 0.82 |  | 23.53 | Fe3+M1+M2 |
|  | 0.38 | −0.20 | 50.49 | 76.47 | Hematite |

a Isomer shift, b Quadrupole splitting, c Magnetic hyperfine field.

References:

Nightingale Jr, E. (1959) Phenomenological theory of ion solvation. Effective radii of hydrated ions. The Journal of Physical Chemistry, 63, 1381-1387.

Tansel, B. (2012) Significance of thermodynamic and physical characteristics on permeation of ions during membrane separation: Hydrated radius, hydration free energy and viscous effects. Separation and Purification Technology, 86, 119-126.

Volkov, A.G. and Deamer, D.W. (2020) Liquid-liquid interfaces theory and methods. CRC press.