Table 1

The speciﬁc capacitance of the composite at given cycle and retention rate .

| Sample | 1 st cycle(F/g) | 10 thcycle(F/g) | 100 thcycle(F/g) | 800 thcycle(F/g) | 1000 thcycle(F/g) | Capacitance retention rate (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Composite | 75.8 | 75.7 | 66.7 | 66.7 | 66.7 | 88% |