Suplemental Table 1. Synthesis of the results.

|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **S** | **Site** | **Sherd** | **Ceramic type** | **Form** | **Surface treatment** | **Plastic technique** | **Plastic design** | **Fabric** |
| 1 | Bordo Marcial | C206-182 | Ordinario Alisado | OL5 | Smoothing | - | - | F |
| 2 | Bordo Marcial | C206-3 | Ordinario Alisado | OL5 | Smoothing | - | - | GGC |
| 3 | Bordo Marcial | C651-5 | Gris Pulido | CU2 | Polishing (Pu2) | - | - | MF |
| 4 | Bordo Marcial | C655-20 | Ordinario Alisado | CU2 | Smoothing | - | - | GGC |
| 5 | Bordo Marcial | C659-1 | Gris Pulido | JA2 | Polishing (Pu1) | - | - | MMCST |
| 6 | Bordo Marcial | C678-37 | Gris Pulido | CU6 | Polishing (Pu2) | - | - | GGC |
| 7 | Bordo Marcial | C654-T1 | Gris Pulido | CU6 | Polishing (Pu2) | - | - | GV |
| 8 | Bordo Marcial | C668-T5 | Gris Pulido | OL2 | Polishing (Pu2) | - | - | F |
| 9 | Bordo Marcial | C653-32 | Ante Pulido | VA1/JO1 | Polishing (Pu2) | - | - | MF |
| 10 | Bordo Marcial | C866-T1 | Gris Pulido | JA2 | Polishing (Pu2) | - | - | GGCM |
| 11 | Bordo Marcial | C660-T4 | Ante Pulido | JA2 | Polishing (Pu1) | - | - | GGC |
| 12 | Bordo Marcial | C653-30 | Ordinario Alisado | OL2 | Smoothing | - | - | GGC |
| 13 | Bordo Marcial | C674-T1 | Ante Pulido | OL1 | Polishing (Pu1) | Appliqué | Anthropomorphic face | GGC |
| 14 | Bordo Marcial | C650-T4a | Gris Pulido | CU2 | Polishing (Pu2) | - | - | FSA |
| 15 | Bordo Marcial | C659-T2 | Río Diablo | JA3 | Polishing (Pu2) | Incising | Geometric. Lines and dots | MCG |
| 16 | Bordo Marcial | C213-T3 | Rojo Pulido | JAD1 | Polishing (Pu2), Painting (red) | - | - | F |
| 17 | Bordo Marcial | C682-T3 | Gris Inciso | CA1 | Polishing (Pu2) | Incising | Geometric. Lines and dots | FSA |
| 18 | Bordo Marcial | C650-T2 | Ordinario Alisado | JA1 | Smoothing | - | - | GGC |
| 19 | Bordo Marcial | C208-T8 | Ordinario Rojo | Restricted | Smoothing, Slip (red) | Appliqué/ Incising | Cut strip | GGC |
| 20 | Bordo Marcial | C212-T1 | Gris Pulido | ¿CU2? | Polishing (Pu1) | Incising | Short lines | GGCM |
| 21 | Bordo Marcial | C161-1 | Vaquerías | ¿CU6? | Polishing (Pu2) | Painting | Geometric. Lines and dots | MMC |
| 22 | Bordo Marcial | C217-5 | Vaquerías | Restricted | Polishing (Pu2), Slip | Painting | Geometric. Lines | MMC |
| 23 | Bordo Marcial | C206-T2 | Vaquerías | ¿Restricted? | Polishing (Pu2), Slip | Painting | Geometric. Lines and figures | MMC |
| 24 | Bordo Marcial | C217-1 | Vaquerías | Restricted | Polishing (Pu2) | Painting | Geometric. Lines and figures | MMC |
| 25 | Bordo Marcial | C217-6 | Vaquerías | Open | Polishing (Pu2) | Painting | Geometric. Lines and figures | MCG |
| 26 | Bordo Marcial | C653-5 | Vaquerías | ¿Open? | Polishing (Pu2), Slip | Painting | Geometric. Lines | MMC |
| 27 | Bordo Marcial | C650-T1 | Vaquerías | ¿Restricted? | Polishing (Pu2), Slip | Painting | Geometric. Lines | MMC |
| 28 | Bordo Marcial | C206-181 | Vaquerías | Restricted | Polishing (Pu2), Slip | Painting | Geometric. Lines and figures | MCG |
| 29 | Bordo Marcial | C654-T2 | Vaquerías | Open | Polishing (Pu2), Slip | Painting | Geometric. Lines and figures | MMC |
| 30 | Bordo Marcial | C217-10 | Vaquerías | ¿Restricted? | Polishing (Pu2) | Painting | Geometric. Lines | MMC |
| 31 | Cardonal | C246-23 | Ante Pulido | OL2 | Polishing (Pu2) | - | - | FSA |
| 32 | Cardonal | C253-3 | Ordinario Rojo | CA1 | Polishing (Pu1), Slip (red) | **-** |  | MISG |
| 33 | Cardonal | C230-7 | Ante Pulido | OL6 | Polishing (Pu2) | - | - | F |
| 34 | Cardonal | C246-14 | Gris Pulido | CU2 | Polishing (Pu2) | Appliqué/Incising | Ornithomorph | F |
| 35 | Cardonal | C495-12 | Gris Pulido | JO1/VA1 | Polishing (Pu2) | - | - | MCG |
| 36 | Cardonal | C517-T7b | Ordinario Alisado | OL6 | Smoothing | - | - | GGC |
| 37 | Cardonal | C495-40 | Ordinario Alisado | OL6 | Smoothing | - | - | GGCM |
| 38 | Cardonal | C65-T32 | Ordinario Alisado | CA1 | Smoothing | - | - | GGCM |
| 39 | Cardonal | C70-T10 | Gris Pulido | CU2 | Polishing (Pu2) | - | - | FSA |
| 40 | Cardonal | C10-T70 | Ordinario Pulido | CA1 | Polishing (Pu2) |  |  | MISG |
| 41 | Cardonal | C54-T21 | Ante Pulido | JA u OL | Polishing (Pu2) | Appliqué/Incising | Ornithomorph | FSA |
| 42 | Cardonal | C70-T4 | Gris Inciso | VE | Polishing (Pu2) | Modelling/Incising | Zoomorph. *Quirquincho* | FSA |
| 43 | Cardonal | C70-T7 | Ordinario Alisado | OL5 | Smoothing | - | - | GGC |
| 44 | Cardonal | C27-T73 | Ordinario Rojo | CA1 | Smoothing, Slip (red) | - | - | GGCM |
| 45 | Cardonal | C44-T35 | Ordinario Alisado | OL6 | Smoothing | - | - | GGCM |
| 46 | Cardonal | C128-T12 | Ordinario Pulido | JA1 | Polishing (Pu2) | Appliqué | Zoomorphic head | GPMM |
| 47 | Cardonal | C139-T21 | Ordinario Alisado | OC | Smoothing | - | - | GGC |
| 48 | Cardonal | C145-T8 | Ordinario Alisado | OL5 | Smoothing | - | - | GGC |
| 49 | Cardonal | C193-T1 | Ante Pulido | OL5 | Polishing (Pu2) | - | - | MCG |
| 50 | Cardonal | C191-T2 | Gris Pulido | JA1 | Polishing (Pu2) | - | - | MMCST |
| 51 | Cardonal | C396-T1 | Ante Pulido | OL2 | Polishing (Pu2) | - | - | F |
| 52 | Cardonal | C399-T1 | Gris Inciso | JA1 | Polishing (Pu2) | Incising | Concentric circles | FD |
| 53 | Cardonal | C368-2 | Gris Pulido | CU1 | Polishing (Pu2) | - | - | GGC |
| 54 | Cardonal | C281-T6 | Gris Pulido | CU1 | Polishing (Pu1) | Appliqué/Incising | Ornithomorph | MCG |
| 55 | Cardonal | C426-1 | Gris Pulido | CU4 | Polishing (Pu2) | - | - | FD |
| 56 | Cardonal | C313-1 | Gris Pulido | JA1 | Polishing (Pu2) | - | - | MF |
| 57 | Cardonal | C340-T23 | Gris Pulido | CU2 | Polishing (Pu2) | - | - | F |
| 58 | Cardonal | C431-T3 | Gris Pulido | JO1/JA2 | Polishing (Pu2) | - | - | MCG |
| 59 | Cardonal | C412-T12 | Gris Pulido | JA1 | Polishing (Pu1) | - | - | GGCM |
| 60 | Cardonal | C416-4 | Ante Pulido | JA1 | Polishing (Pu2) | - | - | GGCM |
| 61 | Cardonal | C400-T2 | Gris Pulido | JO1 | Polishing (Pu2) | - | - | GGCM |
| 62 | Cardonal | C386-T6 | Ordinario Alisado | OL5 | Smoothing | - | - | GGC |
| 63 | Cardonal | C347-T2 | Ordinario Alisado | OL6 | Smoothing | - | - | GGC |
| 64 | Cardonal | C391-T9c | Ordinario Alisado | CA1 | Smoothing | - | - | GGC |
| 65 | Cardonal | C380-T3 | Ordinario Alisado | OL6 | Smoothing | - | - | GGCM |
| 66 | Cardonal | C388-T8 | Ordinario Alisado | OL5 | Smoothing | - | - | GGCM |
| 67 | Cardonal | C400-T3 | Ordinario Alisado | OL5 | Smoothing | - | - | GGC |
| 68 | Cardonal | C400-T1 | Ordinario Alisado | JA2 | Smoothing | - | - | GGC |
| 69 | Cardonal | C381-T8 | Ordinario Alisado | OL5 | Smoothing | - | - | GGC |
| 70 | Cardonal | C330-15 | Ordinario Alisado | OL5 | Smoothing | - | - | GGC |
| 71 | Cardonal | C321-T4 | Ordinario Alisado | OL1 | Smoothing | Appliqué | Anthropomorphic face | GGC |
| 72 | Cardonal | C1220-T1 | Ordinario Alisado | OL6 | Smoothing | - | - | GGC |
| 73 | Cardonal | C1221-T10B | Ordinario Alisado | JA1 | Smoothing | - | - | GGC |
| 74 | Cardonal | C290-7 | Ordinario Alisado | JA1 | Smoothing | - | - | GGC |
| 75 | Cardonal | C242-HE8-1 | Gris Inciso | Restricted | Polishing (Pu2) | Incising | Geometric. Lines | MCG |
| 76 | Cardonal | Laz084 | Rojo sobre Ante | Restricted | Polishing (Pu2) | Painting | Geometric. Lines | GM |
| 77 | Cardonal | C70-3 | Ordinario Pintado | Restricted | Smoothing | Painting | Geometric. Lines | GGCM |
| 78 | Cardonal | C36-T19 | Ordinario Inciso | Restricted | Smoothing | Incising | Geometric. Lines | GGCM |
| 79 | Cardonal | C46-T6 | Ordinario Pulido | Restricted | Polishing (Pu1) | - | - | MCG |
| 80 | Cardonal | C322-T18 | Río Diablo | Restricted | Polishing (Pu2) | Incising | Geometric. Lines and dots | MCG |
| 81 | Cardonal | C113-T22 | Ordinario Rojo | Restricted | Smoothing, Slip (red) | - | - | GGC |
| 82 | Cardonal | C419-1 | Rojo Pulido | Restricted | Polishing (Pu2), Painting (red) | - | - | FD |
| 83 | Cardonal | Laz454 | Condorhuasi Rojo sobre Ante | Restricted | Polishing (Pu2), | Painting | Geometric. Lines | FVV |
| 84 | Cardonal | C75-38 | Vaquerías | Open | Polishing (Pu2) | Painting | Geometric. Lines | MMC |
| 85 | Cardonal | C26-T45 | Vaquerías | Open | Polishing (Pu2), Slip | Painting | Geometric. Lines and figures | MMC |
| 86 | Cardonal | C84-T3 | Vaquerías | ¿Open? | Polishing (Pu2) | Painting | Geometric. Lines | MMC |
| 87 | Cardonal | C80-9 | Vaquerías | Open | Polishing (Pu2), Slip | Painting | Geometric. Lines and figures | MCM |
| 88 | Cardonal | C250-3 | Vaquerías | Restricted | Polishing (Pu2), Slip | Painting | Geometric. Lines and figures | MMC |
| 89 | Cardonal | C274-T1 | Vaquerías | Open | Polishing (Pu2) | Painting | Geometric. Lines | MCG |
| 90 | Cardonal | C255-H1 | Vaquerías | Restricted | Polishing (Pu2), Slip | Painting | Geometric. Lines and figures | MMC |
| 91 | Cardonal | C271-T1 | Vaquerías | Restricted | Polishing (Pu2), Slip | Painting | Geometric. Lines and figures | MCM |
| 92 | Cardonal | V31 | Vaquerías | ¿Open? | Polishing (Pu2), Slip | Painting | Geometric. Lines and figures | MMC |
| 93 | Cardonal | C260-3 | Vaquerías | Open | Polishing (Pu2) | Painting | Geometric. Lines | MCG |
| 94 | Cardonal | C241-104 | Vaquerías | Restricted | Polishing (Pu2), Slip | Painting | Geometric. Lines | MMC |
| 95 | Cardonal | C242-11 | Vaquerías | Restricted | Polishing (Pu2) | Painting | Geometric. Lines | MTM |
| 96 | Cardonal | C259-38 | Vaquerías | Open | Polishing (Pu2) | Painting | Geometric. Lines | MMC |
| 97 | Cardonal | C259-7 | Vaquerías | Restricted | Polishing (Pu2), Slip | Painting | Geometric. Lines and figures | MMC |
| 98 | Cardonal | Laz083 | Vaquerías | Open | Polishing (Pu2) | Painting | Geometric. Lines | MMC |