Supplementary Material

The goddess’ new clothes: the carving and polychromy of the Parthenon Sculptures

Giovanni Verri1,*, Hero Granger-Taylor2, Ian Jenkins3, Tracey Sweek3, Katarzyna Weglowska3 & William Thomas Wootton4,*
1 Art Institute of Chicago, Illinois, US

2 Independent scholar, London, UK

3 British Museum, London, UK

4 King’s College, London, UK
* Authors for correspondence ✉ gverri@artic.edu; will.wootton@kcl.ac.uk

Received: 29 January 2022; Revised: 19 November 2022; Accepted: 24 November 2022

Table S1: Areas where evidence for carving and colour was revealed: East Pediment (EP); West Pediment (WP); East Frieze (EF)). Unless otherwise indicated, the identification of Egyptian blue was undertaken using VIL imaging and confirmed in select cases with Raman and SEM-EDX analysis. SEM-EDX and Raman analysis were performed on microscopic samples (<0.5mm diameter) collected from the surface of the sculpture, as indicated. The sample locations, marked by a white arrow, are in the corresponding figures as indicated in the table.

| Figure | Location | Toolmarks | Blue | White | Purple | Degradation products |
| --- | --- | --- | --- | --- | --- | --- |
| EP A (Helios) and B (Horses) | Sea | Claw chisel Rasp Polishing | Egyptian blue - VIL |  |  |  |
| EP E (Demeter?) and F (Persephone?) | ‘Empty space’ below seat | Point chisel Drill | Egyptian blue - VIL |  |  |  |
| EP G (Hebe?) | ‘Empty space’ underneath dress | Point chisel | Egyptian blue - VIL |  |  |  |
| EP K (Hestia?) | Decorative element on dress |  | Egyptian blue - VIL |  |  |  |
| EP L and M (see Figure 7 for sampling location) | Decorative element on EP L’s dress and spread over rock by EP L’s feet | Claw chisel Drill Flat chisel and channelling tool Rasp | Egyptian blue - VIL - Raman: 1085, 571, 430cm-1 - SEM-EDX: Cu, Si, Ca, Na | Calcium phosphate (mixed with Egyptian blue) - Raman: 963cm-1 - SEM-EDX: Ca, P |  | Calcium oxalate Superficial layer - Raman: 1472, 910, 506, 495cm-1 - SEM-EDX: Ca with Fe impurities |
| EP L (Dione?) and M (Aphrodite?) | Decorative element at the intersection between dress of EP M and spread | Claw chisel Drill Flat chisel and channelling tool Rasp |  |  | Unknown compound likely including an anthraquinone - FORS: c. 528, 570nm - XRF: Ca, Fe |  |
| WP B (Kekrops?) | Snake skin | Point chisel Claw chisel | Egyptian blue - VIL |  |  |  |
| WP N (Iris?) (see Figure 9 for sampling location) | Belt | Point chisel | Egyptian blue - VIL - Raman: 1085, 571, 430cm-1 - SEM-EDX: Cu, Si, Ca, Na | Calcium sulphate (mixed with Egyptian blue) - Raman: 412, 491, 1005, 1135cm-1 - SEM-EDX: Ca, S |  |  |
| WP T (Kreusa?) | Decorative element on textile and surface of rock |  | Egyptian blue - VIL |  |  |  |
| EF Block V, Figure 32 (see Figure 10 for sampling location) | Dress |  | Egyptian blue - VIL - Raman: 1085, 571, 430cm-1 - SEM-EDX: Cu, Si, Ca, Na | Calcium phosphate (mixed with Egyptian blue) - Raman: 963cm-1 - SEM-EDX: Ca, P |  |  |

Supplementary figures

Figure S1. Figure EP L. Visible and VIL images of the side.

Figure S2. Figure EP L. Visible, VIL details and line drawing of the ‘leg’.

Figure S3. Figure EP L. Visible, VIL details and line drawing of the ‘hand’.

Figure S4. Figure EP L. Visible, VIL details and line drawing of the ‘foot’.

Figure S5. Figure EP L. (Left) Detail of EP L’s shin, showing fragmentary Egyptian blue under the orange calcium oxalate layer. The orange layer is likely the result of natural degradation processes. (Right) Cross-section from the location indicated in Figure 7, showing Egyptian blue particles in a calcium phosphate matrix. The blue paint layer is applied above a calcium phosphate layer and under the orange calcium oxalate layer.