Weathering evolution in lutites of the K/Pg transitioned red beds of the Tremp Group (Tremp-Isona Basin, south Pyrenees)

J. BASTIDA, R. LINARES, A.M. LÓPEZ BUENDÍA, M.C. OSÁCAR, J. ROSELL AND M. ZARROCA

DOI: 10.1180/claymin.2017.052.1.08

Table 1. Mineralogical composition.

| REF | UNs | UNI | FAC | LIT | SEC | SS | Q | F | C | D | Py | He | Gy | Si | K | I | Ch | Sm | Kf1 | If1 | Chf1 | Smf1 | I + Ch f1 | C6N | (I + Ch)/(K + S) | S/K |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| G1 | 2 | 2 | 2 | 2 | 16 | 58 | 20 | 2.3 | 19 | 0.7 | 0.0 | 0.0 | 0 | 0.9 | 8 | 44 | 6 | 0.9 | 14 | 75 | 10 | 2 | 85 | 1 | 5.6 | 0.12 |
| G2 | 2 | 2 | 2 | 2 | 9 | 61 | 8 | 0.8 | 30 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 14 | 42 | 5 | 0.7 | 22 | 69 | 7 | 1 | 77 | 1 | 3.3 | 0.05 |
| G3 | 2 | 2 | 2 | 2 | 9 | 46 | 15 | 0.0 | 38 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 9 | 29 | 7 | 1.0 | 20 | 64 | 14 | 2 | 78 | 1 | 3.5 | 0.10 |
| G4 | 2 | 2 | 2 | 2 | 9 | 63 | 10 | 0.6 | 26 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 11 | 27 | 20 | 5.6 | 18 | 42 | 31 | 9 | 74 | 2 | 2.8 | 0.50 |
| G7 | 1 | 1 | 1 | 1 | 8 | 38 | 32 | 0.0 | 30 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 0 | 34 | 3 | 1.5 | 0 | 88 | 8 | 4 | 96 | 1 | 24.4 |  |
| G8 | 2 | 2 | 2 | 2 | 8 | 51 | 10 | 1.0 | 37 | 0.0 | 0.0 | 0.2 | 0 | 0.0 | 9 | 31 | 11 | 0.0 | 17 | 60 | 22 | 0 | 83 | 1 | 4.7 | 0.00 |
| G9 | 2 | 2 | 2 | 2 | 8 | 26 | 22 | 1.1 | 50 | 0.0 | 0.0 | 0.3 | 0 | 0.0 | 5 | 18 | 0 | 2.8 | 20 | 70 | 0 | 11 | 70 | 1 | 2.3 | 0.53 |
| G10 | 3 | 3 | 2 | 4 | 8 | 55 | 12 | 0.4 | 32 | 0.5 | 0.0 | 0.0 | 0 | 0.0 | 11 | 33 | 8 | 2.3 | 21 | 60 | 15 | 4 | 75 | 1 | 3.0 | 0.20 |
| G11 | 3 | 3 | 2 | 2 | 8 | 31 | 20 | 0.3 | 48 | 0.0 | 0.0 | 0.9 | 0 | 0.0 | 6 | 12 | 10 | 2.4 | 19 | 40 | 34 | 8 | 74 | 3 | 2.8 | 0.41 |
| G12 | 1 | 1 | 1 | 1 | 13 | 26 | 5 | 0.4 | 68 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 1 | 23 | 2 | 0.0 | 4 | 87 | 9 | 0 | 96 | 1 | 24.7 | 0.00 |
| G13 | 2 | 2 | 2 | 2 | 13 | 24 | 14 | 0.4 | 61 | 0.0 | 0.8 | 0.0 | 0 | 0.0 | 11 | 11 | 2 | 0.5 | 45 | 44 | 9 | 2 | 53 | 3 | 1.1 | 0.05 |
| G14 | 2 | 2 | 2 | 6 | 13 | 47 | 7 | 0.0 | 45 | 0.0 | 0.0 | 0.6 | 0 | 0.0 | 21 | 21 | 5 | 1.1 | 44 | 44 | 10 | 2 | 54 | 3 | 1.2 | 0.05 |
| G15 | 2 | 2 | 2 | 1 | 13 | 51 | 9 | 0.7 | 39 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 18 | 24 | 8 | 0.7 | 35 | 47 | 16 | 1 | 63 | 3 | 1.7 | 0.04 |
| G16 | 2 | 2 | 2 | 6 | 13 | 42 | 19 | 0.4 | 38 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 37 | 50 | 10 | 2.0 | 16 | 21 | 4 | 1 | 61 | 2 | 1.6 | 0.05 |
| G17 | 2 | 2 | 2 | 6 | 13 | 71 | 27 | 1.6 | 0 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 29 | 27 | 13 | 1.5 | 41 | 39 | 18 | 2 | 57 | 2 | 1.3 | 0.05 |
| G18 | 2 | 2 | 2 | 6 | 13 | 24 | 12 | 0.4 | 63 | 0.0 | 0.0 | 0.9 | 0 | 0.0 | 9 | 12 | 3 | 0.0 | 39 | 49 | 12 | 0 | 61 | 3 | 1.6 | 0.00 |
| G19 | 2 | 2 | 2 | 2 | 13 | 58 | 40 | 1.2 | 0 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 28 | 21 | 10 | 0.0 | 47 | 36 | 16 | 0 | 53 | 2 | 1.1 | 0.00 |
| G 20 | 2 | 2 | 2 | 2 | 1 | 45 | 19 | 1.7 | 34 | 0.0 | 0.0 | 0.9 | 0 | 0.0 | 10 | 18 | 11 | 5.2 | 23 | 39 | 25 | 12 | 65 | 3 | 1.8 | 0.50 |
| G 21 | 2 | 2 | 2 | 2 | 1 | 40 | 21 | 0.6 | 38 | 0.0 | 0.0 | 0.9 | 0 | 0.0 | 9 | 16 | 11 | 5.3 | 21 | 39 | 27 | 13 | 66 | 3 | 1.9 | 0.62 |
| G 22 | 3 | 3 | 2 | 3 | 1 | 57 | 10 | 0.9 | 32 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 13 | 25 | 14 | 3.9 | 24 | 44 | 25 | 7 | 70 | 2 | 2.3 | 0.29 |
| G 23 | 3 | 3 | 2 | 2 | 1 | 56 | 12 | 0.7 | 31 | 0.0 | 0.0 | 0.5 | 0 | 0.0 | 11 | 8 | 18 | 18.3 | 20 | 15 | 33 | 33 | 48 | 3 | 0.9 | 1.67 |
| G 24 | 3 | 3 | 2 | 2 | 1 | 54 | 14 | 0.8 | 31 | 0.0 | 0.0 | 0.9 | 0 | 0.0 | 6 | 30 | 14 | 2.9 | 11 | 56 | 27 | 5 | 83 | 1 | 5.0 | 0.47 |
| G 25 | 3 | 3 | 2 | 2 | 1 | 38 | 12 | 0.8 | 49 | 0.0 | 0.0 | 0.8 | 0 | 0.0 | 10 | 14 | 7 | 7.3 | 26 | 36 | 19 | 19 | 55 | 3 | 1.2 | 0.74 |
| G 26 | 3 | 3 | 2 | 2 | 1 | 33 | 12 | 0.6 | 54 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 8 | 11 | 8 | 5.5 | 25 | 35 | 23 | 17 | 58 | 3 | 1.4 | 0.67 |
| G 27 | 3 | 3 | 2 | 2 | 1 | 89 | 16 | 4.8 | 25 | 0.0 | 0.0 | 1.2 | 0 | 0.0 | 12 | 18 | 14 | 45.0 | 13 | 21 | 15 | 51 | 36 | 4 | 0.6 | 3.77 |
| G28 | 2 | 2 | 2 | 2 | 7 | 22 | 20 | 1.5 | 57 | 0.0 | 0.3 | 0.0 | 0 | 0.0 | 5 | 11 | 5 | 1.7 | 22 | 48 | 22 | 8 | 71 | 3 | 2.4 | 0.35 |
| G29 | 2 | 2 | 2 | 3 | 7 | 45 | 17 | 1.1 | 35 | 0.8 | 1.1 | 0.0 | 0 | 0.0 | 11 | 20 | 12 | 1.8 | 23 | 45 | 27 | 4 | 73 | 3 | 2.7 | 0.17 |
| G30 | 2 | 2 | 2 | 2 | 7 | 57 | 17 | 0.0 | 25 | 0.4 | 0.6 | 0.2 | 0 | 0.0 | 18 | 33 | 0 | 5.8 | 31 | 58 | 0 | 10 | 58 | 2 | 1.4 | 0.32 |
| G31 | 3 | 3 | 2 | 4 | 7 | 22 | 35 | 0.2 | 3 | 2.4 | 0.0 | 2.2 | 34 | 0.0 | 6 | 5 | 7 | 4.7 | 26 | 22 | 31 | 21 | 53 | 5 | 1.1 | 0.82 |
| G32 | 3 | 3 | 2 | 4 | 7 | 18 | 43 | 0.0 | 14 | 3.0 | 0.0 | 2.1 | 19 | 0.0 | 5 | 3 | 2 | 8.0 | 26 | 16 | 13 | 44 | 30 | 5 | 0.4 | 1.71 |
| G33 | 3 | 3 | 2 | 4 | 7 | 74 | 8 | 0.4 | 6 | 0.0 | 0.0 | 0.1 | 11 | 0.0 | 16 | 32 | 18 | 7.4 | 22 | 43 | 25 | 10 | 68 | 2 | 2.1 | 0.45 |
| G34 | 3 | 3 | 2 | 3 | 7 | 35 | 25 | 1.5 | 36 | 0.0 | 0.2 | 1.3 | 0 | 0.0 | 11 | 14 | 7 | 4.0 | 30 | 39 | 19 | 11 | 58 | 3 | 1.4 | 0.38 |
| G38 | 3 | 3 | 2 | 2 | 7 | 52 | 14 | 0.0 | 42 | 0.0 | 0.0 | 0.1 | 0 | 0.0 | 21 | 13 | 9 | 8.9 | 41 | 26 | 17 | 17 | 42 | 6 | 0.7 | 0.42 |
| G41 | 3 | 3 | 2 | 2 | 12 | 58 | 21 | 0.0 | 42 | 0.3 | 0.1 | 0.4 | 0 | 0.0 | 10 | 9 | 0 | 38.7 | 18 | 15 | 0 | 67 | 15 | 4 | 0.2 | 3.70 |
| G42 | 3 | 3 | 2 | 2 | 12 | 61 | 21 | 0.2 | 17 | 0.1 | 0.0 | 0.3 | 0 | 0.0 | 23 | 28 | 5 | 4.5 | 38 | 47 | 8 | 7 | 55 | 2 | 1.2 | 0.20 |
| G43 | 3 | 3 | 2 | 2 | 12 | 30 | 21 | 0.1 | 47 | 0.5 | 0.2 | 0.4 | 0 | 0.0 | 13 | 13 | 5 | 0.0 | 42 | 43 | 15 | 0 | 58 | 3 | 1.4 | 0.00 |
| G44 | 3 | 3 | 2 | 2 | 12 | 53 | 17 | 1.2 | 28 | 0.0 | 0.0 | 0.5 | 0 | 0.0 | 21 | 23 | 7 | 1.7 | 40 | 43 | 14 | 3 | 57 | 2 | 1.3 | 0.08 |
| G45 | 3 | 3 | 2 | 2 | 12 | 31 | 20 | 1.4 | 46 | 0.5 | 0.3 | 0.2 | 0 | 0.0 | 12 | 16 | 3 | 0.8 | 37 | 52 | 8 | 3 | 60 | 3 | 1.5 | 0.07 |
| G46 | 3 | 3 | 2 | 2 | 12 | 31 | 22 | 1.2 | 45 | 0.5 | 0.2 | 0.2 | 0 | 0.0 | 11 | 36 | 14 | 3.5 | 17 | 56 | 21 | 5 | 77 | 1 | 3.4 | 0.32 |
| G47 | 3 | 3 | 2 | 2 | 12 | 30 | 21 | 0.1 | 47 | 0.5 | 0.2 | 0.4 | 0 | 0.0 | 11 | 13 | 5 | 1.1 | 38 | 43 | 16 | 4 | 59 | 3 | 1.4 | 0.10 |
| G48 | 3 | 3 | 2 | 4 | 12 | 53 | 17 | 1.2 | 28 | 0.0 | 0.0 | 0.5 | 0 | 0.0 | 7 | 40 | 6 | 0.0 | 13 | 76 | 11 | 0 | 87 | 1 | 6.7 | 0.00 |
| G49 | 3 | 3 | 2 | 4 | 12 | 61 | 20 | 0.2 | 17 | 0.4 | 0.4 | 0.2 | 0 | 0.0 | 22 | 27 | 4 | 7.3 | 37 | 45 | 6 | 12 | 51 | 2 | 1.1 | 0.33 |
| G50 | 45 | 5 | 3 | 1 | 12 | 61 | 17 | 0.4 | 18 | 0.4 | 0.5 | 0.3 | 0 | 0.0 | 5 | 45 | 10 | 0.7 | 9 | 73 | 17 | 1 | 90 | 1 | 9.2 | 0.12 |
| G51 | 2 | 2 | 2 | 2 | 6 | 44 | 19 | 0.3 | 36 | 0.7 | 0.3 | 0.0 | 0 | 0.0 | 8 | 29 | 7 | 0.5 | 18 | 65 | 16 | 1 | 90 | 1 | 4.2 | 0.06 |
| G52 | 2 | 2 | 2 | 6 | 6 | 34 | 26 | 4.5 | 36 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 6 | 11 | 8 | 9.3 | 16 | 31 | 25 | 28 | 56 | 3 | 1.3 | 1.69 |
| G53 | 2 | 2 | 2 | 2 | 6 | 47 | 22 | 0.0 | 30 | 0.1 | 0.0 | 0.6 | 0 | 0.0 | 25 | 4 | 9 | 8.9 | 54 | 9 | 19 | 19 | 27 | 6 | 0.4 | 0.35 |
| G54 | 2 | 2 | 2 | 6 | 6 | 38 | 23 | 0.0 | 37 | 0.4 | 0.2 | 0.2 | 0 | 0.0 | 6 | 17 | 14 | 1.4 | 15 | 44 | 37 | 4 | 81 | 3 | 4.4 | 0.25 |
| G55 | 2 | 2 | 2 | 3 | 6 | 39 | 22 | 0.5 | 38 | 0.0 | 0.1 | 0.1 | 0 | 0.0 | 17 | 21 | 0 | 0.6 | 44 | 54 | 0 | 2 | 54 | 3 | 1.2 | 0.04 |
| G56 | 2 | 2 | 2 | 3 | 6 | 51 | 24 | 0.2 | 24 | 0.2 | 0.3 | 0.2 | 0 | 0.0 | 10 | 33 | 8 | 0.0 | 20 | 64 | 16 | 0 | 80 | 1 | 3.9 | 0.00 |
| G57 | 1 | 1 | 1 | 1 | 4 | 24 | 10 | 0.4 | 66 | 0.0 | 0.0 | 0.3 | 0 | 0.0 | 11 | 12 | 0 | 0.0 | 3 | 21 | 0 | 0 | 21 | 3 | 1.1 | 0.00 |
| G58 | 1 | 1 | 1 | 1 | 4 | 41 | 18 | 0.7 | 39 | 0.2 | 0.7 | 0.0 | 0 | 0.0 | 14 | 20 | 4 | 2.8 | 33 | 49 | 11 | 7 | 60 | 3 | 1.5 | 0.20 |
| G59 | 1 | 1 | 1 | 1 | 4 | 36 | 2 | 1.4 | 59 | 1.6 | 0.4 | 0.0 | 0 | 0.0 | 10 | 21 | 5 | 0.0 | 27 | 58 | 15 | 0 | 73 | 1 | 2.7 | 0.00 |
| G60 | 45 | 5 | 3 | 1 | SS | 38 | 21 | 1.6 | 35 | 0.2 | 0.0 | 0.4 | 2 | 0.0 | 3 | 26 | 8 | 1.2 | 13 | 71 | 13 | 3 | 88 | 1 | 7.6 | 0.38 |
| G61 | 45 | 5 | 3 | 1 | SS | 43 | 24 | 0.2 | 32 | 0.0 | 0.2 | 0.4 | 0 | 0.0 | 5 | 31 | 5 | 1.5 | 13 | 71 | 13 | 3 | 84 | 1 | 5.2 | 0.28 |
| G62 | 45 | 5 | 3 | 1 | SS | 51 | 17 | 0.1 | 32 | 0.3 | 0.0 | 0.5 | 0 | 0.0 | 6 | 40 | 5 | 0.0 | 12 | 79 | 9 | 0 | 88 | 1 | 7.2 | 0.00 |
| G63 | 45 | 4 | 2 | 2 | SS | 56 | 38 | 0.5 | 5 | 0.3 | 0.1 | 0.1 | 0 | 0.0 | 6 | 40 | 5 | 0.0 | 20 | 71 | 7 | 2 | 78 | 1 | 7.2 | 0.00 |
| G64 | 3 | 3 | 2 | 2 | SS | 52 | 17 | 6.5 | 23 | 0.0 | 0.0 | 0.0 | 0 | 0.6 | 22 | 24 | 4 | 2.4 | 42 | 45 | 8 | 5 | 53 | 2 | 1.2 | 0.11 |
| G65 | 3 | 3 | 2 | 6 | SS | 50 | 18 | 2.9 | 26 | 0.0 | 0.0 | 0.0 | 0 | 2.8 | 20 | 11 | 5 | 13.8 | 40 | 22 | 11 | 28 | 32 | 6 | 0.5 | 0.68 |
| G66 | 3 | 3 | 2 | 6 | SS | 27 | 22 | 6.1 | 43 | 0.0 | 0.0 | 0.0 | 0 | 1.5 | 11 | 11 | 3 | 2.2 | 39 | 42 | 12 | 8 | 53 | 3 | 1.1 | 0.21 |
| G67 | 3 | 3 | 2 | 2 | SS | 30 | 15 | 2.6 | 51 | 0.0 | 0.0 | 1.0 | 0 | 0.8 | 3 | 19 | 4 | 3.8 | 11 | 65 | 12 | 13 | 77 | 1 | 3.3 | 1.17 |
| G68 | 1 | 1 | 1 | 1 | SS | 72 | 21 | 4.0 | 4 | 0.0 | 0.0 | 0.0 | 0 | 0.0 | 18 | 53 | 0 | 0.0 | 26 | 74 | 0 | 0 | 74 | 1 | 2.9 | 0.00 |
| G71 | 2 | 2 | 2 | 2 | SS | 34 | 25 | 3.4 | 35 | 0.0 | 0.0 | 0.0 | 3 | 0.0 | 6 | 19 | 6 | 2.9 | 18 | 56 | 17 | 9 | 73 | 1 | 2.7 | 0.47 |
| G72 | 3 | 3 | 2 | 2 | SS | 47 | 21 | 3.3 | 24 | 0.0 | 0.0 | 1.7 | 0 | 1.8 | 27 | 7 | 10 | 3.8 | 57 | 14 | 22 | 8 | 36 | 6 | 0.6 | 0.14 |
| G81 | 3 | 3 | 4 | 5 | SG | 17 | 26 | 1.3 | 47 | 0.0 | 0.0 | 0.0 | 9 | 0.0 | 4 | 6 | 5 | 1.8 | 23 | 38 | 28 | 11 | 67 | 3 | 2.0 | 0.47 |
| G82 | 3 | 3 | 4 | 5 | SG | 16 | 34 | 1.0 | 7 | 7.3 | 0.0 | 0.0 | 34 | 0.0 | 6 | 3 | 3 | 3.5 | 37 | 21 | 21 | 22 | 41 | 5 | 0.7 | 0.58 |
| G83 | 3 | 3 | 4 | 5 | SG | 14 | 14 | 1.9 | 42 | 3.5 | 0.0 | 0.0 | 24 | 0.0 | 3 | 8 | 2 | 0.9 | 18 | 59 | 16 | 7 | 75 | 3 | 3.0 | 0.35 |
| G84 | 3 | 3 | 4 | 5 | SG | 17 | 16 | 2.5 | 9 | 0.0 | 0.0 | 0.0 | 55 | 0.0 | 2 | 10 | 4 | 0.7 | 14 | 61 | 21 | 4 | 82 | 5 | 4.5 | 0.29 |
| G85 | 3 | 3 | 4 | 5 | SG | 18 | 22 | 1.6 | 49 | 0.0 | 0.0 | 0.0 | 9 | 0.0 | 6 | 7 | 4 | 1.9 | 31 | 38 | 21 | 10 | 47 | 3 | 1.4 | 0.33 |

UNs, stratigraphical unit used for Anova analysis; UNI, stratigraphical unit (1: Grey Unit, 2: Lower Red Unit, 3: Upper Red Unit, 4: Marine Eocene, 5: Continental Eocene); FAC, facies type (1: Lacustrine, 2: fluviatile, 3: marine, 4: evaporite); LIT, group of related lithologies (1: interbedded limestones, 2: lutites only, 3: lutites and sandstones, 4: occurrence of gypsum nodules, 5: occurrence of evaporite beds, 6: occurrence of caliche nodules); SEC, number of the stratigraphical section or Sp (for sampling points) and SG (for samples of old open pits at Les Gesseres); SS, total sheet silicates; Q, quartz; F, feldspars; C, calcite; D, dolomite; PY, pyrite; H, hematite; Gy, gypsum; Si, siderite; K, kaolinite; I, illite; Ch, chlorite; Sm, smectite; Kf1, kaolinite in the clay fraction; If1, illite in the clay fraction; Chf1, chlorite in the clay fraction; Smf1, smectite in clay fraction; ICh f1, (illite + chlorite) in clay fraction.

Supplementary Table 2a. ANOVA for stratigraphical  units

| Units i | Units j | Mean diffreences | Standard | Sig. | 95% confidence interval |
| --- | --- | --- | --- | --- | --- |
| Dependent |  |  | (i–j) | error |  |  |  |
| variable |  |  |  |  |  | Lower | Upper |
|  |  |  |  |  |  | límit | límit |
| Sheet sil. | 1 | 2 | –5.26 | 7.36 | 0.916 | –26.4 | 15.9 |
|  |  | 3 | –1.43 | 7.21 | 0.998 | –22.1 | 19.3 |
|  |  | 45 | –10.31 | 9.81 | 0.776 | –38.5 | 17.9 |
|  | 2 | 1 | 5.26 | 7.36 | 0.916 | –15.9 | 26.4 |
|  |  | 3 | 3.83 | 4.32 | 0.853 | –8.6 | 16.2 |
|  |  | 45 | –5.05 | 7.94 | 0.939 | –27.8 | 17.7 |
|  | 3 | 1 | 1.43 | 7.21 | 0.998 | –19.3 | 22.1 |
|  |  | 2 | –3.83 | 4.32 | 0.853 | –16.2 | 8.6 |
|  |  | 45 | –8.88 | 7.79 | 0.73 | –31.2 | 13.5 |
|  | 45 | 1 | 10.31 | 9.81 | 0.776 | –17.9 | 38.5 |
|  |  | 2 | 5.05 | 7.94 | 0.939 | –17.7 | 27.8 |
|  |  | 3 | 8.88 | 7.79 | 0.73 | –13.5 | 31.2 |
| Quartz | 1 | 2 | –4.32 | 3.57 | 0.692 | –14.6 | 5.9 |
|  |  | 3 | –4.89 | 3.49 | 0.583 | –14.9 | 5.1 |
|  |  | 45 | –8.92 | 4.75 | 0.327 | –22.6 | 4.7 |
|  | 2 | 1 | 4.32 | 3.57 | 0.692 | –5.9 | 14.6 |
|  |  | 3 | –0.57 | 2.1 | 0.995 | –6.6 | 5.4 |
|  |  | 45 | –4.6 | 3.85 | 0.699 | –15.6 | 6.4 |
|  | 3 | 1 | 4.89 | 3.49 | 0.583 | –5.1 | 14.9 |
|  |  | 2 | 0.57 | 2.1 | 0.995 | –5.4 | 6.6 |
|  |  | 45 | –4.03 | 3.77 | 0.768 | –14.9 | 6.8 |
|  | 45 | 1 | 8.92 | 4.75 | 0.327 | –4.7 | 22.6 |
|  |  | 2 | 4.6 | 3.85 | 0.699 | –6.4 | 15.6 |
|  |  | 3 | 4.03 | 3.77 | 0.768 | –6.8 | 14.9 |
| Feldspars | 1 | 2 | 0.17 | 0.64 | 0.995 | –1.7 | 2 |
|  |  | 3 | –0.31 | 0.63 | 0.969 | –2.1 | 1.5 |
|  |  | 45 | 0.58 | 0.85 | 0.927 | –1.9 | 3 |
|  | 2 | 1 | –0.17 | 0.64 | 0.995 | –2 | 1.7 |
|  |  | 3 | –0.49 | 0.38 | 0.647 | –1.6 | 0.6 |
|  |  | 45 | 0.41 | 0.69 | 0.951 | –1.6 | 2.4 |
|  | 3 | 1 | 0.31 | 0.63 | 0.969 | –1.5 | 2.1 |
|  |  | 2 | 0.49 | 0.38 | 0.647 | –0.6 | 1.6 |
|  |  | 45 | 0.89 | 0.68 | 0.632 | –1.1 | 2.8 |
|  | 45 | 1 | –0.58 | 0.85 | 0.927 | –3 | 1.9 |
|  |  | 2 | –0.41 | 0.69 | 0.951 | –2.4 | 1.6 |
|  |  | 3 | –0.89 | 0.68 | 0.632 | –2.8 | 1.1 |
| Calcite | 1 | 2 | 9.56 | 7.17 | 0.622 | –11 | 30.2 |
|  |  | 3 | 11.82 | 7.02 | 0.424 | –8.3 | 32 |
|  |  | 45 | 20.09 | 9.56 | 0.23 | –7.4 | 47.5 |
|  | 2 | 1 | –9.56 | 7.17 | 0.622 | –30.2 | 11 |
|  |  | 3 | 2.26 | 4.21 | 0.962 | –9.8 | 14.4 |
|  |  | 45 | 10.53 | 7.73 | 0.606 | –11.7 | 32.7 |
|  | 3 | 1 | –11.82 | 7.02 | 0.424 | –32 | 8.3 |
|  |  | 2 | –2.26 | 4.21 | 0.962 | –14.4 | 9.8 |
|  |  | 45 | 8.27 | 7.59 | 0.757 | –13.5 | 30.1 |
|  | 45 | 1 | –20.09 | 9.56 | 0.23 | –47.5 | 7.4 |
|  |  | 2 | –10.53 | 7.73 | 0.606 | –32.7 | 11.7 |
|  |  | 3 | –8.27 | 7.59 | 0.757 | –30.1 | 13.5 |
| Dolomite | 1 | 2 | 0.16 | 0.49 | 0.99 | –1.2 | 1.6 |
|  |  | 3 | –0.31 | 0.48 | 0.935 | –1.7 | 1.1 |
|  |  | 45 | 0.05 | 0.65 | 1 | –1.8 | 1.9 |
|  | 2 | 1 | –0.16 | 0.49 | 0.99 | –1.6 | 1.2 |
|  |  | 3 | –0.47 | 0.29 | 0.438 | –1.3 | 0.3 |
|  |  | 45 | –0.12 | 0.53 | 0.997 | –1.6 | 1.4 |
|  | 3 | 1 | 0.31 | 0.48 | 0.935 | –1.1 | 1.7 |
|  |  | 2 | 0.47 | 0.29 | 0.438 | –0.3 | 1.3 |
|  |  | 45 | 0.36 | 0.52 | 0.924 | –1.1 | 1.8 |
|  | 45 | 1 | –0.05 | 0.65 | 1 | –1.9 | 1.8 |
|  |  | 2 | 0.12 | 0.53 | 0.997 | –1.4 | 1.6 |
|  |  | 3 | –0.36 | 0.52 | 0.924 | –1.8 | 1.1 |
| Pyrite | 1 | 2 | 0.04 | 0.1 | 0.987 | –0.3 | 0.3 |
|  |  | 3 | 0.13 | 0.1 | 0.624 | –0.2 | 0.4 |
|  |  | 45 | 0 | 0.13 | 1 | –0.4 | 0.4 |
|  | 2 | 1 | –0.04 | 0.1 | 0.987 | –0.3 | 0.3 |
|  |  | 3 | 0.09 | 0.06 | 0.479 | –0.1 | 0.3 |
|  |  | 45 | –0.03 | 0.11 | 0.992 | –0.3 | 0.3 |
|  | 3 | 1 | –0.13 | 0.1 | 0.624 | –0.4 | 0.2 |
|  |  | 2 | –0.09 | 0.06 | 0.479 | –0.3 | 0.1 |
|  |  | 45 | –0.13 | 0.11 | 0.7 | –0.4 | 0.2 |
|  | 45 | 1 | 0 | 0.13 | 1 | –0.4 | 0.4 |
|  |  | 2 | 0.03 | 0.11 | 0.992 | –0.3 | 0.3 |
|  |  | 3 | 0.13 | 0.11 | 0.7 | –0.2 | 0.4 |
| Hematite | 1 | 2 | –0.16 | 0.22 | 0.912 | –0.8 | 0.5 |
|  |  | 3 | –0.45 | 0.22 | 0.245 | –1.1 | 0.2 |
|  |  | 45 | –0.38 | 0.29 | 0.644 | –1.2 | 0.5 |
|  | 2 | 1 | 0.16 | 0.22 | 0.912 | –0.5 | 0.8 |
|  |  | 3 | –0.29 | 0.13 | 0.194 | –0.7 | 0.1 |
|  |  | 45 | –0.22 | 0.24 | 0.835 | –0.9 | 0.5 |
|  | 3 | 1 | 0.45 | 0.22 | 0.245 | –0.2 | 1.1 |
|  |  | 2 | 0.29 | 0.13 | 0.194 | –0.1 | 0.7 |
|  |  | 45 | 0.07 | 0.23 | 0.994 | –0.6 | 0.7 |
|  | 45 | 1 | 0.38 | 0.29 | 0.644 | –0.5 | 1.2 |
|  |  | 2 | 0.22 | 0.24 | 0.835 | –0.5 | 0.9 |
|  |  | 3 | –0.07 | 0.23 | 0.994 | –0.7 | 0.6 |
| Gypsum | 1 | 2 | –0.11 | 4.19 | 1 | –12.2 | 11.9 |
|  |  | 3 | –6.13 | 4.1 | 0.529 | –17.9 | 5.7 |
|  |  | 45 | –0.48 | 5.59 | 1 | –16.5 | 15.6 |
|  | 2 | 1 | 0.11 | 4.19 | 1 | –11.9 | 12.2 |
|  |  | 3 | –6.02 | 2.46 | 0.124 | –13.1 | 1.1 |
|  |  | 45 | –0.37 | 4.52 | 1 | –13.3 | 12.6 |
|  | 3 | 1 | 6.13 | 4.1 | 0.529 | –5.7 | 17.9 |
|  |  | 2 | 6.02 | 2.46 | 0.124 | –1.1 | 13.1 |
|  |  | 45 | 5.65 | 4.44 | 0.656 | –7.1 | 18.4 |
|  | 45 | 1 | 0.48 | 5.59 | 1 | –15.6 | 16.5 |
|  |  | 2 | 0.37 | 4.52 | 1 | –12.6 | 13.3 |
|  |  | 3 | –5.65 | 4.44 | 0.656 | –18.4 | 7.1 |
| Siderite | 1 | 2 | –0.04 | 0.21 | 0.999 | –0.6 | 0.6 |
|  |  | 3 | –0.23 | 0.2 | 0.722 | –0.8 | 0.3 |
|  |  | 45 | 0 | 0.28 | 1 | –0.8 | 0.8 |
|  | 2 | 1 | 0.04 | 0.21 | 0.999 | –0.6 | 0.6 |
|  |  | 3 | –0.2 | 0.12 | 0.451 | –0.5 | 0.2 |
|  |  | 45 | 0.04 | 0.22 | 0.999 | –0.6 | 0.7 |
|  | 3 | 1 | 0.23 | 0.2 | 0.722 | –0.3 | 0.8 |
|  |  | 2 | 0.2 | 0.12 | 0.451 | –0.2 | 0.5 |
|  |  | 45 | 0.23 | 0.22 | 0.767 | –0.4 | 0.9 |
|  | 45 | 1 | 0 | 0.28 | 1 | –0.8 | 0.8 |
|  |  | 2 | –0.04 | 0.22 | 0.999 | –0.7 | 0.6 |
|  |  | 3 | –0.23 | 0.22 | 0.767 | –0.9 | 0.4 |
| Kaolinite | 1 | 2 | –4.56 | 3.34 | 0.603 | –14.1 | 5 |
|  |  | 3 | –2.56 | 3.27 | 0.892 | –11.9 | 6.8 |
|  |  | 45 | 3.72 | 4.45 | 0.873 | –9 | 16.5 |
|  | 2 | 1 | 4.56 | 3.34 | 0.603 | –5 | 14.1 |
|  |  | 3 | 2 | 1.96 | 0.792 | –3.6 | 7.6 |
|  |  | 45 | 8.28 | 3.6 | 0.163 | –2 | 18.6 |
|  | 3 | 1 | 2.56 | 3.27 | 0.892 | –6.8 | 11.9 |
|  |  | 2 | –2 | 1.96 | 0.792 | –7.6 | 3.6 |
|  |  | 45 | 6.28 | 3.53 | 0.374 | –3.9 | 16.4 |
|  | 45 | 1 | –3.72 | 4.45 | 0.873 | –16.5 | 9 |
|  |  | 2 | –8.28 | 3.6 | 0.163 | –18.6 | 2 |
|  |  | 3 | –6.28 | 3.53 | 0.374 | –16.4 | 3.9 |
| Illite | 1 | 2 | 3.61 | 4.95 | 0.912 | –10.6 | 17.8 |
|  |  | 3 | 10.49 | 4.85 | 0.208 | –3.4 | 24.4 |
|  |  | 45 | –9.19 | 6.6 | 0.588 | –28.1 | 9.8 |
|  | 2 | 1 | –3.61 | 4.95 | 0.912 | –17.8 | 10.6 |
|  |  | 3 | 6.88 | 2.91 | 0.145 | –1.5 | 15.2 |
|  |  | 45 | –12.8 | 5.34 | 0.136 | –28.1 | 2.5 |
|  | 3 | 1 | –10.49 | 4.85 | 0.208 | –24.4 | 3.4 |
|  |  | 2 | –6.88 | 2.91 | 0.145 | –15.2 | 1.5 |
|  |  | 45 | –19.67 | 5.24 | 0.005 | –34.7 | –4.6 |
|  | 45 | 1 | 9.19 | 6.6 | 0.588 | –9.8 | 28.1 |
|  |  | 2 | 12.8 | 5.34 | 0.136 | –2.5 | 28.1 |
|  |  | 3 | 19.67 | 5.24 | 0.005 | 4.6 | 34.7 |
| Chlorite | 1 | 2 | –5.09 | 2.05 | 0.115 | –11 | 0.8 |
|  |  | 3 | –4.65 | 2.01 | 0.158 | –10.4 | 1.1 |
|  |  | 45 | –4.05 | 2.74 | 0.537 | –11.9 | 3.8 |
|  | 2 | 1 | 5.09 | 2.05 | 0.115 | –0.8 | 11 |
|  |  | 3 | 0.44 | 1.21 | 0.987 | –3 | 3.9 |
|  |  | 45 | 1.04 | 2.21 | 0.974 | –5.3 | 7.4 |
|  | 3 | 1 | 4.65 | 2.01 | 0.158 | –1.1 | 10.4 |
|  |  | 2 | –0.44 | 1.21 | 0.987 | –3.9 | 3 |
|  |  | 45 | 0.6 | 2.17 | 0.994 | –5.6 | 6.8 |
|  | 45 | 1 | 4.05 | 2.74 | 0.537 | –3.8 | 11.9 |
|  |  | 2 | –1.04 | 2.21 | 0.974 | –7.4 | 5.3 |
|  |  | 3 | –0.6 | 2.17 | 0.994 | –6.8 | 5.6 |
| Smectite | 1 | 2 | –1.69 | 3.27 | 0.966 | –11.1 | 7.7 |
|  |  | 3 | –5.93 | 3.2 | 0.339 | –15.1 | 3.3 |
|  |  | 45 | 0.04 | 4.36 | 1 | –12.5 | 12.6 |
|  | 2 | 1 | 1.69 | 3.27 | 0.966 | –7.7 | 11.1 |
|  |  | 3 | –4.24 | 1.92 | 0.194 | –9.8 | 1.3 |
|  |  | 45 | 1.73 | 3.53 | 0.97 | –8.4 | 11.9 |
|  | 3 | 1 | 5.93 | 3.2 | 0.339 | –3.3 | 15.1 |
|  |  | 2 | 4.24 | 1.92 | 0.194 | –1.3 | 9.8 |
|  |  | 45 | 5.97 | 3.46 | 0.403 | –4 | 15.9 |
|  | 45 | 1 | –0.04 | 4.36 | 1 | –12.6 | 12.5 |
|  |  | 2 | –1.73 | 3.53 | 0.97 | –11.9 | 8.4 |
|  |  | 3 | –5.97 | 3.46 | 0.403 | –15.9 | 4 |
| K–f1 | 1 | 2 | –11.91 | 5.33 | 0.183 | –27.2 | 3.4 |
| (kaolinite in |  | 3 | –12.51 | 5.21 | 0.135 | –27.5 | 2.5 |
| clay |  | 45 | 2.23 | 7.09 | 0.992 | –18.1 | 22.6 |
| fraction) | 2 | 1 | 11.91 | 5.33 | 0.183 | –3.4 | 27.2 |
|  |  | 3 | –0.6 | 3.13 | 0.998 | –9.6 | 8.4 |
|  |  | 45 | 14.14 | 5.74 | 0.12 | –2.3 | 30.6 |
|  | 3 | 1 | 12.51 | 5.21 | 0.135 | –2.5 | 27.5 |
|  |  | 2 | 0.6 | 3.13 | 0.998 | –8.4 | 9.6 |
|  |  | 45 | 14.74 | 5.63 | 0.088 | –1.4 | 30.9 |
|  | 45 | 1 | –2.23 | 7.09 | 0.992 | –22.6 | 18.1 |
|  |  | 2 | –14.14 | 5.74 | 0.12 | –30.6 | 2.3 |
|  |  | 3 | –14.74 | 5.63 | 0.088 | –30.9 | 1.4 |
| I–f1 | 1 | 2 | 14.44 | 7.44 | 0.297 | –6.9 | 35.8 |
| (illite in |  | 3 | 23.16 | 7.28 | 0.024 | 2.3 | 44.1 |
| the clay |  | 45 | –10.08 | 9.91 | 0.793 | –38.5 | 18.4 |
| fraction) | 2 | 1 | –14.44 | 7.44 | 0.297 | –35.8 | 6.9 |
|  |  | 3 | 8.72 | 4.37 | 0.273 | –3.8 | 21.3 |
|  |  | 45 | –24.52 | 8.02 | 0.032 | –47.5 | –1.5 |
|  | 3 | 1 | –23.16 | 7.28 | 0.024 | –44.1 | –2.3 |
|  |  | 2 | –8.72 | 4.37 | 0.273 | –21.3 | 3.8 |
|  |  | 45 | –33.24 | 7.87 | 0.001 | –55.8 | –10.6 |
|  | 45 | 1 | 10.08 | 9.91 | 0.793 | –18.4 | 38.5 |
|  |  | 2 | 24.52 | 8.02 | 0.032 | 1.5 | 47.5 |
|  |  | 3 | 33.24 | 7.87 | 0.001 | 10.6 | 55.8 |
| Ch–f1 | 1 | 2 | –9.02 | 3.82 | 0.145 | –20 | 1.9 |
| (chlorite |  | 3 | –10.66 | 3.73 | 0.052 | –21.4 | 0.1 |
| in the clay |  | 45 | –4.59 | 5.08 | 0.845 | –19.2 | 10 |
| fraction) | 2 | 1 | 9.02 | 3.82 | 0.145 | –1.9 | 20 |
|  |  | 3 | –1.64 | 2.24 | 0.91 | –8.1 | 4.8 |
|  |  | 45 | 4.42 | 4.11 | 0.764 | –7.4 | 16.2 |
|  | 3 | 1 | 10.66 | 3.73 | 0.052 | –0.1 | 21.4 |
|  |  | 2 | 1.64 | 2.24 | 0.91 | –4.8 | 8.1 |
|  |  | 45 | 6.07 | 4.04 | 0.525 | –5.5 | 17.7 |
|  | 45 | 1 | 4.59 | 5.08 | 0.845 | –10 | 19.2 |
|  |  | 2 | –4.42 | 4.11 | 0.764 | –16.2 | 7.4 |
|  |  | 3 | –6.07 | 4.04 | 0.525 | –17.7 | 5.5 |
| Smectite–f1 | 1 | 2 | –3.87 | 5.2 | 0.907 | –18.8 | 11.1 |
| (smectite |  | 3 | –12.66 | 5.09 | 0.114 | –27.3 | 2 |
| in the clay |  | 45 | –0.22 | 6.92 | 1 | –20.1 | 19.7 |
| fraction) | 2 | 1 | 3.87 | 5.2 | 0.907 | –11.1 | 18.8 |
|  |  | 3 | –8.79 | 3.05 | 0.049 | –17.6 | 0 |
|  |  | 45 | 3.65 | 5.6 | 0.935 | –12.4 | 19.7 |
|  | 3 | 1 | 12.66 | 5.09 | 0.114 | –2 | 27.3 |
|  |  | 2 | 8.79 | 3.05 | 0.049 | 0 | 17.6 |
|  |  | 45 | 12.44 | 5.5 | 0.175 | –3.4 | 28.2 |
|  | 45 | 1 | 0.22 | 6.92 | 1 | –19.7 | 20.1 |
|  |  | 2 | –3.65 | 5.6 | 0.935 | –19.7 | 12.4 |
|  |  | 3 | –12.44 | 5.5 | 0.175 | –28.2 | 3.4 |
| I+Ch* | 1 | 2 | 3.65 | 7.51 | 0.971 | –17.9 | 25.2 |
| (illite + |  | 3 | 12.84 | 7.35 | 0.391 | –8.3 | 33.9 |
| chlorite in |  | 45 | –15.56 | 10 | 0.495 | –44.3 | 13.2 |
| the clay | 2 | 1 | –3.65 | 7.51 | 0.971 | –25.2 | 17.9 |
| fraction) |  | 3 | 9.2 | 4.41 | 0.237 | –3.5 | 21.9 |
|  |  | 45 | –19.2 | 8.09 | 0.142 | –42.4 | 4 |
|  | 3 | 1 | –12.84 | 7.35 | 0.391 | –33.9 | 8.3 |
|  |  | 2 | –9.2 | 4.41 | 0.237 | –21.9 | 3.5 |
|  |  | 45 | –28.4 | 7.94 | 0.008 | –51.2 | –5.6 |
|  | 45 | 1 | 15.56 | 10 | 0.495 | –13.2 | 44.3 |
|  |  | 2 | 19.2 | 8.09 | 0.142 | –4 | 42.4 |
|  |  | 3 | 28.4 | 7.94 | 0.008 | 5.6 | 51,2 |
| Units with significant differences |  |  | The means difference is significant at the 0.05 level. |  |

Supplementary Table 2b. Descriptive statistics of groups of related lithological features. L: group of related lithologies. Other labels as in Table 2.

| L |  | N | Mean | St dev | St err | Min | Max |  | L |  | N | Mean | St dev | St err | Min | Max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Sheet sil. | 11 | 43.7 | 14.17 | 4.27 | 24.0 | 71.6 |  | 4 | Sheet sil. | 6 | 47.2 | 22.31 | 9.11 | 18.0 | 74.0 |
|  | Quartz | 11 | 15.9 | 8.78 | 2.65 | 2.0 | 31.8 |  |  | Quartz | 6 | 22.2 | 13.79 | 5.63 | 7.7 | 43.0 |
|  | Feldspars | 11 | 0.9 | 1.14 | 0.34 | 0.0 | 4.0 |  |  | Feldspars | 6 | 0.4 | 0.41 | 0.17 | 0.0 | 1.2 |
|  | Calcite | 11 | 38.4 | 19.66 | 5.93 | 3.8 | 68.5 |  |  | Calcite | 6 | 16.9 | 11.57 | 4.72 | 3.0 | 32.0 |
|  | Dolomite | 11 | 0.2 | 0.47 | 0.14 | 0.0 | 1.6 |  |  | Dolomite | 6 | 1.1 | 1.31 | 0.54 | 0.0 | 3.0 |
|  | Pyrite | 11 | 0.2 | 0.26 | 0.08 | 0.0 | 0.7 |  |  | Pyrite | 6 | 0.1 | 0.22 | 0.09 | 0.0 | 0.5 |
|  | Hematite | 11 | 0.2 | 0.30 | 0.09 | 0.0 | 0.9 |  |  | Hematite | 6 | 0.8 | 1.03 | 0.42 | 0.0 | 2.2 |
|  | Gypsum | 11 | 0.2 | 0.72 | 0.22 | 0.0 | 2.4 |  |  | Gypsum | 6 | 10.7 | 13.82 | 5.64 | 0.0 | 34.0 |
|  | Siderite | 11 | 0.0 | 0.00 | 0.00 | 0.0 | 0.0 |  |  | Siderite | 6 | 0.0 | 0.00 | 0.00 | 0.0 | 0.0 |
|  | Kaolinite | 11 | 8.4 | 6.34 | 1.91 | 0.0 | 18.5 |  |  | Kaolinite | 6 | 11.3 | 7.00 | 2.86 | 4.7 | 22.4 |
|  | Illite | 11 | 29.8 | 12.17 | 3.67 | 11.9 | 53.1 |  |  | Illite | 6 | 23.4 | 15.65 | 6.39 | 3.0 | 40.4 |
|  | Chlorite | 11 | 4.7 | 3.31 | 1.00 | 0.0 | 10.4 |  |  | Chlorite | 6 | 7.6 | 5.65 | 2.31 | 2.4 | 18.3 |
|  | Smectite | 11 | 0.8 | 0.91 | 0.27 | 0.0 | 2.8 |  |  | Smectite | 6 | 5.0 | 3.24 | 1.32 | 0.0 | 8.0 |
|  | Kaolinite–f1 | 11 | 15.8 | 12.45 | 3.76 | 0.0 | 35.1 |  |  | Kaolinite–f1 | 6 | 24.1 | 7.77 | 3.17 | 13.0 | 36.7 |
|  | Illite–f1 | 11 | 65.5 | 19.90 | 6.00 | 21.3 | 88.2 |  |  | Illite–f1 | 6 | 43.7 | 22.46 | 9.17 | 16.4 | 76.2 |
|  | Chlorite–f1 | 11 | 10.0 | 5.76 | 1.74 | 0.0 | 17.0 |  |  | Chlorite–f1 | 6 | 16.9 | 9.12 | 3.72 | 6.4 | 30.8 |
|  | Smectite–f1 | 11 | 1.8 | 2.27 | 0.68 | 0.0 | 6.7 |  |  | Smectite–f1 | 6 | 15.3 | 15.96 | 6.52 | 0.0 | 44.3 |
|  | (I+Ch)in f1 | 11 | 75.9 | 21.86 | 6.59 | 21.3 | 96.1 |  |  | (I+Ch)in f1 | 6 | 60.6 | 20.24 | 8.26 | 29.8 | 87.0 |
| 2 | Sheet sil. | 33 | 45.7 | 14.71 | 2.56 | 22.0 | 89.1 |  | 5 | Sheet sil. | 5 | 16.2 | 1.57 | 0.70 | 13.8 | 18.1 |
|  | Quartz | 33 | 18.8 | 6.77 | 1.18 | 7.8 | 40.4 |  |  | Quartz | 5 | 22.5 | 8.22 | 3.67 | 14.0 | 34.3 |
|  | Feldspars | 33 | 1.2 | 1.46 | 0.26 | 0.0 | 6.5 |  |  | Feldspars | 5 | 1.7 | 0.56 | 0.25 | 1.0 | 2.5 |
|  | Calcite | 33 | 35.5 | 14.12 | 2.46 | 0.0 | 61.0 |  |  | Calcite | 5 | 31.0 | 20.90 | 9.35 | 7.3 | 49.4 |
|  | Dolomite | 33 | 0.1 | 0.22 | 0.04 | 0.0 | 0.7 |  |  | Dolomite | 5 | 2.2 | 3.25 | 1.45 | 0.0 | 7.3 |
|  | Pyrite | 33 | 0.1 | 0.19 | 0.03 | 0.0 | 0.8 |  |  | Pyrite | 5 | 0.0 | 0.00 | 0.00 | 0.0 | 0.0 |
|  | Hematite | 33 | 0.4 | 0.43 | 0.08 | 0.0 | 1.7 |  |  | Hematite | 5 | 0.0 | 0.00 | 0.00 | 0.0 | 0.0 |
|  | Gypsum | 33 | 0.1 | 0.48 | 0.08 | 0.0 | 2.8 |  |  | Gypsum | 5 | 26.5 | 19.36 | 8.66 | 8.9 | 55.5 |
|  | Siderite | 33 | 0.1 | 0.38 | 0.07 | 0.0 | 1.8 |  |  | Siderite | 5 | 0.0 | 0.00 | 0.00 | 0.0 | 0.0 |
|  | Kaolinite | 33 | 12.4 | 6.77 | 1.18 | 3.2 | 27.7 |  |  | Kaolinite | 5 | 4.0 | 1.69 | 0.76 | 2.3 | 5.9 |
|  | Illite | 33 | 20.8 | 10.68 | 1.86 | 4.1 | 43.6 |  |  | Illite | 5 | 6.9 | 2.47 | 1.10 | 3.4 | 10.1 |
|  | Chlorite | 33 | 7.6 | 4.87 | 0.85 | 0.0 | 19.8 |  |  | Chlorite | 5 | 3.5 | 0.90 | 0.40 | 2.2 | 4.7 |
|  | Smectite | 33 | 5.8 | 10.01 | 1.74 | 0.0 | 45.0 |  |  | Smectite | 5 | 1.7 | 1.09 | 0.49 | 0.7 | 3.5 |
|  | Kaolinite–f1 | 33 | 27.4 | 12.77 | 2.22 | 10.8 | 56.5 |  |  | Kaolinite–f1 | 5 | 24.6 | 9.37 | 4.19 | 14.1 | 37.0 |
|  | Illite–f1 | 33 | 45.4 | 17.80 | 3.10 | 8.8 | 75.2 |  |  | Illite–f1 | 5 | 43.3 | 16.62 | 7.44 | 20.9 | 60.6 |
|  | Chlorite–f1 | 33 | 16.2 | 8.95 | 1.56 | 0.0 | 33.8 |  |  | Chlorite–f1 | 5 | 21.4 | 4.42 | 1.98 | 16.1 | 28.4 |
|  | Smectite–f1 | 33 | 11.0 | 14.33 | 2.50 | 0.0 | 66.7 |  |  | Smectite–f1 | 5 | 10.7 | 6.68 | 2.99 | 4.2 | 21.6 |
|  | (I+Ch)in f1 | 33 | 61.9 | 17.39 | 3.03 | 15.3 | 90.2 |  |  | (I+Ch)in f1 | 5 | 62.5 | 17.46 | 7.81 | 41.5 | 81.7 |
| 3 | Sheet sil. | 5 | 45.4 | 8.92 | 3.99 | 35.0 | 57.1 |  | 6 | Sheet sil. | 8 | 41.7 | 15.04 | 5.32 | 23.9 | 71.3 |
|  | Quartz | 5 | 19.7 | 6.02 | 2.69 | 10.4 | 25.0 |  |  | Quartz | 8 | 19.5 | 6.89 | 2.43 | 7.1 | 27.1 |
|  | Feldspars | 5 | 0.8 | 0.52 | 0.23 | 0.2 | 1.5 |  |  | Feldspars | 8 | 2.0 | 2.30 | 0.81 | 0.0 | 6.1 |
|  | Calcite | 5 | 32.9 | 5.50 | 2.46 | 24.0 | 38.0 |  |  | Calcite | 8 | 35.9 | 17.87 | 6.32 | 0.0 | 62.5 |
|  | Dolomite | 5 | 0.2 | 0.37 | 0.16 | 0.0 | 0.8 |  |  | Dolomite | 8 | 0.1 | 0.16 | 0.06 | 0.0 | 0.4 |
|  | Pyrite | 5 | 0.3 | 0.44 | 0.20 | 0.0 | 1.1 |  |  | Pyrite | 8 | 0.0 | 0.00 | 0.00 | 0.0 | 0.0 |
|  | Hematite | 5 | 0.3 | 0.56 | 0.25 | 0.0 | 1.3 |  |  | Hematite | 8 | 0.2 | 0.35 | 0.13 | 0.0 | 0.9 |
|  | Gypsum | 5 | 0.0 | 0.00 | 0.00 | 0.0 | 0.0 |  |  | Gypsum | 8 | 0.0 | 0.00 | 0.00 | 0.0 | 0.0 |
|  | Siderite | 5 | 0.0 | 0.00 | 0.00 | 0.0 | 0.0 |  |  | Siderite | 8 | 0.5 | 1.05 | 0.37 | 0.0 | 2.8 |
|  | Kaolinite | 5 | 12.4 | 2.98 | 1.33 | 10.3 | 17.3 |  |  | Kaolinite | 8 | 17.3 | 11.60 | 4.10 | 5.5 | 37.2 |
|  | Illite | 5 | 22.7 | 6.92 | 3.09 | 13.8 | 32.6 |  |  | Illite | 8 | 20.0 | 13.63 | 4.82 | 10.6 | 50.3 |
|  | Chlorite | 5 | 8.3 | 5.59 | 2.50 | 0.0 | 14.4 |  |  | Chlorite | 8 | 7.7 | 4.43 | 1.57 | 2.9 | 14.1 |
|  | Smectite | 5 | 2.0 | 1.82 | 0.82 | 0.0 | 4.0 |  |  | Smectite | 8 | 3.9 | 4.90 | 1.73 | 0.0 | 13.8 |
|  | Kaolinite–f1 | 5 | 28.4 | 9.60 | 4.29 | 20.2 | 44.2 |  |  | Kaolinite–f1 | 8 | 31.1 | 12.94 | 4.57 | 14.8 | 43.6 |
|  | Illite–f1 | 5 | 49.5 | 9.65 | 4.31 | 39.4 | 63.8 |  |  | Illite–f1 | 8 | 36.6 | 10.71 | 3.79 | 21.3 | 49.5 |
|  | Chlorite–f1 | 5 | 17.5 | 10.79 | 4.83 | 0.0 | 27.3 |  |  | Chlorite–f1 | 8 | 16.0 | 10.41 | 3.68 | 4.4 | 37.0 |
|  | Smectite–f1 | 5 | 4.7 | 4.50 | 2.01 | 0.0 | 11.4 |  |  | Smectite–f1 | 8 | 9.0 | 11.70 | 4.14 | 0.0 | 27.7 |
|  | (I+Ch)in f1 | 5 | 66.9 | 10.51 | 4.70 | 54.2 | 79.8 |  |  | (I+Ch)in f1 | 8 | 57.0 | 13.47 | 4.76 | 32.2 | 81.5 |

Supplementary Table 2c. ANOVA of mineral contents for groups of lithological features. (Li, Lj : groups of related lithologies).

| Dependent Li | Lj | Mean diffreences | Standard | Sig. | 95% confidence interval |
| --- | --- | --- | --- | --- | --- |
| variables |  |  | (i–j) | error |  |  |  |
| Sheet sil. | 1 | 2 | –2.01 | 5.11 | 1 | –19.6 | 15.5 |
|  |  | 3 | –1.71 | 7.91 | 1 | –28.9 | 25.5 |
|  |  | 4 | –3.44 | 7.44 | 0.999 | –29 | 22.1 |
|  |  | 5 | 27.49 | 7.91 | 0.046 | 0.3 | 54.7 |
|  |  | 6 | 2.03 | 6.81 | 1 | –21.4 | 25.5 |
|  | 2 | 1 | 2.01 | 5.11 | 1 | –15.5 | 19.6 |
|  |  | 3 | 0.3 | 7.04 | 1 | –23.9 | 24.5 |
|  |  | 4 | –1.43 | 6.51 | 1 | –23.8 | 20.9 |
|  |  | 5 | 29.5 | 7.04 | 0.007 | 5.3 | 53.7 |
|  |  | 6 | 4.04 | 5.78 | 0.992 | –15.8 | 23.9 |
|  | 3 | 1 | 1.71 | 7.91 | 1 | –25.5 | 28.9 |
|  |  | 2 | –0.3 | 7.04 | 1 | –24.5 | 23.9 |
|  |  | 4 | –1.73 | 8.88 | 1 | –32.2 | 28.8 |
|  |  | 5 | 29.2 | 9.27 | 0.094 | –2.7 | 61.1 |
|  |  | 6 | 3.75 | 8.36 | 0.999 | –25 | 32.5 |
|  | 4 | 1 | 3.44 | 7.44 | 0.999 | –22.1 | 29 |
|  |  | 2 | 1.43 | 6.51 | 1 | –20.9 | 23.8 |
|  |  | 3 | 1.73 | 8.88 | 1 | –28.8 | 32.2 |
|  |  | 5 | 30.93 | 8.88 | 0.045 | 0.4 | 61.4 |
|  |  | 6 | 5.47 | 7.92 | 0.993 | –21.8 | 32.7 |
|  | 5 | 1 | –27.49 | 7.91 | 0.046 | –54.7 | –0.3 |
|  |  | 2 | –29.5 | 7.04 | 0.007 | –53.7 | –5.3 |
|  |  | 3 | –29.2 | 9.27 | 0.094 | –61.1 | 2.7 |
|  |  | 4 | –30.93 | 8.88 | 0.045 | –61.4 | –0.4 |
|  |  | 6 | –25.45 | 8.36 | 0.115 | –54.2 | 3.3 |
|  | 6 | 1 | –2.03 | 6.81 | 1 | –25.5 | 21.4 |
|  |  | 2 | –4.04 | 5.78 | 0.992 | –23.9 | 15.8 |
|  |  | 3 | –3.75 | 8.36 | 0.999 | –32.5 | 25 |
|  |  | 4 | –5.47 | 7.92 | 0.993 | –32.7 | 21.8 |
|  |  | 5 | 25.45 | 8.36 | 0.115 | –3.3 | 54.2 |
| Quartz | 1 | 2 | –2.83 | 2.77 | 0.958 | –12.4 | 6.7 |
|  |  | 3 | –3.75 | 4.3 | 0.979 | –18.5 | 11 |
|  |  | 4 | –6.22 | 4.04 | 0.795 | –20.1 | 7.7 |
|  |  | 5 | –6.56 | 4.3 | 0.801 | –21.3 | 8.2 |
|  |  | 6 | –3.53 | 3.7 | 0.969 | –16.3 | 9.2 |
|  | 2 | 1 | 2.83 | 2.77 | 0.958 | –6.7 | 12.4 |
|  |  | 3 | –0.92 | 3.82 | 1 | –14.1 | 12.2 |
|  |  | 4 | –3.39 | 3.54 | 0.968 | –15.5 | 8.8 |
|  |  | 5 | –3.72 | 3.82 | 0.965 | –16.9 | 9.4 |
|  |  | 6 | –0.7 | 3.14 | 1 | –11.5 | 10.1 |
|  | 3 | 1 | 3.75 | 4.3 | 0.979 | –11 | 18.5 |
|  |  | 2 | 0.92 | 3.82 | 1 | –12.2 | 14.1 |
|  |  | 4 | –2.46 | 4.83 | 0.998 | –19.1 | 14.1 |
|  |  | 5 | –2.8 | 5.04 | 0.997 | –20.1 | 14.5 |
|  |  | 6 | 0.23 | 4.54 | 1 | –15.4 | 15.8 |
|  | 4 | 1 | 6.22 | 4.04 | 0.795 | –7.7 | 20.1 |
|  |  | 2 | 3.39 | 3.54 | 0.968 | –8.8 | 15.5 |
|  |  | 3 | 2.46 | 4.83 | 0.998 | –14.1 | 19.1 |
|  |  | 5 | –0.34 | 4.83 | 1 | –16.9 | 16.2 |
|  |  | 6 | 2.69 | 4.3 | 0.995 | –12.1 | 17.5 |
|  | 5 | 1 | 6.56 | 4.3 | 0.801 | –8.2 | 21.3 |
|  |  | 2 | 3.72 | 3.82 | 0.965 | –9.4 | 16.9 |
|  |  | 3 | 2.8 | 5.04 | 0.997 | –14.5 | 20.1 |
|  |  | 4 | 0.34 | 4.83 | 1 | –16.2 | 16.9 |
|  |  | 6 | 3.03 | 4.54 | 0.994 | –12.6 | 18.6 |
|  | 6 | 1 | 3.53 | 3.7 | 0.969 | –9.2 | 16.3 |
|  |  | 2 | 0.7 | 3.14 | 1 | –10.1 | 11.5 |
|  |  | 3 | –0.23 | 4.54 | 1 | –15.8 | 15.4 |
|  |  | 4 | –2.69 | 4.3 | 0.995 | –17.5 | 12.1 |
|  |  | 5 | –3.03 | 4.54 | 0.994 | –18.6 | 12.6 |
| Feldspars | 1 | 2 | –0.31 | 0.49 | 0.995 | –2 | 1.4 |
|  |  | 3 | 0.05 | 0.76 | 1 | –2.5 | 2.7 |
|  |  | 4 | 0.48 | 0.71 | 0.994 | –2 | 2.9 |
|  |  | 5 | –0.76 | 0.76 | 0.961 | –3.4 | 1.8 |
|  |  | 6 | –1.08 | 0.65 | 0.735 | –3.3 | 1.2 |
|  | 2 | 1 | 0.31 | 0.49 | 0.995 | –1.4 | 2 |
|  |  | 3 | 0.36 | 0.67 | 0.998 | –1.9 | 2.7 |
|  |  | 4 | 0.78 | 0.62 | 0.9 | –1.4 | 2.9 |
|  |  | 5 | –0.45 | 0.67 | 0.994 | –2.8 | 1.9 |
|  |  | 6 | –0.77 | 0.55 | 0.851 | –2.7 | 1.1 |
|  | 3 | 1 | –0.05 | 0.76 | 1 | –2.7 | 2.5 |
|  |  | 2 | –0.36 | 0.67 | 0.998 | –2.7 | 1.9 |
|  |  | 4 | 0.42 | 0.85 | 0.998 | –2.5 | 3.3 |
|  |  | 5 | –0.81 | 0.89 | 0.973 | –3.9 | 2.2 |
|  |  | 6 | –1.14 | 0.8 | 0.843 | –3.9 | 1.6 |
|  | 4 | 1 | –0.48 | 0.71 | 0.994 | –2.9 | 2 |
|  |  | 2 | –0.78 | 0.62 | 0.9 | –2.9 | 1.4 |
|  |  | 3 | –0.42 | 0.85 | 0.998 | –3.3 | 2.5 |
|  |  | 5 | –1.23 | 0.85 | 0.832 | –4.2 | 1.7 |
|  |  | 6 | –1.56 | 0.76 | 0.521 | –4.2 | 1 |
|  | 5 | 1 | 0.76 | 0.76 | 0.961 | –1.8 | 3.4 |
|  |  | 2 | 0.45 | 0.67 | 0.994 | –1.9 | 2.8 |
|  |  | 3 | 0.81 | 0.89 | 0.973 | –2.2 | 3.9 |
|  |  | 4 | 1.23 | 0.85 | 0.832 | –1.7 | 4.2 |
|  |  | 6 | –0.33 | 0.8 | 0.999 | –3.1 | 2.4 |
|  | 6 | 1 | 1.08 | 0.65 | 0.735 | –1.2 | 3.3 |
|  |  | 2 | 0.77 | 0.55 | 0.851 | –1.1 | 2.7 |
|  |  | 3 | 1.14 | 0.8 | 0.843 | –1.6 | 3.9 |
|  |  | 4 | 1.56 | 0.76 | 0.521 | –1 | 4.2 |
|  |  | 5 | 0.33 | 0.8 | 0.999 | –2.4 | 3.1 |
| Calcite | 1 | 2 | 2.95 | 5.42 | 0.998 | –15.7 | 21.6 |
|  |  | 3 | 5.49 | 8.39 | 0.994 | –23.4 | 34.3 |
|  |  | 4 | 21.53 | 7.9 | 0.207 | –5.6 | 48.7 |
|  |  | 5 | 7.36 | 8.39 | 0.978 | –21.5 | 36.2 |
|  |  | 6 | 2.48 | 7.23 | 1 | –22.4 | 27.3 |
|  | 2 | 1 | –2.95 | 5.42 | 0.998 | –21.6 | 15.7 |
|  |  | 3 | 2.54 | 7.47 | 1 | –23.1 | 28.2 |
|  |  | 4 | 18.58 | 6.91 | 0.22 | –5.2 | 42.3 |
|  |  | 5 | 4.41 | 7.47 | 0.996 | –21.3 | 30.1 |
|  |  | 6 | –0.47 | 6.13 | 1 | –21.6 | 20.6 |
|  | 3 | 1 | –5.49 | 8.39 | 0.994 | –34.3 | 23.4 |
|  |  | 2 | –2.54 | 7.47 | 1 | –28.2 | 23.1 |
|  |  | 4 | 16.04 | 9.42 | 0.716 | –16.4 | 48.4 |
|  |  | 5 | 1.87 | 9.84 | 1 | –32 | 35.7 |
|  |  | 6 | –3.02 | 8.87 | 1 | –33.5 | 27.5 |
|  | 4 | 1 | –21.53 | 7.9 | 0.207 | –48.7 | 5.6 |
|  |  | 2 | –18.58 | 6.91 | 0.22 | –42.3 | 5.2 |
|  |  | 3 | –16.04 | 9.42 | 0.716 | –48.4 | 16.4 |
|  |  | 5 | –14.17 | 9.42 | 0.81 | –46.6 | 18.2 |
|  |  | 6 | –19.05 | 8.4 | 0.409 | –47.9 | 9.8 |
|  | 5 | 1 | –7.36 | 8.39 | 0.978 | –36.2 | 21.5 |
|  |  | 2 | –4.41 | 7.47 | 0.996 | –30.1 | 21.3 |
|  |  | 3 | –1.87 | 9.84 | 1 | –35.7 | 32 |
|  |  | 4 | 14.17 | 9.42 | 0.81 | –18.2 | 46.6 |
|  |  | 6 | –4.88 | 8.87 | 0.997 | –35.4 | 25.6 |
|  | 6 | 1 | –2.48 | 7.23 | 1 | –27.3 | 22.4 |
|  |  | 2 | 0.47 | 6.13 | 1 | –20.6 | 21.6 |
|  |  | 3 | 3.02 | 8.87 | 1 | –27.5 | 33.5 |
|  |  | 4 | 19.05 | 8.4 | 0.409 | –9.8 | 47.9 |
|  |  | 5 | 4.88 | 8.87 | 0.997 | –25.6 | 35.4 |
| Dolomite | 1 | 2 | 0.11 | 0.33 | 1 | –1 | 1.2 |
|  |  | 3 | 0.05 | 0.51 | 1 | –1.7 | 1.8 |
|  |  | 4 | –0.8 | 0.48 | 0.731 | –2.4 | 0.8 |
|  |  | 5 | –1.91 | 0.51 | 0.023 | –3.7 | –0.2 |
|  |  | 6 | 0.19 | 0.44 | 0.999 | –1.3 | 1.7 |
|  | 2 | 1 | –0.11 | 0.33 | 1 | –1.2 | 1 |
|  |  | 3 | –0.06 | 0.45 | 1 | –1.6 | 1.5 |
|  |  | 4 | –0.91 | 0.42 | 0.461 | –2.3 | 0.5 |
|  |  | 5 | –2.02 | 0.45 | 0.003 | –3.6 | –0.5 |
|  |  | 6 | 0.08 | 0.37 | 1 | –1.2 | 1.4 |
|  | 3 | 1 | –0.05 | 0.51 | 1 | –1.8 | 1.7 |
|  |  | 2 | 0.06 | 0.45 | 1 | –1.5 | 1.6 |
|  |  | 4 | –0.85 | 0.57 | 0.82 | –2.8 | 1.1 |
|  |  | 5 | –1.96 | 0.6 | 0.071 | –4 | 0.1 |
|  |  | 6 | 0.14 | 0.54 | 1 | –1.7 | 2 |
|  | 4 | 1 | 0.8 | 0.48 | 0.731 | –0.8 | 2.4 |
|  |  | 2 | 0.91 | 0.42 | 0.461 | –0.5 | 2.3 |
|  |  | 3 | 0.85 | 0.57 | 0.82 | –1.1 | 2.8 |
|  |  | 5 | –1.11 | 0.57 | 0.586 | –3.1 | 0.9 |
|  |  | 6 | 0.99 | 0.51 | 0.587 | –0.8 | 2.7 |
|  | 5 | 1 | 1.91 | 0.51 | 0.023 | 0.2 | 3.7 |
|  |  | 2 | 2.02 | 0.45 | 0.003 | 0.5 | 3.6 |
|  |  | 3 | 1.96 | 0.6 | 0.071 | –0.1 | 4 |
|  |  | 4 | 1.11 | 0.57 | 0.586 | –0.9 | 3.1 |
|  |  | 6 | 2.1 | 0.54 | 0.016 | 0.3 | 4 |
|  | 6 | 1 | –0.19 | 0.44 | 0.999 | –1.7 | 1.3 |
|  |  | 2 | –0.08 | 0.37 | 1 | –1.4 | 1.2 |
|  |  | 3 | –0.14 | 0.54 | 1 | –2 | 1.7 |
|  |  | 4 | –0.99 | 0.51 | 0.587 | –2.7 | 0.8 |
|  |  | 5 | –2.1 | 0.54 | 0.016 | –4 | –0.3 |
| Pyrite | 1 | 2 | 0.08 | 0.07 | 0.949 | –0.2 | 0.3 |
|  |  | 3 | –0.17 | 0.11 | 0.811 | –0.6 | 0.2 |
|  |  | 4 | 0.08 | 0.11 | 0.99 | –0.3 | 0.5 |
|  |  | 5 | 0.17 | 0.11 | 0.818 | –0.2 | 0.6 |
|  |  | 6 | 0.15 | 0.1 | 0.797 | –0.2 | 0.5 |
|  | 2 | 1 | –0.08 | 0.07 | 0.949 | –0.3 | 0.2 |
|  |  | 3 | –0.25 | 0.1 | 0.314 | –0.6 | 0.1 |
|  |  | 4 | 0 | 0.09 | 1 | –0.3 | 0.3 |
|  |  | 5 | 0.09 | 0.1 | 0.976 | –0.3 | 0.4 |
|  |  | 6 | 0.07 | 0.08 | 0.979 | –0.2 | 0.4 |
|  | 3 | 1 | 0.17 | 0.11 | 0.811 | –0.2 | 0.6 |
|  |  | 2 | 0.25 | 0.1 | 0.314 | –0.1 | 0.6 |
|  |  | 4 | 0.25 | 0.13 | 0.576 | –0.2 | 0.7 |
|  |  | 5 | 0.34 | 0.13 | 0.276 | –0.1 | 0.8 |
|  |  | 6 | 0.32 | 0.12 | 0.227 | –0.1 | 0.7 |
|  | 4 | 1 | –0.08 | 0.11 | 0.99 | –0.5 | 0.3 |
|  |  | 2 | 0 | 0.09 | 1 | –0.3 | 0.3 |
|  |  | 3 | –0.25 | 0.13 | 0.576 | –0.7 | 0.2 |
|  |  | 5 | 0.09 | 0.13 | 0.992 | –0.4 | 0.5 |
|  |  | 6 | 0.07 | 0.12 | 0.995 | –0.3 | 0.5 |
|  | 5 | 1 | –0.17 | 0.11 | 0.818 | –0.6 | 0.2 |
|  |  | 2 | –0.09 | 0.1 | 0.976 | –0.4 | 0.3 |
|  |  | 3 | –0.34 | 0.13 | 0.276 | –0.8 | 0.1 |
|  |  | 4 | –0.09 | 0.13 | 0.992 | –0.5 | 0.4 |
|  |  | 6 | –0.02 | 0.12 | 1 | –0.4 | 0.4 |
|  | 6 | 1 | –0.15 | 0.1 | 0.797 | –0.5 | 0.2 |
|  |  | 2 | –0.07 | 0.08 | 0.979 | –0.4 | 0.2 |
|  |  | 3 | –0.32 | 0.12 | 0.227 | –0.7 | 0.1 |
|  |  | 4 | –0.07 | 0.12 | 0.995 | –0.5 | 0.3 |
|  |  | 5 | 0.02 | 0.12 | 1 | –0.4 | 0.4 |
| Hematite | 1 | 2 | –0.18 | 0.17 | 0.954 | –0.8 | 0.4 |
|  |  | 3 | –0.11 | 0.26 | 0.999 | –1 | 0.8 |
|  |  | 4 | –0.63 | 0.24 | 0.255 | –1.5 | 0.2 |
|  |  | 5 | 0.21 | 0.26 | 0.986 | –0.7 | 1.1 |
|  |  | 6 | 0 | 0.22 | 1 | –0.8 | 0.8 |
|  | 2 | 1 | 0.18 | 0.17 | 0.954 | –0.4 | 0.8 |
|  |  | 3 | 0.07 | 0.23 | 1 | –0.7 | 0.9 |
|  |  | 4 | –0.46 | 0.21 | 0.47 | –1.2 | 0.3 |
|  |  | 5 | 0.38 | 0.23 | 0.745 | –0.4 | 1.2 |
|  |  | 6 | 0.17 | 0.19 | 0.975 | –0.5 | 0.8 |
|  | 3 | 1 | 0.11 | 0.26 | 0.999 | –0.8 | 1 |
|  |  | 2 | –0.07 | 0.23 | 1 | –0.9 | 0.7 |
|  |  | 4 | –0.53 | 0.29 | 0.656 | –1.5 | 0.5 |
|  |  | 5 | 0.31 | 0.3 | 0.958 | –0.7 | 1.4 |
|  |  | 6 | 0.1 | 0.27 | 1 | –0.8 | 1 |
|  | 4 | 1 | 0.63 | 0.24 | 0.255 | –0.2 | 1.5 |
|  |  | 2 | 0.46 | 0.21 | 0.47 | –0.3 | 1.2 |
|  |  | 3 | 0.53 | 0.29 | 0.656 | –0.5 | 1.5 |
|  |  | 5 | 0.84 | 0.29 | 0.158 | –0.2 | 1.8 |
|  |  | 6 | 0.63 | 0.26 | 0.329 | –0.3 | 1.5 |
|  | 5 | 1 | –0.21 | 0.26 | 0.986 | –1.1 | 0.7 |
|  |  | 2 | –0.38 | 0.23 | 0.745 | –1.2 | 0.4 |
|  |  | 3 | –0.31 | 0.3 | 0.958 | –1.4 | 0.7 |
|  |  | 4 | –0.84 | 0.29 | 0.158 | –1.8 | 0.2 |
|  |  | 6 | –0.21 | 0.27 | 0.989 | –1.2 | 0.7 |
|  | 6 | 1 | 0 | 0.22 | 1 | –0.8 | 0.8 |
|  |  | 2 | –0.17 | 0.19 | 0.975 | –0.8 | 0.5 |
|  |  | 3 | –0.1 | 0.27 | 1 | –1 | 0.8 |
|  |  | 4 | –0.63 | 0.26 | 0.329 | –1.5 | 0.3 |
|  |  | 5 | 0.21 | 0.27 | 0.989 | –0.7 | 1.2 |
| Gypsum | 1 | 2 | 0.14 | 2.2 | 1 | –7.4 | 7.7 |
|  |  | 3 | 0.22 | 3.4 | 1 | –11.5 | 11.9 |
|  |  | 4 | –10.45 | 3.2 | 0.074 | –21.5 | 0.6 |
|  |  | 5 | –26.23 | 3.4 | 0 | –37.9 | –14.5 |
|  |  | 6 | 0.22 | 2.93 | 1 | –9.9 | 10.3 |
|  | 2 | 1 | –0.14 | 2.2 | 1 | –7.7 | 7.4 |
|  |  | 3 | 0.08 | 3.03 | 1 | –10.3 | 10.5 |
|  |  | 4 | –10.58 | 2.8 | 0.022 | –20.2 | –1 |
|  |  | 5 | –26.367 | 3.03 | 0 | –36.8 | –16 |
|  |  | 6 | 0.08 | 2.49 | 1 | –8.5 | 8.6 |
|  | 3 | 1 | –0.22 | 3.4 | 1 | –11.9 | 11.5 |
|  |  | 2 | –0.08 | 3.03 | 1 | –10.5 | 10.3 |
|  |  | 4 | –10.67 | 3.82 | 0.185 | –23.8 | 2.5 |
|  |  | 5 | –26.45 | 3.99 | 0 | –40.2 | –12.7 |
|  |  | 6 | 0 | 3.6 | 1 | –12.4 | 12.4 |
|  | 4 | 1 | 10.45 | 3.2 | 0.074 | –0.6 | 21.5 |
|  |  | 2 | 10.58 | 2.8 | 0.022 | 1 | 20.2 |
|  |  | 3 | 10.67 | 3.82 | 0.185 | –2.5 | 23.8 |
|  |  | 5 | –15.78 | 3.82 | 0.009 | –28.9 | –2.7 |
|  |  | 6 | 10.67 | 3.41 | 0.097 | –1 | 22.4 |
|  | 5 | 1 | 26.23 | 3.4 | 0 | 14.5 | 37.9 |
|  |  | 2 | 26.37 | 3.03 | 0 | 16 | 36.8 |
|  |  | 3 | 26.45 | 3.99 | 0 | 12.7 | 40.2 |
|  |  | 4 | 15.78 | 3.82 | 0.009 | 2.7 | 28.9 |
|  |  | 6 | 26.45 | 3.6 | 0 | 14.1 | 38.8 |
|  | 6 | 1 | –0.22 | 2.93 | 1 | –10.3 | 9.9 |
|  |  | 2 | –0.08 | 2.49 | 1 | –8.6 | 8.5 |
|  |  | 3 | 0 | 3.6 | 1 | –12.4 | 12.4 |
|  |  | 4 | –10.67 | 3.41 | 0.097 | –22.4 | 1 |
|  |  | 5 | –26.45 | 3.6 | 0 | –38.8 | –14.1 |
| Siderite | 1 | 2 | –0.13 | 0.16 | 0.985 | –0.7 | 0.4 |
|  |  | 3 | 0 | 0.24 | 1 | –0.8 | 0.8 |
|  |  | 4 | 0 | 0.23 | 1 | –0.8 | 0.8 |
|  |  | 5 | 0 | 0.24 | 1 | –0.8 | 0.8 |
|  |  | 6 | –0.53 | 0.21 | 0.271 | –1.2 | 0.2 |
|  | 2 | 1 | 0.13 | 0.16 | 0.985 | –0.4 | 0.7 |
|  |  | 3 | 0.13 | 0.21 | 0.997 | –0.6 | 0.9 |
|  |  | 4 | 0.13 | 0.2 | 0.995 | –0.6 | 0.8 |
|  |  | 5 | 0.13 | 0.21 | 0.997 | –0.6 | 0.9 |
|  |  | 6 | –0.4 | 0.18 | 0.389 | –1 | 0.2 |
|  | 3 | 1 | 0 | 0.24 | 1 | –0.8 | 0.8 |
|  |  | 2 | –0.13 | 0.21 | 0.997 | –0.9 | 0.6 |
|  |  | 4 | 0 | 0.27 | 1 | –0.9 | 0.9 |
|  |  | 5 | 0 | 0.28 | 1 | –1 | 1 |
|  |  | 6 | –0.53 | 0.25 | 0.506 | –1.4 | 0.3 |
|  | 4 | 1 | 0 | 0.23 | 1 | –0.8 | 0.8 |
|  |  | 2 | –0.13 | 0.2 | 0.995 | –0.8 | 0.6 |
|  |  | 3 | 0 | 0.27 | 1 | –0.9 | 0.9 |
|  |  | 5 | 0 | 0.27 | 1 | –0.9 | 0.9 |
|  |  | 6 | –0.53 | 0.24 | 0.443 | –1.4 | 0.3 |
|  | 5 | 1 | 0 | 0.24 | 1 | –0.8 | 0.8 |
|  |  | 2 | –0.13 | 0.21 | 0.997 | –0.9 | 0.6 |
|  |  | 3 | 0 | 0.28 | 1 | –1 | 1 |
|  |  | 4 | 0 | 0.27 | 1 | –0.9 | 0.9 |
|  |  | 6 | –0.53 | 0.25 | 0.506 | –1.4 | 0.3 |
|  | 6 | 1 | 0.53 | 0.21 | 0.271 | –0.2 | 1.2 |
|  |  | 2 | 0.4 | 0.18 | 0.389 | –0.2 | 1 |
|  |  | 3 | 0.53 | 0.25 | 0.506 | –0.3 | 1.4 |
|  |  | 4 | 0.53 | 0.24 | 0.443 | –0.3 | 1.4 |
|  |  | 5 | 0.53 | 0.25 | 0.506 | –0.3 | 1.4 |
| Kaolinite | 1 | 2 | –4.03 | 2.46 | 0.749 | –12.5 | 4.4 |
|  |  | 3 | –4.08 | 3.82 | 0.949 | –17.2 | 9 |
|  |  | 4 | –2.91 | 3.59 | 0.985 | –15.3 | 9.4 |
|  |  | 5 | 4.32 | 3.82 | 0.935 | –8.8 | 17.4 |
|  |  | 6 | –8.89 | 3.29 | 0.215 | –20.2 | 2.4 |
|  | 2 | 1 | 4.03 | 2.46 | 0.749 | –4.4 | 12.5 |
|  |  | 3 | –0.05 | 3.4 | 1 | –11.7 | 11.6 |
|  |  | 4 | 1.12 | 3.14 | 1 | –9.7 | 11.9 |
|  |  | 5 | 8.35 | 3.4 | 0.316 | –3.3 | 20 |
|  |  | 6 | –4.86 | 2.79 | 0.695 | –14.4 | 4.7 |
|  | 3 | 1 | 4.08 | 3.82 | 0.949 | –9 | 17.2 |
|  |  | 2 | 0.05 | 3.4 | 1 | –11.6 | 11.7 |
|  |  | 4 | 1.17 | 4.28 | 1 | –13.6 | 15.9 |
|  |  | 5 | 8.4 | 4.48 | 0.622 | –7 | 23.8 |
|  |  | 6 | –4.81 | 4.03 | 0.92 | –18.7 | 9.1 |
|  | 4 | 1 | 2.91 | 3.59 | 0.985 | –9.4 | 15.3 |
|  |  | 2 | –1.12 | 3.14 | 1 | –11.9 | 9.7 |
|  |  | 3 | –1.17 | 4.28 | 1 | –15.9 | 13.6 |
|  |  | 5 | 7.23 | 4.28 | 0.723 | –7.5 | 22 |
|  |  | 6 | –5.98 | 3.82 | 0.783 | –19.1 | 7.2 |
|  | 5 | 1 | –4.32 | 3.82 | 0.935 | –17.4 | 8.8 |
|  |  | 2 | –8.35 | 3.4 | 0.316 | –20 | 3.3 |
|  |  | 3 | –8.4 | 4.48 | 0.622 | –23.8 | 7 |
|  |  | 4 | –7.23 | 4.28 | 0.723 | –22 | 7.5 |
|  |  | 6 | –13.21 | 4.03 | 0.072 | –27.1 | 0.7 |
|  | 6 | 1 | 8.89 | 3.29 | 0.215 | –2.4 | 20.2 |
|  |  | 2 | 4.86 | 2.79 | 0.695 | –4.7 | 14.4 |
|  |  | 3 | 4.81 | 4.03 | 0.92 | –9.1 | 18.7 |
|  |  | 4 | 5.98 | 3.82 | 0.783 | –7.2 | 19.1 |
|  |  | 5 | 13.21 | 4.03 | 0.072 | –0.7 | 27.1 |
| Illite | 1 | 2 | 8.97 | 3.92 | 0.399 | –4.5 | 22.4 |
|  |  | 3 | 7.15 | 6.08 | 0.924 | –13.7 | 28 |
|  |  | 4 | 6.46 | 5.72 | 0.936 | –13.2 | 26.1 |
|  |  | 5 | 22.86 | 6.08 | 0.023 | 2 | 43.8 |
|  |  | 6 | 9.79 | 5.23 | 0.626 | –8.2 | 27.8 |
|  | 2 | 1 | –8.97 | 3.92 | 0.399 | –22.4 | 4.5 |
|  |  | 3 | –1.82 | 5.41 | 1 | –20.4 | 16.8 |
|  |  | 4 | –2.51 | 5 | 0.998 | –19.7 | 14.7 |
|  |  | 5 | 13.9 | 5.41 | 0.267 | –4.7 | 32.5 |
|  |  | 6 | 0.82 | 4.44 | 1 | –14.4 | 16.1 |
|  | 3 | 1 | –7.15 | 6.08 | 0.924 | –28 | 13.7 |
|  |  | 2 | 1.82 | 5.41 | 1 | –16.8 | 20.4 |
|  |  | 4 | –0.69 | 6.82 | 1 | –24.1 | 22.8 |
|  |  | 5 | 15.72 | 7.12 | 0.441 | –8.8 | 40.2 |
|  |  | 6 | 2.64 | 6.42 | 0.999 | –19.4 | 24.7 |
|  | 4 | 1 | –6.46 | 5.72 | 0.936 | –26.1 | 13.2 |
|  |  | 2 | 2.51 | 5 | 0.998 | –14.7 | 19.7 |
|  |  | 3 | 0.69 | 6.82 | 1 | –22.8 | 24.1 |
|  |  | 5 | 16.41 | 6.82 | 0.34 | –7 | 39.9 |
|  |  | 6 | 3.33 | 6.08 | 0.998 | –17.6 | 24.2 |
|  | 5 | 1 | –22.86 | 6.08 | 0.023 | –43.8 | –2 |
|  |  | 2 | –13.9 | 5.41 | 0.267 | –32.5 | 4.7 |
|  |  | 3 | –15.72 | 7.12 | 0.441 | –40.2 | 8.8 |
|  |  | 4 | –16.41 | 6.82 | 0.34 | –39.9 | 7 |
|  |  | 6 | –13.07 | 6.42 | 0.534 | –35.2 | 9 |
|  | 6 | 1 | –9.79 | 5.23 | 0.626 | –27.8 | 8.2 |
|  |  | 2 | –0.82 | 4.44 | 1 | –16.1 | 14.4 |
|  |  | 3 | –2.64 | 6.42 | 0.999 | –24.7 | 19.4 |
|  |  | 4 | –3.33 | 6.08 | 0.998 | –24.2 | 17.6 |
|  |  | 5 | 13.07 | 6.42 | 0.534 | –9 | 35.2 |
| Chlorite | 1 | 2 | –2.85 | 1.59 | 0.668 | –8.3 | 2.6 |
|  |  | 3 | –3.59 | 2.46 | 0.83 | –12.1 | 4.9 |
|  |  | 4 | –2.89 | 2.32 | 0.905 | –10.9 | 5.1 |
|  |  | 5 | 1.2 | 2.46 | 0.999 | –7.3 | 9.7 |
|  |  | 6 | –3.03 | 2.12 | 0.842 | –10.3 | 4.3 |
|  | 2 | 1 | 2.85 | 1.59 | 0.668 | –2.6 | 8.3 |
|  |  | 3 | –0.74 | 2.19 | 1 | –8.3 | 6.8 |
|  |  | 4 | –0.04 | 2.03 | 1 | –7 | 6.9 |
|  |  | 5 | 4.05 | 2.19 | 0.639 | –3.5 | 11.6 |
|  |  | 6 | –0.18 | 1.8 | 1 | –6.4 | 6 |
|  | 3 | 1 | 3.59 | 2.46 | 0.83 | –4.9 | 12.1 |
|  |  | 2 | 0.74 | 2.19 | 1 | –6.8 | 8.3 |
|  |  | 4 | 0.7 | 2.77 | 1 | –8.8 | 10.2 |
|  |  | 5 | 4.79 | 2.89 | 0.738 | –5.1 | 14.7 |
|  |  | 6 | 0.56 | 2.6 | 1 | –8.4 | 9.5 |
|  | 4 | 1 | 2.89 | 2.32 | 0.905 | –5.1 | 10.9 |
|  |  | 2 | 0.04 | 2.03 | 1 | –6.9 | 7 |
|  |  | 3 | –0.7 | 2.77 | 1 | –10.2 | 8.8 |
|  |  | 5 | 4.08 | 2.77 | 0.822 | –5.4 | 13.6 |
|  |  | 6 | –0.14 | 2.47 | 1 | –8.6 | 8.3 |
|  | 5 | 1 | –1.2 | 2.46 | 0.999 | –9.7 | 7.3 |
|  |  | 2 | –4.05 | 2.19 | 0.639 | –11.6 | 3.5 |
|  |  | 3 | –4.79 | 2.89 | 0.738 | –14.7 | 5.1 |
|  |  | 4 | –4.08 | 2.77 | 0.822 | –13.6 | 5.4 |
|  |  | 6 | –4.23 | 2.6 | 0.755 | –13.2 | 4.7 |
|  | 6 | 1 | 3.03 | 2.12 | 0.842 | –4.3 | 10.3 |
|  |  | 2 | 0.18 | 1.8 | 1 | –6 | 6.4 |
|  |  | 3 | –0.56 | 2.6 | 1 | –9.5 | 8.4 |
|  |  | 4 | 0.14 | 2.47 | 1 | –8.3 | 8.6 |
|  |  | 5 | 4.23 | 2.6 | 0.755 | –4.7 | 13.2 |
| Smectite | 1 | 2 | –5.06 | 2.6 | 0.582 | –14 | 3.9 |
|  |  | 3 | –1.28 | 4.02 | 1 | –15.1 | 12.6 |
|  |  | 4 | –4.19 | 3.79 | 0.941 | –17.2 | 8.8 |
|  |  | 5 | –0.98 | 4.02 | 1 | –14.8 | 12.9 |
|  |  | 6 | –3.15 | 3.47 | 0.974 | –15.1 | 8.8 |
|  | 2 | 1 | 5.06 | 2.6 | 0.582 | –3.9 | 14 |
|  |  | 3 | 3.78 | 3.58 | 0.951 | –8.5 | 16.1 |
|  |  | 4 | 0.88 | 3.31 | 1 | –10.5 | 12.3 |
|  |  | 5 | 4.09 | 3.58 | 0.933 | –8.2 | 16.4 |
|  |  | 6 | 1.91 | 2.94 | 0.994 | –8.2 | 12 |
|  | 3 | 1 | 1.28 | 4.02 | 1 | –12.6 | 15.1 |
|  |  | 2 | –3.78 | 3.58 | 0.951 | –16.1 | 8.5 |
|  |  | 4 | –2.9 | 4.52 | 0.995 | –18.4 | 12.6 |
|  |  | 5 | 0.31 | 4.72 | 1 | –15.9 | 16.5 |
|  |  | 6 | –1.87 | 4.25 | 0.999 | –16.5 | 12.8 |
|  | 4 | 1 | 4.19 | 3.79 | 0.941 | –8.8 | 17.2 |
|  |  | 2 | –0.88 | 3.31 | 1 | –12.3 | 10.5 |
|  |  | 3 | 2.9 | 4.52 | 0.995 | –12.6 | 18.4 |
|  |  | 5 | 3.21 | 4.52 | 0.992 | –12.3 | 18.7 |
|  |  | 6 | 1.04 | 4.03 | 1 | –12.8 | 14.9 |
|  | 5 | 1 | 0.98 | 4.02 | 1 | –12.9 | 14.8 |
|  |  | 2 | –4.09 | 3.58 | 0.933 | –16.4 | 8.2 |
|  |  | 3 | –0.31 | 4.72 | 1 | –16.5 | 15.9 |
|  |  | 4 | –3.21 | 4.52 | 0.992 | –18.7 | 12.3 |
|  |  | 6 | –2.17 | 4.25 | 0.998 | –16.8 | 12.5 |
|  | 6 | 1 | 3.15 | 3.47 | 0.974 | –8.8 | 15.1 |
|  |  | 2 | –1.91 | 2.94 | 0.994 | –12 | 8.2 |
|  |  | 3 | 1.87 | 4.25 | 0.999 | –12.8 | 16.5 |
|  |  | 4 | –1.04 | 4.03 | 1 | –14.9 | 12.8 |
|  |  | 5 | 2.17 | 4.25 | 0.998 | –12.5 | 16.8 |
| K–f1 | 1 | 2 | –11.61 | 4.19 | 0.191 | –26 | 2.8 |
|  |  | 3 | –12.57 | 6.48 | 0.588 | –34.9 | 9.7 |
|  |  | 4 | –8.33 | 6.1 | 0.865 | –29.3 | 12.6 |
|  |  | 5 | –8.86 | 6.48 | 0.865 | –31.1 | 13.4 |
|  |  | 6 | –15.33 | 5.59 | 0.201 | –34.5 | 3.9 |
|  | 2 | 1 | 11.61 | 4.19 | 0.191 | –2.8 | 26 |
|  |  | 3 | –0.96 | 5.77 | 1 | –20.8 | 18.9 |
|  |  | 4 | 3.28 | 5.34 | 0.996 | –15.1 | 21.6 |
|  |  | 5 | 2.75 | 5.77 | 0.999 | –17.1 | 22.6 |
|  |  | 6 | –3.72 | 4.74 | 0.987 | –20 | 12.6 |
|  | 3 | 1 | 12.57 | 6.48 | 0.588 | –9.7 | 34.9 |
|  |  | 2 | 0.96 | 5.77 | 1 | –18.9 | 20.8 |
|  |  | 4 | 4.24 | 7.28 | 0.997 | –20.8 | 29.3 |
|  |  | 5 | 3.71 | 7.6 | 0.999 | –22.4 | 29.8 |
|  |  | 6 | –2.76 | 6.85 | 0.999 | –26.3 | 20.8 |
|  | 4 | 1 | 8.33 | 6.1 | 0.865 | –12.6 | 29.3 |
|  |  | 2 | –3.28 | 5.34 | 0.996 | –21.6 | 15.1 |
|  |  | 3 | –4.24 | 7.28 | 0.997 | –29.3 | 20.8 |
|  |  | 5 | –0.53 | 7.28 | 1 | –25.5 | 24.5 |
|  |  | 6 | –7 | 6.49 | 0.947 | –29.3 | 15.3 |
|  | 5 | 1 | 8.86 | 6.48 | 0.865 | –13.4 | 31.1 |
|  |  | 2 | –2.75 | 5.77 | 0.999 | –22.6 | 17.1 |
|  |  | 3 | –3.71 | 7.6 | 0.999 | –29.8 | 22.4 |
|  |  | 4 | 0.53 | 7.28 | 1 | –24.5 | 25.5 |
|  |  | 6 | –6.47 | 6.85 | 0.97 | –30 | 17.1 |
|  | 6 | 1 | 15.33 | 5.59 | 0.201 | –3.9 | 34.5 |
|  |  | 2 | 3.72 | 4.74 | 0.987 | –12.6 | 20 |
|  |  | 3 | 2.76 | 6.85 | 0.999 | –20.8 | 26.3 |
|  |  | 4 | 7 | 6.49 | 0.947 | –15.3 | 29.3 |
|  |  | 5 | 6.47 | 6.85 | 0.97 | –17.1 | 30 |
| I–f1 | 1 | 2 | 20.12 | 6.08 | 0.066 | –0.8 | 41 |
| (illte in the clay |  | 3 | 16.04 | 9.42 | 0.715 | –16.3 | 48.4 |
| fraction) |  | 4 | 21.79 | 8.86 | 0.315 | –8.7 | 52.3 |
|  |  | 5 | 22.2 | 9.42 | 0.364 | –10.2 | 54.6 |
|  |  | 6 | 28.89 | 8.11 | 0.038 | 1 | 56.8 |
|  | 2 | 1 | –20.12 | 6.08 | 0.066 | –41 | 0.8 |
|  |  | 3 | –4.08 | 8.38 | 0.999 | –32.9 | 24.7 |
|  |  | 4 | 1.67 | 7.75 | 1 | –25 | 28.3 |
|  |  | 5 | 2.08 | 8.38 | 1 | –26.7 | 30.9 |
|  |  | 6 | 8.77 | 6.88 | 0.896 | –14.9 | 32.4 |
|  | 3 | 1 | –16.04 | 9.42 | 0.715 | –48.4 | 16.3 |
|  |  | 2 | 4.08 | 8.38 | 0.999 | –24.7 | 32.9 |
|  |  | 4 | 5.75 | 10.57 | 0.998 | –30.6 | 42.1 |
|  |  | 5 | 6.16 | 11.04 | 0.997 | –31.8 | 44.1 |
|  |  | 6 | 12.85 | 9.95 | 0.891 | –21.4 | 47.1 |
|  | 4 | 1 | –21.79 | 8.86 | 0.315 | –52.3 | 8.7 |
|  |  | 2 | –1.67 | 7.75 | 1 | –28.3 | 25 |
|  |  | 3 | –5.75 | 10.57 | 0.998 | –42.1 | 30.6 |
|  |  | 5 | 0.41 | 10.57 | 1 | –35.9 | 36.7 |
|  |  | 6 | 7.09 | 9.43 | 0.989 | –25.3 | 39.5 |
|  | 5 | 1 | –22.2 | 9.42 | 0.364 | –54.6 | 10.2 |
|  |  | 2 | –2.08 | 8.38 | 1 | –30.9 | 26.7 |
|  |  | 3 | –6.16 | 11.04 | 0.997 | –44.1 | 31.8 |
|  |  | 4 | –0.41 | 10.57 | 1 | –36.7 | 35.9 |
|  |  | 6 | 6.69 | 9.95 | 0.993 | –27.5 | 40.9 |
|  | 6 | 1 | –28.89 | 8.11 | 0.038 | –56.8 | –1 |
|  |  | 2 | –8.77 | 6.88 | 0.896 | –32.4 | 14.9 |
|  |  | 3 | –12.85 | 9.95 | 0.891 | –47.1 | 21.4 |
|  |  | 4 | –7.09 | 9.43 | 0.989 | –39.5 | 25.3 |
|  |  | 5 | –6.69 | 9.95 | 0.993 | –40.9 | 27.5 |
| Ch–f1 | 1 | 2 | –6.26 | 3 | 0.508 | –16.6 | 4.1 |
| (chlorite |  | 3 | –7.5 | 4.65 | 0.761 | –23.5 | 8.5 |
| in the clay |  | 4 | –6.92 | 4.38 | 0.776 | –22 | 8.1 |
| fraction) |  | 5 | –11.42 | 4.65 | 0.317 | –27.4 | 4.6 |
|  |  | 6 | –6.05 | 4.01 | 0.807 | –19.8 | 7.7 |
|  | 2 | 1 | 6.26 | 3 | 0.508 | –4.1 | 16.6 |
|  |  | 3 | –1.24 | 4.14 | 1 | –15.5 | 13 |
|  |  | 4 | –0.66 | 3.83 | 1 | –13.8 | 12.5 |
|  |  | 5 | –5.17 | 4.14 | 0.904 | –19.4 | 9.1 |
|  |  | 6 | 0.2 | 3.4 | 1 | –11.5 | 11.9 |
|  | 3 | 1 | 7.5 | 4.65 | 0.761 | –8.5 | 23.5 |
|  |  | 2 | 1.24 | 4.14 | 1 | –13 | 15.5 |
|  |  | 4 | 0.58 | 5.22 | 1 | –17.4 | 18.5 |
|  |  | 5 | –3.93 | 5.46 | 0.991 | –22.7 | 14.8 |
|  |  | 6 | 1.44 | 4.92 | 1 | –15.5 | 18.4 |
|  | 4 | 1 | 6.92 | 4.38 | 0.776 | –8.1 | 22 |
|  |  | 2 | 0.66 | 3.83 | 1 | –12.5 | 13.8 |
|  |  | 3 | –0.58 | 5.22 | 1 | –18.5 | 17.4 |
|  |  | 5 | –4.51 | 5.22 | 0.98 | –22.5 | 13.5 |
|  |  | 6 | 0.86 | 4.66 | 1 | –15.2 | 16.9 |
|  | 5 | 1 | 11.42 | 4.65 | 0.317 | –4.6 | 27.4 |
|  |  | 2 | 5.17 | 4.14 | 0.904 | –9.1 | 19.4 |
|  |  | 3 | 3.93 | 5.46 | 0.991 | –14.8 | 22.7 |
|  |  | 4 | 4.51 | 5.22 | 0.98 | –13.5 | 22.5 |
|  |  | 6 | 5.37 | 4.92 | 0.944 | –11.5 | 22.3 |
|  | 6 | 1 | 6.05 | 4.01 | 0.807 | –7.7 | 19.8 |
|  |  | 2 | –0.2 | 3.4 | 1 | –11.9 | 11.5 |
|  |  | 3 | –1.44 | 4.92 | 1 | –18.4 | 15.5 |
|  |  | 4 | –0.86 | 4.66 | 1 | –16.9 | 15.2 |
|  |  | 5 | –5.37 | 4.92 | 0.944 | –22.3 | 11.5 |
| Sm–f1 | 1 | 2 | –9.17 | 4.22 | 0.46 | –23.7 | 5.3 |
| (smectite in |  | 3 | –2.89 | 6.54 | 0.999 | –25.4 | 19.6 |
| the clay |  | 4 | –13.46 | 6.15 | 0.451 | –34.6 | 7.7 |
| fraction) |  | 5 | –8.83 | 6.54 | 0.871 | –31.3 | 13.7 |
|  |  | 6 | –7.19 | 5.63 | 0.896 | –26.6 | 12.2 |
|  | 2 | 1 | 9.17 | 4.22 | 0.46 | –5.3 | 23.7 |
|  |  | 3 | 6.28 | 5.82 | 0.947 | –13.7 | 26.3 |
|  |  | 4 | –4.29 | 5.38 | 0.986 | –22.8 | 14.2 |
|  |  | 5 | 0.34 | 5.82 | 1 | –19.7 | 20.3 |
|  |  | 6 | 1.98 | 4.78 | 0.999 | –14.4 | 18.4 |
|  | 3 | 1 | 2.89 | 6.54 | 0.999 | –19.6 | 25.4 |
|  |  | 2 | –6.28 | 5.82 | 0.947 | –26.3 | 13.7 |
|  |  | 4 | –10.57 | 7.34 | 0.837 | –35.8 | 14.7 |
|  |  | 5 | –5.94 | 7.67 | 0.987 | –32.3 | 20.4 |
|  |  | 6 | –4.3 | 6.91 | 0.995 | –28.1 | 19.5 |
|  | 4 | 1 | 13.46 | 6.15 | 0.451 | –7.7 | 34.6 |
|  |  | 2 | 4.29 | 5.38 | 0.986 | –14.2 | 22.8 |
|  |  | 3 | 10.57 | 7.34 | 0.837 | –14.7 | 35.8 |
|  |  | 5 | 4.63 | 7.34 | 0.995 | –20.6 | 29.9 |
|  |  | 6 | 6.27 | 6.55 | 0.968 | –16.2 | 28.8 |
|  | 5 | 1 | 8.83 | 6.54 | 0.871 | –13.7 | 31.3 |
|  |  | 2 | –0.34 | 5.82 | 1 | –20.3 | 19.7 |
|  |  | 3 | 5.94 | 7.67 | 0.987 | –20.4 | 32.3 |
|  |  | 4 | –4.63 | 7.34 | 0.995 | –29.9 | 20.6 |
|  |  | 6 | 1.64 | 6.91 | 1 | –22.1 | 25.4 |
|  | 6 | 1 | 7.19 | 5.63 | 0.896 | –12.2 | 26.6 |
|  |  | 2 | –1.98 | 4.78 | 0.999 | –18.4 | 14.4 |
|  |  | 3 | 4.3 | 6.91 | 0.995 | –19.5 | 28.1 |
|  |  | 4 | –6.27 | 6.55 | 0.968 | –28.8 | 16.2 |
|  |  | 5 | –1.64 | 6.91 | 1 | –25.4 | 22.1 |
| I+Ch* | 1 | 2 | 13.99 | 6.16 | 0.408 | –7.2 | 35.2 |
| (Illite + chlorite |  | 3 | 8.95 | 9.55 | 0.971 | –23.9 | 41.8 |
| in the clay |  | 4 | 15.28 | 8.98 | 0.716 | –15.6 | 46.2 |
| fraction) |  | 5 | 13.37 | 9.55 | 0.852 | –19.5 | 46.2 |
|  |  | 6 | 18.84 | 8.23 | 0.397 | –9.4 | 47.1 |
|  | 2 | 1 | –13.99 | 6.16 | 0.408 | –35.2 | 7.2 |
|  |  | 3 | –5.04 | 8.5 | 0.996 | –34.2 | 24.2 |
|  |  | 4 | 1.29 | 7.86 | 1 | –25.7 | 28.3 |
|  |  | 5 | –0.62 | 8.5 | 1 | –29.8 | 28.6 |
|  |  | 6 | 4.86 | 6.98 | 0.992 | –19.1 | 28.8 |
|  | 3 | 1 | –8.95 | 9.55 | 0.971 | –41.8 | 23.9 |
|  |  | 2 | 5.04 | 8.5 | 0.996 | –24.2 | 34.2 |
|  |  | 4 | 6.33 | 10.72 | 0.996 | –30.5 | 43.2 |
|  |  | 5 | 4.42 | 11.2 | 0.999 | –34.1 | 42.9 |
|  |  | 6 | 9.9 | 10.09 | 0.964 | –24.8 | 44.6 |
|  | 4 | 1 | –15.28 | 8.98 | 0.716 | –46.2 | 15.6 |
|  |  | 2 | –1.29 | 7.86 | 1 | –28.3 | 25.7 |
|  |  | 3 | –6.33 | 10.72 | 0.996 | –43.2 | 30.5 |
|  |  | 5 | –1.91 | 10.72 | 1 | –38.8 | 34.9 |
|  |  | 6 | 3.56 | 9.56 | 1 | –29.3 | 36.4 |
|  | 5 | 1 | –13.37 | 9.55 | 0.852 | –46.2 | 19.5 |
|  |  | 2 | 0.62 | 8.5 | 1 | –28.6 | 29.8 |
|  |  | 3 | –4.42 | 11.2 | 0.999 | –42.9 | 34.1 |
|  |  | 4 | 1.91 | 10.72 | 1 | –34.9 | 38.8 |
|  |  | 6 | 5.47 | 10.09 | 0.998 | –29.2 | 40.2 |
|  | 6 | 1 | –18.84 | 8.23 | 0.397 | –47.1 | 9.4 |
|  |  | 2 | –4.86 | 6.98 | 0.992 | –28.8 | 19.1 |
|  |  | 3 | –9.9 | 10.09 | 0.964 | –44.6 | 24.8 |
|  |  | 4 | –3.56 | 9.56 | 1 | –36.4 | 29.3 |
|  |  | 5 | –5.47 | 10.09 | 0.998 | –40.2 | 29.2 |
| IChSK_r | 1 | 2 | –0.45 | 0.24 | 0.63 | –1.29 | 0.38 |
|  |  | 3 | –0.08 | 0.38 | 1.00 | –1.37 | 1.22 |
|  |  | 4 | –0.49 | 0.35 | 0.86 | –1.71 | 0.73 |
|  |  | 5 | –0.31 | 0.38 | 0.98 | –1.61 | 0.98 |
|  |  | 6 | –0.28 | 0.32 | 0.98 | –1.40 | 0.83 |
|  | 2 | 1 | 0.45 | 0.24 | 0.63 | –0.38 | 1.29 |
|  |  | 3 | 0.37 | 0.34 | 0.94 | –0.78 | 1.53 |
|  |  | 4 | –0.04 | 0.31 | 1.00 | –1.10 | 1.03 |
|  |  | 5 | 0.14 | 0.34 | 1.00 | –1.01 | 1.29 |
|  |  | 6 | 0.17 | 0.28 | 1.00 | –0.77 | 1.12 |
|  | 3 | 1 | 0.08 | 0.38 | 1.00 | –1.22 | 1.37 |
|  |  | 2 | –0.37 | 0.34 | 0.94 | –1.53 | 0.78 |
|  |  | 4 | –0.41 | 0.42 | 0.97 | –1.87 | 1.04 |
|  |  | 5 | –0.24 | 0.44 | 1.00 | –1.75 | 1.28 |
|  |  | 6 | –0.20 | 0.40 | 1.00 | –1.57 | 1.17 |
|  | 4 | 1 | 0.49 | 0.35 | 0.86 | –0.73 | 1.71 |
|  |  | 2 | 0.04 | 0.31 | 1.00 | –1.03 | 1.10 |
|  |  | 3 | 0.41 | 0.42 | 0.97 | –1.04 | 1.87 |
|  |  | 5 | 0.18 | 0.42 | 1.00 | –1.28 | 1.63 |
|  |  | 6 | 0.21 | 0.38 | 1.00 | –1.09 | 1.51 |
|  | 5 | 1 | 0.31 | 0.38 | 0.98 | –0.98 | 1.61 |
|  |  | 2 | –0.14 | 0.34 | 1.00 | –1.29 | 1.01 |
|  |  | 3 | 0.24 | 0.44 | 1.00 | –1.28 | 1.75 |
|  |  | 4 | –0.18 | 0.42 | 1.00 | –1.63 | 1.28 |
|  |  | 6 | 0.03 | 0.40 | 1.00 | –1.33 | 1.40 |
|  | 6 | 1 | 0.28 | 0.32 | 0.98 | –0.83 | 1.40 |
|  |  | 2 | –0.17 | 0.28 | 1.00 | –1.12 | 0.77 |
|  |  | 3 | 0.20 | 0.40 | 1.00 | –1.17 | 1.57 |
|  |  | 4 | –0.21 | 0.38 | 1.00 | –1.51 | 1.09 |
|  |  | 5 | –0.03 | 0.40 | 1.00 | –1.40 | 1.33 |
| SK_r | 1 | 2 | 16.56 | 4.37 | 0.02 | 1.52 | 31.59 |
|  |  | 3 | 16.90 | 6.78 | 0.30 | –6.39 | 40.19 |
|  |  | 4 | 16.83 | 6.38 | 0.24 | –5.09 | 38.74 |
|  |  | 5 | 7.49 | 6.78 | 0.94 | –15.80 | 30.78 |
|  |  | 6 | 17.71 | 5.84 | 0.12 | –2.36 | 37.77 |
|  | 2 | 1 | –16.56 | 4.37 | 0.02 | –31.59 | –1.52 |
|  |  | 3 | 0.34 | 6.03 | 1.00 | –20.38 | 21.06 |
|  |  | 4 | 0.27 | 5.58 | 1.00 | –18.89 | 19.44 |
|  |  | 5 | –9.06 | 6.03 | 0.81 | –29.79 | 11.66 |
|  |  | 6 | 1.15 | 4.95 | 1.00 | –15.87 | 18.16 |
|  | 3 | 1 | –16.90 | 6.78 | 0.30 | –40.19 | 6.39 |
|  |  | 2 | –0.34 | 6.03 | 1.00 | –21.06 | 20.38 |
|  |  | 4 | –0.07 | 7.61 | 1.00 | –26.22 | 26.08 |
|  |  | 5 | –9.41 | 7.94 | 0.92 | –36.72 | 17.90 |
|  |  | 6 | 0.80 | 7.16 | 1.00 | –23.81 | 25.42 |
|  | 4 | 1 | –16.83 | 6.38 | 0.24 | –38.74 | 5.09 |
|  |  | 2 | –0.27 | 5.58 | 1.00 | –19.44 | 18.89 |
|  |  | 3 | 0.07 | 7.61 | 1.00 | –26.08 | 26.22 |
|  |  | 5 | –9.34 | 7.61 | 0.91 | –35.48 | 16.81 |
|  |  | 6 | 0.88 | 6.78 | 1.00 | –22.44 | 24.20 |
|  | 5 | 1 | –7.49 | 6.78 | 0.94 | –30.78 | 15.80 |
|  |  | 2 | 9.06 | 6.03 | 0.81 | –11.66 | 29.79 |
|  |  | 3 | 9.41 | 7.94 | 0.92 | –17.90 | 36.72 |
|  |  | 4 | 9.34 | 7.61 | 0.91 | –16.81 | 35.48 |
|  |  | 6 | 10.21 | 7.16 | 0.84 | –14.41 | 34.83 |
|  | 6 | 1 | –17.71 | 5.84 | 0.12 | –37.77 | 2.36 |
|  |  | 2 | –1.15 | 4.95 | 1.00 | –18.16 | 15.87 |
|  |  | 3 | –0.80 | 7.16 | 1.00 | –25.42 | 23.81 |
|  |  | 4 | –0.88 | 6.78 | 1.00 | –24.20 | 22.44 |
|  |  | 5 | –10.21 | 7.16 | 0.84 | –34.83 | 14.41 |
| IChSK_rf1 | 1 | 2 | 6.29 | 1.26 | 0.00 | 1.96 | 10.62 |
|  |  | 3 | 6.14 | 1.95 | 0.09 | –0.57 | 12.85 |
|  |  | 4 | 6.04 | 1.84 | 0.07 | –0.27 | 12.36 |
|  |  | 5 | 6.11 | 1.95 | 0.10 | –0.60 | 12.82 |
|  |  | 6 | 6.82 | 1.68 | 0.01 | 1.04 | 12.60 |
|  | 2 | 1 | –6.29 | 1.26 | 0.00 | –10.62 | –1.96 |
|  |  | 3 | –0.15 | 1.74 | 1.00 | –6.12 | 5.82 |
|  |  | 4 | –0.24 | 1.61 | 1.00 | –5.77 | 5.28 |
|  |  | 5 | –0.18 | 1.74 | 1.00 | –6.15 | 5.79 |
|  |  | 6 | 0.53 | 1.43 | 1.00 | –4.37 | 5.44 |
|  | 3 | 1 | –6.14 | 1.95 | 0.09 | –12.85 | 0.57 |
|  |  | 2 | 0.15 | 1.74 | 1.00 | –5.82 | 6.12 |
|  |  | 4 | –0.10 | 2.19 | 1.00 | –7.63 | 7.44 |
|  |  | 5 | –0.03 | 2.29 | 1.00 | –7.90 | 7.84 |
|  |  | 6 | 0.68 | 2.06 | 1.00 | –6.41 | 7.77 |
|  | 4 | 1 | –6.04 | 1.84 | 0.07 | –12.36 | 0.27 |
|  |  | 2 | 0.24 | 1.61 | 1.00 | –5.28 | 5.77 |
|  |  | 3 | 0.10 | 2.19 | 1.00 | –7.44 | 7.63 |
|  |  | 5 | 0.07 | 2.19 | 1.00 | –7.46 | 7.60 |
|  |  | 6 | 0.78 | 1.95 | 1.00 | –5.94 | 7.50 |
|  | 5 | 1 | –6.11 | 1.95 | 0.10 | –12.82 | 0.60 |
|  |  | 2 | 0.18 | 1.74 | 1.00 | –5.79 | 6.15 |
|  |  | 3 | 0.03 | 2.29 | 1.00 | –7.84 | 7.90 |
|  |  | 4 | –0.07 | 2.19 | 1.00 | –7.60 | 7.46 |
|  |  | 6 | 0.71 | 2.06 | 1.00 | –6.38 | 7.80 |
|  | 6 | 1 | –6.82 | 1.68 | 0.01 | –12.60 | –1.04 |
|  |  | 2 | –0.53 | 1.43 | 1.00 | –5.44 | 4.37 |
|  |  | 3 | –0.68 | 2.06 | 1.00 | –7.77 | 6.41 |
|  |  | 4 | –0.78 | 1.95 | 1.00 | –7.50 | 5.94 |
|  |  | 5 | –0.71 | 2.06 | 1.00 | –7.80 | 6.38 |
| SK_rf1 | 1 | 2 | –0.46 | 0.25 | 0.66 | –1.33 | 0.41 |
|  |  | 3 | –0.08 | 0.38 | 1.00 | –1.40 | 1.24 |
|  |  | 4 | –0.49 | 0.36 | 0.87 | –1.74 | 0.76 |
|  |  | 5 | –0.32 | 0.38 | 0.98 | –1.64 | 1.01 |
|  |  | 6 | –0.28 | 0.33 | 0.98 | –1.43 | 0.86 |
|  | 2 | 1 | 0.46 | 0.25 | 0.66 | –0.41 | 1.33 |
|  |  | 3 | 0.38 | 0.34 | 0.94 | –0.78 | 1.54 |
|  |  | 4 | –0.03 | 0.31 | 1.00 | –1.11 | 1.04 |
|  |  | 5 | 0.14 | 0.34 | 1.00 | –1.02 | 1.30 |
|  |  | 6 | 0.18 | 0.28 | 0.99 | –0.78 | 1.13 |
|  | 3 | 1 | 0.08 | 0.38 | 1.00 | –1.24 | 1.40 |
|  |  | 2 | –0.38 | 0.34 | 0.94 | –1.54 | 0.78 |
|  |  | 4 | –0.41 | 0.43 | 0.97 | –1.87 | 1.05 |
|  |  | 5 | –0.24 | 0.44 | 1.00 | –1.76 | 1.29 |
|  |  | 6 | –0.20 | 0.40 | 1.00 | –1.58 | 1.18 |
|  | 4 | 1 | 0.49 | 0.36 | 0.87 | –0.76 | 1.74 |
|  |  | 2 | 0.03 | 0.31 | 1.00 | –1.04 | 1.11 |
|  |  | 3 | 0.41 | 0.43 | 0.97 | –1.05 | 1.87 |
|  |  | 5 | 0.18 | 0.43 | 1.00 | –1.29 | 1.64 |
|  |  | 6 | 0.21 | 0.38 | 1.00 | –1.09 | 1.52 |
|  | 5 | 1 | 0.32 | 0.38 | 0.98 | –1.01 | 1.64 |
|  |  | 2 | –0.14 | 0.34 | 1.00 | –1.30 | 1.02 |
|  |  | 3 | 0.24 | 0.44 | 1.00 | –1.29 | 1.76 |
|  |  | 4 | –0.18 | 0.43 | 1.00 | –1.64 | 1.29 |
|  |  | 6 | 0.03 | 0.40 | 1.00 | –1.34 | 1.41 |
|  | 6 | 1 | 0.28 | 0.33 | 0.98 | –0.86 | 1.43 |
|  |  | 2 | –0.18 | 0.28 | 0.99 | –1.13 | 0.78 |
|  |  | 3 | 0.20 | 0.40 | 1.00 | –1.18 | 1.58 |
|  |  | 4 | –0.21 | 0.38 | 1.00 | –1.52 | 1.09 |
|  |  | 5 | –0.03 | 0.40 | 1.00 | –1.41 | 1.34 |
| Groups with significant differences |  |  | The means difference is significant |
|  |  |  |  |  | at the 0.05 level. |  |

# Text boxes

Supplementary Figure 1. Dendrogram of mineralogical compositions. Result of hierarchical cluster analysis (Ward method) using square euclidean distances, allowing the classification of the samples in six groups (Table 1, column C6N), showing more significant differences between groups (verified by the Scheffé test), than that found with five, four or three groups.