## KLAPROTHITE, PÉLIGOTITE AND OTTOHAHNITE: NEW URANYL SULFATE MINERALS / ANTHONY R. KAMPF ET AL.

## Klaprothite, péligotite and ottohahnite, three new minerals with bidentate UO7–SO4 linkages from the Blue Lizard mine, San Juan County, Utah, USA

# Anthony R. Kampf1,*, Jakub Plášil2, Anatoly V. Kasatkin3, Joe Marty4 and Jiří Čejka5

Table 3. Powder X-ray data for klaprothite, péligotite and ottohahnite.

Klaprothite

| Iobs | dobs |  | dcalc | Icalc | hkl |  |  | Iobs | dobs |  | dcalc | Icalc | hkl |  | Iobs | dobs |  | dcalc | Icalc | hkl |  | Iobs | dobs |  | dcalc | Icalc | hkl |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30 | 10.27 |  | 10.3150 | 28 | 0 0 2 |  |  | 31 | 2.716 |  | 2.7292 | 19 | 2 2 4 |  | 16 | 2.0613 |  | 2.0630 | 13 | 0 0 10 |  | 11 | 1.6489 |  | 1.6547 | 3 | 1 8 |
| 68 | 9.72 |  | 9.7129 | 76 | 1 0 0 |  |  |  |  |  | 2.7068 | 4 | 3 1 |  | 10 | 2.0244 |  | 2.0365 | 4 | 2 4 3 |  |  |  |  | 1.6525 | 3 | 3 8 |
|  |  |  | 8.8115 | 4 | 0 1 1 |  |  |  |  |  | 2.7028 | 3 | 3 4 |  |  |  |  | 2.0328 | 3 | 4 1 4 |  |  |  |  | 1.6455 | 2 | 4 2 7 |
|  |  |  | 7.6777 | 7 | 0 2 |  |  |  |  |  | 2.6966 | 6 | 3 2 0 |  |  |  |  | 2.0261 | 2 | 3 8 |  |  |  |  | 1.6391 | 2 | 5 1 5 |
| 97 | 7.09 |  | 7.0838 | 100 | 0 1 2 |  |  |  |  |  | 2.6679 | 2 | 3 2 |  |  |  |  | 2.0103 | 2 | 3 6 |  |  |  |  | 1.6374 | 2 | 3 11 |
|  |  |  | 6.8795 | 4 | 1 1 0 |  |  | 22 | 2.646 |  | 2.6657 | 6 | 3 1 3 |  |  |  |  | 1.9957 | 2 | 4 2 3 |  | 23 | 1.6233 |  | 1.6288 | 2 | 3 3 8 |
|  |  |  | 6.5891 | 6 | 1 0 2 |  |  |  |  |  | 2.6545 | 6 | 1 5 |  |  |  |  | 1.9825 | 2 | 4 5 |  |  |  |  | 1.6272 | 6 | 1 1 12 |
|  |  |  | 6.3250 | 2 | 1 1 1 |  |  |  |  |  | 2.6486 | 5 | 2 3 1 |  | 17 | 1.9504 |  | 1.9584 | 6 | 1 0 10 |  |  |  |  | 1.6242 | 3 | 4 1 8 |
| 36 | 6.04 |  | 6.0309 | 40 | 1 2 |  |  |  |  |  | 2.6244 | 4 | 2 0 6 |  |  |  |  | 1.9549 | 4 | 4 1 |  |  |  |  | 1.6232 | 2 | 2 5 5 |
|  |  |  | 5.6186 | 3 | 0 1 3 |  |  |  |  |  | 2.6135 | 6 | 1 2 6 |  |  |  |  | 1.9404 | 3 | 0 5 1 |  |  |  |  | 1.6210 | 2 | 3 5 |
| 31 | 5.467 |  | 5.4585 | 41 | 1 1 2 |  |  | 35 | 2.570 |  | 2.5904 | 7 | 1 3 4 |  | 48 | 1.9136 |  | 1.9254 | 13 | 1 2 |  |  |  |  | 1.6188 | 2 | 6 0 0 |
| 77 | 5.158 |  | 5.1575 | 82 | 0 0 4 |  |  |  |  |  | 2.5787 | 6 | 0 0 8 |  |  |  |  | 1.9217 | 3 | 3 4 1 |  |  |  |  | 1.6152 | 2 | 1 2 |
| 28 | 4.835 |  | 4.8722 | 25 | 0 4 |  |  |  |  |  | 2.5743 | 9 | 2 6 |  |  |  |  | 1.9196 | 5 | 4 3 |  | 12 | 1.5931 |  | 1.6020 | 4 | 1 12 |
|  |  |  | 4.8565 | 3 | 2 0 0 |  |  |  |  |  | 2.5596 | 7 | 2 3 2 |  |  |  |  | 1.9186 | 2 | 3 3 5 |  |  |  |  | 1.5943 | 2 | 3 5 3 |
|  |  |  | 4.7421 | 11 | 0 2 1 |  |  |  |  |  | 2.5523 | 8 | 0 3 5 |  |  |  |  | 1.9165 | 2 | 0 4 |  |  |  |  | 1.5919 | 3 | 5 5 |
| 14 | 4.557 |  | 4.5585 | 13 | 0 1 4 |  |  |  |  |  | 2.5341 | 2 | 2 1 6 |  |  |  |  | 1.9156 | 3 | 2 10 |  |  |  |  | 1.5810 | 3 | 3 9 |
|  |  |  | 4.3750 | 2 | 1 1 |  |  |  |  |  | 2.5276 | 2 | 3 5 |  |  |  |  | 1.9147 | 3 | 4 3 1 |  | 12 | 1.5640 |  | 1.5689 | 3 | 6 3 |
| 58 | 4.330 |  | 4.3553 | 32 | 1 2 0 |  |  | 17 | 2.500 |  | 2.5245 | 4 | 2 4 |  |  |  |  | 1.9118 | 2 | 4 2 4 |  |  |  |  | 1.5601 | 4 | 3 4 7 |
|  |  |  | 4.3213 | 9 | 2 1 |  |  |  |  |  | 2.5218 | 4 | 0 2 7 |  |  |  |  | 1.9109 | 9 | 1 5 0 |  | 16 | 1.5361 |  | 1.5404 | 3 | 3 3 9 |
|  |  |  | 4.2929 | 23 | 1 0 4 |  |  |  |  |  | 2.4929 | 8 | 0 1 8 |  |  |  |  | 1.9080 | 7 | 5 1 |  |  |  |  | 1.5392 | 2 | 1 6 |
| 46 | 4.194 |  | 4.2160 | 33 | 1 2 |  |  |  |  |  | 2.4797 | 2 | 3 4 |  |  |  |  | 1.8976 | 5 | 1 5 1 |  |  |  |  | 1.5350 | 2 | 3 11 |
|  |  |  | 4.2038 | 2 | 1 2 1 |  |  |  |  |  | 2.4753 | 5 | 1 6 |  | 27 | 1.8751 |  | 1.8833 | 7 | 1 8 |  |  |  |  | 1.5341 | 2 | 2 4 |
|  |  |  | 4.1571 | 14 | 2 0 2 |  |  |  |  |  | 2.4363 | 2 | 0 4 0 |  |  |  |  | 1.8778 | 5 | 4 7 |  | 11 | 1.5129 |  | 1.5291 | 2 | 2 1 12 |
|  |  |  | 4.1411 | 2 | 2 1 1 |  |  | 8 | 2.415 |  | 2.4282 | 2 | 4 0 0 |  |  |  |  | 1.8752 | 5 | 2 7 |  |  |  |  | 1.5265 | 3 | 5 1 |
| 13 | 3.960 |  | 3.9757 | 5 | 0 2 3 |  |  |  |  |  | 2.4195 | 3 | 0 4 1 |  |  |  |  | 1.8737 | 4 | 0 10 |  |  |  |  | 1.5091 | 2 | 3 12 |
|  |  |  | 3.9286 | 7 | 1 1 4 |  |  |  |  |  | 2.4034 | 2 | 1 0 8 |  |  |  |  | 1.8717 | 2 | 5 1 1 |  | 10 | 1.4898 |  | 1.4980 | 2 | 1 12 |
| 28 | 3.811 |  | 3.8237 | 17 | 2 1 2 |  |  |  |  |  | 2.3743 | 7 | 1 2 |  |  |  |  | 1.8702 | 2 | 4 3 2 |  |  |  |  | 1.4899 | 2 | 5 9 |
|  |  |  | 3.7983 | 11 | 2 3 |  |  | 34 | 2.357 |  | 2.3671 | 4 | 1 2 7 |  | 17 | 1.8492 |  | 1.8597 | 8 | 2 10 |  |  |  |  | 1.4879 | 2 | 2 6 3 |
|  |  |  | 3.7194 | 3 | 1 5 |  |  |  |  |  | 2.3634 | 9 | 1 8 |  |  |  |  | 1.8555 | 2 | 5 3 |  |  |  |  | 1.4848 | 3 | 0 5 9 |
| 13 | 3.572 |  | 3.5710 | 14 | 1 2 3 |  |  |  |  |  | 2.3613 | 2 | 0 3 6 |  |  |  |  | 1.8483 | 9 | 3 1 8 |  | 12 | 1.4687 |  | 1.4736 | 2 | 0 0 14 |
|  |  |  | 3.5419 | 3 | 0 2 4 |  |  |  |  |  | 2.3576 | 3 | 4 1 |  | 27 | 1.8145 |  | 1.8298 | 5 | 3 4 3 |  |  |  |  | 1.4724 | 2 | 5 5 |
| 100 | 3.434 |  | 3.4537 | 8 | 2 1 |  |  |  |  |  | 2.3522 | 6 | 3 5 |  |  |  |  | 1.8252 | 6 | 3 9 |  |  |  |  | 1.4715 | 4 | 4 11 |
|  |  |  | 3.4453 | 15 | 2 4 |  |  |  |  |  | 2.3381 | 7 | 0 4 |  |  |  |  | 1.8171 | 2 | 1 2 10 |  |  |  |  | 1.4645 | 2 | 2 10 |
|  |  |  | 3.4397 | 68 | 2 2 0 |  |  |  |  |  | 2.3335 | 3 | 1 1 8 |  |  |  |  | 1.8133 | 2 | 3 8 |  | 13 | 1.4456 |  | 1.4508 | 3 | 2 7 |
|  |  |  | 3.4083 | 5 | 0 6 |  |  | 19 | 2.303 |  | 2.3106 | 3 | 2 2 6 |  |  |  |  | 1.8114 | 9 | 4 7 |  |  |  |  | 1.4473 | 2 | 5 4 3 |
|  |  |  | 3.3739 | 15 | 2 2 |  |  |  |  |  | 2.3065 | 6 | 3 1 |  |  |  |  | 1.8092 | 3 | 2 3 |  |  |  |  | 1.4467 | 2 | 1 5 9 |
| 37 | 3.227 |  | 3.2424 | 9 | 0 1 6 |  |  |  |  |  | 2.3030 | 2 | 4 1 1 |  |  |  |  | 1.8045 | 2 | 5 2 0 |  |  |  |  | 1.4404 | 2 | 6 3 |
|  |  |  | 3.2376 | 14 | 3 0 0 |  |  |  |  |  | 2.2964 | 4 | 0 4 3 |  |  |  |  | 1.8027 | 3 | 2 0 10 |  |  |  |  | 1.4336 | 2 | 5 1 8 |
|  |  |  | 3.2211 | 6 | 1 2 4 |  |  |  |  |  | 2.2914 | 3 | 3 2 |  | 16 | 1.7881 |  | 1.7980 | 5 | 1 3 9 |  | 17 | 1.4213 |  | 1.4292 | 2 | 3 5 |
|  |  |  | 3.2172 | 9 | 1 6 |  |  |  |  |  | 2.2744 | 3 | 3 2 4 |  |  |  |  | 1.7931 | 3 | 2 5 1 |  |  |  |  | 1.4257 | 3 | 2 14 |
|  |  |  | 3.2089 | 4 | 0 3 1 |  |  | 10 | 2.260 |  | 2.2657 | 2 | 2 6 |  |  |  |  | 1.7908 | 3 | 2 3 8 |  |  |  |  | 1.4225 | 2 | 6 7 |
|  |  |  | 3.1625 | 4 | 2 2 2 |  |  |  |  |  | 2.2607 | 5 | 4 3 |  |  |  |  | 1.7835 | 4 | 2 4 |  |  |  |  | 1.4204 | 3 | 4 4 7 |
|  |  |  | 3.1210 | 5 | 2 1 4 |  |  |  |  |  | 2.2526 | 4 | 3 3 1 |  |  |  |  | 1.7709 | 2 | 0 4 8 |  |  |  |  | 1.4158 | 2 | 3 1 12 |
| 65 | 3.082 |  | 3.1049 | 15 | 1 1 |  |  | 11 | 2.215 |  | 2.2268 | 6 | 4 1 2 |  | 16 | 1.7528 |  | 1.7623 | 5 | 0 5 5 |  | 10 | 1.4010 |  | 1.4106 | 4 | 2 14 |
|  |  |  | 3.0966 | 10 | 1 0 6 |  |  |  |  |  | 2.2165 | 2 | 3 6 |  |  |  |  | 1.7541 | 4 | 5 5 |  |  |  |  | 1.4013 | 3 | 3 6 3 |
|  |  |  | 3.0807 | 6 | 1 3 0 |  |  |  |  |  | 2.2098 | 4 | 1 4 3 |  |  |  |  | 1.7508 | 2 | 4 3 4 |  |  |  |  | 1.3929 | 2 | 1 6 7 |
|  |  |  | 3.0725 | 5 | 3 1 0 |  |  |  |  |  | 2.1964 | 2 | 3 0 6 |  |  |  |  | 1.7488 | 3 | 2 10 |  | 15 | 1.3795 |  | 1.3893 | 2 | 1 2 |
|  |  |  | 3.0682 | 38 | 1 2 |  |  |  |  |  | 2.1927 | 2 | 2 1 |  |  |  |  | 1.7337 | 4 | 4 2 6 |  |  |  |  | 1.3842 | 2 | 4 5 5 |
| 61 | 3.012 |  | 3.0257 | 10 | 1 3 1 |  |  |  |  |  | 2.1891 | 2 | 3 3 2 |  | 26 | 1.7159 |  | 1.7294 | 7 | 4 1 |  |  |  |  | 1.3830 | 2 | 1 12 |
|  |  |  | 3.0154 | 41 | 2 4 |  |  | 19 | 2.179 |  | 2.1845 | 4 | 3 4 |  |  |  |  | 1.7199 | 2 | 4 4 0 |  |  |  |  | 1.3770 | 2 | 7 1 |
|  |  |  | 2.9917 | 12 | 3 2 |  |  |  |  |  | 2.1812 | 5 | 4 1 |  |  |  |  | 1.7146 | 6 | 1 5 5 |  | 9 | 1.3531 |  | 1.3544 | 3 | 0 14 |
| 12 | 2.930 |  | 2.9518 | 10 | 2 2 3 |  |  |  |  |  | 2.1766 | 3 | 2 3 5 |  |  |  |  | 1.7124 | 6 | 4 3 |  |  |  |  | 1.3474 | 2 | 1 6 |
|  |  |  | 2.9136 | 7 | 1 3 2 |  |  |  |  |  | 2.1733 | 3 | 4 2 0 |  |  |  |  | 1.7063 | 2 | 5 1 4 |  | 15 | 1.3361 |  | 1.3416 | 2 | 4 11 |
|  |  |  | 2.8951 | 2 | 1 6 |  |  |  |  |  | 2.1584 | 4 | 2 3 |  |  |  |  | 1.7053 | 2 | 0 10 |  |  |  |  | 1.3406 | 2 | 4 13 |
| 26 | 2.816 |  | 2.8349 | 14 | 3 1 2 |  |  |  |  |  | 2.1429 | 2 | 0 6 |  |  |  |  | 1.6972 | 4 | 4 7 |  |  |  |  | 1.3391 | 4 | 7 1 |
|  |  |  | 2.8248 | 3 | 1 4 |  |  |  |  |  | 2.1282 | 2 | 2 7 |  | 25 | 1.6852 |  | 1.6930 | 3 | 0 1 12 |  |  |  |  | 1.3356 | 2 | 7 1 2 |
|  |  |  | 2.8210 | 2 | 0 1 7 |  |  | 18 | 2.100 |  | 2.1180 | 7 | 4 3 |  |  |  |  | 1.6922 | 3 | 5 5 |  |  |  |  | 1.3262 | 3 | 5 9 |
|  |  |  | 2.8078 | 7 | 2 1 5 |  |  |  |  |  | 2.1080 | 4 | 2 4 |  |  |  |  | 1.6907 | 3 | 2 2 10 |  | 9 | 1.3166 |  | 1.3189 | 2 | 1 5 11 |
|  |  |  | 2.7929 | 7 | 2 6 |  |  |  |  |  | 2.1028 | 3 | 3 5 |  |  |  |  | 1.6820 | 3 | 4 3 5 |  |  |  |  | 1.3157 | 2 | 7 5 |
|  |  |  | 2.7622 | 2 | 1 3 3 |  |  |  |  |  | 2.0962 | 5 | 2 1 8 |  |  |  |  | 1.6808 | 2 | 3 2 |  | 11 | 1.2955 |  | 1.3046 | 2 | 2 2 14 |
|  |  |  |  |  |  |  |  |  |  |  | 2.0929 | 5 | 1 6 |  |  |  |  | 1.6795 | 4 | 3 1 |  |  |  |  | 1.2960 | 2 | 1 8 |
|  |  |  |  |  |  |  |  |  |  |  | 2.0834 | 2 | 0 10 |  |  |  |  | 1.6787 | 3 | 1 12 |  |  |  |  | 1.2928 | 2 | 1 16 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.2889 | 3 | 7 5 |

Péligotite

| Iobs | dobs |  | dcalc | Icalc | hkl |  | Iobs | dobs |  | dcalc | Icalc | hkl |  | Iobs | dobs |  | dcalc | Icalc | hkl |  | Iobs | dobs |  | dcalc | Icalc | hkl |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 39 | 10.19 |  | 10.2146 | 42 | 0 0 1 |  | 18 | 2.816 |  | 2.8199 | 3 | 3 |  | 7 | 2.1394 |  | 2.1448 | 3 | 2 4 2 |  |  |  |  | 1.7115 | 4 | 3 5 1 |
|  |  |  | 9.9546 | 11 | 0 1 0 |  |  |  |  | 2.8161 | 14 | 1 3 2 |  |  |  |  | 2.1378 | 6 | 4 2 0 |  | 13 | 1.6908 |  | 1.7052 | 2 | 4 0 |
| 48 | 9.51 |  | 9.4341 | 70 | 1 0 0 |  |  |  |  | 2.8083 | 5 | 0 3 2 |  |  |  |  | 2.1221 | 7 | 1 |  |  |  |  | 1.7039 | 2 | 0 3 |
| 32 | 8.15 |  | 8.1378 | 49 | 1 0 1 |  |  |  |  | 2.7966 | 3 | 0 1 |  | 3 | 2.0958 |  | 2.0842 | 3 | 1 1 5 |  |  |  |  | 1.7024 | 2 | 0 0 6 |
| 100 | 7.11 |  | 7.2014 | 44 | 0 1 1 |  |  |  |  | 2.7552 | 7 | 2 3 1 |  |  |  |  | 2.0823 | 2 | 4 |  |  |  |  | 1.6952 | 4 | 5 3 2 |
|  |  |  | 7.0589 | 56 | 0 1 |  |  |  |  | 2.7511 | 2 | 3 2 1 |  |  |  |  | 2.0622 | 3 | 2 1 5 |  |  |  |  | 1.6893 | 6 | 3 1 6 |
|  |  |  | 6.8744 | 8 | 1 1 0 |  | 24 | 2.717 |  | 2.7295 | 9 | 2 2 3 |  | 11 | 2.0459 |  | 2.0429 | 16 | 0 0 5 |  |  |  |  | 1.6756 | 2 | 5 2 |
|  |  |  | 6.8209 | 12 | 1 0 |  |  |  |  | 2.7240 | 5 | 2 3 0 |  |  |  |  | 2.0242 | 2 | 0 4 |  |  |  |  | 1.6725 | 2 | 0 6 |
|  |  |  | 6.3716 | 10 | 1 1 1 |  |  |  |  | 2.7146 | 4 | 3 1 |  | 9 | 1.9919 |  | 2.0037 | 3 | 2 4 |  | 8 | 1.6605 |  | 1.6659 | 2 | 2 1 |
| 32 | 6.23 |  | 6.2316 | 34 | 1 1 |  |  |  |  | 2.7107 | 5 | 2 1 |  |  |  |  | 2.0022 | 5 | 4 1 4 |  |  |  |  | 1.6636 | 2 | 2 4 |
|  |  |  | 6.1384 | 3 | 0 1 |  |  |  |  | 2.6934 | 7 | 1 |  |  |  |  | 1.9909 | 5 | 0 5 0 |  |  |  |  | 1.6555 | 3 | 3 5 |
|  |  |  | 5.2411 | 11 | 1 1 |  |  |  |  | 2.6913 | 6 | 1 1 |  |  |  |  | 1.9875 | 2 | 2 1 |  |  |  |  | 1.6524 | 2 | 4 3 |
|  |  |  | 5.2088 | 10 | 1 |  |  |  |  | 2.6700 | 8 | 2 3 |  |  |  |  | 1.9837 | 2 | 4 3 1 |  |  |  |  | 1.6347 | 2 | 3 0 |
|  |  |  | 5.1209 | 3 | 1 0 2 |  |  |  |  | 2.6492 | 2 | 2 0 |  |  |  |  | 1.9656 | 5 | 4 3 2 |  |  |  |  | 1.6334 | 2 | 4 1 |
| 63 | 5.14 |  | 5.1073 | 71 | 0 0 2 |  | 21 | 2.639 |  | 2.6450 | 7 | 3 2 2 |  |  |  |  | 1.9590 | 2 | 3 4 0 |  |  |  |  | 1.6316 | 2 | 5 |
| 8 | 4.79 |  | 4.8175 | 8 | 2 0 1 |  |  |  |  | 2.6324 | 10 | 3 1 3 |  |  |  |  | 1.9557 | 2 | 3 4 2 |  | 15 | 1.6235 |  | 1.6276 | 2 | 5 0 5 |
| 43 | 4.54 |  | 4.5994 | 15 | 1 1 2 |  |  |  |  | 2.6206 | 10 | 2 2 |  |  |  |  | 1.9535 | 2 | 5 0 2 |  |  |  |  | 1.6247 | 2 | 2 5 |
|  |  |  | 4.5815 | 22 | 0 1 2 |  |  |  |  | 2.6044 | 4 | 2 |  |  |  |  | 1.9516 | 2 | 3 1 5 |  |  |  |  | 1.6230 | 5 | 1 |
|  |  |  | 4.5100 | 23 | 0 2 1 |  |  |  |  | 2.5605 | 2 | 2 0 4 |  | 26 | 1.9434 |  | 1.9449 | 20 | 5 0 |  |  |  |  | 1.6208 | 4 | 0 2 6 |
|  |  |  | 4.4396 | 2 | 0 1 |  | 17 | 2.552 |  | 2.5566 | 6 | 2 3 |  |  |  |  | 1.9409 | 4 | 2 |  |  |  |  | 1.6185 | 2 | 1 1 |
| 53 | 4.307 |  | 4.3880 | 22 | 2 0 |  |  |  |  | 2.5537 | 5 | 0 0 4 |  |  |  |  | 1.9357 | 2 | 1 5 |  |  |  |  | 1.6110 | 2 | 1 5 4 |
|  |  |  | 4.3663 | 2 | 2 1 1 |  |  |  |  | 2.5508 | 3 | 2 |  |  |  |  | 1.9335 | 6 | 3 5 |  |  |  |  | 1.6084 | 2 | 1 2 |
|  |  |  | 4.3071 | 2 | 2 1 |  |  |  |  | 2.5434 | 3 | 2 2 |  |  |  |  | 1.9238 | 2 | 1 1 |  |  |  |  | 1.6056 | 2 | 4 3 5 |
|  |  |  | 4.2896 | 13 | 1 2 1 |  |  |  |  | 2.5269 | 4 | 3 1 |  | 30 | 1.9131 |  | 1.9229 | 4 | 3 3 4 |  |  |  |  | 1.6044 | 2 | 6 1 |
|  |  |  | 4.2757 | 18 | 2 1 0 |  |  |  |  | 2.4886 | 2 | 0 4 0 |  |  |  |  | 1.9163 | 7 | 2 5 |  | 6 | 1.5889 |  | 1.5988 | 2 | 6 1 |
|  |  |  | 4.2498 | 11 | 1 0 |  | 9 | 2.471 |  | 2.4855 | 6 | 0 1 4 |  |  |  |  | 1.9153 | 2 | 3 0 |  |  |  |  | 1.5905 | 2 | 2 5 4 |
| 21 | 4.078 |  | 4.0689 | 12 | 2 0 2 |  |  |  |  | 2.4653 | 3 | 2 4 |  |  |  |  | 1.9132 | 16 | 5 1 |  |  |  |  | 1.5841 | 3 | 1 6 |
|  |  |  | 4.0485 | 18 | 0 2 |  |  |  |  | 2.4617 | 4 | 0 4 |  |  |  |  | 1.9101 | 8 | 2 |  |  |  |  | 1.5752 | 2 | 3 |
| 13 | 3.852 |  | 3.8792 | 4 | 2 1 |  |  |  |  | 2.4509 | 2 | 4 0 1 |  |  |  |  | 1.8917 | 2 | 0 5 |  | 7 | 1.5602 |  | 1.5690 | 3 | 2 6 0 |
|  |  |  | 3.8530 | 9 | 1 |  |  |  |  | 2.4396 | 3 | 1 |  |  |  |  | 1.8893 | 2 | 3 |  |  |  |  | 1.5645 | 2 | 1 |
|  |  |  | 3.7967 | 3 | 2 1 2 |  |  |  |  | 2.4291 | 4 | 0 4 1 |  | 12 | 1.8716 |  | 1.8879 | 3 | 3 |  |  |  |  | 1.5638 | 2 | 0 5 |
| 16 | 3.754 |  | 3.7667 | 7 | 1 2 |  |  |  |  | 2.4110 | 2 | 1 4 0 |  |  |  |  | 1.8868 | 2 | 5 0 0 |  |  |  |  | 1.5604 | 3 | 3 4 |
|  |  |  | 3.7369 | 15 | 2 2 |  |  |  |  | 2.4088 | 2 | 4 0 2 |  |  |  |  | 1.8853 | 2 | 5 0 3 |  |  |  |  | 1.5483 | 3 | 4 |
| 19 | 3.598 |  | 3.6274 | 14 | 1 1 |  | 18 | 2.392 |  | 2.4069 | 4 | 0 1 |  |  |  |  | 1.8684 | 3 | 4 4 |  | 11 | 1.5317 |  | 1.5424 | 3 | 1 6 |
|  |  |  | 3.6133 | 3 | 1 2 2 |  |  |  |  | 2.4005 | 5 | 0 3 3 |  |  |  |  | 1.8670 | 6 | 4 |  |  |  |  | 1.5358 | 4 | 3 3 |
|  |  |  | 3.6007 | 7 | 0 2 2 |  |  |  |  | 2.3951 | 2 | 1 4 1 |  |  |  |  | 1.8549 | 3 | 3 4 3 |  |  |  |  | 1.5346 | 2 | 0 4 |
| 20 | 3.526 |  | 3.5282 | 27 | 1 0 3 |  |  |  |  | 2.3921 | 4 | 1 3 |  | 10 | 1.8430 |  | 1.8514 | 3 | 2 5 1 |  |  |  |  | 1.5331 | 2 | 3 3 6 |
|  |  |  | 3.4921 | 9 | 2 2 1 |  |  |  |  | 2.3870 | 5 | 4 1 1 |  |  |  |  | 1.8460 | 3 | 5 3 |  |  |  |  | 1.5243 | 2 | 2 2 |
|  |  |  | 3.4372 | 3 | 2 2 0 |  |  |  |  | 2.3806 | 3 | 3 |  |  |  |  | 1.8425 | 2 | 0 2 |  |  |  |  | 1.5171 | 2 | 2 0 7 |
| 73 | 3.418 |  | 3.4319 | 35 | 2 1 |  |  |  |  | 2.3663 | 5 | 1 2 4 |  |  |  |  | 1.8374 | 2 | 1 4 4 |  |  |  |  | 1.5151 | 3 | 4 |
|  |  |  | 3.4105 | 28 | 2 0 |  | 20 | 2.340 |  | 2.3585 | 4 | 4 0 0 |  |  |  |  | 1.8288 | 2 | 2 1 |  |  |  |  | 1.4844 | 2 | 1 7 |
|  |  |  | 3.4049 | 29 | 0 0 3 |  |  |  |  | 2.3530 | 3 | 0 3 |  |  |  |  | 1.8264 | 2 | 5 2 1 |  | 4 | 1.4599 |  | 1.4693 | 2 | 2 4 |
|  |  |  | 3.3182 | 6 | 0 3 0 |  |  |  |  | 2.3460 | 9 | 3 3 1 |  |  |  |  | 1.8190 | 2 | 1 |  |  |  |  | 1.4624 | 3 | 5 6 |
| 11 | 3.249 |  | 3.2695 | 8 | 3 0 1 |  |  |  |  | 2.3319 | 2 | 4 2 |  | 15 | 1.8065 |  | 1.8134 | 5 | 3 3 |  | 3 | 1.4307 |  | 1.4356 | 2 | 1 5 |
|  |  |  | 3.2021 | 6 | 0 3 |  |  |  |  | 2.3303 | 2 | 2 |  |  |  |  | 1.8088 | 2 | 5 2 |  |  |  |  | 1.4299 | 2 | 3 6 3 |
|  |  |  | 3.1601 | 6 | 2 2 |  |  |  |  | 2.3197 | 2 | 3 0 4 |  |  |  |  | 1.8058 | 6 | 1 3 5 |  |  |  |  | 1.4286 | 2 | 2 1 |
| 74 | 3.121 |  | 3.1379 | 31 | 1 3 0 |  |  |  |  | 2.3119 | 3 | 4 1 |  |  |  |  | 1.8045 | 2 | 2 5 2 |  |  |  |  | 1.4100 | 2 | 6 |
|  |  |  | 3.1198 | 40 | 3 1 1 |  | 11 | 2.279 |  | 2.3008 | 5 | 1 |  |  |  |  | 1.7955 | 4 | 5 2 |  |  |  |  | 1.4078 | 2 | 1 7 0 |
|  |  |  | 3.1158 | 20 | 2 2 |  |  |  |  | 2.2910 | 5 | 1 0 |  |  |  |  | 1.7783 | 3 | 2 5 |  | 8 | 1.3829 |  | 1.3922 | 3 | 0 6 |
|  |  |  | 3.0972 | 10 | 1 3 1 |  |  |  |  | 2.2816 | 3 | 3 3 2 |  |  |  |  | 1.7742 | 2 | 5 2 3 |  |  |  |  | 1.3908 | 2 | 7 1 2 |
|  |  |  | 3.0840 | 6 | 3 0 2 |  |  |  |  | 2.2600 | 3 | 1 4 2 |  |  |  |  | 1.7689 | 2 | 5 2 0 |  |  |  |  | 1.3831 | 5 | 5 5 |
|  |  |  | 3.0793 | 6 | 2 1 3 |  |  |  |  | 2.2579 | 2 | 1 4 |  |  |  |  | 1.7647 | 4 | 0 4 |  |  |  |  | 1.3822 | 2 | 4 6 1 |
| 34 | 3.058 |  | 3.0684 | 6 | 2 1 |  |  |  |  | 2.2547 | 2 | 2 4 |  |  |  |  | 1.7624 | 2 | 1 0 6 |  | 5 | 1.3578 |  | 1.3548 | 2 | 3 |
|  |  |  | 3.0650 | 30 | 1 |  |  |  |  | 2.2454 | 2 | 2 |  | 16 | 1.7584 |  | 1.7593 | 2 | 0 4 |  |  |  |  | 1.3471 | 3 | 7 1 4 |
|  |  |  | 3.0485 | 6 | 1 1 |  | 16 | 2.212 |  | 2.2371 | 8 | 3 2 |  |  |  |  | 1.7576 | 6 | 4 4 1 |  | 8 | 1.3356 |  | 1.3401 | 2 | 5 1 7 |
| 11 | 2.983 |  | 3.0054 | 13 | 3 1 0 |  |  |  |  | 2.2198 | 5 | 0 2 |  |  |  |  | 1.7522 | 4 | 4 3 4 |  |  |  |  | 1.3395 | 2 | 7 2 1 |
|  |  |  | 2.9919 | 2 | 1 0 |  |  |  |  | 2.2172 | 3 | 1 2 |  |  |  |  | 1.7473 | 2 | 5 1 4 |  |  |  |  | 1.3387 | 2 | 1 4 |
|  |  |  | 2.9625 | 2 | 3 1 2 |  |  |  |  | 2.2082 | 4 | 2 4 0 |  | 16 | 1.7263 |  | 1.7351 | 9 | 4 1 |  |  |  |  | 1.3369 | 2 | 7 1 0 |
|  |  |  | 2.9533 | 2 | 0 3 |  |  |  |  | 2.2052 | 3 | 4 1 3 |  |  |  |  | 1.7338 | 2 | 0 5 3 |  |  |  |  | 1.3361 | 2 | 2 5 6 |
|  |  |  | 2.9296 | 3 | 3 2 |  |  |  |  | 2.1940 | 3 | 4 0 |  |  |  |  | 1.7296 | 3 | 4 |  |  |  |  | 1.3350 | 3 | 4 6 |
|  |  |  | 2.9110 | 2 | 1 2 3 |  |  |  |  | 2.1876 | 4 | 4 1 |  |  |  |  | 1.7286 | 3 | 0 3 |  |  |  |  | 1.3342 | 2 | 7 3 |
|  |  |  | 2.8468 | 4 | 1 3 |  |  |  |  | 2.1857 | 4 | 4 3 |  |  |  |  | 1.7242 | 2 | 2 |  |  |  |  |  |  |  |
|  |  |  | 2.8429 | 2 | 1 3 |  |  |  |  | 2.1639 | 2 | 2 2 |  |  |  |  | 1.7186 | 2 | 4 |  |  |  |  |  |  |  |
|  |  |  | 2.8368 | 3 | 0 2 3 |  |  |  |  | 2.1535 | 2 | 4 2 |  |  |  |  | 1.7166 | 4 | 1 3 |  |  |  |  |  |  |  |

Ottohahnite

| Iobs | dobs |  | dcalc | Icalc | hkl |  | Iobs | dobs |  | dcalc | Icalc | hkl |  | Iobs | dobs |  | dcalc | Icalc | hkl |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 12 | 12.67 |  | 12.5801 | 10 | 0 0 1 |  |  |  |  | 3.3808 | 4 | 2 0 2 |  |  |  |  | 2.2322 | 2 | 4 1 |
| 3 | 10.64 |  | 10.6016 | 2 | 0 1 0 |  |  |  |  | 3.2077 | 3 | 1 3 |  | 6 | 2.198 |  | 2.2136 | 3 | 4 |
|  |  |  | 10.5726 | 2 | 0 1 |  | 35 | 3.156 |  | 3.1607 | 23 | 2 2 |  |  |  |  | 2.1935 | 2 | 4 0 |
| 10 | 9.54 |  | 9.5744 | 10 | 1 0 0 |  |  |  |  | 3.1410 | 4 | 1 |  |  |  |  | 2.1900 | 2 | 4 2 |
| 7 | 8.92 |  | 8.9150 | 11 | 0 1 |  | 31 | 3.088 |  | 3.1023 | 22 | 4 |  | 29 | 2.122 |  | 2.1405 | 2 | 4 |
| 32 | 7.64 |  | 7.6513 | 27 | 1 0 |  |  |  |  | 3.0984 | 2 | 2 1 |  |  |  |  | 2.1312 | 6 | 2 5 |
|  |  |  | 7.4672 | 6 | 1 |  |  |  |  | 3.0831 | 2 | 0 3 1 |  |  |  |  | 2.1269 | 2 | 4 2 |
| 41 | 6.81 |  | 6.8221 | 20 | 0 1 1 |  |  |  |  | 3.0651 | 4 | 4 |  |  |  |  | 2.1248 | 3 | 6 |
|  |  |  | 6.7990 | 11 | 0 2 |  |  |  |  | 3.0489 | 3 | 0 4 |  |  |  |  | 2.1234 | 2 | 1 2 4 |
|  |  |  | 6.7766 | 3 | 1 1 |  | 63 | 2.977 |  | 2.9948 | 4 | 3 |  |  |  |  | 2.1203 | 3 | 0 5 0 |
|  |  |  | 6.7616 | 4 | 1 0 1 |  |  |  |  | 2.9923 | 2 | 1 4 |  |  |  |  | 2.1058 | 4 | 4 1 1 |
|  |  |  | 6.6621 | 5 | 1 1 0 |  |  |  |  | 2.9861 | 17 | 1 1 3 |  |  |  |  | 2.0931 | 2 | 3 |
| 100 | 6.21 |  | 6.2047 | 100 | 2 |  |  |  |  | 2.9798 | 2 | 3 |  | 10 | 2.071 |  | 2.0682 | 6 | 6 |
| 27 | 5.28 |  | 5.3008 | 12 | 0 2 0 |  |  |  |  | 2.9763 | 15 | 3 1 |  | 9 | 2.0106 |  | 2.0140 | 2 | 3 4 |
|  |  |  | 5.2863 | 15 | 0 2 |  |  |  |  | 2.9670 | 2 | 2 2 |  |  |  |  | 2.0095 | 2 | 3 2 |
|  |  |  | 5.0567 | 2 | 1 2 |  |  |  |  | 2.9456 | 4 | 3 1 0 |  |  |  |  | 1.9882 | 2 | 7 |
| 19 | 4.992 |  | 5.0333 | 11 | 1 1 |  |  |  |  | 2.9431 | 15 | 2 3 |  | 10 | 1.9642 |  | 1.9774 | 3 | 7 |
|  |  |  | 4.9591 | 2 | 0 1 |  | 42 | 2.913 |  | 2.9176 | 14 | 0 2 |  |  |  |  | 1.9754 | 2 | 0 2 5 |
|  |  |  | 4.9338 | 8 | 1 |  |  |  |  | 2.9078 | 15 | 2 2 1 |  |  |  |  | 1.9477 | 2 | 3 |
| 39 | 4.650 |  | 4.6894 | 7 | 1 0 2 |  |  |  |  | 2.8579 | 4 | 2 |  |  |  |  | 1.9377 | 2 | 4 3 |
|  |  |  | 4.6826 | 11 | 1 2 |  |  |  |  | 2.8399 | 2 | 5 |  | 35 | 1.9076 |  | 1.9146 | 2 | 1 3 |
|  |  |  | 4.6268 | 6 | 0 1 2 |  | 16 | 2.795 |  | 2.8180 | 2 | 5 |  |  |  |  | 1.9135 | 8 | 4 1 |
|  |  |  | 4.6148 | 7 | 0 3 |  |  |  |  | 2.7910 | 2 | 2 0 3 |  |  |  |  | 1.9104 | 2 | 1 3 |
|  |  |  | 4.6086 | 4 | 1 0 |  |  |  |  | 2.7850 | 3 | 1 3 1 |  |  |  |  | 1.9088 | 9 | 0 4 3 |
|  |  |  | 4.5296 | 7 | 1 |  |  |  |  | 2.7727 | 4 | 0 2 3 |  |  |  |  | 1.9020 | 4 | 0 7 |
| 24 | 4.465 |  | 4.4575 | 14 | 0 2 |  |  |  |  | 2.7644 | 2 | 0 5 |  |  |  |  | 1.8815 | 2 | 3 |
|  |  |  | 4.3875 | 2 | 1 2 0 |  | 5 | 2.660 |  | 2.6558 | 2 | 3 1 1 |  | 23 | 1.8604 |  | 1.8752 | 3 | 3 3 |
|  |  |  | 4.3796 | 2 | 2 |  |  |  |  | 2.6447 | 2 | 0 3 2 |  |  |  |  | 1.8687 | 3 | 3 |
| 15 | 4.301 |  | 4.3096 | 10 | 0 3 |  |  |  |  | 2.5385 | 2 | 3 1 |  |  |  |  | 1.8624 | 2 | 2 |
|  |  |  | 4.2539 | 2 | 2 1 |  | 10 | 2.513 |  | 2.5284 | 2 | 2 4 |  |  |  |  | 1.8593 | 4 | 1 5 1 |
| 18 | 4.153 |  | 4.1934 | 3 | 0 0 3 |  |  |  |  | 2.5160 | 4 | 0 0 5 |  |  |  |  | 1.8553 | 4 | 0 6 |
|  |  |  | 4.1529 | 8 | 2 1 0 |  |  |  |  | 2.4824 | 3 | 0 1 |  |  |  |  | 1.8399 | 2 | 1 7 |
|  |  |  | 4.1084 | 6 | 2 0 1 |  | 10 | 2.456 |  | 2.4679 | 4 | 4 0 |  | 12 | 1.7895 |  | 1.8074 | 2 | 1 |
|  |  |  | 3.8466 | 2 | 0 1 |  |  |  |  | 2.4316 | 2 | 4 1 |  |  |  |  | 1.7914 | 3 | 3 5 |
|  |  |  | 3.8301 | 2 | 3 |  |  |  |  | 2.4301 | 2 | 1 4 |  |  |  |  | 1.7851 | 3 | 3 1 |
| 12 | 3.802 |  | 3.8048 | 6 | 1 3 |  | 11 | 2.402 |  | 2.4257 | 2 | 1 5 |  |  |  |  | 1.7693 | 2 | 4 2 2 |
|  |  |  | 3.6405 | 2 | 1 2 1 |  |  |  |  | 2.4029 | 2 | 1 2 |  |  |  |  | 1.7491 | 2 | 2 0 6 |
| 12 | 3.558 |  | 3.5916 | 3 | 2 |  |  |  |  | 2.3992 | 4 | 2 4 |  | 8 | 1.7343 |  | 1.7375 | 5 | 6 0 |
|  |  |  | 3.5339 | 2 | 0 3 0 |  |  |  |  | 2.3813 | 3 | 1 |  | 13 | 1.7021 |  | 1.7154 | 3 | 5 2 |
|  |  |  | 3.5242 | 4 | 0 3 |  |  |  |  | 2.3587 | 2 | 1 |  |  |  |  | 1.7113 | 2 | 5 |
| 52 | 3.462 |  | 3.4917 | 3 | 1 |  | 11 | 2.294 |  | 2.3017 | 3 | 3 2 |  |  |  |  | 1.7083 | 4 | 6 |
|  |  |  | 3.4750 | 32 | 3 0 |  |  |  |  | 2.2871 | 2 | 4 1 |  |  |  |  | 1.6962 | 3 | 2 5 |
|  |  |  | 3.4440 | 3 | 4 |  |  |  |  | 2.2775 | 2 | 3 3 |  |  |  |  | 1.6904 | 2 | 4 0 4 |
|  |  |  | 3.4316 | 3 | 0 4 |  | 13 | 2.255 |  | 2.2586 | 3 | 4 |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  | 2.2539 | 5 | 3 0 3 |  |  |  |  |  |  |  |

Only calculated lines with I > 2 are shown.