Alteration of nanocrystalline Calcium Silicate Hydrate (C-S-H) at pH 9.2 and room temperature: a combined mineralogical and chemical study.

Nicolas C.M. Marty1, Sylvain Grangeon1, Fabienne Warmont2 and Catherine Lerouge1

1.	BRGM, 45060 Orléans Cedex 2, France

2. CRMD, FRE 3520- CNRS – Université d’Orléans, 45071 Orléans Cedex 2, France

Corresponding author

Tel.: +33 2 38 64 33 43; fax: +33 2 38 64 30 62

E-mail address: n.marty@brgm.fr (Nicolas Marty)

Postal address: BRGM, D3E/SVP, 3 Avenue C. Guillemin, F-45060 Orléans, Cedex 2, France

Keywords: Calcium Silicate Hydrate, C-S-H, dissolution, kinetics, alteration product

Running title: Alteration of nanocrystalline C-S-H

Appendix: Evolution of chemical composition with time and dissolution rate calculations

Table A 1: Fluid chemistry and calculation of dissolution rates from the CSH_1.5 experiment.

| Initial time (min) | Final time (min) | Sampled mass (g) | Flow rate (mL min-1) | pH (in) | pH (out) | Si (out)(1) (mol L-1) | Ca (out)(1) (mol L-1) | Si-final mass (g) | Si-average mass (g) | Estimated C/S(2) | Measured C/S | Estimated molar mass (g mol-1) | Estimated specific surface area (m2 g-1) | Si-dissolution rate (mol m-2 s-1) | Ca-dissolution rate (mol m-2 s-1) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | 1.1934 |  |  | 1.22(4)/1.22(5) |  |  |  |  |
| 15 | 65 | 24.83 | 0.497 | 9.25 | 11.05 | 3.55E-04 | 7.89E-03 | 1.0728(3) | 1.0735 | 1.22 |  | 166.07 | 433.5 | 6.30E-12 | 1.15E-10 |
| 65 | 117 | 26.78 | 0.515 | 9.25 | 10.82 | 4.41E-04 | 7.70E-03 | 1.0708 | 1.0718 | 1.21 |  | 165.72 | 435.1 | 8.12E-12 | 1.17E-10 |
| 117 | 1192 | 530.69 | 0.494 | 9.25 | 9.69 | 1.30E-03 | 4.87E-03 | 0.9590 | 1.0149 | 1.16 |  | 161.84 | 452.8 | 2.33E-11 | 7.51E-11 |
| 1192 | 1241 | 24.56 | 0.501 | 9.25 | 9.53 | 1.76E-03 | 3.80E-03 | 0.9522 | 0.9556 | 1.11 |  | 157.97 | 470.4 | 3.27E-11 | 6.35E-11 |
| 1241 | 1463 | 109.99 | 0.495 | 9.25 | 9.52 | 1.72E-03 | 3.69E-03 | 0.9225 | 0.9373 | 1.10 |  | 157.03 | 474.6 | 3.19E-11 | 6.23E-11 |
| 1474 | 1517 | 21.65 | 0.504 | 9.25 | 9.47 | 1.80E-03 | 3.42E-03 | 0.9164 | 0.9194 | 1.09 |  | 156.04 | 479.1 | 3.42E-11 | 5.99E-11 |
| 1517 | 2572 | 514.73 | 0.488 | 9.25 | 9.44 | 1.94E-03 | 2.77E-03 | 0.7643 | 0.8403 | 1.04 |  | 152.26 | 496.3 | 3.78E-11 | 5.20E-11 |
| 2572 | 2629 | 27.33 | 0.479 | 9.25 | 9.40 | 2.15E-03 | 2.45E-03 | 0.7556 | 0.7599 | 0.99 |  | 148.43 | 513.7 | 4.40E-11 | 5.07E-11 |
| 2629 | 2833 | 100.48 | 0.493 | 9.25 | 9.40 | 2.15E-03 | 2.43E-03 | 0.7236 | 0.7396 | 0.98 |  | 147.53 | 517.8 | 4.62E-11 | 5.32E-11 |
| 2833 | 2883 | 24.56 | 0.491 | 9.25 | 9.40 | 2.16E-03 | 2.41E-03 | 0.7159 | 0.7198 | 0.97 |  | 146.66 | 521.8 | 4.70E-11 | 5.42E-11 |
| 2883 | 4047 | 565.08 | 0.485 | 9.25 | 9.38 | 2.22E-03 | 2.13E-03 | 0.5368 | 0.6264 | 0.91 |  | 142.48 | 540.8 | 5.31E-11 | 5.58E-11 |
| 4047 | 4112 | 29.74 | 0.458 | 9.25 | 9.39 | 2.23E-03 | 1.98E-03 | 0.5277 | 0.5323 | 0.86 | 0.82(5) | 138.25 | 560.1 | 5.70E-11 | 5.89E-11 |
| 4112 | 4359 | 119.63 | 0.484 | 9.25 | 9.39 | 2.22E-03 | 1.93E-03 | 0.4912 | 0.5095 | 0.85 |  | 137.17 | 565.0 | 6.23E-11 | 6.40E-11 |
| 4359 | 4408 | 23.58 | 0.481 | 9.25 | 9.39 | 2.20E-03 | 1.86E-03 | 0.4842 | 0.4877 | 0.83 |  | 136.15 | 569.6 | 6.36E-11 | 6.45E-11 |
| 4408 | 5517 | 534.06 | 0.482 | 9.25 | 9.34 | 2.14E-03 | 1.66E-03 | 0.3330 | 0.4086 | 0.78 |  | 132.16 | 587.8 | 7.16E-11 | 7.10E-11 |
| 5517 | 5557 | 19.49 | 0.487 | 9.25 | 9.34 | 2.01E-03 | 1.45E-03 | 0.3279 | 0.3304 | 0.73 |  | 128.21 | 605.8 | 8.17E-11 | 8.03E-11 |
| 5557 | 5738 | 86.54 | 0.478 | 9.25 | 9.35 | 1.99E-03 | 1.44E-03 | 0.3059 | 0.3169 | 0.72 |  | 127.44 | 609.2 | 8.23E-11 | 8.22E-11 |
| 5738 | 5802 | 30.86 | 0.482 | 9.25 | 9.36 | 1.99E-03 | 1.39E-03 | 0.2982 | 0.3021 | 0.71 |  | 126.60 | 613.1 | 8.62E-11 | 8.51E-11 |
| 5802 | 9802 | 1918.35 | 0.480 | 9.26 | 9.28 | 7.66E-04 | 4.72E-04 | 0.1328 | 0.2155 | 0.53 |  | 112.60 | 676.7 | 4.20E-11 | 4.87E-11 |
| 9802 | 9832 | 13.64 | 0.455 | 9.26 | 9.27 | 1.02E-04 | 3.49E-05 | 0.1327 | 0.1327 | 0.35 | 0.20(5) | 98.72 | 739.9 | 7.83E-12 | 7.64E-12 |

(1) Input Ca and Si concentration were below the detection limit ([Ca] < 1.2 10-5 m and [Si] < 8.3 10-6 m) and were therefore assumed to be 0.

(2) Estimation based on the linear regression shown in Fig. 6

(3) Corrected assuming almost 10% of impurities

(4) Calculated from TGA/DSC results

(5) Direct measurement by TEM/EDX

Grey values were obtained after total C-S-H dissolution and therefore were not considered.

Table A 2: Fluid chemistry and calculation of dissolution rates from the CSH_1.4 experiment.

| Initial time (min) | Final time (min) | Sampled mass (g) | Flow rate (mL min-1) | pH (in) | pH (out) | Si (out)(1) (mol L-1) | Ca (out)(1) (mol L-1) | Si-final mass (g) | Si-average mass (g) | Estimated C/S(2) | Measured C/S | Estimated molar mass (g mol-1) | Estimated specific surface area (m2 g-1) | Si-dissolution rate (mol m-2 s-1) | Ca-dissolution rate (mol m-2 s-1) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | 1.1876 |  |  | 1.22(4)/1.21(5) |  |  |  |  |
| 0 | 48 | 27.66 | 0.576 | 9.22 | 10.28 | 3.05E-04 | 7.52E-03 | 1.1046(3) | 1.1053 | 1.22 |  | 166.25 | 432.7 | 6.12E-12 | 1.24E-10 |
| 48 | 132 | 48.59 | 0.578 | 9.22 | 10.24 | 3.33E-04 | 7.25E-03 | 1.1019 | 1.1033 | 1.22 |  | 165.97 | 434.0 | 6.70E-12 | 1.20E-10 |
| 132 | 186 | 31.24 | 0.579 | 9.22 | 10.02 | 5.63E-04 | 6.03E-03 | 1.0990 | 1.1005 | 1.21 |  | 165.68 | 435.3 | 1.13E-11 | 1.00E-10 |
| 186 | 358 | 99.96 | 0.581 | 9.22 | 9.81 | 8.94E-04 | 5.02E-03 | 1.0843 | 1.0916 | 1.21 |  | 165.21 | 437.4 | 1.81E-11 | 8.45E-11 |
| 358 | 1366 | 590.69 | 0.586 | 9.22 | 9.41 | 1.50E-03 | 2.81E-03 | 0.9402 | 1.0123 | 1.17 |  | 162.76 | 448.6 | 3.22E-11 | 5.16E-11 |
| 1366 | 1410 | 25.34 | 0.576 | 9.22 | 9.37 | 1.74E-03 | 2.22E-03 | 0.9332 | 0.9367 | 1.15 |  | 160.57 | 458.5 | 3.88E-11 | 4.32E-11 |
| 1410 | 1740 | 192.09 | 0.582 | 9.22 | 9.32 | 1.73E-03 | 2.13E-03 | 0.8800 | 0.9066 | 1.14 | 1.13(5) | 159.80 | 462.1 | 4.02E-11 | 4.34E-11 |
| 1740 | 1782 | 24.00 | 0.572 | 9.22 | 9.29 | 1.82E-03 | 2.10E-03 | 0.8730 | 0.8765 | 1.13 |  | 159.02 | 465.6 | 4.24E-11 | 4.34E-11 |
| 1782 | 2786 | 585.49 | 0.583 | 9.22 | 9.28 | 1.79E-03 | 1.94E-03 | 0.7086 | 0.7908 | 1.10 |  | 156.85 | 475.5 | 4.63E-11 | 4.58E-11 |
| 2786 | 2830 | 25.68 | 0.584 | 9.22 | 9.30 | 1.77E-03 | 1.87E-03 | 0.7015 | 0.7050 | 1.07 |  | 154.67 | 485.4 | 5.03E-11 | 4.96E-11 |
| 2830 | 3106 | 158.94 | 0.576 | 9.22 | 9.30 | 1.76E-03 | 1.83E-03 | 0.6585 | 0.6800 | 1.06 | 1.11(5) | 154.00 | 488.4 | 5.08E-11 | 4.97E-11 |
| 3106 | 3153 | 26.83 | 0.571 | 9.22 | 9.30 | 1.72E-03 | 1.85E-03 | 0.6514 | 0.6550 | 1.05 |  | 153.33 | 491.5 | 5.09E-11 | 5.20E-11 |
| 3153 | 4301 | 666.64 | 0.581 | 9.20 | 9.30 | 1.71E-03 | 1.76E-03 | 0.4797 | 0.5656 | 1.02 |  | 150.85 | 502.8 | 5.81E-11 | 5.87E-11 |
| 4301 | 4347 | 26.65 | 0.579 | 9.20 | 9.31 | 1.61E-03 | 1.61E-03 | 0.4734 | 0.4765 | 0.99 |  | 148.36 | 514.1 | 6.34E-11 | 6.43E-11 |
| 4347 | 4602 | 146.27 | 0.574 | 9.20 | 9.29 | 1.59E-03 | 1.60E-03 | 0.4390 | 0.4562 | 0.98 | 0.95(5) | 147.74 | 516.9 | 6.45E-11 | 6.61E-11 |
| 4602 | 4641 | 22.50 | 0.577 | 9.20 | 9.28 | 1.54E-03 | 1.54E-03 | 0.4339 | 0.4364 | 0.97 |  | 147.13 | 519.7 | 6.53E-11 | 6.72E-11 |
| 4641 | 5728 | 627.87 | 0.578 | 9.20 | 9.30 | 1.34E-03 | 1.30E-03 | 0.3121 | 0.3730 | 0.94 |  | 144.78 | 530.3 | 6.52E-11 | 6.73E-11 |
| 5728 | 5776 | 27.76 | 0.578 | 9.20 | 9.30 | 1.04E-03 | 1.02E-03 | 0.3080 | 0.3100 | 0.91 |  | 142.42 | 541.1 | 5.95E-11 | 6.41E-11 |
| 5776 | 5973 | 113.99 | 0.579 | 9.20 | 9.25 | 1.02E-03 | 1.00E-03 | 0.2915 | 0.2997 | 0.90 | 0.84(5)/1.02(6)/0.96(6) | 141.50 | 545.3 | 6.02E-11 | 6.57E-11 |

(1) Input Ca and Si concentration were below the detection limit ([Ca] < 1.2 10-5 m and [Si] < 8.3 10-6 m) and were therefore assumed to be 0.

(2) Estimation based on the linear regression shown in Fig. 6

(3) Corrected assuming almost 7% of impurities

(4) Calculated from TGA/DSC results

(5) Direct measurement by TEM/EDX

(6) Direct measurement by EPMA

Table A 3: Fluid chemistry and calculation of dissolution rates extracted from the CSH_0.9 experiment.

|  | Final time (min) | Sampled mass (g) | Flow rate (mL min-1) | pH (in) | pH (out) | Si (out)(1) (mol L-1) | Ca (out)(1) (mol L-1) | Si-final mass (g) | Si-average mass (g) | Estimated C/S(2) | Measured C/S | Estimated molar mass (g mol-1) | Estimated specific surface area (m2 g-1) | Si-dissolution rate (mol m-2 s-1) | Ca-dissolution rate (mol m-2 s-1) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | 1.1751 |  |  | 0.85(4)/0.85(5) |  |  |  |  |
| 0 | 84 | 47.73 | 0.568 | 9.22 | 9.40 | 4.99E-04 | 2.23E-03 | 1.1661(3) | 1.1677 | 0.85 |  | 137.44 | 563.8 | 7.18E-12 | 3.78E-11 |
| 84 | 138 | 30.68 | 0.568 | 9.22 | 9.41 | 6.07E-04 | 2.20E-03 | 1.1635 | 1.1648 | 0.85 |  | 137.35 | 564.2 | 8.75E-12 | 3.73E-11 |
| 138 | 310 | 97.14 | 0.565 | 9.22 | 9.35 | 7.79E-04 | 1.93E-03 | 1.1532 | 1.1584 | 0.85 |  | 137.20 | 564.8 | 1.12E-11 | 3.28E-11 |
| 310 | 1318 | 575.70 | 0.571 | 9.22 | 9.32 | 1.35E-03 | 1.45E-03 | 1.0468 | 1.1000 | 0.84 |  | 136.44 | 568.3 | 2.06E-11 | 2.63E-11 |
| 1318 | 1362 | 25.11 | 0.571 | 9.22 | 9.32 | 1.50E-03 | 1.32E-03 | 1.0416 | 1.0442 | 0.83 |  | 135.75 | 571.4 | 2.39E-11 | 2.54E-11 |
| 1362 | 1692 | 186.30 | 0.565 | 9.22 | 9.30 | 1.51E-03 | 1.28E-03 | 1.0036 | 1.0226 | 0.82 |  | 135.51 | 572.5 | 2.42E-11 | 2.50E-11 |
| 1692 | 1734 | 24.00 | 0.572 | 9.22 | 9.30 | 1.55E-03 | 1.28E-03 | 0.9985 | 1.0011 | 0.82 |  | 135.27 | 573.6 | 2.57E-11 | 2.59E-11 |
| 1734 | 2738 | 571.09 | 0.569 | 9.22 | 9.27 | 1.53E-03 | 1.24E-03 | 0.8806 | 0.9396 | 0.81 |  | 134.59 | 576.7 | 2.68E-11 | 2.66E-11 |
| 2738 | 2782 | 25.00 | 0.568 | 9.22 | 9.28 | 1.54E-03 | 1.22E-03 | 0.8754 | 0.8780 | 0.80 |  | 133.91 | 579.8 | 2.86E-11 | 2.82E-11 |
| 2782 | 3058 | 154.98 | 0.562 | 9.22 | 9.26 | 1.46E-03 | 1.15E-03 | 0.8452 | 0.8603 | 0.80 | 0.83(5) | 133.70 | 580.8 | 2.73E-11 | 2.68E-11 |
| 3058 | 3105 | 26.14 | 0.556 | 9.22 | 9.25 | 1.47E-03 | 1.16E-03 | 0.8401 | 0.8426 | 0.80 |  | 133.49 | 581.7 | 2.79E-11 | 2.75E-11 |
| 3105 | 4253 | 651.60 | 0.568 | 9.20 | 9.26 | 1.51E-03 | 1.18E-03 | 0.7098 | 0.7749 | 0.79 |  | 132.71 | 585.3 | 3.14E-11 | 3.11E-11 |
| 4253 | 4299 | 26.09 | 0.567 | 9.20 | 9.27 | 1.48E-03 | 1.16E-03 | 0.7047 | 0.7073 | 0.78 |  | 131.94 | 588.8 | 3.36E-11 | 3.38E-11 |
| 4299 | 4472 | 97.08 | 0.561 | 9.20 | 9.27 | 1.42E-03 | 1.12E-03 | 0.6866 | 0.6956 | 0.78 | 0.76(5)/0.82(6) | 131.79 | 589.4 | 3.23E-11 | 3.27E-11 |

(1) Input Ca and Si concentration were below the detection limit ([Ca] < 1.2 10-5 m and [Si] < 8.3 10-6 m) and were therefore assumed to be 0.

(2) Estimation based on the linear regression shown in Fig. 6

(3) Corrected assuming almost 0.5% of impurities

(4) Calculated from TGA/DSC results

(5) Direct measurement by TEM/EDX

(6) Direct measurement by EPMA