TABLE 5. Calculated and observed structure factors for Pb2(OH)3(NO3). 

##########################
# 
# h,k,l, Fc-squared, Fo-squared, sigma(Fo-squared) and status flag 
# 
data_pbtaftor 
_shelx_title ' pbtaftor in Immm 9 01 ganz neu' 
_shelx_refln_list_code          4 
_shelx_F_calc_maximum     1105.92 
_exptl_crystal_F_000      1776.00 
_reflns_d_resolution_high  0.7109 
 
loop_ 
 _symmetry_equiv_pos_as_xyz 
 'x, y, z' 
 '-x, -y, z' 
 '-x, y, -z' 
 'x, -y, -z' 
 'x+1/2, y+1/2, z+1/2' 
 '-x+1/2, -y+1/2, z+1/2' 
 '-x+1/2, y+1/2, -z+1/2' 
 'x+1/2, -y+1/2, -z+1/2' 
 '-x, -y, -z' 
 'x, y, -z' 
 'x, -y, z' 
 '-x, y, z' 
 '-x+1/2, -y+1/2, -z+1/2' 
 'x+1/2, y+1/2, -z+1/2' 
 'x+1/2, -y+1/2, z+1/2' 
 '-x+1/2, y+1/2, z+1/2' 
 
_cell_length_a     8.3140 
_cell_length_b     8.5450 
_cell_length_c    17.2100 
_cell_angle_alpha  90.000 
_cell_angle_beta   90.000 
_cell_angle_gamma  90.000 
 
_shelx_F_squared_multiplier     1.000 
 
loop_ 
 _refln_index_h 
 _refln_index_k 
 _refln_index_l 
 _refln_F_squared_calc 
 _refln_F_squared_meas 
 _refln_F_squared_sigma 
 _refln_observed_status 
   2   0   0  1021383.69   797302.00  20985.17 o 
   4   0   0  1007203.75   828979.06  31072.97 o 
   6   0   0   348865.31   307014.56   6834.39 o 
   8   0   0   304671.78   295502.84   6128.31 o 
  10   0   0   112340.13   109235.61   6010.98 o 
   1   1   0      236.69     1042.06     38.11 o 
   3   1   0      467.73      539.03     34.96 o 
   5   1   0       31.42       60.49     33.74 o 
   7   1   0       91.17      155.07    105.83 o 
   9   1   0      928.01     1000.47     95.64 o 
  11   1   0      263.25      143.05    186.66 o 
   0   2   0   978461.69   996355.56  17267.91 o 
   2   2   0  1223064.75  1318374.00  53621.34 o 
   4   2   0   762668.44   713628.19  37772.82 o 
   6   2   0   502162.19   478050.44  15264.48 o 
   8   2   0   219036.08   222486.97   4012.09 o 
  10   2   0   118850.36   133907.55   3732.26 o 
   1   3   0     1092.30     1710.99     50.85 o 
   3   3   0     3038.92     3212.23     86.96 o 
   5   3   0     7587.49     7657.57    260.07 o 
   7   3   0     1916.26     2103.21    150.38 o 
   9   3   0      643.56      841.09    171.47 o 
  11   3   0      342.43      347.78    236.73 o 
   0   4   0   939304.50  1001306.38  38459.69 o 
   2   4   0   743487.38   795501.31  13038.16 o 
   4   4   0   478769.28   488940.00  10528.09 o 
   6   4   0   308086.38   292788.84  13026.42 o 
   8   4   0   187144.89   190429.23   3792.17 o 
  10   4   0    96527.13   107489.08   3815.83 o 
   1   5   0     2292.22     2652.72     95.37 o 
   3   5   0      467.74      506.81     57.16 o 
   5   5   0     3233.91     3387.92    116.08 o 
   7   5   0     1991.63     1954.95    185.98 o 
   9   5   0     5217.78     4796.19    266.76 o 
   0   6   0   300005.84   309857.13   7785.71 o 
   2   6   0   443608.97   467392.38   7751.45 o 
   4   6   0   287448.41   287119.06   3446.79 o 
   6   6   0   251102.22   238820.53   4161.07 o 
   8   6   0   105462.28   103225.62   2914.93 o 
  10   6   0    67086.91    66775.63   3621.90 o 
   1   7   0      162.81      260.27     63.41 o 
   3   7   0     1705.13     1938.85    106.46 o 
   5   7   0     4065.98     3631.93    218.32 o 
   7   7   0     4288.04     3507.45    191.83 o 
   9   7   0     2598.86     3362.13    278.93 o 
   0   8   0   264943.28   271842.00   6062.90 o 
   2   8   0   176143.91   178813.83   5563.22 o 
   4   8   0   163530.67   158606.28   3926.90 o 
   6   8   0    90178.33    85183.27   1701.00 o 
   8   8   0    71827.91    67474.76   2327.53 o 
   1   9   0      118.15       58.03    114.29 o 
   3   9   0     1593.38     1577.34    235.05 o 
   5   9   0      696.53      711.70    173.75 o 
   7   9   0     4818.07     3781.10    217.97 o 
   0  10   0    80999.81    83216.52   4792.17 o 
   2  10   0    86243.30    86641.05   1973.65 o 
   4  10   0    72217.61    71793.41   1981.26 o 
   6  10   0    52323.63    47050.96   1747.47 o 
   1  11   0       61.55       60.80    155.44 o 
   3  11   0     1176.21     1657.04   1117.88 o 
   0  12   0    44403.07    43399.42   2450.91 o 
   1   0   1     2696.07     2437.48    159.83 o 
   3   0   1      302.70      575.61     33.41 o 
   5   0   1    17461.73    15879.18    369.89 o 
   7   0   1    20148.94    19405.34    318.40 o 
   9   0   1    28802.22    29355.88    659.23 o 
  11   0   1    17266.95    18034.56    765.67 o 
   2   1   1     5780.29     4522.10    126.31 o 
   4   1   1      712.37      802.52     41.18 o 
   6   1   1      673.07      672.32     34.24 o 
   8   1   1      793.31      741.79     45.96 o 
  10   1   1      634.41      610.66     97.43 o 
   1   2   1     4295.06     5148.41     51.55 o 
   3   2   1    10429.74    10459.97    227.74 o 
   5   2   1    22555.58    22270.05    323.31 o 
   7   2   1    17926.76    18202.49    216.41 o 
   9   2   1    19300.37    19846.22    397.37 o 
  11   2   1    14342.10    16169.21    532.26 o 
   0   3   1    22921.00    20882.41    287.77 o 
   2   3   1     2721.52     2704.69     41.29 o 
   4   3   1    35920.97    35097.76    639.59 o 
   6   3   1    11000.46    10580.38    137.80 o 
   8   3   1    12061.56    12351.20    220.17 o 
  10   3   1     2171.08     2518.69    146.40 o 
   1   4   1       57.85      121.77     26.84 o 
   3   4   1     7461.61     7762.11     93.25 o 
   5   4   1    11026.24    11326.00    253.48 o 
   7   4   1    21361.91    21246.15    577.68 o 
   9   4   1    16640.51    18240.56    441.17 o 
  11   4   1    14043.27    15897.04    582.80 o 
   0   5   1    48485.91    49116.00    685.66 o 
   2   5   1    49520.65    48906.93    485.43 o 
   4   5   1    27464.95    27929.86    278.93 o 
   6   5   1    20857.38    20484.87    391.33 o 
   8   5   1    12476.56    12313.79    292.95 o 
  10   5   1     7870.91     7866.72    329.18 o 
   1   6   1      422.63      502.31     42.22 o 
   3   6   1    13843.61    14042.06    206.54 o 
   5   6   1    10390.57    10085.79    147.07 o 
   7   6   1    13393.81    13453.29    275.17 o 
   9   6   1     7952.06     8192.56    271.45 o 
   0   7   1    49170.38    50765.26    688.39 o 
   2   7   1    49723.19    50364.91    488.91 o 
   4   7   1    42217.73    41878.34    460.26 o 
   6   7   1    30773.70    31168.97    429.97 o 
   8   7   1    16337.35    16103.99    443.19 o 
   1   8   1      230.18      304.33     56.81 o 
   3   8   1     2211.94     2370.80     74.41 o 
   5   8   1     4981.84     4821.38    141.21 o 
   7   8   1     7551.89     7070.32    227.99 o 
   0   9   1    52301.90    53003.44   1538.98 o 
   2   9   1    57186.36    58308.81   1024.31 o 
   4   9   1    30373.64    29633.36    469.63 o 
   6   9   1    24766.63    23059.78    573.07 o 
   1  10   1      444.78      333.18    109.03 o 
   3  10   1     1284.71     1295.26    131.96 o 
   5  10   1     3277.41     3333.79    164.92 o 
   0  11   1    36616.19    41601.60   1334.40 o 
   2  11   1    32490.04    33561.01    833.40 o 
   4  11   1    29579.35    30440.29    895.01 o 
   2   0   2    20115.17    15728.83    718.72 o 
   4   0   2      148.17      225.07     50.80 o 
   6   0   2      327.53      330.27     46.25 o 
   8   0   2     1187.71     1295.45     86.64 o 
  10   0   2      112.78      242.89    125.73 o 
   1   1   2      108.93      490.55     13.62 o 
   3   1   2     5832.91     5706.36    142.05 o 
   5   1   2     1627.21     1476.93     64.49 o 
   7   1   2       45.11       60.31     67.20 o 
   9   1   2       67.40       95.85     57.72 o 
  11   1   2       90.95      103.95    126.58 o 
   0   2   2    18997.55    17007.36    559.73 o 
   2   2   2     1386.32     1648.51     30.17 o 
   4   2   2      954.56     1073.21     59.62 o 
   6   2   2      247.95      206.37     39.65 o 
   8   2   2     1057.97     1028.56     68.23 o 
  10   2   2       58.00      132.89     94.04 o 
   1   3   2    12491.46    13892.84    156.92 o 
   3   3   2      795.17      870.86     35.65 o 
   5   3   2     1837.41     1958.91     56.32 o 
   7   3   2      844.64      870.66     56.28 o 
   9   3   2       47.16      296.42     97.33 o 
  11   3   2      100.37     -139.16    139.16 o 
   0   4   2      922.73     1029.81     39.16 o 
   2   4   2      591.61      805.55     43.54 o 
   4   4   2      199.23      258.28     28.41 o 
   6   4   2      235.24      358.11     51.45 o 
   8   4   2       84.11       44.35     70.31 o 
  10   4   2      176.54       60.56    137.46 o 
   1   5   2     1030.24     1192.37     42.35 o 
   3   5   2       28.53       66.00     29.84 o 
   5   5   2       12.42       49.94     41.64 o 
   7   5   2      316.87      286.59     87.30 o 
   9   5   2       17.35       64.03    127.29 o 
   0   6   2       48.60      259.44     63.34 o 
   2   6   2      326.35      359.37     39.97 o 
   4   6   2       50.18      102.27     45.07 o 
   6   6   2      211.54      255.39     70.67 o 
   8   6   2      737.31      646.09    108.13 o 
  10   6   2       35.95      441.92    187.75 o 
   1   7   2       39.19      213.09     53.78 o 
   3   7   2      929.06      992.64     54.18 o 
   5   7   2      353.07      462.15     92.84 o 
   7   7   2        9.27      180.65    102.49 o 
   9   7   2       90.72      269.39    159.57 o 
   0   8   2      962.52      884.55     81.44 o 
   2   8   2      950.10      802.77     60.99 o 
   4   8   2       51.46      122.44     62.84 o 
   6   8   2      579.81      486.59    105.32 o 
   8   8   2       85.14      215.62    145.90 o 
   1   9   2      151.99      194.82     75.65 o 
   3   9   2      510.47      466.90    100.94 o 
   5   9   2       60.52      125.04    100.20 o 
   7   9   2        5.54      -54.63    121.48 o 
   0  10   2      517.94      890.34    201.10 o 
   2  10   2       25.47       -6.91     92.71 o 
   4  10   2      220.36      348.66    143.03 o 
   6  10   2        2.81      149.47    138.64 o 
   1  11   2       45.04       74.62    119.36 o 
   3  11   2        1.57      300.87    126.67 o 
   1   0   3     3870.34     3651.57    189.56 o 
   3   0   3    27412.33    25541.77   1248.01 o 
   5   0   3    24349.89    21406.21    305.25 o 
   7   0   3    26349.25    27016.63    656.98 o 
   9   0   3    19879.48    20795.53    515.23 o 
  11   0   3    16269.15    17931.51   1039.92 o 
   0   1   3      807.04      907.26     20.08 o 
   2   1   3    18537.02    17731.45    669.37 o 
   4   1   3       65.12      134.51     20.71 o 
   6   1   3     3071.43     3210.27     74.77 o 
   8   1   3      204.40      303.55     70.67 o 
  10   1   3      666.96      915.59     94.09 o 
   1   2   3     1247.06     1486.58     21.41 o 
   3   2   3    12558.71    11651.23    169.41 o 
   5   2   3    22925.30    22151.88    698.41 o 
   7   2   3    23267.91    24019.35    323.65 o 
   9   2   3    19378.83    20685.90    404.31 o 
  11   2   3    14272.55    15539.32    571.96 o 
   0   3   3    63719.56    62850.83   2035.12 o 
   2   3   3    19151.03    19804.14    163.48 o 
   4   3   3    28395.32    27523.01    524.65 o 
   6   3   3     5695.55     6058.67    193.28 o 
   8   3   3     5782.67     5898.55    129.37 o 
  10   3   3     2083.03     2286.73    183.99 o 
   1   4   3     1747.73     1846.83     34.16 o 
   3   4   3     5901.79     6786.38     82.64 o 
   5   4   3    12500.26    12843.63    194.56 o 
   7   4   3    15080.09    15356.78    271.90 o 
   9   4   3    15851.79    16480.15    461.34 o 
   0   5   3    42596.34    41865.39   1359.58 o 
   2   5   3    64172.97    64481.27    582.32 o 
   4   5   3    23591.44    24208.63    348.56 o 
   6   5   3    24756.28    25196.96    546.96 o 
   8   5   3     9864.17     9767.66    230.89 o 
  10   5   3     7414.13     6901.66    273.48 o 
   1   6   3      136.14      206.78     45.29 o 
   3   6   3     2108.93     2468.19     63.10 o 
   5   6   3     6942.94     7308.71    120.99 o 
   7   6   3    10242.73    10311.91    267.55 o 
   9   6   3    10969.48    11495.91    364.10 o 
   0   7   3    60558.95    63732.14   1002.41 o 
   2   7   3    41260.60    42388.97    465.17 o 
   4   7   3    45743.31    45880.09    516.42 o 
   6   7   3    23649.60    22331.18    381.92 o 
   8   7   3    17889.11    17756.63    603.07 o 
   1   8   3      298.40      338.65     59.99 o 
   3   8   3     1714.21     1903.19    115.07 o 
   5   8   3     3887.31     3767.18    122.40 o 
   7   8   3     5737.01     5276.41    176.98 o 
   0   9   3    40378.01    41361.45   1635.58 o 
   2   9   3    44653.23    46231.61    638.52 o 
   4   9   3    32437.45    31991.53    568.47 o 
   6   9   3    28108.46    26061.55    616.80 o 
   1  10   3       70.26      207.49    114.30 o 
   3  10   3     1176.85     1364.22    112.54 o 
   5  10   3     2353.44     2144.27    155.81 o 
   0  11   3    35391.41    37908.98   1325.53 o 
   2  11   3    29193.62    30176.04    739.07 o 
   4  11   3    29152.48    27539.06    753.78 o 
   2   0   4  1129630.38  1227381.38  33593.47 o 
   4   0   4   778136.81   708195.19  12963.66 o 
   6   0   4   483041.19   449007.25   7755.89 o 
   8   0   4   236755.48   237727.31   6210.29 o 
  10   0   4   129246.01   136161.23   3953.55 o 
   1   1   4       77.94      548.12     16.97 o 
   3   1   4     6736.49     6392.28    176.02 o 
   5   1   4      820.79      762.93     44.36 o 
   7   1   4      182.30      280.86     42.27 o 
   9   1   4      512.64      483.38     60.28 o 
  11   1   4       33.68      209.27    150.93 o 
   0   2   4  1120582.25  1264003.13  32873.84 o 
   2   2   4   932744.56  1002684.31   8039.97 o 
   4   2   4   654266.88   636921.81  18091.89 o 
   6   2   4   421632.47   404118.28  11145.72 o 
   8   2   4   246068.05   252614.70   4471.49 o 
  10   2   4   111578.20   121265.91   2975.16 o 
   1   3   4     5271.50     5089.64     97.90 o 
   3   3   4       21.17       80.37     35.36 o 
   5   3   4     1053.76     1020.61     51.89 o 
   7   3   4       82.55      110.13     67.20 o 
   9   3   4     2022.66     2072.94    115.46 o 
  11   3   4     1130.46     2075.82    583.90 o 
   0   4   4   786725.25   887982.50  19898.65 o 
   2   4   4   645260.88   684068.50   9983.47 o 
   4   4   4   526876.88   539052.88   6339.17 o 
   6   4   4   289055.69   289769.59   4975.80 o 
   8   4   4   161871.16   161342.25   3131.90 o 
  10   4   4    85979.05    89498.97   2501.18 o 
   1   5   4     1079.13     1113.13     40.20 o 
   3   5   4      145.32      162.83     37.54 o 
   5   5   4     1184.69     1309.17     64.79 o 
   7   5   4     4480.20     4409.82    111.87 o 
   9   5   4     2802.81     3028.61    214.25 o 
   0   6   4   443143.38   474119.75  14477.37 o 
   2   6   4   399825.47   400249.41   5314.66 o 
   4   6   4   273925.00   279229.31   3145.82 o 
   6   6   4   186974.45   181089.09   2937.16 o 
   8   6   4   110017.49   107787.84   2222.10 o 
   1   7   4      219.89      175.56     44.24 o 
   3   7   4     4611.44     4619.68     88.35 o 
   5   7   4     2084.80     2136.05     82.48 o 
   7   7   4     3876.88     3918.31    201.69 o 
   9   7   4     3051.49     2787.95    178.95 o 
   0   8   4   198620.88   204313.94   4930.50 o 
   2   8   4   204321.55   206924.75   3547.11 o 
   4   8   4   143157.92   141195.39   1747.25 o 
   6   8   4   100485.39    93532.05   1752.32 o 
   8   8   4    51711.99    49714.63   1360.78 o 
   1   9   4       93.98      272.15     81.75 o 
   3   9   4     1138.77     1177.96     89.42 o 
   5   9   4     3782.67     3152.68    146.94 o 
   7   9   4     4708.56     4899.77    237.30 o 
   0  10   4    88956.76    88155.92   2286.29 o 
   2  10   4    78085.02    78657.62   1716.05 o 
   4  10   4    64319.63    60162.72   1360.91 o 
   6  10   4    44658.63    38966.79   1002.40 o 
   1  11   4      602.80      515.64    133.94 o 
   3  11   4     1479.72     1423.70    168.10 o 
   1   0   5     5145.89     5050.83     68.58 o 
   3   0   5     3124.10     2906.58    129.41 o 
   5   0   5    31725.38    29669.34   1007.19 o 
   7   0   5    22256.46    22345.37    867.11 o 
   9   0   5    24019.42    25796.70    576.52 o 
  11   0   5    13234.58    15719.18   1028.32 o 
   0   1   5    20656.04    19572.47    383.15 o 
   2   1   5     2304.83     2120.91     84.42 o 
   4   1   5     5244.50     5433.51    198.28 o 
   6   1   5       55.63      169.82     32.80 o 
   8   1   5      593.00      665.76     63.06 o 
  10   1   5      130.24      333.02    127.14 o 
   1   2   5     7027.43     7255.80     85.05 o 
   3   2   5    20133.36    19025.06    508.44 o 
   5   2   5    22603.64    22015.58    498.88 o 
   7   2   5    17033.57    17624.80    478.99 o 
   9   2   5    17193.50    17724.11    403.27 o 
  11   2   5    13121.57    13309.82    535.67 o 
   0   3   5    31184.20    30637.55    767.07 o 
   2   3   5    23252.33    22835.90    209.58 o 
   4   3   5    15868.48    15345.39    319.75 o 
   6   3   5    10135.43    10295.08    253.15 o 
   8   3   5     5616.65     5724.12    212.55 o 
  10   3   5     2242.63     2321.62    164.30 o 
   1   4   5      241.48      262.90     31.08 o 
   3   4   5     3690.56     4183.54     60.76 o 
   5   4   5     8561.42     9153.43    130.40 o 
   7   4   5    19307.29    20033.79    861.81 o 
   9   4   5    14828.44    15349.11    410.05 o 
   0   5   5    66082.30    67253.05   1735.76 o 
   2   5   5    38176.77    37138.24    413.87 o 
   4   5   5    35085.19    35323.29    363.08 o 
   6   5   5    12336.76    12583.65    260.76 o 
   8   5   5    10871.34    10838.76    308.07 o 
  10   5   5     5257.27     5207.03    233.85 o 
   1   6   5      252.66      328.03     38.02 o 
   3   6   5     6377.43     6500.24    150.05 o 
   5   6   5     5365.89     5429.43    192.99 o 
   7   6   5     9747.38     9729.83    241.03 o 
   9   6   5     8541.04     8399.87    316.35 o 
   0   7   5    36974.99    39983.48    861.79 o 
   2   7   5    47600.46    47669.07    643.94 o 
   4   7   5    30670.37    31077.83    438.62 o 
   6   7   5    31179.48    30884.72   1104.58 o 
   8   7   5    14678.41    14475.28    598.42 o 
   1   8   5       41.51       70.95     49.88 o 
   3   8   5      690.89      810.27     65.36 o 
   5   8   5     3704.05     3569.66    120.62 o 
   7   8   5     6663.84     6428.28    246.43 o 
   0   9   5    40678.15    43704.88   1285.81 o 
   2   9   5    40873.80    42066.87    592.18 o 
   4   9   5    31379.53    29860.94    585.47 o 
   6   9   5    23162.90    23116.49    550.93 o 
   1  10   5      520.76      542.72    140.67 o 
   3  10   5     1526.46     1534.96    123.09 o 
   5  10   5     3141.62     2981.02    158.20 o 
   0  11   5    27928.01    29598.56   1621.65 o 
   2  11   5    29521.26    30921.58    761.95 o 
   4  11   5    24578.65    23224.80    638.85 o 
   0   0   6    22840.44    18349.20   1177.18 o 
   2   0   6     1018.14     1363.09     37.81 o 
   4   0   6     1696.94     1671.23     40.85 o 
   6   0   6      282.00      365.34     38.47 o 
   8   0   6     2962.36     2850.18    241.54 o 
  10   0   6      171.89      310.34    220.12 o 
   1   1   6      108.86      345.74     23.66 o 
   3   1   6      490.37      709.13     31.19 o 
   5   1   6     1194.21     1211.91     60.31 o 
   7   1   6       35.40      114.09     34.87 o 
   9   1   6      166.04      103.25     57.16 o 
  11   1   6       67.02      -94.18    230.19 o 
   0   2   6      788.01     1114.28     33.89 o 
   2   2   6      695.43      967.45     29.88 o 
   4   2   6     6987.42     7200.47    201.20 o 
   6   2   6     1917.97     1916.31     71.31 o 
   8   2   6      912.71     1023.04     82.47 o 
  10   2   6      121.49      130.85    158.45 o 
   1   3   6       35.65      145.60     19.68 o 
   3   3   6      634.07      763.48     36.10 o 
   5   3   6       46.21       50.92     30.73 o 
   7   3   6      150.49      155.18     40.30 o 
   9   3   6       52.27      157.05    103.98 o 
   0   4   6     2000.55     2197.38     52.09 o 
   2   4   6    11257.46    10760.75    143.62 o 
   4   4   6      979.43      967.32     44.19 o 
   6   4   6      767.37      877.41     44.03 o 
   8   4   6       43.05       43.43    106.64 o 
  10   4   6      782.50      752.23    190.50 o 
   1   5   6      230.69      320.33     40.88 o 
   3   5   6     1636.88     1708.22     45.63 o 
   5   5   6      192.80      228.17     49.97 o 
   7   5   6      266.11      307.03     66.42 o 
   9   5   6      173.32      404.97    139.25 o 
   0   6   6       40.90      218.52     54.62 o 
   2   6   6     2086.76     2132.31     54.75 o 
   4   6   6     1174.18     1441.23     61.13 o 
   6   6   6     1706.42     1626.22     67.12 o 
   8   6   6       28.80       77.95    112.27 o 
   1   7   6        2.63       14.41     58.19 o 
   3   7   6       89.32      183.46     53.66 o 
   5   7   6       48.35      173.45     66.27 o 
   7   7   6        1.54      201.07    155.08 o 
   9   7   6      222.54      155.35    192.73 o 
   0   8   6     4288.45     4725.49    355.05 o 
   2   8   6     1153.88     1298.09     81.78 o 
   4   8   6      314.72      271.88     71.75 o 
   6   8   6       26.51      132.10    109.17 o 
   8   8   6      296.56      674.06    167.55 o 
   1   9   6      126.47      249.93     82.44 o 
   3   9   6      141.26      166.23     76.21 o 
   5   9   6      213.19      178.40    112.44 o 
   7   9   6       44.56      257.63    159.34 o 
   0  10   6      251.21      382.15    192.61 o 
   2  10   6       84.73      213.93    103.01 o 
   4  10   6     1240.62     1182.50    142.76 o 
   1  11   6        6.34      132.81    131.73 o 
   3  11   6      147.79      454.20    140.95 o 
   1   0   7       68.08      122.67     21.74 o 
   3   0   7    11603.07    10460.03    428.61 o 
   5   0   7    12428.26    11508.94    255.53 o 
   7   0   7    22234.27    21638.84    390.87 o 
   9   0   7    13711.05    14242.18    519.06 o 
  11   0   7    15486.32    16380.77    983.70 o 
   0   1   7     3867.50     4094.84     71.62 o 
   2   1   7     2916.54     2821.00    103.47 o 
   4   1   7     2284.68     2145.00    149.83 o 
   6   1   7     4637.30     4378.83    128.46 o 
   8   1   7      636.37      724.64     68.60 o 
  10   1   7      361.05      394.12    119.45 o 
   1   2   7       65.61      116.77     17.78 o 
   3   2   7     5257.50     5066.25    136.21 o 
   5   2   7     8170.53     8427.72    227.41 o 
   7   2   7    19000.07    18859.56    579.04 o 
   9   2   7    19656.65    20317.71    635.31 o 
  11   2   7    15608.58    16957.40    644.78 o 
   0   3   7    17724.33    17038.67    325.44 o 
   2   3   7    25701.88    24768.08    294.74 o 
   4   3   7     5765.63     6011.74    156.32 o 
   6   3   7    11533.21    11430.43    157.30 o 
   8   3   7     4386.53     4508.76    141.58 o 
  10   3   7     5124.66     4854.96    243.02 o 
   1   4   7     2053.48     2112.87     50.63 o 
   3   4   7     7571.21     7607.74    129.52 o 
   5   4   7    17429.39    17155.52    367.77 o 
   7   4   7    13472.20    13802.00    298.63 o 
   9   4   7    11765.40    11968.25    347.65 o 
   0   5   7    22240.86    23159.21    496.49 o 
   2   5   7    30964.02    31004.74    397.91 o 
   4   5   7    32768.83    32367.35    480.13 o 
   6   5   7    23555.92    24308.51    681.10 o 
   8   5   7    12382.93    13271.42    509.80 o 
  10   5   7     5424.66     5177.09    331.91 o 
   1   6   7     1823.54     2013.41     49.65 o 
   3   6   7     2391.81     2451.09     55.69 o 
   5   6   7     9706.04     9906.96    255.53 o 
   7   6   7     8208.74     8145.30    216.71 o 
   9   6   7    12099.92    12532.79    649.19 o 
   0   7   7    65142.86    65750.99   1587.11 o 
   2   7   7    42207.48    42356.29    658.58 o 
   4   7   7    33538.57    34443.88    462.87 o 
   6   7   7    18434.04    17661.00    449.53 o 
   8   7   7    14487.63    14746.03    508.17 o 
   1   8   7      727.17      922.67     86.05 o 
   3   8   7     2841.21     3013.55    101.24 o 
   5   8   7     6338.92     6031.82    220.75 o 
   7   8   7     5059.94     4820.56    275.44 o 
   0   9   7    42367.74    44455.33   1001.33 o 
   2   9   7    37052.22    37148.87    693.43 o 
   4   9   7    36510.48    35575.52    754.80 o 
   6   9   7    21281.29    20705.52    596.72 o 
   1  10   7        7.04      172.30    110.54 o 
   3  10   7      954.12      817.36    106.36 o 
   5  10   7     1006.84      900.78    148.84 o 
   0  11   7    36535.54    36711.12   1300.82 o 
   2  11   7    31831.93    32988.19    902.49 o 
   0   0   8  1041465.00   992747.44  51228.03 o 
   2   0   8   803173.00   811003.50  24179.48 o 
   4   0   8   592150.00   586921.69  13697.63 o 
   6   0   8   353111.63   322459.97   4913.84 o 
   8   0   8   207231.25   190799.23   3909.43 o 
  10   0   8    99776.81   105442.79   3672.36 o 
   1   1   8        1.04      116.40     27.63 o 
   3   1   8     6965.45     6594.60    231.95 o 
   5   1   8        4.57      100.62     42.26 o 
   7   1   8      209.79      319.71     51.96 o 
   9   1   8        8.06      -38.95    124.57 o 
   0   2   8   786529.50   794332.38  28165.03 o 
   2   2   8   790344.44   806855.25  17315.79 o 
   4   2   8   513658.75   530814.13  14571.75 o 
   6   2   8   328723.00   315427.50   7423.45 o 
   8   2   8   166823.81   167761.78   6575.05 o 
  10   2   8    96372.38    97188.88   2583.48 o 
   1   3   8     1827.13     1839.50     63.29 o 
   3   3   8     2173.02     2052.71     42.07 o 
   5   3   8      487.89      626.52     53.85 o 
   7   3   8     4293.86     4409.31    129.75 o 
   9   3   8      571.13      677.65    137.49 o 
   0   4   8   552927.06   572715.50  25565.96 o 
   2   4   8   489628.38   509539.63   7258.46 o 
   4   4   8   374963.41   370660.47   6707.91 o 
   6   4   8   253494.16   262121.63   6572.49 o 
   8   4   8   151922.69   157218.20   4315.59 o 
  10   4   8    73205.86    73325.60   2411.88 o 
   1   5   8     1412.69     1506.14     60.51 o 
   3   5   8     3196.75     3149.34     78.46 o 
   5   5   8     3042.35     3145.96    145.24 o 
   7   5   8     1616.47     1752.61     82.55 o 
   9   5   8     2107.19     2026.93    210.94 o 
   0   6   8   314623.41   330583.28   6311.50 o 
   2   6   8   289724.75   291728.72   4738.32 o 
   4   6   8   239286.80   242283.00   3424.11 o 
   6   6   8   153647.39   159704.30   3808.79 o 
   8   6   8    92725.26    96606.98   2802.12 o 
   1   7   8      310.08      307.32     47.97 o 
   3   7   8       54.17      152.92     53.27 o 
   5   7   8     3280.71     3405.17    110.97 o 
   7   7   8     2862.84     2694.60    154.07 o 
   0   8   8   171623.41   173975.13   4149.10 o 
   2   8   8   135800.55   135914.22   1794.97 o 
   4   8   8   128524.13   124784.79   2052.34 o 
   6   8   8    82342.83    81772.92   2283.59 o 
   1   9   8      271.35      243.37    101.02 o 
   3   9   8     1153.56     1121.99    102.78 o 
   5   9   8     2017.97     1879.96    159.95 o 
   0  10   8    70899.85    68147.44   2022.62 o 
   2  10   8    73369.83    71614.88   1674.64 o 
   4  10   8    52510.56    52573.29   1206.02 o 
   1  11   8        7.44      229.35    135.92 o 
   1   0   9      444.45      398.09     51.41 o 
   3   0   9     8443.48     8016.02    329.60 o 
   5   0   9     7856.82     7045.38    180.75 o 
   7   0   9    15544.59    15207.35    395.44 o 
   9   0   9    15988.12    15688.68    782.83 o 
   0   1   9     1974.61     1919.95    123.91 o 
   2   1   9     1326.96     1316.68     55.54 o 
   4   1   9      472.47      545.33     56.13 o 
   6   1   9     1704.07     1816.25     91.20 o 
   8   1   9      902.82      961.52     48.11 o 
  10   1   9      599.60      698.77    154.27 o 
   1   2   9       26.69       76.25     30.48 o 
   3   2   9     3712.56     3691.59     70.43 o 
   5   2   9    10950.97    10829.47    396.81 o 
   7   2   9    17872.95    17678.18    648.48 o 
   9   2   9    14359.51    14346.43    509.39 o 
   0   3   9     7806.05     7712.81    115.52 o 
   2   3   9    11264.52    11345.93    242.77 o 
   4   3   9    13528.64    13262.17    436.92 o 
   6   3   9     8261.40     8163.20    258.53 o 
   8   3   9     4836.43     4781.34    374.08 o 
  10   3   9     2490.94     2436.92    175.24 o 
   1   4   9     3039.28     3038.28     76.32 o 
   3   4   9     5813.96     6097.29    141.70 o 
   5   4   9    12090.60    12288.76    286.71 o 
   7   4   9    10323.55    10332.25    373.34 o 
   9   4   9    13253.50    13776.05    664.25 o 
   0   5   9    26117.33    25171.16    627.55 o 
   2   5   9    29249.67    28777.95    398.32 o 
   4   5   9    17552.30    17475.70    341.13 o 
   6   5   9    18881.26    18998.72    479.59 o 
   8   5   9     9854.19    10162.01    487.82 o 
   1   6   9      426.36      480.90     37.30 o 
   3   6   9     3417.51     3534.43     87.02 o 
   5   6   9     9101.17     9288.19    166.80 o 
   7   6   9     9818.15    10752.56    446.10 o 
   9   6   9     8363.13     8043.06    346.63 o 
   0   7   9    38996.94    40220.17    942.83 o 
   2   7   9    34621.56    35154.39    409.09 o 
   4   7   9    31525.67    31857.05    571.46 o 
   6   7   9    17828.92    17910.62    384.70 o 
   8   7   9    12050.37    11254.76    631.93 o 
   1   8   9      506.35      619.29     83.84 o 
   3   8   9     3152.86     3312.64    111.94 o 
   5   8   9     4318.39     3863.40    240.88 o 
   7   8   9     5012.18     4802.16    340.67 o 
   0   9   9    40902.33    42531.07   1013.50 o 
   2   9   9    33669.35    33781.98    677.77 o 
   4   9   9    26383.87    27669.11    646.83 o 
   6   9   9    18139.57    18310.35    549.46 o 
   1  10   9       40.23      209.41    109.71 o 
   3  10   9      753.33      654.34    112.72 o 
   0  11   9    29339.72    29636.49   2233.69 o 
   0   0  10      800.26      995.14    161.37 o 
   2   0  10    13756.25    12535.55    322.07 o 
   4   0  10      639.04      875.63     78.33 o 
   6   0  10     2320.80     2247.20     98.25 o 
   8   0  10       85.56      101.82    156.48 o 
  10   0  10      746.56      582.47    266.46 o 
   1   1  10        5.73      100.81     24.24 o 
   3   1  10      401.79      409.06     38.11 o 
   5   1  10      177.65      248.15     34.54 o 
   7   1  10       37.71       91.99     89.37 o 
   9   1  10        0.40      -86.77    122.51 o 
   0   2  10    10034.16     9733.86    193.69 o 
   2   2  10     1393.15     1592.55     46.45 o 
   4   2  10     2961.83     3349.01    142.21 o 
   6   2  10      718.32      694.77     48.84 o 
   8   2  10     1527.13     1411.09     86.43 o 
  10   2  10      432.25      584.84    154.84 o 
   1   3  10     1756.66     1724.47     45.07 o 
   3   3  10      161.83      153.39     38.16 o 
   5   3  10      476.38      473.78     72.06 o 
   7   3  10      320.43      322.96     69.18 o 
   9   3  10        1.26      258.55    128.23 o 
   0   4  10     1218.37     1312.15     71.90 o 
   2   4  10     2241.82     2434.99     68.66 o 
   4   4  10     2224.36     2401.86     83.90 o 
   6   4  10     1470.20     1538.31    125.46 o 
   8   4  10      784.15      862.98    106.91 o 
   1   5  10      316.27      328.32     41.59 o 
   3   5  10       12.94       48.36     31.70 o 
   5   5  10       39.08      103.25     50.53 o 
   7   5  10       73.73        3.59     72.91 o 
   9   5  10      114.64      122.18    176.66 o 
   0   6  10     2033.07     2156.94     86.98 o 
   2   6  10      528.74      630.16     47.37 o 
   4   6  10     1911.81     1806.32     88.59 o 
   6   6  10     1325.35     1064.76     75.59 o 
   8   6  10     1718.02     1849.76    194.19 o 
   1   7  10       22.93      119.63     57.49 o 
   3   7  10       77.26      142.97     47.11 o 
   5   7  10      199.59      274.27     90.35 o 
   7   7  10       95.38      496.98    165.18 o 
   0   8  10      310.72      443.32    101.60 o 
   2   8  10     2394.20     2354.62    105.69 o 
   4   8  10      748.44      814.92    102.64 o 
   6   8  10     1701.22     1523.85    163.52 o 
   1   9  10       32.46       80.99    104.82 o 
   3   9  10      379.18      317.54     94.81 o 
   5   9  10       99.63       30.55    106.81 o 
   0  10  10     1687.57     1688.55    222.34 o 
   2  10  10      872.56      966.91    111.13 o 
   4  10  10     1127.63     1217.19    203.72 o 
   1   0  11     1588.46     1437.08     74.14 o 
   3   0  11    20550.73    18489.87    361.27 o 
   5   0  11    11917.94    11711.93    393.48 o 
   7   0  11    16138.75    15813.46    506.59 o 
   9   0  11    11454.08    10246.03    533.88 o 
   0   1  11      650.43      603.46     40.23 o 
   2   1  11     5182.36     5324.44    178.52 o 
   4   1  11      110.41      208.97     36.72 o 
   6   1  11     2647.08     2757.23    145.63 o 
   8   1  11      311.05      261.03     85.79 o 
  10   1  11      482.45      488.46    166.71 o 
   1   2  11       40.81      118.09     47.26 o 
   3   2  11     4202.35     4137.95    151.12 o 
   5   2  11    12099.27    12072.08    374.12 o 
   7   2  11    17252.45    17635.01    709.44 o 
   9   2  11    13510.44    13630.56    573.89 o 
   0   3  11    26665.51    25890.75    583.20 o 
   2   3  11    14808.75    13873.45    260.90 o 
   4   3  11    14604.76    14605.10    621.72 o 
   6   3  11     3619.25     3809.72    122.74 o 
   8   3  11     2955.02     2721.33    177.52 o 
  10   3  11     1687.46     1886.66    383.40 o 
   1   4  11     2852.05     2760.06    114.45 o 
   3   4  11     4377.91     4514.02    126.01 o 
   5   4  11     9391.46     9650.31    278.77 o 
   7   4  11     7576.14     7038.29    184.86 o 
   9   4  11    10697.28    10213.91    528.69 o 
   0   5  11    23976.27    23158.30    647.73 o 
   2   5  11    36076.68    36264.94    487.81 o 
   4   5  11    14848.81    14093.56    455.80 o 
   6   5  11    18818.38    18098.15    755.68 o 
   8   5  11     7342.67     6980.42    274.57 o 
   1   6  11       38.58      164.81     44.32 o 
   3   6  11      511.60      551.29     42.87 o 
   5   6  11     4745.62     4683.93    177.63 o 
   7   6  11     7162.63     7129.95    435.83 o 
   0   7  11    41413.19    43025.36    822.66 o 
   2   7  11    27961.12    27617.85    512.50 o 
   4   7  11    31363.79    30164.99    769.14 o 
   6   7  11    14302.79    14296.73    482.55 o 
   1   8  11      303.12      262.74     84.54 o 
   3   8  11     1960.02     1819.37    164.29 o 
   5   8  11     2439.60     2526.82    176.79 o 
   0   9  11    28418.89    29257.70    843.45 o 
   2   9  11    28146.73    29041.70    797.47 o 
   4   9  11    23672.78    23421.87    625.08 o 
   1  10  11        5.67       95.53    139.15 o 
   3  10  11      501.53      527.91    130.11 o 
   0   0  12   437027.91   437679.28  25069.82 o 
   2   0  12   536080.31   521299.16   6262.34 o 
   4   0  12   374871.06   359538.09   6585.09 o 
   6   0  12   301317.44   293328.59   8490.59 o 
   8   0  12   144947.64   137399.89   3468.40 o 
  10   0  12    82095.58    81080.63   3516.71 o 
   1   1  12       33.59      116.68     31.18 o 
   3   1  12      307.56      354.78     39.23 o 
   5   1  12       45.93      130.95     61.85 o 
   7   1  12      163.70      363.12    111.58 o 
   9   1  12        8.68      227.24    162.80 o 
   0   2  12   532028.06   525637.38   7778.07 o 
   2   2  12   480160.94   467222.25  14071.97 o 
   4   2  12   333816.06   333762.84   6168.89 o 
   6   2  12   228746.86   224648.00   5019.12 o 
   8   2  12   135442.86   136139.08   3934.10 o 
   1   3  12        6.87       69.56     29.74 o 
   3   3  12      100.48      130.89     33.26 o 
   5   3  12       59.97      194.41     63.04 o 
   7   3  12      702.11      749.61     77.49 o 
   9   3  12     1366.03     1326.97    156.79 o 
   0   4  12   382384.16   386275.44  10919.35 o 
   2   4  12   316164.31   321922.59   7362.45 o 
   4   4  12   297060.19   297427.88   6548.04 o 
   6   4  12   175807.55   178186.69   6335.36 o 
   8   4  12   111318.59   111552.28   5444.69 o 
   1   5  12       63.47      100.48     37.50 o 
   3   5  12     1664.00     1586.04     79.72 o 
   5   5  12      743.89      708.78     47.36 o 
   7   5  12     2326.74     2241.05    162.92 o 
   0   6  12   274551.28   275609.66   5813.26 o 
   2   6  12   216531.38   218505.09   3001.26 o 
   4   6  12   168901.88   165093.17   3096.35 o 
   6   6  12    99900.51    96836.14   3119.98 o 
   8   6  12    68513.50    68036.45   3365.77 o 
   1   7  12      178.95       37.30     64.37 o 
   3   7  12      399.19      484.03     71.72 o 
   5   7  12     1873.40     1848.80    158.47 o 
   7   7  12     2260.37     2594.82    263.21 o 
   0   8  12   113570.78   112737.63   2463.34 o 
   2   8  12   115863.71   119568.91   1815.54 o 
   4   8  12    91434.65    89117.32   1893.73 o 
   6   8  12    66593.66    63199.88   2111.73 o 
   1   9  12      498.32      721.49    150.78 o 
   3   9  12     1195.80     1221.47    124.80 o 
   5   9  12     3311.14     3079.41    324.26 o 
   0  10  12    55822.89    59402.71   1804.38 o 
   2  10  12    55207.78    56530.93   1473.86 o 
   1   0  13      613.73      601.00     55.04 o 
   3   0  13     9109.20     8244.60    159.69 o 
   5   0  13    13881.54    13660.90    814.90 o 
   7   0  13    13932.79    13324.81    378.99 o 
   9   0  13     9026.42     8617.88    426.55 o 
   0   1  13      643.21      882.44    107.97 o 
   2   1  13      388.75      456.39     38.27 o 
   4   1  13     3514.97     3603.39    145.00 o 
   6   1  13      804.62      788.00    129.66 o 
   8   1  13      398.59      408.45     96.02 o 
   1   2  13      231.15      279.62     46.42 o 
   3   2  13     6390.07     6004.04    137.35 o 
   5   2  13     5971.73     5995.43    163.16 o 
   7   2  13    13118.89    12590.88    499.56 o 
   9   2  13    11401.73    11041.74    363.95 o 
   0   3  13    10304.11    10184.08    195.28 o 
   2   3  13    26143.94    25215.93    514.72 o 
   4   3  13     1344.23     1274.25     64.16 o 
   6   3  13     6582.41     6840.42    169.88 o 
   8   3  13     1041.47      899.87    106.70 o 
   1   4  13      661.68      700.10     47.12 o 
   3   4  13     2695.84     2679.96     65.88 o 
   5   4  13     9362.90     9448.37    272.80 o 
   7   4  13     7869.82     7895.80    369.47 o 
   9   4  13     8427.38     7605.06    394.31 o 
   0   5  13    22530.88    22455.35    658.66 o 
   2   5  13    14118.09    14189.12    370.51 o 
   4   5  13    23204.39    23562.96    803.16 o 
   6   5  13     9709.99     9753.11    575.29 o 
   8   5  13     7478.21     7235.99    391.58 o 
   1   6  13      545.28      583.44     54.38 o 
   3   6  13      611.40      573.66     57.90 o 
   5   6  13     3725.85     3491.70    280.22 o 
   7   6  13     5070.50     4671.78    376.22 o 
   0   7  13    29602.66    31564.03    666.94 o 
   2   7  13    26736.46    28359.54    517.14 o 
   4   7  13    16363.59    15593.16    346.79 o 
   6   7  13    13114.07    12443.53    568.89 o 
   1   8  13      276.63      371.85     90.07 o 
   3   8  13      971.67     1137.00    140.72 o 
   5   8  13     3718.54     4393.10    381.20 o 
   0   9  13    23274.75    24192.09    746.81 o 
   2   9  13    17602.64    17946.72    410.42 o 
   4   9  13    24875.01    24959.41   1075.32 o 
   1  10  13       11.47      321.62    141.08 o 
   0   0  14      212.21      455.08     82.96 o 
   2   0  14     3797.00     3998.46    105.98 o 
   4   0  14     1274.78     1454.92    116.87 o 
   6   0  14     5038.29     4654.50    293.12 o 
   8   0  14     1515.44     1561.23    188.45 o 
   1   1  14       42.62      111.38     39.87 o 
   3   1  14      331.44      241.02     28.99 o 
   5   1  14      140.36      171.13     98.14 o 
   7   1  14        5.04      -38.75     70.11 o 
   9   1  14      136.13      498.22    170.46 o 
   0   2  14     4739.88     4754.35    283.86 o 
   2   2  14     1943.63     1931.97     82.71 o 
   4   2  14     3541.95     3618.05    142.90 o 
   6   2  14     1368.65     1166.36     84.88 o 
   8   2  14     1602.37     1344.83    127.07 o 
   1   3  14     1788.02     1603.56    114.09 o 
   3   3  14       30.43       57.39     37.20 o 
   5   3  14     1310.98     1166.00     63.35 o 
   7   3  14      104.46      171.99     91.40 o 
   9   3  14       66.20      701.33    235.69 o 
   0   4  14     1498.94     1606.33     84.71 o 
   2   4  14     4865.86     4986.65    103.16 o 
   4   4  14     1532.13     1345.70    113.37 o 
   6   4  14     3055.26     3011.07    169.20 o 
   8   4  14     1074.69     1278.18    490.14 o 
   1   5  14       58.31      120.46     49.26 o 
   3   5  14       26.59      118.61     45.03 o 
   5   5  14       30.09      -69.47     69.47 o 
   7   5  14      232.88      309.47    160.04 o 
   0   6  14     7777.80     8185.92    437.17 o 
   2   6  14     1899.85     1844.12     77.62 o 
   4   6  14     3828.47     3827.66    163.70 o 
   6   6  14      414.00      495.85    136.49 o 
   1   7  14        5.62        1.35     76.76 o 
   3   7  14      362.65      371.87     90.30 o 
   5   7  14        4.38       -6.24    107.00 o 
   0   8  14     2316.78     2105.56    182.72 o 
   2   8  14     2339.66     2049.68    112.03 o 
   4   8  14     1807.55     1881.56    147.62 o 
   1   9  14      118.00       24.91    104.67 o 
   3   9  14        5.98        7.22    137.34 o 
   1   0  15      964.04      900.35     66.93 o 
   3   0  15      337.97      364.88     46.78 o 
   5   0  15     9962.41    11070.98    477.31 o 
   7   0  15     8352.01     8514.69    380.48 o 
   9   0  15    12240.01    11785.86    679.84 o 
   0   1  15      844.78     1025.01    105.86 o 
   2   1  15      474.81      512.42     48.42 o 
   4   1  15     2113.24     2219.85    228.10 o 
   6   1  15      368.90      288.46     95.16 o 
   8   1  15      452.55      599.73    112.99 o 
   1   2  15      523.22      581.66     76.91 o 
   3   2  15     4735.63     4554.34    127.75 o 
   5   2  15     5458.07     5546.31    297.81 o 
   7   2  15     8481.57     8506.14    414.59 o 
   0   3  15     7509.26     7374.09    182.55 o 
   2   3  15     7543.67     7513.30    198.12 o 
   4   3  15     5280.93     5290.72    204.25 o 
   6   3  15     6168.79     5794.57    284.99 o 
   8   3  15     4024.62     3785.20    292.70 o 
   1   4  15       89.81      143.21     46.19 o 
   3   4  15     2360.14     2105.59     91.49 o 
   5   4  15     6175.76     6135.91    237.41 o 
   7   4  15     8827.35     8406.24    436.54 o 
   0   5  15    19636.19    18200.58    436.90 o 
   2   5  15    13884.68    13103.76    271.70 o 
   4   5  15    18669.44    17957.79   1148.70 o 
   6   5  15     8620.15     8499.14    698.07 o 
   1   6  15      240.89      208.17     63.47 o 
   3   6  15     4393.50     4050.16    248.11 o 
   5   6  15     3439.71     3432.14    197.65 o 
   7   6  15     5545.63     4786.44    343.34 o 
   0   7  15    24360.54    25397.42   1165.27 o 
   2   7  15    24919.54    24349.22    555.59 o 
   4   7  15    15946.02    16582.66    618.85 o 
   6   7  15    14291.62    13704.07    758.60 o 
   1   8  15      199.72      362.59    102.74 o 
   3   8  15      658.25     1034.47    202.33 o 
   0   9  15    23593.73    24163.67    922.69 o 
   2   9  15    24199.73    24767.23   1154.38 o 
   0   0  16   343199.06   367503.00  14601.85 o 
   2   0  16   328643.13   344581.38   4838.14 o 
   4   0  16   236786.45   226500.81   5326.43 o 
   6   0  16   164985.64   161945.22   3901.20 o 
   8   0  16    93784.31    92177.40   3268.06 o 
   1   1  16        2.18      129.28     55.42 o 
   3   1  16      497.26      425.17     68.60 o 
   5   1  16       48.14       95.75    104.61 o 
   7   1  16      135.86      270.67    117.49 o 
   0   2  16   338612.00   352161.66   7611.36 o 
   2   2  16   268604.81   270436.44   3073.60 o 
   4   2  16   236172.97   241531.14   6824.52 o 
   6   2  16   139575.16   136092.78   3200.31 o 
   8   2  16    93988.52    97271.22   3344.54 o 
   1   3  16       24.49      105.38     46.09 o 
   3   3  16      504.66      520.17     53.03 o 
   5   3  16      709.89      700.09     81.61 o 
   7   3  16      877.91      911.83    135.47 o 
   0   4  16   205414.91   210027.45   3311.70 o 
   2   4  16   230817.58   231147.42   3472.06 o 
   4   4  16   155010.98   150820.33   4558.61 o 
   6   4  16   128172.70   125868.94   6314.19 o 
   1   5  16      246.98      155.57     63.72 o 
   3   5  16      699.89      623.45    101.86 o 
   5   5  16     1449.11     1389.51    179.81 o 
   7   5  16     1075.29     1127.10    187.69 o 
   0   6  16   148200.56   152264.45   5032.27 o 
   2   6  16   126895.34   128700.04   3824.70 o 
   4   6  16   114246.73   114593.15   4569.97 o 
   6   6  16    75321.41    69302.81   3388.76 o 
   1   7  16      113.08      354.81     90.85 o 
   3   7  16      242.29      321.75    159.35 o 
   5   7  16     1298.57     1238.22    138.04 o 
   0   8  16    74543.09    73166.48   2271.14 o 
   2   8  16    75162.60    74497.50   1990.06 o 
   4   8  16    58708.41    56076.27   2902.71 o 
   1   0  17      104.32      205.08     95.87 o 
   3   0  17     4852.69     4870.75    152.52 o 
   5   0  17     3271.50     3020.74    199.15 o 
   7   0  17     7359.13     7090.85    344.09 o 
   0   1  17      937.01      824.67     82.48 o 
   2   1  17      178.40      259.21     47.63 o 
   4   1  17      581.18      697.15     68.49 o 
   6   1  17      592.58      543.42    160.13 o 
   8   1  17      676.01      783.02    143.84 o 
   1   2  17       82.45      156.13     48.06 o 
   3   2  17      873.21      843.46     63.76 o 
   5   2  17     5250.69     4830.18    195.48 o 
   7   2  17     7979.40     8097.93    279.16 o 
   0   3  17     3534.22     3484.68    130.17 o 
   2   3  17     5614.12     5768.15    157.57 o 
   4   3  17     4494.94     4410.58    223.40 o 
   6   3  17     3609.35     3366.74    177.55 o 
   1   4  17      918.36      832.74     71.82 o 
   3   4  17     3269.11     3024.26    115.97 o 
   5   4  17     5169.31     4661.07    198.14 o 
   7   4  17     4908.88     4645.69    287.21 o 
   0   5  17    11261.37    11177.25    643.68 o 
   2   5  17    10563.89     9554.67    336.28 o 
   4   5  17     8921.29     8539.57    549.50 o 
   6   5  17     8400.64     7183.98    358.35 o 
   1   6  17      225.93      482.44     85.52 o 
   3   6  17     1002.82      931.69    105.57 o 
   5   6  17     4440.23     3894.68    271.92 o 
   0   7  17    16927.03    15609.44    497.51 o 
   2   7  17    16988.97    16331.32    581.41 o 
   4   7  17    13333.13    12507.64    770.56 o 
   1   8  17      141.32      373.59    118.44 o 
   0   0  18     2541.58     2492.57    499.00 o 
   2   0  18     4538.26     4908.23    323.49 o 
   4   0  18     2502.26     2767.16    208.88 o 
   6   0  18     2954.74     3637.45    415.20 o 
   1   1  18      132.50      275.87     68.33 o 
   3   1  18       80.44      151.12     56.81 o 
   5   1  18       59.67      503.34    136.83 o 
   7   1  18       20.21       15.39    166.27 o 
   0   2  18     4122.52     4350.31    145.61 o 
   2   2  18     5672.69     5668.12    181.44 o 
   4   2  18     1539.73     1514.87    111.59 o 
   6   2  18     1819.61     1721.64    154.57 o 
   1   3  18       85.96      139.62     68.53 o 
   3   3  18       12.72       39.87    111.23 o 
   5   3  18       35.80       10.51    119.69 o 
   7   3  18       21.47       97.28    150.90 o 
   0   4  18     3479.07     3520.54    270.44 o 
   2   4  18     1051.72     1027.76    106.08 o 
   4   4  18     4527.64     4486.90    184.63 o 
   6   4  18     1726.25     1421.77    154.08 o 
   1   5  18       16.24       95.76     77.85 o 
   3   5  18       84.12      306.68    105.42 o 
   5   5  18        3.51      -41.37    136.50 o 
   0   6  18     3035.33     2796.79    290.23 o 
   2   6  18     2279.36     2215.51    139.51 o 
   4   6  18     2130.44     2181.71    182.98 o 
   1   7  18       58.79       45.47    121.24 o 
   3   7  18      140.06      388.06    315.97 o 
   0   8  18     1425.88     1096.01    201.54 o 
   1   0  19      739.80      840.22     88.81 o 
   3   0  19     2221.41     2546.26    175.79 o 
   5   0  19     5526.70     5155.17    354.86 o 
   7   0  19     6038.28     5406.09    322.17 o 
   0   1  19     4089.04     4046.84    152.91 o 
   2   1  19      481.62      619.13     72.09 o 
   4   1  19      616.34      691.64    174.14 o 
   6   1  19       24.97      394.05    166.96 o 
   1   2  19      498.14      536.12     61.85 o 
   3   2  19     2550.88     2476.27    124.80 o 
   5   2  19     6527.25     6208.70    240.26 o 
   0   3  19     6030.00     6193.04    489.87 o 
   2   3  19     4535.98     4268.75    184.55 o 
   4   3  19     6757.79     6734.81    339.00 o 
   6   3  19     2770.31     2865.49    203.51 o 
   1   4  19      137.08      217.27     84.83 o 
   3   4  19     1271.42     1131.10    134.48 o 
   5   4  19     2392.11     1943.01    151.75 o 
   0   5  19    17037.12    17986.15    660.92 o 
   2   5  19    12544.23    12238.05    369.27 o 
   4   5  19     7927.03     7817.86    538.15 o 
   1   6  19       10.07      334.12    133.01 o 
   3   6  19     1372.87     1467.44    237.07 o 
   0   7  19    10773.82     9621.88    416.12 o 
   2   7  19    15316.97    15170.42    664.50 o 
   0   0  20   189894.97   212116.00   6552.17 o 
   2   0  20   168320.47   186686.16   4184.20 o 
   4   0  20   140035.20   150452.80   4278.71 o 
   6   0  20    94724.09    96971.55   3332.05 o 
   1   1  20       37.36       63.81     85.13 o 
   3   1  20      204.99      207.37    137.44 o 
   5   1  20       23.17      120.04    155.87 o 
   0   2  20   164756.58   176922.31   3853.11 o 
   2   2  20   152070.09   163057.20   2795.04 o 
   4   2  20   133140.41   140145.70   2954.04 o 
   6   2  20    93297.95    89568.39   2419.68 o 
   1   3  20      199.33      386.29     95.72 o 
   3   3  20        9.42       77.84    121.40 o 
   5   3  20      527.98      634.19    168.03 o 
   0   4  20   140130.77   150073.33   4207.49 o 
   2   4  20   128500.58   136335.00   3132.26 o 
   4   4  20    97746.74    95962.61   2612.96 o 
   1   5  20        9.13      276.47    130.97 o 
   3   5  20       40.46      252.94    136.05 o 
   0   6  20    84946.91    87268.41   3868.60 o 
   2   6  20    86150.09    88331.40   3471.01 o 
   1   0  21      507.37      699.68    156.64 o 
   3   0  21      917.21      825.22    224.33 o 
   5   0  21     5440.02     5344.40    323.67 o 
   0   1  21      613.80      942.76    152.41 o 
   2   1  21      473.46      669.31    144.12 o 
   4   1  21      553.69      820.86    171.10 o 
   1   2  21      535.16      831.21    145.06 o 
   3   2  21     2198.97     2463.99    168.46 o 
   5   2  21     3689.91     2997.72    670.32 o 
   0   3  21     4896.45     5529.56    561.70 o 
   2   3  21     3445.20     3619.19    245.67 o 
   4   3  21     2548.27     2506.58    208.68 o 
   1   4  21       10.36      284.84    138.95 o 
   3   4  21     1085.39      998.59    161.61 o 
   0   5  21     8953.02     8966.17    422.02 o 
   2   5  21     6551.59     5631.70    243.25 o 
   0   0  22     2126.92     2242.38    281.80 o 
   2   0  22     1761.70     1602.67    165.94 o 
   4   0  22     2785.30     3127.80    299.75 o 
   1   1  22        4.13      141.47    107.93 o 
   3   1  22       24.19       87.76    131.46 o 
   0   2  22     2931.57     3074.73    334.70 o 
   2   2  22     1963.38     2018.46    155.27 o 
   4   2  22     2406.73     2843.53    304.04 o 
   1   3  22       18.40      284.31    125.56 o 
   3   3  22       64.96      -26.22    142.79 o 
   0   4  22     2079.29     2185.60    360.02 o 
   2   4  22     3346.18     3229.56    188.63 o 
   1   0  23      165.14      448.52    278.07 o 
   3   0  23      294.00       45.32    211.43 o 
   0   1  23      337.52      415.76    472.02 o 
   2   1  23      303.90      520.14    145.75 o 
   1   2  23      139.63      325.28    134.97 o 
   3   2  23     1632.62     1865.72    184.81 o 
   0   3  23     2153.21     2459.14    284.22 o 
   2   3  23     2835.47     2817.81    298.81 o 
   0   0  24   105792.41   113206.74  10284.30 o 
   1   1  24        7.04      111.16    143.79 o