Magnetic behaviour of trioctahedral mica-2M1 occurring in a magnetic anomaly zone
 S. Pini, M. Affronte and M.F. Brigatti, Mineralogical Magazine, October 2008

Crystallographic coordinates and equivalent isotropic displacement parameters (A2  103) for crystal PBA-90-94 (2M1 polytype, space group C2/c). U(eq) is defined as one third of the trace of the orthogonalized Uij tensor (available on request).

|  | x | y | z | U(eq) | U11 | U22 | U33 | U23 | U13 | U12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O(11) | 0.7400(3) | 0.3157(2) | 0.1655(1) | 22(1) | 19(1) | 26(1) | 21(1) | 2(1) | 1(1) | -7(1) |
| O(21) | 0.2398(3) | 0.3519(2) | 0.1660(1) | 22(1) | 21(1) | 24(1) | 20(1) | -1(1) | -2(1) | 7(1) |
| O(22) | 0.4369(3) | 0.0837(2) | 0.1659(1) | 24(1) | 36(1) | 13(1) | 25(1) | 1(1) | 7(1) | 1(1) |
| O(31) | 0.4327(3) | 0.2507(2) | 0.0542(1) | 14(1) | 14(1) | 13(1) | 14(1) | 0(1) | 0(1) | 4(1) |
| O(32) | 0.9365(3) | 0.4183(2) | 0.0543(1) | 13(1) | 15(1) | 13(1) | 12(1) | 0(1) | 0(1) | 4(1) |
| O(4) | 0.9342(3) | 0.0830(2) | 0.0515(1) | 17(1) | 18(1) | 15(1) | 19(1) | 1(1) | 1(1) | 4(1) |
| T(1) | 0.4618(1) | 0.2503(1) | 0.1374(1) | 8(1) | 7(1) | 5(1) | 12(1) | 0(1) | 1(1) | 2(1) |
| T(2) | 0.9632(1) | 0.4174(1) | 0.1373(1) | 11(1) | 10(1) | 9(1) | 15(1) | 2(1) | 2(1) | 3(1) |
| M(1) | 0.75 | 0.25 | 0 | 11(1) | 9(1) | 8(1) | 15(1) | -1(1) | 1(1) | 6(1) |
| M(2) | 0.2465(1) | 0.0820(1) | 0.0000(1) | 12(1) | 14(1) | 8(1) | 14(1) | 0(1) | 1(1) | 9(1) |
| A | 0 | 0.0844(1) | 0.25 | 36(1) | 33(1) | 29(1) | 47(1) | 0 | 4(1) | 0 |