SUPPLEMENTARY TABLE S1. Crystallographic coordinates, occupancies, equivalent isotropic (Å2) and anisotropic displacement parameters of the studied micas.

Sample TF2_1

| Site | Atom | x/a | y/b | z/c | Occupancy | Uiso/equiv | U11 | U22 | U33 | U23 | U13 | U12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| K | K+ | 0 | ½ | 0 | 0.937(1) | 0.0287 | 0.0291(4) | 0.0296(4) | 0.0272(3) | 0 | 0.0044(3) | 0 |
| M1 | Mg2+ | 0 | 0 | ½ | 0.971(2) | 0.0097 | 0.0084(4) | 0.0077(4) | 0.0136(4) | 0 | 0.0031(2) | 0 |
|  | Fe2+ |  |  |  | 0.029(1) |  |  |  |  |  |  |  |
| M2 | Mg2+ | 0 | 0.33174(6) | ½ | 0.975(2) | 0.0095 | 0.0074(2) | 0.0085(3) | 0.0125(3) | 0 | 0.00157(16) | 0 |
|  | Fe2+ |  |  |  | 0.025(2) |  |  |  |  |  |  |  |
| T | Si, Si4+ | 0.07514(6) | 0.16663(3) | 0.22481(3) | 1.003(7) | 0.0092 | 0.0080(1) | 0.0086(1) | 0.0111(1) | -0.0002(1) | 0.00181(8) | -0.0002(1) |
| O1 | O, O2- | 0.3209(2) | 0.2344(1) | 0.16603(9) | 1.000(7) | 0.0180 | 0.0165(4) | 0.0230(5) | 0.0148(4) | -0.0013(3) | 0.0033(3) | -0.0059(3) |
| O2 | O, O2- | 0.0245(3) | 0 | 0.1661(1) | 1.000(7) | 0.0180 | 0.0247(6) | 0.0142(6) | 0.0139(5) | 0 | 0.0004(5) | 0 |
| O3 | O, O2- | 0.1305(1) | 0.16657(9) | 0.39020(8) | 1.000(7) | 0.0092 | 0.0085(3) | 0.0089(3) | 0.0103(3) | -0.0003(3) | 0.0020(2) | 0.0000(3) |
| O4 | F- | 0.1333(2) | 0.5 | 0.4016(1) | 1.000 | 0.0120 | 0.0102(4) | 0.0124(4) | 0.0134(4) | 0 | 0.0017(3) | 0 |

Sample TF2_2

| Site | Atom | x/a | y/b | z/c | Occupancy | Uiso/equiv | U11 | U22 | U33 | U23 | U13 | U12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| K | K+ | 0 | ½ | 0 | 0.927(1) | 0.0287 | 0.0288(2) | 0.0303(3) | 0.0269(2) | 0 | 0.0047(2) | 0 |
| M1 | Mg2+ | 0 | 0 | ½ | 0.984(2) | 0.0093 | 0.0080(3) | 0.0073(3) | 0.0131(3) | 0 | 0.0032(2) | 0 |
|  | Fe2+ |  |  |  | 0.016(1) |  |  |  |  |  |  |  |
| M2 | Mg2+ | 0 | 0.33195(4) | ½ | 0.981(2) | 0.0093 | 0.0069(2) | 0.0084(2) | 0.0127(2) | 0 | 0.0019(1) | 0 |
|  | Fe2+ |  |  |  | 0.019(2) |  |  |  |  |  |  |  |
| T | Si, Si4+ | 0.07506(4) | 0.16663(2) | 0.22492(2) | 1.001(7) | 0.0091 | 0.0081(1) | 0.0087(1) | 0.0108(1) | -0.00019(6) | 0.00204(6) | -0.00009(5) |
| O1 | O, O2- | 0.3205(1) | 0.23484(8) | 0.16606(6) | 1.000(7) | 0.0181 | 0.0164(2) | 0.0234(3) | 0.0148(2) | -0.0015(2) | 0.0033(2) | -0.0064(2) |
| O2 | O, O2- | 0.0249(2) | 0 | 0.16604(9) | 1.000(7) | 0.0182 | 0.0251(4) | 0.0134(3) | 0.0154(3) | 0 | 0.0016(3) | 0 |
| O3 | O, O2- | 0.1302(1) | 0.16662(5) | 0.39024(6) | 1.000(7) | 0.0093 | 0.0087(2) | 0.0089(2) | 0.0104(2) | -0.0004(1) | 0.0020(2) | -0.0001(1) |
| O4 | F- | 0.1335(1) | 0.5 | 0.40160(7) | 1.000 | 0.0118 | 0.0099(2) | 0.0116(3) | 0.0137(3) | 0 | 0.0020(2) | 0 |

Sample TF7_1

| Site | Atom | x/a | y/b | z/c | Occupancy | Uiso/equiv | U11 | U22 | U33 | U23 | U13 | U12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| K | K+ | 0 | ½ | 0 | 0.9352(18) | 0.0330 | 0.0329(7) | 0.0346(7) | 0.0321(7) | 0 | 0.0069(5) | 0 |
| M1 | Mg2+ | 0 | 0 | ½ | 1.0014(9) | 0.0133 | 0.0099(5) | 0.0110(6) | 0.0197(7) | 0 | 0.0044(5) | 0 |
| M2 | Mg2+ | 0 | 0.3317(1) | ½ | 1.0010(9) | 0.0130 | 0.0090(4) | 0.0113(4) | 0.0189(5) | 0 | 0.0030(3) | 0 |
| T | Si. Si4+ | 0.0748(1) | 0.16663(6) | 0.22508(6) | 1.000(7) | 0.0123 | 0.0102(2) | 0.0118(2) | 0.0156(2) | -0.0003(2) | 0.0038(2) | -0.0003(2) |
| O1 | O, O2- | 0.3208(3) | 0.2342(2) | 0.1659(2) | 1.000(7) | 0.0210 | 0.0173(6) | 0.0259(8) | 0.0206(7) | -0.0014(6) | 0.0054(6) | -0.0057(6) |
| O2 | O, O2- | 0.0230(5) | 0 | 0.1659(3) | 1.000(7) | 0.0222 | 0.026(1) | 0.018(1) | 0.021(1) | 0 | 0.0023(9) | 0 |
| O3 | O, O2- | 0.1301(3) | 0.1666(2) | 0.3907(2) | 1.000(7) | 0.0122 | 0.0089(5) | 0.0111(5) | 0.0173(6) | -0.0001(5) | 0.0041(4) | 0.0005(4) |
| O4 | F- | 0.1336(3) | 0.5 | 0.4021(2) | 1.000 | 0.0140 | 0.0099(6) | 0.0148(7) | 0.0180(8) | 0 | 0.0044(6) | 0 |

Sample TF7_2

| Site | Atom | x/a | y/b | z/c | Occupancy | Uiso/equiv | U11 | U22 | U33 | U23 | U13 | U12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| K | K+ | 0 | ½ | 0 | 0.9292(7) | 0.0287 | 0.0301(3) | 0.0302(2) | 0.0258(2) | 0 | 0.0050(1) | 0 |
| M1 | Mg2+ | 0 | 0 | ½ | 0.9939(6) | 0.0090 | 0.0079(1) | 0.0074(1) | 0.0120(2) | 0 | 0.0024(1) | 0 |
| M2 | Mg2+ | 0 | 0.33144(3) | ½ | 0.9968(8) | 0.0090 | 0.00776(9) | 0.00741(9) | 0.0119(1) | 0 | 0.00232(7) | 0 |
| T | Si, Si4+ | 0.07505(3) | 0.16663(1) | 0.22480(1) | 1.005(7) | 0.0089 | 0.00869(5) | 0.00823(5) | 0.00992(6) | -0.00002(4) | 0.00210(4) | -0.00001(3) |
| O1 | O, O2- | 0.32166(9) | 0.23382(5) | 0.16621(4) | 1.000(7) | 0.0182 | 0.0172(2) | 0.0237(2) | 0.0141(2) | -0.0016(1) | 0.0037(1) | -0.0063(1) |
| O2 | O, O2- | 0.0233(1) | 0 | 0.16628(6) | 1.000(7) | 0.0182 | 0.0263(3) | 0.0135(2) | 0.0141(2) | 0 | 0.0012(2) | 0 |
| O3 | O, O2- | 0.13022(6) | 0.16656(3) | 0.39036(4) | 1.000(7) | 0.0088 | 0.0089(1) | 0.0081(1) | 0.0096(1) | -0.00009(8) | 0.00203(9) | 0.00012(8) |
| O4 | F- | 0.13323(8) | 0.5 | 0.40212(5) | 1.000 | 0.0107 | 0.0099(1) | 0.0102(1) | 0.0119(2) | 0 | 0.0020(1) | 0 |

Sample TF10_1

| Site | Atom | x/a | y/b | z/c | Occupancy | Uiso/equiv | U11 | U22 | U33 | U23 | U13 | U12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| K | K+ | 0 | ½ | 0 | 0.9289(7) | 0.0279 | 0.0289(2) | 0.0292(2) | 0.0256(2) | 0 | 0.0044(1) | 0 |
| M1 | Mg2+ | 0 | 0 | ½ | 0.9931(6) | 0.0084 | 0.0067(2) | 0.0066(2) | 0.0120(2) | 0 | 0.0022(1) | 0 |
| M2 | Mg2+ | 0 | 0. 33163(3) | ½ | 0.9996(8) | 0.0084 | 0.0065(1) | 0.0070(1) | 0.0117(1) | 0 | 0.00195(8) | 0 |
| T | Si, Si4+ | 0.07515(3) | 0.16662(2) | 0.22488(2) | 1.004(7) | 0.0082 | 0.00737(6) | 0.00746(6) | 0.00978(7) | -0.00005(4) | 0.00180(4) | 0.00000(4) |
| O1 | O, O2- | 0.3213(1) | 0.23430(6) | 0.16616(5) | 1.000(7) | 0.0173 | 0.0153(2) | 0.0230(2) | 0.0139(2) | -0.0014(2) | 0.0032(1) | -0.0063(2) |
| O2 | O, O2- | 0.0240(2) | 0 | 0.16609(7) | 1.000(7) | 0.0173 | 0.0256(3) | 0.0118(2) | 0.0135(3) | 0 | 0.0009(2) | 0 |
| O3 | O, O2- | 0.13026(7) | 0.16653(4) | 0.39034(4) | 1.000(7) | 0.0081 | 0.00740(1) | 0.0080(1) | 0.0091(2) | -0.0001(1) | 0.0017(1) | 0.00013(9) |
| O4 | F- | 0.13342(9) | 0.5 | 0.40208(5) | 1.000 | 0.0101 | 0.0090(2) | 0.0094(2) | 0.0180(2) | 0 | 0.0018(1) | 0 |

Sample TF10_2

| Site | Atom | x/a | y/b | z/c | Occupancy | Uiso/equiv | U11 | U22 | U33 | U23 | U13 | U12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| K | K+ | 0 | ½ | 0 | 0.9339(8) | 0.0308 | 0.0311(3) | 0.0313(3) | 0.0301(3) | 0 | 0.0058(2) | 0 |
| M1 | Mg2+ | 0 | 0 | ½ | 0.9956(7) | 0.0107 | 0.0089(2) | 0.0081(2) | 0.0156(2) | 0 | 0.0034(2) | 0 |
| M2 | Mg2+ | 0 | 0. 33159(4) | ½ | 0.9986(8) | 0.0105 | 0.0085(1) | 0.0084(2) | 0.0149(2) | 0 | 0.0028(1) | 0 |
| T | Si, Si4+ | 0.07511(4) | 0.16664(2) | 0.22480(2) | 1.003(7) | 0.0106 | 0.00948(9) | 0.00909(8) | 0.01352(9) | -0.00001(7) | 0.00287(6) | -0.00003(6) |
| O1 | O, O2- | 0.3215(1) | 0.23400(9) | 0.16615(7) | 1.000(7) | 0.0200 | 0.0185(3) | 0.0245(3) | 0.0178(3) | -0.0013(2) | 0.0049(2) | -0.0064(2) |
| O2 | O, O2- | 0.0234(2) | 0 | 0.1662(1) | 1.000(7) | 0.0200 | 0.0275(5) | 0.0147(3) | 0.0173(4) | 0 | 0.0020(3) | 0 |
| O3 | O, O2- | 0.1302(1) | 0.16647(6) | 0.39041(6) | 1.000(7) | 0.0105 | 0.0095(2) | 0.0090(2) | 0.0131(2) | -0.0003(2) | 0.0027(2) | 0.0000(1) |
| O4 | F- | 0.1333 (1) | 0.5 | 0.40210(7) | 1.000 | 0.0123 | 0.0107(2) | 0.0109(2) | 0.0156(3) | 0 | 0.0029(2) | 0 |

SUPPLEMENTARY TABLE S2. Selected bond distances (Å) of the studied micas.

|  | TF2_1 | TF2_2 | TF7_1 | TF7_2 | TF10_1 | TF10_2 |
| --- | --- | --- | --- | --- | --- | --- |
| T-O1 | 1.647(1) | 1.646(1) | 1.650(2) | 1.648(1) | 1.648(1) | 1.649(1) |
| T-O1' | 1.649(1) | 1.647(1) | 1.650(2) | 1.648(1) | 1.648(1) | 1.649(1) |
| T-O2 | 1.647(1) | 1.647(0) | 1.650(1) | 1.648(0) | 1.648(0) | 1.648(0) |
| T-O3 | 1.650(1) | 1.649(1) | 1.653(2) | 1.651(0) | 1.650(0) | 1.652(1) |
| <T-O> | 1.648(1) | 1.647(1) | 1.651(2) | 1.649(0) | 1.649(0) | 1.650(1) |
| M1-O4(x2) | 2.024(1) | 2.023(1) | 2.021(2) | 2.024(0) | 2.023(1) | 2.024(1) |
| M1-O3(x4) | 2.080(1) | 2.079(1) | 2.077(1) | 2.079(0) | 2.079(0) | 2.079(1) |
| <M1-O> | 2.061(1) | 2.060(1) | 2.058(1) | 2.061(0) | 2.060(0) | 2.060(1) |
| M2-O4(x2) | 2.032(1) | 2.030(1) | 2.031(1) | 2.032(0) | 2.031(0) | 2.031(1) |
| M2-O3(x2) | 2.071(1) | 2.070(1) | 2.067(2) | 2.068(0) | 2.069(0) | 2.069(1) |
| M2-O3'(x2) | 2.077(1) | 2.078(1) | 2.077(1) | 2.079(0) | 2.078(0) | 2.079(1) |
| <M2-O> | 2.060(1) | 2.059(5) | 2.058(1) | 2.059(0) | 2.059(0) | 2.060(1) |
| <M-O> | 2.060(1) | 2.060(1) | 2.058(1) | 2.060(1) | 2.060(0) | 2.060(1) |
| K-O1(x4) | 2.988(1) | 2.991(1) | 2.987(2) | 2.984(1) | 2.988(1) | 2.986(1) |
| K-O1'(x4) | 3.267(1) | 3.263(1) | 3.269(2) | 3.275(1) | 3.270(1) | 3.274(1) |
| K-O2 (x2) | 2.988(1) | 2.990(1) | 2.981(3) | 2.985(1) | 2.987(1) | 2.986(1) |
| K-O2'(x2) | 3.267(1) | 3.263(1) | 3.275(3) | 3.275(1) | 3.270(1) | 3.275(1) |
| <K-O>inner | 2.988(1) | 2.991(1) | 2.984(2) | 2.985(1) | 2.987(1) | 2.986(1) |
| <K-O>outer | 3.267(1) | 3.263(1) | 3.271(2) | 3.275(1) | 3.270(1) | 3.274(1) |
| <K-O> | 3.128(1) | 3.127(1) | 3.127(2) | 3.130(1) | 3.128(1) | 3.130(1) |

SUPPLEMENTARY TABLE S3. Distortional parameters (calculated as indicated in Lacalamita et al., 2011) for the studied micas. Errors on distortion parameters, estimated by varying the refined positional parameters within one standard deviation are in the following ranges: < 0.5% for volumes, thicknesses, projected bond lengths, shifts; 0.1-13% for angles, bond/edge lengths distortions, sheet corrugations, D.M., ΔK-O.

|  | TF2_1 | TF2_2 | TF7_1 | TF7_2 | TF10_1 | TF10_2 |
| --- | --- | --- | --- | --- | --- | --- |
| ttet [Å] | 2.236 | 2.236 | 2.243 | 2.235 | 2.236 | 2.236 |
| BLDT | 0.063 | 0.047 | 0.063 | 0.067 | 0.050 | 0.063 |
| VolumeT [Å3] | 2.295 | 2.293 | 2.305 | 2.300 | 2.298 | 2.301 |
| TQE | 1.0006 | 1.0006 | 1.0007 | 1.0007 | 1.0006 | 1.0005 |
| TAV[°] | 2.49 | 2.67 | 2.98 | 2.95 | 2.45 | 2.28 |
| τ [°] | 110.8 | 110.9 | 111.0 | 110.7 | 110.8 | 110.8 |
| α[°] | 6.17 | 6.00 | 6.25 | 6.40 | 6.21 | 6.32 |
| Δz [Å] | 0.0007 | 0.0002 | 0.0000 | 0.0007 | 0.0007 | 0.0005 |
| D.M. [Å] | 0.497 | 0.494 | 0.510 | 0.510 | 0.505 | 0.510 |
| ψM(1) [°] | 59.15 | 59.13 | 59.24 | 59.23 | 59.20 | 59.23 |
| ψM(2) [°] | 59.12 | 59.12 | 59.24 | 59.20 | 59.19 | 59.22 |
| BLD M(1) | 1.213 | 1.209 | 1.215 | 1.203 | 1.212 | 1.180 |
| ELDM(2) | 5.297 | 5.278 | 5.412 | 5.392 | 5.365 | 5.396 |
| BLDM(1) | 0.901 | 0.945 | 1.215 | 1.272 | 1.270 | 1.275 |
| ELDM(2) | 5.261 | 5.257 | 5.401 | 5.361 | 5.344 | 5.380 |
| ShiftM(2) [Å] | 0.0016 | 0.0014 | 0.0016 | 0.0019 | 0.00017 | 0.00017 |
| VolumeM(1) [Å] | 11.460 | 11.441 | 11.406 | 11.441 | 11.432 | 11.434 |
| OQEM(1) | 1.013 | 1.013 | 1.013 | 1.013 | 1.013 | 1.013 |
| OAVM(1)[°] | 41.21 | 40.79 | 42.84 | 42.65 | 42.26 | 42.75 |
| VolumeM(2) [Å3] | 11.438 | 11.429 | 11.402 | 11.420 | 11.419 | 11.426 |
| OQEM(2) | 1.013 | 1.013 | 1.013 | 1.013 | 1.013 | 1.013 |
| OAVM(2)[°] | 41.46 | 41.35 | 43.25 | 42.76 | 42.47 | 43.02 |
| euM(1)/esM(1) | 1.112 | 1.111 | 1.114 | 1.114 | 1.113 | 1.114 |
| euM(2)/esM(2) | 1.111 | 1.111 | 1.114 | 1.113 | 1.113 | 1.113 |
| toct [Å] | 2.114 | 2.114 | 2.105 | 2.109 | 2.109 | 2.108 |
| tint [Å] | 3.312 | 3.313 | 3.311 | 3.316 | 3.314 | 3.314 |
| ΔK-O [Å] | 0.279 | 0.272 | 0.285 | 0.290 | 0.284 | 0.288 |
| tK-O4 [Å] | 3.944 | 3.944 | 3.950 | 3.948 | 3.948 | 3.948 |

SUPPLEMENTARY TABLE S4. Mean distances (Å) and mean atomic numbers (electrons, e-) of cation sites derived by structure refinements (X-ref) and chemical analyses (EMP). Average error for mean atomic numbers is ( 0.5 e- .

|  | TF2_1 | TF2_2 | TF7_1 | TF7_2 | TF10_1 | TF10_2 |
| --- | --- | --- | --- | --- | --- | --- |
| e- (M1) X-ref | 12.41 | 12.22 | 12.02 | 11.93 | 11.92 | 11.95 |
| e- (M2) X-ref | 12.35 | 12.27 | 12.01 | 11.96 | 12.00 | 11.98 |
| e- (M1+2M2) X-ref | 37.11 | 36.76 | 36.04 | 35.85 | 35.92 | 35.91 |
| e- (M1+2M2) EMP | 36.71 | 36.21 | 36.21 | 36.11 | 36.45 | 36.62 |
| K e- X-ref | 17.80 | 17.61 | 17.77 | 17.65 | 17.65 | 17.74 |
| K e- EMP | 17.06 | 16.71 | 17.22 | 17.53 | 17.22 | 16.79 |
| T e- X-ref | 14.04 | 14.01 | 14.00 | 14.07 | 14.06 | 14.04 |
| T e- EMP | 14.06 | 13.86 | 14.19 | 14.02 | 13.86 | 13.86 |
| <M-O> X-ref | 2.060 | 2.060 | 2.058 | 2.060 | 2.060 | 2.060 |
| <M-O> EMP | 2.070 | 2.067 | 2.073 | 2.070 | 2.072 | 2.070 |
| <T-O> X-ref | 1.648 | 1.647 | 1.651 | 1.649 | 1.649 | 1.650 |
| <T-O> EMP | 1.653 | 1.650 | 1.651 | 1.653 | 1.651 | 1.651 |