Comments on Level A alerts

PLAT075_ALERT_1_A Occupancy 1.018 Greater Than 1.0 for ...... M1

PLAT075_ALERT_1_A Occupancy 1.177 Greater Than 1.0 for ...... M2

Site occupancy factors for both M sites are greater than 1.00 due to the presence of minor Mn (M1) and Fe (M2) admixtures. Because of the insignificant amount of Mn impurity in M1 and the presence of the third component (Al) in M2, they were not involved in the refinement procedure and Mg scattering curve was used. Resulting eref values, as well as the assumed cation distribution, are given in Table 5 in the paper.