**Radiation defects in lime mortars and plasters studied by EPR spectroscopy**

Zuzanna Kabacińska1\*, Danuta Michalska2, Bernadeta Dobosz3

*1Institute of Chemistry and Technical Electrochemistry, Poznań University of Technology, Berdychowo 4, 60-965 Poznań, Poland*

# *2Institute of Geology, Faculty of Geographical and Geological Sciences, Adam Mickiewicz University, Krygowskiego 12, 61-680 Poznań, Poland*

*3Medical Physics and Radiospectroscopy Division, Faculty of Physics, Adam Mickiewicz University, Uniwersytetu Poznańskiego 2, 61-614 Poznań, Poland*

\*Corresponding author: zuziakab@amu.edu.pl

**Supplementary Information**

**Fig. S1** EPR spectra of UV- and γ-irradiated samples Hip10 (a, b), Hip8 (c, d) and 61H (e, f), and simulated signals present in those spectra (g). γ dose for samples Hip10 and Hip8 was 1 kGy, and 2.21 kGy for sample 61H. Spectra were normalized using Mn2+ signal as a reference.

**Fig S2.** Experimental and simulated spectra of sample Hip 10 after 6 hours of UV irradiation.



**Fig. S1** EPR spectra of UV- and γ-irradiated samples Hip10 (a, b), Hip8 (c, d) and 61H (e, f), and simulated signals present in those spectra (g). γ dose for samples Hip10 and Hip8 was 1 kGy, and 2.21 kGy for sample 61H. Spectra were normalized using Mn2+ signal as a reference.



**Fig S2.** Experimental and simulated spectra of sample Hip 10 after 6 hours of UV irradiation.