Supplementary Information

Figure S1. The size distribution of the LaVO4 nanoparticles.

Figure S2. SEM images and XRD patterns of LnVO4 nanoparticles, a-b) PrVO4, c-d) NdVO4, e-f) SmVO4, g-h) EuVO4, i-j) GdVO4, k-l) TbVO4, m-n) DyVO4, o-p) HoVO4, q-r) ErVO4, s-t) TmVO4, u-v) YbVO4, w-x) LuVO4

Figure S3. TEM and SEM images of ErVO4 nanoparticles.

Figure S4. SEM image of HoVO4 nanoparticles

Figure S5. a) TEM image of LaVO4 nanoparticles synthesized at  the molar ratio n(La3+):n(NH4VO3)=1:1; b) TEM image of LaVO4 nanoparticles synthesized at  the molar ratio n(La3+):n(NH4VO3)=2:1

Figure S6. SEM images of YVO4 nanoparticles annealed at 600 oC for 2h.