SUPPORTING INFORMATION

Tetra-octyloxy and octylthio substituted lead phthalocyanines: Synthesis, characterization, liquid crystalline properties and study of thin films

Sinem Tuncel, Tamara V. Basova,  Vitaly G. Kiselev, Sergei A. Gromilov, Irina V. Jushina, Mahmut Durmuş, Ayse Gül Gürek, Vefa Ahsen

-------------------------------------------------------------------

- The geometries of the species discussed in the manuscript (B3LYP/LANL2DZ geometry optimization).

PbPc1a

---------------------------------------------------------------------

Center     Atomic     Atomic              Coordinates (Angstroms)

Number     Number      Type              X           Y           Z

---------------------------------------------------------------------

1          7             0       -2.006166    0.339035    1.487394

2          7             0        0.339035    2.006166    1.487394

3          7             0        2.006166   -0.339035    1.487394

4          7             0       -0.339035   -2.006166    1.487394

5          6             0       -2.969489   -0.648966    1.295786

6          6             0       -2.594176    1.588906    1.294261

7          6             0       -1.588906   -2.594176    1.294261

8          6             0        0.648966   -2.969489    1.295786

9          6             0        2.594176   -1.588906    1.294261

10          6             0        2.969489    0.648966    1.295786

11          6             0        1.588906    2.594176    1.294261

12          6             0       -0.648966    2.969489    1.295786

13          7             0       -2.782642   -1.977573    1.263155

14          7             0       -1.977573    2.782642    1.263155

15          7             0        2.782642    1.977573    1.263155

16          7             0        1.977573   -2.782642    1.263155

17          6             0       -1.401037   -4.022720    1.036952

18          6             0        0.000000   -4.262488    1.038446

19          6             0       -4.262488    0.000000    1.038446

20          6             0       -4.022720    1.401037    1.036952

21          6             0        0.000000    4.262488    1.038446

22          6             0        1.401037    4.022720    1.036952

23          6             0        4.262488    0.000000    1.038446

24          6             0        4.022720   -1.401037    1.036952

25          6             0       -2.300241   -5.067539    0.779280

26          6             0        0.526018   -5.533956    0.785228

27          6             0       -5.533956   -0.526018    0.785228

28          6             0       -5.067539    2.300241    0.779280

29          6             0       -0.526018    5.533956    0.785228

30          6             0        2.300241    5.067539    0.779280

31          6             0        5.533956    0.526018    0.785228

32          6             0        5.067539   -2.300241    0.779280

33          6             0       -0.379761   -6.590526    0.543455

34          6             0       -1.781251   -6.352154    0.542644

35          1             0       -2.472620   -7.167393    0.357781

36          6             0        0.379761    6.590526    0.543455

37          6             0        1.781251    6.352154    0.542644

38          1             0        2.472620    7.167393    0.357781

39          6             0        6.352154   -1.781251    0.542644

40          6             0        6.590526   -0.379761    0.543455

41          6             0       -6.590526    0.379761    0.543455

42          6             0       -6.352154    1.781251    0.542644

43          1             0       -7.167393    2.472620    0.357781

44          1             0        1.600459   -5.691503    0.773587

45          1             0       -3.370586   -4.885740    0.767331

46          1             0       -1.600459    5.691503    0.773587

47          1             0        3.370586    4.885740    0.767331

48          1             0        5.691503    1.600459    0.773587

49          1             0        4.885740   -3.370586    0.767331

50          1             0       -5.691503   -1.600459    0.773587

51          1             0       -4.885740    3.370586    0.767331

52         82             0        0.000000    0.000000    2.631929

53         16             0       -0.362034    8.247804    0.254127

54          6             0        1.117413    9.296833   -0.300904

55          1             0        1.823605    9.371249    0.533229

56          1             0        1.598932    8.785303   -1.141429

57          6             0        0.618503   10.690405   -0.717575

58          1             0       -0.118143   10.590356   -1.527554

59          1             0        0.100884   11.166004    0.128294

60          6             0        1.778050   11.599605   -1.186455

61          1             0        2.298792   11.122206   -2.031686

62          1             0        2.518655   11.698193   -0.376819

63          6             0        1.298883   13.004594   -1.612466

64          1             0        0.786157   13.486587   -0.764818

65          1             0        0.549325   12.905304   -2.413826

66         16             0       -8.247804   -0.362034    0.254127

67          6             0       -9.296833    1.117413   -0.300904

68          1             0       -9.371249    1.823605    0.533229

69          1             0       -8.785303    1.598932   -1.141429

70          6             0      -10.690405    0.618503   -0.717575

71          1             0      -10.590356   -0.118143   -1.527554

72          1             0      -11.166004    0.100884    0.128294

73          6             0      -11.599605    1.778050   -1.186455

74          1             0      -11.122206    2.298792   -2.031686

75          1             0      -11.698193    2.518655   -0.376819

76          6             0      -13.004594    1.298883   -1.612466

77          1             0      -13.486587    0.786157   -0.764818

78          1             0      -12.905304    0.549325   -2.413826

79         16             0        0.362034   -8.247804    0.254127

80          6             0       -1.117413   -9.296833   -0.300904

81          1             0       -1.823605   -9.371249    0.533229

82          1             0       -1.598932   -8.785303   -1.141429

83          6             0       -0.618503  -10.690405   -0.717575

84          1             0        0.118143  -10.590356   -1.527554

85          1             0       -0.100884  -11.166004    0.128294

86          6             0       -1.778050  -11.599605   -1.186455

87          1             0       -2.298792  -11.122206   -2.031686

88          1             0       -2.518655  -11.698193   -0.376819

89          6             0       -1.298883  -13.004594   -1.612466

90          1             0       -0.786157  -13.486587   -0.764818

91          1             0       -0.549325  -12.905304   -2.413826

92          6             0        9.296833   -1.117413   -0.300904

93          1             0        9.371249   -1.823605    0.533229

94          1             0        8.785303   -1.598932   -1.141429

95          6             0       10.690405   -0.618503   -0.717575

96          1             0       10.590356    0.118143   -1.527554

97          1             0       11.166004   -0.100884    0.128294

98          6             0       11.599605   -1.778050   -1.186455

99          1             0       11.122206   -2.298792   -2.031686

100          1             0       11.698193   -2.518655   -0.376819

101          6             0       13.004594   -1.298883   -1.612466

102          1             0       13.486587   -0.786157   -0.764818

103          1             0       12.905304   -0.549325   -2.413826

104          1             0        7.167393   -2.472620    0.357781

105         16             0        8.247804    0.362034    0.254127

106          6             0       -2.446378  -13.915699   -2.099429

107          1             0       -3.198070  -14.013870   -1.299478

108          1             0       -2.957666  -13.433663   -2.948343

109          6             0       -1.969607  -15.321255   -2.525020

110          1             0       -1.464949  -15.808317   -1.675001

111          1             0       -1.212857  -15.224191   -3.320368

112          6             0       -3.114901  -16.229487   -3.023505

113          1             0       -3.872162  -16.326410   -2.229886

114          1             0       -3.617777  -15.743595   -3.874193

115          6             0       -2.630718  -17.632489   -3.445798

116          1             0       -2.153933  -18.154048   -2.604350

117          1             0       -3.463701  -18.255124   -3.798356

118          1             0       -1.893386  -17.566341   -4.257910

119          6             0      -13.915699    2.446378   -2.099429

120          1             0      -14.013870    3.198070   -1.299478

121          1             0      -13.433663    2.957666   -2.948343

122          6             0      -15.321255    1.969607   -2.525020

123          1             0      -15.808317    1.464949   -1.675001

124          1             0      -15.224191    1.212857   -3.320368

125          6             0      -16.229487    3.114901   -3.023505

126          1             0      -16.326410    3.872162   -2.229886

127          1             0      -15.743595    3.617777   -3.874193

128          6             0      -17.632489    2.630718   -3.445798

129          1             0      -18.154048    2.153933   -2.604350

130          1             0      -18.255124    3.463701   -3.798356

131          1             0      -17.566341    1.893386   -4.257910

132          6             0        2.446378   13.915699   -2.099429

133          1             0        2.957666   13.433663   -2.948343

134          1             0        3.198070   14.013870   -1.299478

135          6             0        1.969607   15.321255   -2.525020

136          1             0        1.464949   15.808317   -1.675001

137          1             0        1.212857   15.224191   -3.320368

138          6             0        3.114901   16.229487   -3.023505

139          1             0        3.617777   15.743595   -3.874193

140          1             0        3.872162   16.326410   -2.229886

141          6             0        2.630718   17.632489   -3.445798

142          1             0        2.153933   18.154048   -2.604350

143          1             0        3.463701   18.255124   -3.798356

144          1             0        1.893386   17.566341   -4.257910

145          6             0       13.915699   -2.446378   -2.099429

146          1             0       13.433663   -2.957666   -2.948343

147          1             0       14.013870   -3.198070   -1.299478

148          6             0       15.321255   -1.969607   -2.525020

149          1             0       15.808317   -1.464949   -1.675001

150          1             0       15.224191   -1.212857   -3.320368

151          6             0       16.229487   -3.114901   -3.023505

152          1             0       15.743595   -3.617777   -3.874193

153          1             0       16.326410   -3.872162   -2.229886

154          6             0       17.632489   -2.630718   -3.445798

155          1             0       18.154048   -2.153933   -2.604350

156          1             0       18.255124   -3.463701   -3.798356

157          1             0       17.566341   -1.893386   -4.257910

---------------------------------------------------------------------

PbPc2a

---------------------------------------------------------------------

Center     Atomic     Atomic              Coordinates (Angstroms)

Number     Number      Type              X           Y           Z

---------------------------------------------------------------------

1          7             0       -1.997129    0.386993    1.182832

2          7             0        0.386993    1.997129    1.182832

3          7             0        1.997129   -0.386993    1.182832

4          7             0       -0.386993   -1.997129    1.182832

5          6             0       -2.982927   -0.578098    0.990715

6          6             0       -2.552864    1.651057    0.989060

7          6             0       -1.651057   -2.552864    0.989060

8          6             0        0.578098   -2.982927    0.990715

9          6             0        2.552864   -1.651057    0.989060

10          6             0        2.982927    0.578098    0.990715

11          6             0        1.651057    2.552864    0.989060

12          6             0       -0.578098    2.982927    0.990715

13          7             0       -2.828876   -1.907390    0.958060

14          7             0       -1.907390    2.828876    0.958060

15          7             0        2.828876    1.907390    0.958060

16          7             0        1.907390   -2.828876    0.958060

17          6             0       -1.496876   -3.982380    0.728162

18          6             0       -0.101365   -4.258767    0.728948

19          6             0       -4.258767    0.101365    0.728948

20          6             0       -3.982380    1.496876    0.728162

21          6             0        0.101365    4.258767    0.728948

22          6             0        1.496876    3.982380    0.728162

23          6             0        4.258767   -0.101365    0.728948

24          6             0        3.982380   -1.496876    0.728162

25          6             0       -2.413402   -4.993792    0.467391

26          6             0        0.391654   -5.538059    0.472438

27          6             0       -5.538059   -0.391654    0.472438

28          6             0       -4.993792    2.413402    0.467391

29          6             0       -0.391654    5.538059    0.472438

30          6             0        2.413402    4.993792    0.467391

31          6             0        5.538059    0.391654    0.472438

32          6             0        4.993792   -2.413402    0.467391

33          6             0       -0.537759   -6.545908    0.223779

34          6             0       -1.928863   -6.286697    0.220445

35          1             0       -2.633463   -7.089382    0.021394

36          6             0        0.537759    6.545908    0.223779

37          6             0        1.928863    6.286697    0.220445

38          1             0        2.633463    7.089382    0.021394

39          6             0        6.286697   -1.928863    0.220445

40          6             0        6.545908   -0.537759    0.223779

41          6             0       -6.545908    0.537759    0.223779

42          6             0       -6.286697    1.928863    0.220445

43          1             0       -7.089382    2.633463    0.021394

44          1             0        1.453770   -5.757414    0.458179

45          1             0       -3.478167   -4.782307    0.454823

46          1             0       -1.453770    5.757414    0.458179

47          1             0        3.478167    4.782307    0.454823

48          1             0        5.757414    1.453770    0.458179

49          1             0        4.782307   -3.478167    0.454823

50          1             0       -5.757414   -1.453770    0.458179

51          1             0       -4.782307    3.478167    0.454823

52         82             0        0.000000    0.000000    2.325726

53          8             0        0.000000    7.792902   -0.019866

54          6             0        0.909458    8.898959   -0.326972

55          1             0        1.595246    9.059717    0.519932

56          1             0        1.503290    8.648331   -1.220188

57          6             0        0.044908   10.133825   -0.576263

58          1             0       -0.647725    9.917066   -1.401282

59          1             0       -0.568848   10.323964    0.314785

60          6             0        0.893696   11.378937   -0.914010

61          1             0        1.530087   11.165278   -1.788072

62          1             0        1.576170   11.601371   -0.077851

63          6             0        0.031115   12.624509   -1.211574

64          1             0       -0.612676   12.837885   -0.343547

65          1             0       -0.645255   12.402944   -2.052572

66          8             0       -7.792902    0.000000   -0.019866

67          6             0       -8.898959    0.909458   -0.326972

68          1             0       -9.059717    1.595246    0.519932

69          1             0       -8.648331    1.503290   -1.220188

70          6             0      -10.133825    0.044908   -0.576263

71          1             0       -9.917066   -0.647725   -1.401282

72          1             0      -10.323964   -0.568848    0.314785

73          6             0      -11.378937    0.893696   -0.914010

74          1             0      -11.165278    1.530087   -1.788072

75          1             0      -11.601371    1.576170   -0.077851

76          6             0      -12.624509    0.031115   -1.211574

77          1             0      -12.837885   -0.612676   -0.343547

78          1             0      -12.402944   -0.645255   -2.052572

79          8             0        0.000000   -7.792902   -0.019866

80          6             0       -0.909458   -8.898959   -0.326972

81          1             0       -1.595246   -9.059717    0.519932

82          1             0       -1.503290   -8.648331   -1.220188

83          6             0       -0.044908  -10.133825   -0.576263

84          1             0        0.647725   -9.917066   -1.401282

85          1             0        0.568848  -10.323964    0.314785

86          6             0       -0.893696  -11.378937   -0.914010

87          1             0       -1.530087  -11.165278   -1.788072

88          1             0       -1.576170  -11.601371   -0.077851

89          6             0       -0.031115  -12.624509   -1.211574

90          1             0        0.612676  -12.837885   -0.343547

91          1             0        0.645255  -12.402944   -2.052572

92          6             0        8.898959   -0.909458   -0.326972

93          1             0        9.059717   -1.595246    0.519932

94          1             0        8.648331   -1.503290   -1.220188

95          6             0       10.133825   -0.044908   -0.576263

96          1             0        9.917066    0.647725   -1.401282

97          1             0       10.323964    0.568848    0.314785

98          6             0       11.378937   -0.893696   -0.914010

99          1             0       11.165278   -1.530087   -1.788072

100          1             0       11.601371   -1.576170   -0.077851

101          6             0       12.624509   -0.031115   -1.211574

102          1             0       12.837885    0.612676   -0.343547

103          1             0       12.402944    0.645255   -2.052572

104          1             0        7.089382   -2.633463    0.021394

105          8             0        7.792902    0.000000   -0.019866

106          6             0       -0.867771  -13.877413   -1.548278

107          1             0       -1.534370  -14.109124   -0.701794

108          1             0       -1.522050  -13.656978   -2.407280

109          6             0       -0.005622  -15.116931   -1.871832

110          1             0        0.652080  -15.338338   -1.015822

111          1             0        0.658076  -14.886957   -2.721072

112          6             0       -0.842017  -16.371173   -2.207159

113          1             0       -1.499537  -16.605876   -1.355503

114          1             0       -1.504353  -16.147518   -3.057974

115          6             0        0.025987  -17.602830   -2.540525

116          1             0        0.675721  -17.866567   -1.694572

117          1             0       -0.593385  -18.478938   -2.774327

118          1             0        0.671271  -17.406306   -3.407902

119          6             0      -13.877413    0.867771   -1.548278

120          1             0      -14.109124    1.534370   -0.701794

121          1             0      -13.656978    1.522050   -2.407280

122          6             0      -15.116931    0.005622   -1.871832

123          1             0      -15.338338   -0.652080   -1.015822

124          1             0      -14.886957   -0.658076   -2.721072

125          6             0      -16.371173    0.842017   -2.207159

126          1             0      -16.605876    1.499537   -1.355503

127          1             0      -16.147518    1.504353   -3.057974

128          6             0      -17.602830   -0.025987   -2.540525

129          1             0      -17.866567   -0.675721   -1.694572

130          1             0      -18.478938    0.593385   -2.774327

131          1             0      -17.406306   -0.671271   -3.407902

132          6             0        0.867771   13.877413   -1.548278

133          1             0        1.522050   13.656978   -2.407280

134          1             0        1.534370   14.109124   -0.701794

135          6             0        0.005622   15.116931   -1.871832

136          1             0       -0.652080   15.338338   -1.015822

137          1             0       -0.658076   14.886957   -2.721072

138          6             0        0.842017   16.371173   -2.207159

139          1             0        1.504353   16.147518   -3.057974

140          1             0        1.499537   16.605876   -1.355503

141          6             0       -0.025987   17.602830   -2.540525

142          1             0       -0.675721   17.866567   -1.694572

143          1             0        0.593385   18.478938   -2.774327

144          1             0       -0.671271   17.406306   -3.407902

145          6             0       13.877413   -0.867771   -1.548278

146          1             0       13.656978   -1.522050   -2.407280

147          1             0       14.109124   -1.534370   -0.701794

148          6             0       15.116931   -0.005622   -1.871832

149          1             0       15.338338    0.652080   -1.015822

150          1             0       14.886957    0.658076   -2.721072

151          6             0       16.371173   -0.842017   -2.207159

152          1             0       16.147518   -1.504353   -3.057974

153          1             0       16.605876   -1.499537   -1.355503

154          6             0       17.602830    0.025987   -2.540525

155          1             0       17.866567    0.675721   -1.694572

156          1             0       18.478938   -0.593385   -2.774327

157          1             0       17.406306    0.671271   -3.407902

---------------------------------------------------------------------

PbPc1b

---------------------------------------------------------------------

Center     Atomic      Atomic             Coordinates (Angstroms)

Number     Number       Type             X           Y           Z

---------------------------------------------------------------------

1          7           0       -0.750422    1.895443    1.932223

2          7           0       -1.895443   -0.750422    1.932223

3          7           0        0.750422   -1.895443    1.932223

4          7           0        1.895443    0.750422    1.932223

5          6           0        0.000000    3.057221    2.124638

6          6           0       -2.090634    2.185797    2.137441

7          6           0        2.185797    2.090634    2.137441

8          6           0        3.057221    0.000000    2.124638

9          6           0        2.090634   -2.185797    2.137441

10          6           0        0.000000   -3.057221    2.124638

11          6           0       -2.185797   -2.090634    2.137441

12          6           0       -3.057221    0.000000    2.124638

13          7           0        1.338732    3.132558    2.151671

14          7           0       -3.132558    1.338732    2.151671

15          7           0       -1.338732   -3.132558    2.151671

16          7           0        3.132558   -1.338732    2.151671

17          6           0        3.615329    2.224571    2.426638

18          6           0        4.180846    0.914029    2.402607

19          6           0       -0.914029    4.180846    2.402607

20          6           0       -2.224571    3.615329    2.426638

21          6           0       -4.180846   -0.914029    2.402607

22          6           0       -3.615329   -2.224571    2.426638

23          6           0        0.914029   -4.180846    2.402607

24          6           0        2.224571   -3.615329    2.426638

25          6           0        4.358953    3.363686    2.761688

26          6           0        5.555058    0.739474    2.691824

27          6           0       -0.739474    5.555058    2.691824

28          6           0       -3.363686    4.358953    2.761688

29          6           0       -5.555058   -0.739474    2.691824

30          6           0       -4.358953   -3.363686    2.761688

31          6           0        0.739474   -5.555058    2.691824

32          6           0        3.363686   -4.358953    2.761688

33          6           0        6.304123    1.894621    3.010763

34          6           0        5.720487    3.182315    3.056654

35          1           0        6.341450    4.034769    3.319622

36          6           0       -6.304123   -1.894621    3.010763

37          6           0       -5.720487   -3.182315    3.056654

38          1           0       -6.341450   -4.034769    3.319622

39          6           0        3.182315   -5.720487    3.056654

40          6           0        1.894621   -6.304123    3.010763

41          6           0       -1.894621    6.304123    3.010763

42          6           0       -3.182315    5.720487    3.056654

43          1           0       -4.034769    6.341450    3.319622

44          1           0        3.879668    4.336499    2.806566

45          1           0       -3.879668   -4.336499    2.806566

46          1           0        4.336499   -3.879668    2.806566

47          1           0       -4.336499    3.879668    2.806566

48         82           0        0.000000    0.000000    0.793987

49          6           0       -6.190250    1.593156    1.030511

50          1           0       -6.683876    2.570856    1.096039

51          1           0       -5.115141    1.748930    0.917203

52          6           0       -6.789999    0.742114   -0.097444

53          1           0       -6.339927   -0.261066   -0.080241

54          1           0       -7.867591    0.608231    0.075219

55          6           0       -6.561783    1.380395   -1.488158

56          1           0       -5.481276    1.513651   -1.657639

57          1           0       -7.007002    2.388124   -1.507739

58          6           0       -7.158580    0.538083   -2.637097

59          1           0       -8.239646    0.408643   -2.468680

60          1           0       -6.717889   -0.471537   -2.613830

61          6           0        1.593156    6.190250    1.030511

62          1           0        2.570856    6.683876    1.096039

63          1           0        1.748930    5.115141    0.917203

64          6           0        0.742114    6.789999   -0.097444

65          1           0       -0.261066    6.339927   -0.080241

66          1           0        0.608231    7.867591    0.075219

67          6           0        1.380395    6.561783   -1.488158

68          1           0        1.513651    5.481276   -1.657639

69          1           0        2.388124    7.007002   -1.507739

70          6           0        0.538083    7.158580   -2.637097

71          1           0        0.408643    8.239646   -2.468680

72          1           0       -0.471537    6.717889   -2.613830

73          6           0        6.190250   -1.593156    1.030511

74          1           0        6.683876   -2.570856    1.096039

75          1           0        5.115141   -1.748930    0.917203

76          6           0        6.789999   -0.742114   -0.097444

77          1           0        6.339927    0.261066   -0.080241

78          1           0        7.867591   -0.608231    0.075219

79          6           0        6.561783   -1.380395   -1.488158

80          1           0        5.481276   -1.513651   -1.657639

81          1           0        7.007002   -2.388124   -1.507739

82          6           0        7.158580   -0.538083   -2.637097

83          1           0        8.239646   -0.408643   -2.468680

84          1           0        6.717889    0.471537   -2.613830

85          6           0       -1.593156   -6.190250    1.030511

86          1           0       -2.570856   -6.683876    1.096039

87          1           0       -1.748930   -5.115141    0.917203

88          6           0       -0.742114   -6.789999   -0.097444

89          1           0        0.261066   -6.339927   -0.080241

90          1           0       -0.608231   -7.867591    0.075219

91          6           0       -1.380395   -6.561783   -1.488158

92          1           0       -1.513651   -5.481276   -1.657639

93          1           0       -2.388124   -7.007002   -1.507739

94          6           0       -0.538083   -7.158580   -2.637097

95          1           0       -0.408643   -8.239646   -2.468680

96          1           0        0.471537   -6.717889   -2.613830

97          1           0        4.034769   -6.341450    3.319622

98          6           0       -6.930955    1.161439   -4.031307

99          6           0       -7.527864    0.320750   -5.180702

100          1           0       -5.849407    1.290506   -4.199689

101          1           0       -7.370899    2.171632   -4.054214

102          6           0       -7.298394    0.942869   -6.575581

103          1           0       -7.089654   -0.690267   -5.158724

104          1           0       -8.609841    0.192927   -5.014942

105          6           0       -7.897677    0.097273   -7.718907

106          1           0       -7.736670    1.952839   -6.597842

107          1           0       -6.217210    1.070404   -6.741526

108          1           0       -7.720203    0.562279   -8.697777

109          1           0       -7.454311   -0.907989   -7.738880

110          1           0       -8.983127   -0.019740   -7.594255

111          6           0       -1.161439   -6.930955   -4.031307

112          6           0       -0.320750   -7.527864   -5.180702

113          1           0       -1.290506   -5.849407   -4.199689

114          1           0       -2.171632   -7.370899   -4.054214

115          6           0       -0.942869   -7.298394   -6.575581

116          1           0        0.690267   -7.089654   -5.158724

117          1           0       -0.192927   -8.609841   -5.014942

118          6           0       -0.097273   -7.897677   -7.718907

119          1           0       -1.952839   -7.736670   -6.597842

120          1           0       -1.070404   -6.217210   -6.741526

121          1           0       -0.562279   -7.720203   -8.697777

122          1           0        0.907989   -7.454311   -7.738880

123          1           0        0.019740   -8.983127   -7.594255

124          6           0        6.930955   -1.161439   -4.031307

125          6           0        7.527864   -0.320750   -5.180702

126          1           0        5.849407   -1.290506   -4.199689

127          1           0        7.370899   -2.171632   -4.054214

128          6           0        7.298394   -0.942869   -6.575581

129          1           0        7.089654    0.690267   -5.158724

130          1           0        8.609841   -0.192927   -5.014942

131          6           0        7.897677   -0.097273   -7.718907

132          1           0        7.736670   -1.952839   -6.597842

133          1           0        6.217210   -1.070404   -6.741526

134          1           0        7.720203   -0.562279   -8.697777

135          1           0        7.454311    0.907989   -7.738880

136          1           0        8.983127    0.019740   -7.594255

137          6           0        1.161439    6.930955   -4.031307

138          6           0        0.320750    7.527864   -5.180702

139          1           0        1.290506    5.849407   -4.199689

140          1           0        2.171632    7.370899   -4.054214

141          6           0        0.942869    7.298394   -6.575581

142          1           0       -0.690267    7.089654   -5.158724

143          1           0        0.192927    8.609841   -5.014942

144          6           0        0.097273    7.897677   -7.718907

145          1           0        1.952839    7.736670   -6.597842

146          1           0        1.070404    6.217210   -6.741526

147          1           0        0.562279    7.720203   -8.697777

148          1           0       -0.907989    7.454311   -7.738880

149          1           0       -0.019740    8.983127   -7.594255

150         16           0       -0.866276   -6.456478    2.771491

151         16           0       -6.456478    0.866276    2.771491

152         16           0        0.866276    6.456478    2.771491

153         16           0        6.456478   -0.866276    2.771491

154          1           0        1.781332   -7.363655    3.222083

155          1           0       -7.363655   -1.781332    3.222083

156          1           0       -1.781332    7.363655    3.222083

157          1           0        7.363655    1.781332    3.222083

---------------------------------------------------------------------

PbPc2b

---------------------------------------------------------------------

Center     Atomic      Atomic             Coordinates (Angstroms)

Number     Number       Type             X           Y           Z

---------------------------------------------------------------------

1          7           0        0.969656   -1.796670    1.825195

2          7           0        1.796670    0.969656    1.825195

3          7           0       -0.969656    1.796670    1.825195

4          7           0       -1.796670   -0.969656    1.825195

5          6           0        0.362801   -3.040536    2.012749

6          6           0        2.333236   -1.924938    2.036622

7          6           0       -1.924938   -2.333236    2.036622

8          6           0       -3.040536   -0.362801    2.012749

9          6           0       -2.333236    1.924938    2.036622

10          6           0       -0.362801    3.040536    2.012749

11          6           0        1.924938    2.333236    2.036622

12          6           0        3.040536    0.362801    2.012749

13          7           0       -0.959429   -3.266850    2.054119

14          7           0        3.266850   -0.959429    2.054119

15          7           0        0.959429    3.266850    2.054119

16          7           0       -3.266850    0.959429    2.054119

17          6           0       -3.329229   -2.638091    2.323207

18          6           0       -4.049271   -1.404156    2.277789

19          6           0        1.404156   -4.049271    2.277789

20          6           0        2.638091   -3.329229    2.323207

21          6           0        4.049271    1.404156    2.277789

22          6           0        3.329229    2.638091    2.323207

23          6           0       -1.404156    4.049271    2.277789

24          6           0       -2.638091    3.329229    2.323207

25          6           0       -3.922809   -3.857797    2.668893

26          6           0       -5.439881   -1.413552    2.561311

27          6           0        1.413552   -5.439881    2.561311

28          6           0        3.857797   -3.922809    2.668893

29          6           0        5.439881    1.413552    2.561311

30          6           0        3.922809    3.857797    2.668893

31          6           0       -1.413552    5.439881    2.561311

32          6           0       -3.857797    3.922809    2.668893

33          6           0       -6.035892   -2.647298    2.911504

34          6           0       -5.296707   -3.845508    2.971602

35          1           0       -5.802654   -4.766293    3.250488

36          6           0        6.035892    2.647298    2.911504

37          6           0        5.296707    3.845508    2.971602

38          1           0        5.802654    4.766293    3.250488

39          6           0       -3.845508    5.296707    2.971602

40          6           0       -2.647298    6.035892    2.911504

41          6           0        2.647298   -6.035892    2.911504

42          6           0        3.845508   -5.296707    2.971602

43          1           0        4.766293   -5.802654    3.250488

44          1           0       -3.328273   -4.763580    2.721071

45          1           0        3.328273    4.763580    2.721071

46          1           0       -4.763580    3.328273    2.721071

47          1           0        4.763580   -3.328273    2.721071

48         82           0        0.000000    0.000000    0.691026

49          6           0        6.344429   -0.645742    1.470834

50          1           0        7.038556   -1.411188    1.834087

51          1           0        5.353233   -1.087768    1.335226

52          6           0        6.873733    0.000000    0.183471

53          1           0        6.190755    0.800509   -0.137180

54          1           0        7.847839    0.468496    0.385629

55          6           0        7.017219   -1.036029   -0.954337

56          1           0        6.041054   -1.509641   -1.145941

57          1           0        7.696643   -1.842082   -0.633411

58          6           0        7.548668   -0.417612   -2.265742

59          1           0        8.526082    0.053538   -2.074664

60          1           0        6.872043    0.390788   -2.586226

61          6           0       -0.645742   -6.344429    1.470834

62          1           0       -1.411188   -7.038556    1.834087

63          1           0       -1.087768   -5.353233    1.335226

64          6           0        0.000000   -6.873733    0.183471

65          1           0        0.800509   -6.190755   -0.137180

66          1           0        0.468496   -7.847839    0.385629

67          6           0       -1.036029   -7.017219   -0.954337

68          1           0       -1.509641   -6.041054   -1.145941

69          1           0       -1.842082   -7.696643   -0.633411

70          6           0       -0.417612   -7.548668   -2.265742

71          1           0        0.053538   -8.526082   -2.074664

72          1           0        0.390788   -6.872043   -2.586226

73          6           0       -6.344429    0.645742    1.470834

74          1           0       -7.038556    1.411188    1.834087

75          1           0       -5.353233    1.087768    1.335226

76          6           0       -6.873733    0.000000    0.183471

77          1           0       -6.190755   -0.800509   -0.137180

78          1           0       -7.847839   -0.468496    0.385629

79          6           0       -7.017219    1.036029   -0.954337

80          1           0       -6.041054    1.509641   -1.145941

81          1           0       -7.696643    1.842082   -0.633411

82          6           0       -7.548668    0.417612   -2.265742

83          1           0       -8.526082   -0.053538   -2.074664

84          1           0       -6.872043   -0.390788   -2.586226

85          6           0        0.645742    6.344429    1.470834

86          1           0        1.411188    7.038556    1.834087

87          1           0        1.087768    5.353233    1.335226

88          6           0        0.000000    6.873733    0.183471

89          1           0       -0.800509    6.190755   -0.137180

90          1           0       -0.468496    7.847839    0.385629

91          6           0        1.036029    7.017219   -0.954337

92          1           0        1.509641    6.041054   -1.145941

93          1           0        1.842082    7.696643   -0.633411

94          6           0        0.417612    7.548668   -2.265742

95          1           0       -0.053538    8.526082   -2.074664

96          1           0       -0.390788    6.872043   -2.586226

97          1           0       -4.766293    5.802654    3.250488

98          6           0        7.692568   -1.445664   -3.408663

99          6           0        8.225364   -0.829571   -4.720347

100          1           0        6.714507   -1.916424   -3.599539

101          1           0        8.368316   -2.254601   -3.086942

102          6           0        8.367395   -1.857647   -5.864162

103          1           0        7.551176   -0.019709   -5.043243

104          1           0        9.204614   -0.360600   -4.531538

105          6           0        8.900897   -1.235231   -7.171554

106          1           0        9.041034   -2.666845   -5.541675

107          1           0        7.388805   -2.325892   -6.053384

108          1           0        8.991655   -1.987443   -7.966433

109          1           0        8.229942   -0.443545   -7.532925

110          1           0        9.892456   -0.787273   -7.017958

111          6           0        1.445664    7.692568   -3.408663

112          6           0        0.829571    8.225364   -4.720347

113          1           0        1.916424    6.714507   -3.599539

114          1           0        2.254601    8.368316   -3.086942

115          6           0        1.857647    8.367395   -5.864162

116          1           0        0.019709    7.551176   -5.043243

117          1           0        0.360600    9.204614   -4.531538

118          6           0        1.235231    8.900897   -7.171554

119          1           0        2.666845    9.041034   -5.541675

120          1           0        2.325892    7.388805   -6.053384

121          1           0        1.987443    8.991655   -7.966433

122          1           0        0.443545    8.229942   -7.532925

123          1           0        0.787273    9.892456   -7.017958

124          6           0       -7.692568    1.445664   -3.408663

125          6           0       -8.225364    0.829571   -4.720347

126          1           0       -6.714507    1.916424   -3.599539

127          1           0       -8.368316    2.254601   -3.086942

128          6           0       -8.367395    1.857647   -5.864162

129          1           0       -7.551176    0.019709   -5.043243

130          1           0       -9.204614    0.360600   -4.531538

131          6           0       -8.900897    1.235231   -7.171554

132          1           0       -9.041034    2.666845   -5.541675

133          1           0       -7.388805    2.325892   -6.053384

134          1           0       -8.991655    1.987443   -7.966433

135          1           0       -8.229942    0.443545   -7.532925

136          1           0       -9.892456    0.787273   -7.017958

137          6           0       -1.445664   -7.692568   -3.408663

138          6           0       -0.829571   -8.225364   -4.720347

139          1           0       -1.916424   -6.714507   -3.599539

140          1           0       -2.254601   -8.368316   -3.086942

141          6           0       -1.857647   -8.367395   -5.864162

142          1           0       -0.019709   -7.551176   -5.043243

143          1           0       -0.360600   -9.204614   -4.531538

144          6           0       -1.235231   -8.900897   -7.171554

145          1           0       -2.666845   -9.041034   -5.541675

146          1           0       -2.325892   -7.388805   -6.053384

147          1           0       -1.987443   -8.991655   -7.966433

148          1           0       -0.443545   -8.229942   -7.532925

149          1           0       -0.787273   -9.892456   -7.017958

150          8           0       -0.317864    6.294215    2.596331

151          8           0        6.294215    0.317864    2.596331

152          8           0        0.317864   -6.294215    2.596331

153          8           0       -6.294215   -0.317864    2.596331

154          1           0       -2.639318    7.098822    3.133607

155          1           0        7.098822    2.639318    3.133607

156          1           0        2.639318   -7.098822    3.133607

157          1           0       -7.098822   -2.639318    3.133607

---------------------------------------------------------------------

2. 1H and 13C NMR studies

The complexes were found to be pure by 1H NMR with all the substituents and ring protons observed in their respective regions. The resonances belonging to ring protons were observed at 8.95 ppm as multiplet and 7.92 ppm as doublet as expected for PbPc1a. For complex PbPc2a ring protons showed at 9.09 ppm as doublet, 8.54 ppm as doublet and 7.63 ppm as triplet. For complex PbPc1b ring protons showed at 8.79 ppm and 7.91 ppm as multiplet. For complex PbPc2b ring protons showed at 9.01 ppm, 7.96 ppm and 7.55 ppm as multiplet. The aliphatic CH2 protons were observed in the range 3.32 to 1.34 ppm for PbPc1a, 4.44 to 1.39 ppm for PbPc2a, 3.25 to 1.38 ppm for PbPc1b and 4.63 to 1.28 ppm for PbPc2b. The methyl protons were observed at 0.90 ppm for PbPc1a, 0.96 ppm for PbPc2a, 0.96 ppm for PbPc1b and 0.92 ppm for PbPc2b as triplet. The presence of isomers for tetra-substituted complexes as well as phthalocyanine aggregation at the concentrations used for the NMR measurements generally lead to broadening of the aromatic signals.

Figure S1. 1H-NMR spectrum of  PbPc1a (solvent - CDCl3).

Figure S2. 13C-NMR spectrum of  PbPc1a (solvent - CDCl3).

Figure S3. 1H-NMR spectrum of  PbPc2a (solvent - CDCl3).

# .

Figure S4. 13C-NMR spectrum of  PbPc2a (solvent - CDCl3).

Figure S5. 1H-NMR spectrum of  PbPc1b (solvent - CDCl3).

Figure S6. 13C-NMR spectrum of  PbPc1b (solvent - CDCl3).

Figure S7. 1H-NMR spectrum of  PbPc2b (solvent - CDCl3).

Figure S8. 13C-NMR spectrum of  PbPc2b (solvent - CDCl3).

3. Mass-spectrosopy characterization of the synthesized species

The mass spectra of complexes were obtained by means of the MALDI-TOF MS technique without matrix. In the presence of 2,5-dihydroxybenzoic acid (DHB) as MALDI matrix, we obtained the mass spectrum of metal-free derivative due to the demetallation of PbPcs in acidic media. The molecular ion peaks for PbPc1a, PbPc2a, PbPc1b, and PbPc2b were observed without matrix at 1296.9 [M](, 1232.7 [M](, 1296.4 [M]( and 1232.5 [M](, respectively. A typical mass spectrum of PbPc1a is given in Fig. S9

# Figure S9. The mass spectrum of the PbPc1a.

4. DSC studies

First heating-cooling cycle

Second heating-cooling cycle

Figure S10. DSC curves of PbPc1a (C: crystal, LC: liquid crystal I: isotropic).

First heating-cooling cycle

Second heating-cooling cycle

Figure S11. DSC curves of PbPc2a (C: crystal, LC: liquid crystal I: isotropic).

First heating-cooling cycle for PbPc1b

Second heating-cooling cycle for PbPc1b

Figure S12. DSC curves of PbPc1b (I: isotropic; A: amorphous).

First heating-cooling cycle

Second heating-cooling cycle

Figure S13. DSC curves of of PbPb2b (C: crystal, LC: liquid crystal I: isotropic)..

5. XRD studies

Figure S14. X-ray diffraction patterns of the PbPc compouds studied.

Figure S15. X-ray diffraction patterns of the thin films of PbPc compounds: the as-deposited films on glass slides (blue) at the room temperature and after thermal treatment (red).