Supplemental Figure 1. Raw EDS spectrum on Ti1-xNbyO2 film.

Supplemental Figure 2. X-ray maps from Ti1-xNbyO2 thin film for a) Ti and b) Nb.

Supplemental Figure 3.  EDS line scan from Ti1-xNbyO2 thin film.  Raw Ti counts are shown in red and raw Nb counts are shown in green.