SUPPLEMENTARY MATERIAL

Silicon Nanowire/Polycaprolactone Composites and Their Impact on Stromal Cell Function

Ke Jiang,+ Giridhar R. Akkaraju,++ and Jeffery L. Coffer*+

+Department of Chemistry, Texas Christian University, Fort Worth, TX, 76129  United States.  E-mail: j.coffer@tcu.edu

++ Department of Biology, Texas Christian University, Fort Worth, TX, 76129  United States

Supplementary Figure 1

Size distribution of SiNWs prepared by (a) VLS route and (b) oxide-assisted VLS route.

Supplementary Figure 2

Photograph of a relatively large, (several cm) freestanding film of PCL / Si NW composite prepared by the printing method.

Supplementary Figure 3

# Text boxes

(b)

(a)

Occurrence (%)

Occurrence (%)

Diameter (nm)

Diameter (nm)

1 cm

Attachment of MSCs cultured on SiNW/PCL composites fabricated by the melting method. Pure SiNW surfaces were used as the control. The terms “SiNW/PCL-2” and “SiNW/PCL-4” indicate that there were either 2 or 4 pieces of PCL film (0.07 mm thick) added onto SiNW surface, respectively, then etched by 0.5 ml of chloroform for each piece of PCL film.

10 µ

20 µm

50 µm

100 µm

20 µm

50 µm

10 µm

20 µm

50 µm

(a)

(b)

(d)

(d)

(e)

(h)

(g)

(h)

(i)

(l)

(c)

(f)