Supplementary Materials for

Selective electrodeposition of Ni into the inter-tubular voids of anodic TiO2 nanotubes for improved photocatalytic properties

Fengxia Liang 1, 2, Jie Zhang 1, Lingxia Zheng 1, 2, Chun-Kwan Tsang 1, 2, Hui Li 1, 2, 3, 4, Shi-Wei Shu 1, 2, Hua Cheng 1, 2, Yang Yang Li 1, 2, 4, *

FIG. S1. Bottom-view SEM image of the as-anodized TiO2 nanotubes stripped off the Ti substrate. The arrows indicate the presence of a thin oxide layer at the bottoms of the inter-tubular voids.

FIG. S2. (a) Top view and (b) cross-sectional SEM images of a Ni/TiO2 composite film fabricated by electrodepositing Ni into thermally annealed TiO2 nanotubes. The anodization and electrodeposition parameters used are the same as those of the sample shown in Fig. 2c-d.