Rapid low-pressure plasma sintering of inkjet printed silver nanoparticles for RFID antennas

Franziska M. Wolf,1,2 Jolke Perelaer,1,2,3* Steffi Stumpf,1,2 Dirk Bollen,4 Frank Kriebel,5 Ulrich S. Schubert1,2,3*

Supporting Information Figure 1. Cross sectional scanning electron microscopy (SEM) images of inkjet printed silver nanoparticles at room temperature (A), after thermal sintering at 100 °C (B, C), 150 °C (D, E) and 200 °C (F, G) and after plasma sintering at 300 W (H, I). The images in the left and right column represent sintering times of 5 and 60 min, respectively.