TABLE I. The minimum amount of ligands required for preparation of the stable aqueous solutions containing 5 mmol of titanium and their pH.

# Text boxes

Compound		Min. requirement (vs. Ti)	pH

Glyceric acid		  5.0 mmol (equal)		5.7

2-hydroxybutxyric acid	 20.0 mmol (4.0 times)	4.8

Leucic acid		 27.5 mmol (5.5 times)	4.3

Quinic acid		  5.0 mmol (equal)		5.6

Mandelic acid		 15.0 mmol (3.0 times)	5.3

1,3-H4pdta		 10.0 mmol (2.0 times)	6.0

1,2-H4pdta		 10.0 mmol (2.0 times)	5.7

H4Cydta			 10.0 mmol (2.0 times)	5.8

EtOH-H3edta		 10.0 mmol (2.0 times)	6.2

H3nta			 10.0 mmol (2.0 times)	5.0

EtOH-H2ida		 12.5 mmol (2.5 times)	5.5

(EtOH)2-gly		 20.0 mmol (4.0 times)	7.6

TEA			 10.0 mmol (2.0 times)	7.4