Supplemental Material:

Composition of AgCu particle samples, from Rietveld refinement, generated under short residence time conditions at various temperatures. Short residence times were achieved when a single furnace and 10 L/min carrier gas flow rate were used.

| Cosolvent | Temperature (oC) | Residence time (s) | Phase abundance (%) |  |
| --- | --- | --- | --- | --- |
|  |  |  | Cu2(OH)3NO3 | CuO | Cu2O | Cu | Ag |
| ET | 400 | 0.41 | 66 | 12 | 0 | 1 | 11* |
| ET | 500 | 0.36 | 63 | 7 | 0 | 0 | 30 |
| ET | 550 | 0.34 | 49 | 15 | 0 | 0 | 36 |
| ET | 600 | 0.32 | 38 | 22 | 0 | 0 | 40 |
| ET | 650 | 0.3 | 32 | 23 | 5 | 0 | 40 |
| ET | 700 | 0.28 | 0 | 13 | 19 | 20 | 48 |
| ET | 750 | 0.27 | 0 | 6 | 19 | 27 | 48 |
| ET | 800 | 0.26 | 0 | 0 | 11 | 41 | 48 |
| ET | 875 | 0.23 | 0 | 0 | 0 | 51 | 49 |
| EG | 400 | 0.41 | 58 | 0 | 0 | 2 | 40 |
| EG | 500 | 0.36 | 11 | 0 | 30 | 12 | 47 |
| EG | 550 | 0.34 | 0 | 0 | 28 | 22 | 50 |
| EG | 600 | 0.32 | 0 | 0 | 20 | 33 | 47 |
| EG | 650 | 0.3 | 0 | 0 | 11 | 36 | 53 |
| EG | 700 | 0.28 | 0 | 0 | 11 | 34 | 55 |
| EG | 750 | 0.27 | 0 | 4 | 11 | 29 | 56 |
| EG | 800 | 0.26 | 0 | 9 | 13 | 25 | 53 |
| EG | 875 | 0.23 | 0 | 0 | 7 | 38 | 55 |

*At 400 oC with the cosolvent of ET, samples contained 10 % AgNO3.

Composition of Cu particle samples, from Rietveld refinement, generated under short residence time conditions at various temperatures. Short residence times were achieved when a single furnace and 10 L/min carrier gas flow rate were used.

| Cosolvent | Temperature (oC) | Residence time (s) | Phase abundance (%) |  |
| --- | --- | --- | --- | --- |
|  |  |  | Cu2(OH)3NO3 | CuO | Cu2O | Cu |
| ET | 400 | 0.41 | 100 | 0 | 0 | 0 |
| ET | 550 | 0.34 | 29 | 50 | 3 | 18 |
| ET | 600 | 0.32 | 26 | 37 | 14 | 23 |
| ET | 650 | 0.3 | 2 | 46 | 10 | 43 |
| ET | 700 | 0.28 | 0 | 36 | 17 | 47 |
| ET | 750 | 0.27 | 0 | 15 | 15 | 69 |
| ET | 800 | 0.26 | 0 | 0 | 5 | 95 |
| ET | 875 | 0.23 | 0 | 10 | 3 | 87 |
| EG | 400 | 0.41 | 91 | 5 | 5 | 0 |  |
| EG | 550 | 0.34 | 6 | 0 | 43 | 51 |  |
| EG | 600 | 0.32 | 12 | 10 | 29 | 49 |  |
| EG | 650 | 0.3 | 0 | 0 | 35 | 65 |  |
| EG | 700 | 0.28 | 0 | 0 | 28 | 72 |  |
| EG | 750 | 0.27 | 0 | 0 | 19 | 81 |  |
| EG | 800 | 0.26 | 0 | 0 | 0 | 100 |  |
| EG | 875 | 0.23 | 0 | 3 | 1 | 96 |  |